## Slide 1
The role of lattice dynamics in the superconductivity enhancement at FeSe/SrTiO3 interface
Jiandong Guo
Institute of Physics, Chinese Academy of Sciences
VASSCAA-9, Aug. 15, 2018, Sydney

## Slide 2
20 K
40 K
60 K
TC/K
Bulk
0 K
FeSe bulk
FeSe/Graphene
Interface Enhanced
FeSe/SrTiO3(001)(110)
FeSe/TiO2
FeSe/BaTiO3
FeSe/strained SrTiO3
Xue et al., APL 2016 Feng et al., Nat. Comm. 2014
Xue et al., PRL 2016 Shen et al., PRL 2017
Wu et al., PNAS 2008
Xue et al., Science 2011
Xue et al., PRB 2016 Feng et al., Nano Lett. 2016
Hosono et al., PNAS 2016 Chen et al., Nat. Mater 2015
K-Doped FeSe Film
K-Doped Bulk FeSe
Liquid Gated FeSe/STO
(Li0.84Fe0.16)OHFe0.98Se
Electron Doped
Tuning the superconductivity of FeSe
Carrier doping & interfacial coupling!

## Slide 3
Electron Energy Loss Spectroscopy (HREELS)
HREELS
Energy
Analyzer
LEED
MBE
system
ARPES
2D resolved HREELS
Ultimate E < 0.7 meV
Ultimate  < 0.1º
q < 0.005Å-1
High detection efficiency
Large momentum range
To probe the interfacial coupling…
Zhu et al., Rev. Sci.Instrum. 86, 083902 (2015)
Notes: 0.002A
3meV

## Slide 4
1uc-FeSe/STO at 35 K
FeSe
STO
Low-energy excitations on FeSe/SrTiO3

## Slide 5
No thickness dependence
No interface effect
Not related to SC enhancement
PRB 97, 035408 (2018)
Fe- and Se-derived phonons

## Slide 6
AFM correlation or spin fluctuation is identical for both FeSe films and bulks. Not enhanced at the interface.
J
spin channel J
Initial pairing in FeSe
DFT calculation:
UTK: Yan Wang
Steve Johnston
ORNL: Tom Berlijn
AFM order or spin fluctuation
Notes: Bulk: colinear; 20 meV the most important. Cal: Checkerboard & colinear

## Slide 7
1uc-FeSe/STO at 35 K
Fuchs-Kliewer (F-K) phonon:
Optical modes of vibration on the surface of ionic crystals, such as oxides.
Penetrating electric field generated by F-K phonons
β mode: 59 meV
α mode: 97 meV
PRB 94, 081116(R) (2016)
STO surface phonons on 1 uc FeSe/SrTiO3

## Slide 8
Gap data: D. L. Feng et al., Nano Letters 16, 1869 (2016)
Penetration Length: ~ 2.5 u.c.
F-K phonons of oxides
Superconductivity Enhancement
Phys. Rev. B 94, 081116(R) (2016)
SrTiO3 phonons penetrating into FeSe

## Slide 9
1uc-FeSe/STO at 35 K
Surface plasmon ρ ~ 150 meV
The microscopic picture…
F. Gervais, PRB 47, 8187 (1993)
G. Verbist, Ferroelectrics 130:1, 27-34 (1992)
Nb:SrTiO3
C Z Bi, JPCM 18, 2553–2561 (2006)
: polaron effective mass
Nb:SrTiO3

## Slide 10
1uc-FeSe/STO
correlated
Nb:STO
uncorrelated
Plasmon vs. phonon

## Slide 11
interfacial polaron
STO lattice can dress electrons in FeSe through the mediation of electric field generated by FK phonons, i.e. interfacial polaron.
The interfacial electron-boson coupling
Interfacial polaronic plasmon

## Slide 12
Additional attractive potential Vpp
J. Devreese, et al. Reports on Progress in Physics 72, 066501 (2009).
γq: Phonon linewidth
Im[]: Lindhard function
Vpp
Non-adiabatic polaron-polaron interaction
Hubbard model with a negative U
half band width: ,
electron density: ,
total attractive potential:
At the coherent length of 1.2 nm, Vpp can enhance the TC to ~70K.
USTC：Zhenyu Zhang et al.
Notes: Give a summary at the beginning. F: force constant, e is the phonon polarization vector and e(m-n) is the unit vector in the direction from electron site m and ion site n

## Slide 13
Superconductivity is enhanced by the non-adiabatic polaron-polaron interaction, i.e. dynamic interfacial polaron.
spin channel J
AFM correlation: <40 K
additional attractive interaction in short range
Local Pairing: ξpair~ 1.2 nm
Dynamic Interfacial Polaron: 40 ~65 K
Summary

## Slide 14
Phonon cal.: Yan Wang, Steve Johnston (UTK)
Bipolaron modeling: Tong Wei, Zhenyu Zhang (USTC)
Shuyuan Zhang
Xuetao Zhu
Jiaqi Guan
Sample growth：
Thank you for your attention!
Acknowledgement

## Slide 15
Dynamic (non-adiabatic) interfacial polaron (ħωB/EF ~ 1.7)
EF ~ 56 meV < ħωB ~ 97 meV
Low phonon energy (ħωB)
High Fermi Energy (EF)
High phonon energy (ħωB)
Low Fermi Energy (EF)
Adiabatic Limit:
Non-adiabatic Limit:
ħωB/EF >> 1
ħωB/EF << 1
Instantaneous response
Retarded response
Metal
1uc-FeSe/STO at 35 K
Beyond the
BCS framework
Dynamic interfacial polarons

## Slide 16
Q.-Y. Wang. et al. CPL 29, 037402, (2012).
2012, STS, Δ~20meV
Liu, D. et al. Nat. Commun. 3, 931, (2012).
2012---Now, ARPES, Δ~15-20meV, Tg~55-70 K
Tan, S. et al. Nat Mater. 12, 634, (2013).
Lee, J. et al. Nature 515, 245, (2014).
Zhang, W.-H. et al. CPL 31, 017401, (2014).
Tconset = 40.2 K Tczero = 23.5 K
2014, ex situ transport
Sun, Y. et al. Sci. Rep. 4, 6040, (2014).
FeSe
SrTiO3
2015, ex situ dimagnetism
Tconset = 65 K
Z. Zhang et al., Sci. Bull. 60, 1301 (2015)
SC enhancement at the FeSe/SrTiO3 interface

## Slide 17
STM & STS
LEED & ARPES
TC ≈ 65-70K
Δ ~ 20 meV
Single-layer FeSe on SrTiO3