## Slide 1: Simple linear relationship between reactive gas flow rate and discharge power at mode transition on reactive sputter deposition of metal oxides
Takeo Nakano, Kei Oya, Kosuke Kimura
Seikei University, Japan
Masayoshi Nagao, Hisashi Ohsaki
National Institute of Advanced Industrial Science and Technology (AIST), Japan
14 Aug, 2018 VASSCAA-9 @SMC Centre, Sydney

## Slide 2: Reactive sputtering process: metal mode & compound mode
Ar
RG
pump
target
Ar
RG
pump
target
substrate
substrate
metal mode
compound (oxide) mode

## Slide 3: Hysteresis in Reactive Sputtering
Region | Deposition rate | Film composition
Metal | High | Metal-rich
Compound | Low | Stoichiometric
3
Transition point information is important!

## Slide 4: Experimental
Chamber: SUS, 25 cmφ x 18 cm h Base Pressure < 5 x 10-5 Pa
Target, Gas: V, Ti, Zr; 50 mmφ Ar 10 sccm + O2, via MFC
Power Source: DC in power regulation
Mode change was monitored by the Voltage jump
Depla, et al., JAP 101 (1987) 13301.

## Slide 5: Power Const. operation
V @ Ar 0.5 Pa

## Slide 6: Flow Const. operation
V @ Ar 0.5 Pa

## Slide 7: Ti & Zr, Q -P plot
Ti @ Ar 0.5 Pa
Zr @ Ar 0.5 Pa

## Slide 8: Berg’s Model
This model is composed of balance equations:
  [at target] Oxidation of metal region vs Sputter etching of oxide region
  [at chamber wall] Oxidation + oxide deposition on metal region vs metal deposition on oxide region
Berg, et al., JVSTA 5 (1987) 202.

## Slide 9: Reproduction of Hysteresis

## Slide 10: Linear Relationship in Q -P map?
In Berg’s model, sputtering yield is constant. Therefore, is proportional to the sputtering emission from (and the etching of) the target.
In practice, is roughly proportional to , where is the primary ion energy (). Mahan and Vantomme, Phys. Rev. B, 61 (2000) 8516.
In Magnetron sputtering discharge, , where is typically . Rossnagel and Kaufman, JVSTA, 6 (1988) 223. Ehiasarian, et al., Vacuum, 65 (2002) 147.

## Slide 11: Linear Relationship in Q -P map?
By the dimensional analysis,
Gas rarefaction at higher power...
  Enhances the efficient delivery of the sputtered atoms to the chamber wall.
  Suppresses the oxygen flux to the target.
both shift the balance to the metallic side, hence shows a good linearity with Q.

## Slide 12: V Q-P plot, pressure dep.
V @ Ar 0.5 Pa
V @ Ar 0.2 Pa
V @ Ar 1.0 Pa
V @ Ar 2.0 Pa

## Slide 13: Q-P plot slope vs pressure
Higher gas pressure (i.e., Lower pumping speed) the slope was reduced and the hysteresis was widen
It is in agreement with the prediction of Berg’s model, and the general behavior or the reactive sputtering.

## Slide 14: Practical usage of this concept
At a certain condition of Ar pressure and flow rate, mode transitions can be predicted by a single experiment.
Films of similar properties can be expected at different discharge power by choosing the deposition conditions in the Q-P map.

## Slide 15: Optical Transmittance of Vanadia films
V @ Ar 0.5 Pa

## Slide 16: Concluding remarks
In reactive sputtering of some metal oxides, M→Ox and Ox→M mode transition points lay on corresponding straight lines in Q-P map.
It denotes the sputtering emission from (and the etching of) the target is effectively proportional to the discharge power.
The concept may be useful in deposition condition selection, and the control of the properties of deposited films.

## Slide 17: Motivation of this study
In actual deposition processes, the target current increase accompanies the target voltage increase;
→Hence the sputtering yield also increases.
Is there any good measure to predict the mode transition conditions?

## Slide 18: Power Const. measurements
Ti / Ar 0.5 Pa, 10 sccm

## Slide 19: Flow Const. measurements
Ti / Ar 0.5 Pa, 10 sccm