## Slide 1
Dependence of Thermal Conductivity of MPCVD Diamond Thin Films on Oxygen Concentration
Fatima tuz Zahra, James Downes
Department of Physics & Astronomy,
Macquarie University, Sydney, Australia.

## Slide 2
Outline
Diamond Growth
CVD Method
Results
Conclusion/Future Work
Properties and Applications

## Slide 3
Insulator when pure and semiconductor (Eg≈ 5.47eV) when doped (Wort & Balmer, 2008)
Application: CMOS, and MEMS/NEMS technology (Sumant et al.,2010)
Fig. 3. Diamond as an actuator in MEMS
https://www.rdmag.com/news/2014/08/thin-diamond-films-provide-new-material-micro-machines
High thermal conductivity (2000-2300 W/m.K)
Application: Thermal management in electronic devices
Fig. 2 Diamond as a heat spreader
https://www.mwrf.com/materials/diamonds-are-gan-pa-s-best-friend
Properties & Applications of Diamond
Fig.1. (a) Crystal structure of diamond, morphological demonstration of (b) plane {111} and (c) plane {100} of diamond lattice
FCC crystal structure with covalently bonded carbon atoms along <111> direction.
34% lattice filled with carbon atoms.
S. Sun et al., Cryst. Eng. Comm., 16, 2290, (2014)
V. S. S. Srikanth and X. Jiang, Synthetic Diamond Films: Preparation, Electrochemistry, Characterization, and Applications, 2011, 21–55

## Slide 4
Classification of Diamond Thin Films (DTFs)
A. V. Sumant, O. Auciello, R. W. Carpick, S. Srinivasan, and J. E. Butler, MRS Bull., 35, 281–288, 2010
UltraNanoCrystalline diamonds (UNCDs)
(≤10 nm)
~5% sp2 bonded carbon
Fig. 4. Morphology of UNCDs
NanoCrystalline diamonds (NCDs)
(>10 nm and ≤100nm)
~1% sp2 bonded carbon
Fig. 5. Morphology of NCDs
MicroCrystalline diamonds (MCDs)
(>100nm )
<1% sp2 bonded carbon
High %Q thin films
with good thermal
transport properties
Fig. 6. Morphology of MCDs
(Yet to be published)

## Slide 5
Restrains low temperature growth, and not economic
Ideal for single production of single crystal diamond
Synthesis Temperature (1300-1700°C)
Typical Pressure (5–6.5 GPa)
Type Ia (low %N)
Type IIb (High %B)
Type IIa (Nitrogen Free)
Type Ib (Substantial %N)
Diamond Growth
Diamond Growth
HPHT#
Chemical Vapour Deposition
Natural Diamond
#HPHT: High Pressure High Temperature
Ideal for low/intermediate temperature and low pressure diamond growth
High quality (%Q) diamond thin films can be achieved
Ideal to grow UNCDs, NCDs, and MCDs at desired process parameters
*E. Salgueiredo, M. Amaral, M. A. Neto, A. J. S. Fernandes, F. J. Oliveira, and R. F. Silva, Vacuum, 85, 701–704, 2011.
where ID and IG are Raman intensities of diamond and graphitic peaks respectively.
Formula to calculate %Q of DTFs*

## Slide 6
Chemical Vapour Deposition (CVD) Method
Microwave Plasma CVD (MPCVD)
Hot Filament CVD
Electrodeless process avoiding the contamination of films due to electrode erosion.
Confinement of plasma in the
centre of the deposition chamber
Vast choice of variation in
process parameters and gas
mixtures
Unstable growth,
High possibility of contamination
Sensitive to oxidizing
and corrosive gases, limited
choice of gas mixtures
Fig. 8. Schematic of HFCVD
Fig. 7. Schematic of MPCVD
P. W. May, Philos. Trans. R. Soc. A Math. Phys. Eng. Sci., vol. 358, no. 1766, pp. 473–495, 2000.

## Slide 7
CVD Method
(Chemical Process)
P. W. May, “Diamond thin films: a 21st-century material,” Philos. Trans. R. Soc. A Math. Phys. Eng. Sci., vol. 358, no. 1766, pp. 473–495, 2000.
Input Gases
(H2 and CH4)
Plasma activation
are created
after
H2+CH4 react
Atomic hydrogen
creates reactive
sites by
abstracting
surface H
reacts with sites, adds C atom to the lattice
Same reaction on adjacent sites, with
continuous H abstraction.
Formation of sp3 bonded diamond lattice
H
Fig. 9. Illustration of diamond formation during CVD
C
C
C
C
C
C
C
C
C
C
C
C
CH3
C
CH3
CH3
H
H
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
C
CH3
CH3
C
C
C
CH3
C
C
C
C
C
C
C
C
C
CH3
CH3
H
H
H
H
H
H
H
H

## Slide 8
MPCVD Method
Process Parameters
Si substrate cleaned using Acetone
Seeded using 10% Acetone and diamond solution.
Substrate pretreatment
Time: 24hrs
Heater: 500 °C
Deposition time, Heater temp.
Substrate temp.:
~700°C
Substrate temperature
Power: 1000 W
Pressure: 40Torr
Microwave power and Gas pressure
H2: 198sccm
CH4: 2sccm
O2: 0.0-1.5sccm
Gas flowrates
Seki Technotron MPCVD system

## Slide 9
C-H-O Diagram
P. K. Bachmann, D. Leers, and H. Lydtin, “Towards a General Concept of Diamond Chemical Vapor-Deposition,” Diam. Relat. Mat., vol. 1, no. 1, pp. 1–12, 1991.
Fig. 10. C-H-O composition diagram
0.995
Expected chemical reactions
A. Inspektor, Y. Liou, T. Mckenna, and R. Messier, Surf. Coatings Technol., vol. 39/40, p. 211, 1989.
Atomic fraction of gas composition

## Slide 10
Structural Analysis
(Raman Spectroscopy)
Fig. 11. Raman spectra of DTFs prepared by varying the oxygen concentration (0.0-1.5sccm)

## Slide 11
Morphology
(Scanning Electron Microscopy (SEM) )
Fig. 12. SEM micrographs of DTFs prepared by varying the oxygen concentration (0.0-1.5sccm)
O2=1.0sccm
10µm
1µm
O2=1.5sccm
10µm
1µm
1µm
O2=0.5sccm
O2=0.0sccm
10µm

## Slide 12
Future Work
Conclusion
Successful growth of MCDs using MPCVD system
Raman analysis confirmed good quality diamond thin films
Increase in oxygen assisted in uniform diamond growth
Oxygen addition enhanced the quality of DTFs by efficient etching of sp2 bonded carbon
The oxygen should be added according to its etching efficiency of carbon
Raman thermography will be used to study the thermal conductivity of the samples.
Low temperature growth of diamond and correlate the structure and morphology to thermal transport properties

## Slide 13
Acknowledgment
Dr. Peter Thang Ha for his assistance in sample preparation
Dr. Alex Fuerbach to train me for Raman spectroscopy
Dr. Chao Shen to train me for SEM analysis

## Slide 14
ThankYou