## Slide 1
Octahedral Engineering and
Interfacial Structure of Heteroepitaxial Complex Oxides
Liang Qiao
University of Electronic Science and Technology of China
2018.08.13

## Slide 2
Welcome to Chengdu

## Slide 3
Extremely flexible crystal structure and chemical composiiton:
Perovskite Rocksalt Wurzite Flourite Rutile Corundum
CaTiO3 MgO ZnO HfO2 TiO2 a-Al2O3
Oxide materials
Fascinating functional properties unparalleled by any other materials:
1. Band gaps: IR = > visible = > UV.
2. Superconducting = > metallic = > semiconducting = > insulating.
3. Ferromagnetic = > paramagnetic = > antiferromagnetic.
4. Dielectric = > ferroelectric = > piezoelectric.
5. Coupling behaviors exceed bulk limit, e.g. multiferroic, thermoelectric (magnetic chromic)….
6. Variable valence states.
Other important technological characters:
1. widely abundant, affordable, and cost-effective
2. Non-toxic, environmentally friendly and compatible
3. Super thermal and chemical stability (and good for extreme conditions)
4. Electronics, spintronics, and photonics applications
5. Electrochemical and redox activity (for chemical and biological sensors)

## Slide 4
Sensor
Energy
Battery
IT
Examples of applications:
Complex oxides
Magnetic
Opto-
electronic
（photo)
catalytic
Electro-chemical
Electro-
chromic
Electronic
Spintronic
Thermo-
chromic
Water
splitting
Thermo-
electric
Solid-state
cooling

## Slide 5
Oxide heterointerfaces: new possibilities
Interface
Thin films:
Hwang et al, Nature Materials (2012)
2014
Physics
2000
Physics
The interface is the device
The interface is still
the device

## Slide 6
Structures of the interface
Interface
Thin films:
Lattice mismatch
Symmetry
mismatch

## Slide 7
Glazer notation: a-a-c+
“+” tilt —> in phase
“-” tilt —> out of phase
Octahedral tilting: bulk oxides

## Slide 8
Octahedral tilting: Strategy for thin films
Half-order diffraction
Coherent Bragg Rod Analysis (COBRA)
STEM-BF
May et al., Phys.Rev.B (2010)
Robust
Quick (relatively)
Straightforward
Average analysis
Not good for SL
Local analysis
Detail info
Limited by sample quality, size & modeling
Local analysis
Detail info
Limited by sample Prep, machine, operation & data analysis
Borisevich et al., ACS Nano (2010)
Feng & Yacoby et al., EES (2014)

## Slide 9
Significance in thin-film systems
He et al., Phys.Rev.Lett (2010)
May et al., Nano.Lett (2014)
Zhai et al., Nat.Comm (2015)
Boschker et al., Phys.Rev.Lett (2012)

## Slide 10
Significance in thin-film systems
Symmetry mismatch
Widely-exist
Previously-ignored
PseudoCubic/PseudoTegragonal ? Not exactly !!
Can affect physics/properties
By altering electronic structure / bonding structure
Re-investigation / new look of some questions
Ferroelectric (CaTiO3) / Ferromagnetism (LaCoO3)
General strategy: Symmetry Engineering
What we know:
What we need to do:

## Slide 11
Cubic (Pm3m)
Non-cubic
Orthorhombic (Pbnm)
CaTiO3 natural mineral
CaTiO3 – the prototype of Perovskite
Lev Perovski
(1792 – 1856)
Gustav Rose
(1798 – 1873)
Theme 1: Symmetry Engineering in Ferroelectric CaTiO3
Notes: Russian mineralogist

## Slide 12
Crystal structural and octahedral distortions
Bulk CaTiO3 @ room temperature
Glazer notation: a-a-c+
“+” tilt —> in phase
“-” tilt —> out of phase
a
b
a
b
c
c
Pbnm
a-a-c+
I4/mcma0a0c-
Pm3m
a0a0a0
Tilting is very strong !

## Slide 13
Polar
distortion
Octahedral
distortion
t < 1
Competing mechanisms
Incipient ferroelectricity

## Slide 14
Choi et al, Science (2004)
Epitaxial strain – enhancing ferroelectricity
BaTiO3
Fong et al, Science (2004)
PbTiO3
Hanei et al, Nature (2004)
SrTiO3

## Slide 15
ab-ePbnm
c-ePbnm
orthorhombic
nonpolar
Pm
P21
monoclinic
polar
Pmc21
Pmn21
orthorhombic
polar
CaTiO3
Can CaTiO3 be ferroelectric ?
Eklund et al, PRB (2009)

## Slide 16
LSAT
Cubic
Pn3mZ (a0a0c0)
a = 3.868 Å
Orthorhombic
Pbnm (a-a-c+)
apc = 3.860 Å
NdGaO3
Strategy: epitaxial strain and symmetry control
NGO
LSAT

## Slide 17
Structural characterization
NGO
CTO
LSAT
CTO
Fully strain and coherent film on both substrate
Film on NGO shows lower symmetry
HAADF-STEM
XRD-OOP & RSM
202
022
XRD-IP (202)PC scan
 | aPC (Å) | bPC (Å) | cPC (Å)
LSAT | 3.868 | 3.868 | 3.801
NGO | 3.855 | 3.865 | 3.816

## Slide 18
LSAT
(204)C
(024)C
(024)C
_
(204)C
_
Symmetry reduction
Film on LSAT doesn’t show obvious monoclinic, near a tetragonal structure.
NGO
Film on NGO show monoclinic (triclinic) distortion, with beta ~91.15 deg.
(206)O
(444)O
(602)O
(444)O
_

## Slide 19
CaTiO3/NGO: a-b+c-
Synchrotron half-order diffraction
CaTiO3/LSAT: a+a+c-(a+a+c0)

## Slide 20
Quantification of octahedral tilts
Rondinelli et al, MRS Bulletin (2012)
a = 4.6
b = 5.4
g = 0.9
a = 7.1
b = 10.2
g = 2.3
NGO a-b+c-
LSAT a-b+c-

## Slide 21
ABF-STEM interface symmetry
CaTiO3 on NGO
CaTiO3 on LSAT
interface
interface

## Slide 22
Ferroelectric and dielectric properties
Strained CaTiO3 is ferroelectric
Film on LSAT show Tc of ~ 140 K and in-plane remnant polarization of 5 mC/cm2
Monoclinic octahedral distortion suppress the ferroelectric transition

## Slide 23
a-b+c-
a+a+c0
a+a+c-
Landua free energy:
LGD modeling: S-T phase diagram

## Slide 24: LaCoO3: unconventional magnetism
Yamaguchi et al., Phys.Rev.B (1996)
Bulk
Epitaxial film
Fuchs et al., Phys.Rev.B (2008) and (2009)
Fita et al., Phys.Rev.B (2008)
Nanoparticle & nanowires
Theme 2: Symmetry Engineering in epitaxial Magnetic LaCoO3

## Slide 25: LaCoO3: unconventional magnetism
Chio et al., Nano.Lett (2012)
Biskup et al., Phys.Rev.Lett (2014)
Chio et al., Chem.Mater. (2014)

## Slide 26
Magnetic phase diagram for ultra-thin LaCoO3 films
5 K
5 K
100 ~ 300 K
Spin ordering
S
1.5
1.1
0.7
0.6 (bulk)
Spin transition
Thickness dependent magnetism for ultra-thin epitaxial LaCoO3
Why thinner films lose magnetism?

## Slide 27
Interfacial structure probed by synchrotron XRD
15 uc
5 uc
15 uc
5 uc film is pseudotetragonal, but 15 uc film is monoclinic
Symmetry change reflection modification of octahedral tilting structure

## Slide 28
a = 7.2 ± 0.5°
g = 0.6 ± 0.3°
a = 0.5 ± 0.5°
g = 0.3 ± 0.3°
5 uc
15 uc
[001]
[110]
a-a-c0
a-a-c0
Quantification of CoO6 octahedral tilts

## Slide 29
[110] Inverted ABF
15 uc
[010] STEM-HAADF
[110] STEM-HAADF
Direct imaging tilts by STEM

## Slide 30
Different octahedral behavior
5 uc
15 uc
Gradual tilt evolution for 15uc film
Octahedral evolution at the heterojunction

## Slide 31
5 uc, a-a-c0
15 uc, a-a-c0
Bulk, a-a-a-
Octahedral tilt and distortion impact magnetic properties
Magnetic No Yes No
Sterbinsky et al., Phys.Rev.B (2012)
EXASF
Yes No
Local octahedral and bonding structure

## Slide 32
t2g
eg
t2g*
eg*
5uc 15uc Bulk LCO/STO LCO/LAO
The key is octahedral volume instead of unit cell volume
Correlation of tilting and magnetism

## Slide 33
[LCO(5uc)/STO(5uc)]3 vs. LCO(15uc)

## Slide 34
Symmetry mismatch at perovakite based heterointerface is widely exist, and should not be ignore
Octahedral mismatch/rotation can impact properties of materials (ferroelectricoty for CaTiO3 and magnetism for LaCoO3).
Symmetry engineering might to work as a new and general strategy to control the functional properties of these materials
Summary

## Slide 35
J. H. Jang, A. Borisevich (TEM), D. J. Singh (theory), Z. Gai (SQUID), R. K. Vasudevan, A. Tselev, A.P. Baddorf (STM), D.B. Geohegan, S.V. Kalinin, H.M. Meyer, H.M. Christen, M.D. Biegalski
Acknowledgements
PNNL: S.A. Chambers, P.V. Sushko, T.C. Droubay, T.C. Kaspar, V. Shutthanandan, T. Varga, M.E. Bowden, G.J. Exarhos, R. Colby, B. Kabius
ANL: Zhenxing Feng, H. Zhou, S.M. Heald,
SSRL: M. Apurva
Penn State: Yijia Gu and Long-qing Chen
Sarah Heigh, Andrew Thomas
Thanks !!