## Slide 1
Electric Field-Tuned Topological Phase Transition in Ultra-Thin Na3Bi
Mark Edmonds
Lecturer
ARC DECRA Fellow
School of Physics and Astronomy

## Slide 2: Acknowledgements
Monash University (STM/ARPES/XPS)
Prof. Michael S. Fuhrer
James Collins
Chang Liu
Dr Jack Hellerstedt
Australian Synchrotron (ARPES/XPS)
Dr Anton Tadich
Advanced Light Source (ARPES)
Dr Sung-Kwan Mo
Dr Hyejin Ryu
Dr Shujie Tang
Singapore University of Technology and Design (Theory/DFT)
Dr Shengyuan Yang
Weikang Wu
National University of Singapore (Theory/DFT)
Dr Lídia C Gomes
Dr João NB Rodrigues
Prof. Shaffique Adam

## Slide 3: Outline
Introduction
- 2D Topological Insulators.
- Electric-field induced topological phase transitions.
Results
- Ultra-thin Na3Bi – Growth and Electronic Properties Characterization
“Platform for a topological transistor”

## Slide 4: 2D Topological Insulators
Graphene
py
px
E
Spin-orbit
coupling
Energy
Bulk Gap
eV
HgTe Quantum Wells
HgxCd1-xTe
HgxCd1-xTe
HgTe
d
d<6.3 nm
Insulator
d>6.3 nm
QSH Insulator
Bernevig et al, Science 314, 1757 (2006)
Bulk Gap
10meV
Konig et al, Science 318, 766 (2007)
Band Inversion
Bulk energy gap with 1D spin-filtered edge states
Kane and Mele, PRL 95, 226801 (2005)

## Slide 5: Wide Bandgap 2D Topological Insulators
How do you turn off a QSH insulator device?
STM/ARPES
Bismuthene EG~0.7 eV Reis et al., Science (2017)
ML WTe2 EG~50 meV Tang et al., Nature Physics (2017)
Metallic Conduction
On
On
EF
Transport
S. Wu et al., Science 359, 76 (2018)
QSH up to 100K in WTe2

## Slide 6: Electric Field Tuned Topological Phase Transition ‘A Topological Transistor’
Dirac Semimetal
QSH Insulator
On
On
0
EC
Field Strength
Off
Topological Dirac semimetals:
Na3Bi: Sci. Rep 5, 14639 (2015)
Quantum spin Hall insulators: 1T’ TMDs: Science 346, 1344 (2014)
EF
EF
EF
Regular Insulator

## Slide 7: Na3Bi: A 3D Topological Dirac Semimetal
Z.K. Liu et al., Science 343, 864 (2014)
Only 2 bands Na 3s and Bi 6p lie near EF
Rotation symmetry protects against gap formation leading to Dirac nodes centred at ±kD
Z. Wang et al., PRB 85, 195320 (2012)
C3 point group

## Slide 8: Dirac Semimetals in 2D
What happens when Na3Bi is confined to 2D?
Spin-Orbit
Coupling
Bulk Na3Bi
kz
Quantum
Confinement
Ultra-Thin Na3Bi
Is few-layer Na3Bi a wide bandgap 2D topological or conventional insulator?

## Slide 9: DFT: Monolayer and Bilayer Na3Bi are TI’s (quantum spin Hall)
Na3Bi Edges
0.30 eV
ML
BL
0.22 eV
Na3Bi Edges
Monolayer
Bilayer
C. Niu et al., PRB 95, 075404 (2017)
Collins et al., arXiv:1805.08378

## Slide 10: Is a topological phase transition expected in ultra-thin Na3Bi?
DFT as a function of E
Collins et al., arXiv:1805.08378

## Slide 11: Key Questions
Is it possible to experimentally isolate ultra-thin Na3Bi?
Is it a wide bandgap 2D topological or conventional insulator?
Can an electric field induce a topological phase transition?

## Slide 12: Molecular Beam Epitaxy Growth of Na3Bi
Substrate
RHEED
RHEED
Turbo
Bi
Na
Shutter
Growth
Na:Bi (10:1)
TNa<TSubstrate<TBi
RHEED
LEED
XPS
Na3Bi is free-standing on Si substrate

## Slide 13: Scanning Tunnelling Microscopy and Spectroscopy
e-
e-
I
V
Visualizing Atomic Structure
x
y
Measure: I as function of V
Determine:
Probing Local Density of States

## Slide 14: Angle-Resolved Photoelectron Spectroscopy
Measure: Ek and 
Determine:
Advanced Light Source (Berkeley, USA)
(EDC’s as a function of hv)

## Slide 15: Ultra-thin Na3Bi: Opening a bandgap
70nm
Valence Band
Conduction Band
ML
BL
Experiment
GGA w/
Na(2) vacancy
GGA Pristine
Bandgap of ML and BL >300 meV; much greater than kT at room temp

## Slide 16: Ultra-thin Na3Bi: ARPES
DFT
ML
BL
70nm
No kz dispersion – Electronically 2D

## Slide 17: Key Questions
Is it possible to experimentally isolate ultra-thin Na3Bi?
Is it a wide bandgap 2D topological or conventional insulator?
Can an electric field induce a topological phase transition?

## Slide 18: Confirming Ultra-Thin Na3Bi is a 2D Topological Insulator
Non-trivial 1D edge state, consistent with a 2D Topological Insulator

## Slide 19: Key Questions
Is it possible to experimentally isolate ultra-thin Na3Bi?
Is it a wide bandgap 2D topological or conventional insulator?
Can an electric field induce a topological phase transition?

## Slide 20: Electric Field: K Dosing
Bandgap (eV)
Exp. Model
Measured
Inferred
Gap is reduced with E-field
Does gap completely close or reopen?

## Slide 21: Electric Field: STM tip-sample distance
1.45 nm (0.828 V/nm)
1.075 nm (1.12 V/nm)
1.02 nm (1.18 V/nm)
10 pA
600 pA
Increasing Tunnelling Current

## Slide 22: Electric field-tuned bandgap and topological transition
ML
BL

## Slide 23: Conclusions
PhD and Postdoc positions available
contact mark.edmonds@monash.edu
Publications on thin film Na3Bi
Growth of Na3Bi: Hellerstedt, et al., Nano Letters 16, 3210 (2016)
F4-TCNQ doping of Na3Bi: Edmonds et al., ACS Appl. Mat. Int. 8, 16412 (2016)
Charge puddling in Na3Bi: Edmonds et al., Science Advances 3, eaao6661 (2017)
Gating Na3Bi on SiO2: Hellerstedt et al., PRMaterials 1, 054203 (2017)
Temperature-dependent n-to-p transition: Liu et al., PRB 96, 235412 (2017)
Large area epitaxial ultra-thin Na3Bi with bulk bandgap >300 meV (2D Topological Insulator)
Electric field induced transition
Topological Insulator (>300 meV) Semi-metal Conventional Insulator (100 meV)
“Platform for a topological transistor”
Electric field-tuned topological phase transition in ultra-thin Na3Bi: arXiv:1805.08378

## Slide 24: Gap closing not explained by tip induced band bending
Battisti et al., PRB 95, 235141 (2017)
Electric field in poorly screened electronic materials (i.e. low-doped semiconductors) can penetrate sample
TIBB observed on (Sr1−xLax )2IrO4

## Slide 25: Converting tunnelling current into tip-sample distance (electric field)
e-
e-
I
V
x
s
Measure relative changes in height
Determine absolute distance, s (Point contact & Mirror Potential)
Barrier height
Determine potential difference,  (Tip & Sample Work function)
(Kelvin Probe)
ln(I) vs z (Linear)
Non-linear
(Mirror Potential)

## Slide 26: Electric Field: STM tip-sample distance
), 1.075 nm (1.12 V/nm), and 1.02 nm (1.18 V/nm)
1.45 nm (0.828 V/nm)
1.075 nm (1.12 V/nm)
1.02 nm (1.18 V/nm)