## Slide 1
Sulfides, Surfaces and Synchrotrons
A/Prof Sarah Harmer
Institute for Nanoscale Science and Technology
College of Science and Engineering
NSRRC

## Slide 2: Transition Metal Sulfides
Sphalerite,
(Zn,Fe)S
Chalcopyrite, CuFeS2
Molybdenite, MoS2
Pyrite
FeS2
Molybdenite is used as a
dry lubricant
Li/FeS2 low T batteries

## Slide 3
Grinding
Production of fractured & cleaved surfaces
Exposure to air, water, activators
Flotation
Exposure of fracture surfaces to water, collectors, depressants, activators and foaming agents.
Roasting & Smelting Or Heap Leaching
Low grade ores
Electrowinning
Extraction of Metals from Sulfide Ores

## Slide 4
Grinding
Production of fractured surfaces
Exposure to air, water, activators
Flotation
Exposure of fracture surfaces to water, collectors, depressants, activators and foaming agents.
Roasting & Smelting Or Heap Leaching
Low grade ores
Electrowinning
Extraction of Metals from Sulfide Ores

## Slide 5
Grinding
Production of fractured surfaces
Exposure to air, water, activators
Flotation
Exposure of fracture surfaces to water, collectors, depressants, activators and foaming agents.
Roasting & Smelting Or Heap Leaching
Low grade ores
Electrowinning
Extraction of Metals from Sulfide Ores
Barrick's Pierina Mine in Peru

## Slide 6
Grinding
Production of fractured surfaces
Exposure to air, water, activators
Flotation
Exposure of fracture surfaces to water, collectors, depressants, activators and foaming agents.
Roasting & Smelting Or Heap Leaching
Low grade ores
Electrowinning
Extraction of Metals from Sulfide Ores
Mt Lyell and Queens river, Tasmania

## Slide 7: The Challenge
Examples:
Composite Minerals
  Incomplete liberation
  Reactions with liberated minerals, i.e Cu Activation
  Regions of differing chemistry
  Texture
  Particle shape
Galvanic mineral-mineral interactions
  Change oxidation and dissolution
  processes
Minerals are inherently heterogeneous, impacting their wettability, processing and separation
Locking of particles
Impact
Compression
T.G. Vizcarra, S.L. Harmer, E.M. Wightman, N.W. Johnson, E.V. Manlapig (2011). Minerals Engineering, 24(8), 807-816.

## Slide 8: The Challenge
Examples:
Composite Minerals
  Incomplete liberation
  Reactions with liberated minerals, i.e Cu Activation
  Regions of differing chemistry
  Texture
  Particle shape
Galvanic mineral-mineral interactions
  Change oxidation and dissolution processes
Minerals are inherently heterogeneous, impacting their wettability, processing and separation
Galvanic Interactions
Chalcopyrite
Pyrite
Al-Harahshesh et al. Int. J. Min Proc. 2006, 80, p 205
Liu Qing You, Environmental Geology, 2007, 52, p11

## Slide 9
Surface Analytical Techniques
Low Energy Electron Diffraction (LEED)
Low Energy Ion Scattering (LEIS)
Scanning Tunneling Microscopy (STM)
Atomic Force Microscopy (AFM)
Photoemission Spectroscopy & X-ray Absorption Spectroscopy
Time of flight Secondary Ion Mass Spectrometry (ToF-SIMS)
nano-Secondary Ion Mass Spectrometry (nanoSIMS)
Si (111) 7x7 reconstruction

## Slide 10
Fractured and Cleaved Mineral Surfaces
ZnS (110)
Cleavage
ZnS (110)
CuFeS2
Fracture
CuFeS2

## Slide 11: God made solids, but surfaces are the work of the devil Wolfgang Pauli
Surfaces are the playgrounds for
solid state physics
E.W. Plummer

## Slide 12
Surface Analytical Techniques
Photoemission Spectroscopy & X-ray Absorption Spectroscopy
Photoemission Electron Microscopy (PEEM)
Scanning Photoemision Electron Microscopy (SPEM)
Scanning Transmission X-ray Microscopy (STXM)
Coherent Diffraction Imaging (CDI)
Time of flight Secondary Ion Mass Spectrometry (ToF-SIMS)
nano-Secondary Ion Mass Spectrometry (nanoSIMS)
Chemical Sensitivity
Spatial Resolution (nm)
IR Micro
Raman Micro
XPS
XFM
PEEM
SEM
TEM
SPM
1000
100
10
1
0.1
Light Micro
STXM
Nano
SIMS

## Slide 13
Electronic Structure of 3d Transition Metal Compounds
Development & Application of in situ Microspectroscopic Analysis of Materials using Synchrotron Radiation
Bio-flotation: A Green Mining process
Fundamental Supports the Applied
*K. Sato, Y. Harada, M.Taguchi, S. Shin, and A.Fujimori ICTMC16 Berlin 2008
*

## Slide 14
Synchrotrons
NSRRC
Australian
Synchrotron
SLS
CLS

## Slide 15
XPS and NEXAFS @ the AS
UHV Fracture Chamber
90-2600eV photon source
Beamline energy resolution of less than 0.1 eV across 3d transition metal 2p lines
Linear and circular polarization
In situ fracture and dosing
Notes: This is the ASRP endstation currently ** in Taiwan. Its capable of both XAS and XPS, it has pre chamber for deposition **** that should be fited with a LEED system in the not to distant future.
It has a cnetral exchange chamber UFO, with load lock, magazine for storage and an UHV fracture chamber for sample prep. The analystical chamber is fitted with a flood gun Al x-ray gun and e analysers.
This equipmetn was used to study sphalerite

## Slide 16
Chalcopyrite, CuFeS2
Polar
Non-polar
(012)
(11-2)
Harmer, S.L., Pratt, A.R., Nesbitt, H.W. and Fleet, M.E. (2004) American Mineralogist, 89 (7), 1026.
G.Donnay, L.M. Corliss, J.D.H. Donnay, N. Elliot and J.M. Hastings: Phys. Rev. 112 (1958) 1917.
Chalcopyrite is the most common & widespread Cu containing mineral found in sulfide deposits.
Structure: chalcopyrite
Unit cell: tetragonal
Bond lengths: Cu-S: 2.302 Å
Fe-S: 2.2566 Å
Bonding: Covalent
Band gap: 0.6 eV (semiconductor)
Local magnetic moment: 3.85 µB
Cleavage: Poor along (012) & (11-2)
Fracture: Conchoidal

## Slide 17: S 2p SXPS spectra from UHV fractured CuFeS2
Surface core level shift formed as a result of fracture
Surface reconstruction to form S dimers
High binding energy tail resulting from ligand to metal charge transfer S 3p - Fe 3d
S 2p
260 eV
810 eV
400 eV
CuFeS2

## Slide 18
S 2p
1hr
pH 4
0.1M KNO3
Tail locked to bulk S2-
S 3p → Fe 3d
NEXAFS S L2,3
S 2p XPS spectra of Chalcopyrite

## Slide 19: XPS of High Spin Transition Metal 2p lines
Chalcopyrite (CuFeS2), FeIII in tetrahedral co-ordination
Bornite (Cu5FeS4), FeIII in tetrahedral and trigonal co-ordination
Accurate fits of the XPS Fe 2p cannot be determined without SRXPS.
Gupta and Sen’s multiplet splitting calculations considered free ions

## Slide 20: TT-Mulitplets: Multiconfigurational Self-consistent Field

## Slide 21: Chalcopyrite Fe 2p and L2,3
Tetrahedral |  |  |  |  |  |  |  |  | 
Slater Integral Reduction | Spin Orbit Coupling | Crystal Field Parameter (10 Dq) (eV) | Charge Transfer Parameters (eV) |  |  |  |  | Lorentzian Broadening | Guassian Broadening
 |  |  | Delta | Udd | Upd | T(eg) | T(t2g) |  | 
0.7 | 1 | -1.4 | -4 | 3 | 4 | 1 | 2 | 0.2 | 0.3

## Slide 22
Nano-Spectroscopy
Scanning Photoemission Spectroscopy (SPEM)
Photoemission Electron Microscopy (PEEM)
Scanning Transmission
X-ray Microscopy (STXM)

## Slide 23: XPEEM
X-ray Photoemission Electron Microscopy
  micro XPS
Photoemission Electron Microscopy (10 nm)
  micro XAS
  magnetic linear and circular dichroism
Low Energy Electron Microscopy (< 5nm spatial resolution)
Micro Low Energy Electron Diffraction
Micro Photoelectron Diffraction
Auger Emission Electron Microscopy

## Slide 24: Leached Chalcopyrite
S 2p fov =10mm
A polished sample of chalcopyrite was leached at pH 1 for 0-30 mins and analysed
using XPEEM.

## Slide 25
O
Sn
CuFeS2 (left) in contact with CuS (right)
Leached at pH 1 for 30 min
Sn
CuFeS2 Leached at pH 1 30 min
FeIII
600
500
400
300
200
100
720
710
700
Photon energy (eV)
706
716
726
100
300
400
200
Intensity
500
600
Fe L2,3
140
120
100
80
60
102
100
98
96
94
92
90
Kinetic energy (eV)
Leached Chalcopyrite (CuFeS2) in contact with Covellite (CuS)

## Slide 26
Analysis of mixed sulphide samples using PEEM
FOV 450μm

## Slide 27
Chalcopyrite,
CuFeS2
Hematite,
Fe2O3
Pyrite,
FeS2
Analysis of mixed sulphide samples using PEEM

## Slide 28
Scanning Transmission X-ray Microscopy (STXM)
X-rays focused using zone plate optics. The sample is rastered at the focus and the transmitted intensity is measured.
Chemical/elemental information is obtained by determining the X-ray absorption by the sample (NEXAFS). Spatial resolution limit of 20nm.
NEXAFS spectra a fixed positions or single image at fixed energy
Samples must be transparent to X-rays energies of interest

## Slide 29: In situ Electrochemical Cell for STXM

## Slide 30: In situ Electrochemical Cell
16 micron
24 micron

## Slide 31
Cu(I)
Cu(0)
Cu(II)

## Slide 32
Sample Preparation
Samples must be thin enough to allow transmission of X-rays at the desired energy.
50-300 nm for Carbon K edge
Up to 1 µm for Copper L edge
Liquid samples are fixed between two windows which are sealed with epoxy resin.
Right: An image of chalcocite in a liquid cell taken at the copper edge. Dark blotches indicate leaching of copper from larger particles.
Middle: Two SiN2 windows are used to hold a liquid sample.
Left: A sample is attached to the holder inside the endstation.
Wet or Dry: does it make a difference to surface chemistry?

## Slide 35: Chalcocite, pH 4 H2SO4 – wet sample
Djurleite – Cu31S16
– Cu+60Cu2+2S2-32
Fuerstenau, M. C., Jameson, G. J., & Yoon, R.-H. (2007). Froth flotation: a century of innovation: Society for Mining, Mettalurgy, and Exploration. pp 251

## Slide 36
Fitted 3D image with 4 spectra:
  Chalcocite, Cu2S
  Djurleite, Cu31S16
  Cu(I) pre-edge feature
  Cu(II)-oxide
Blue = Chalcocite + pre-edge
Green = Djurleite
Red = Cu(II)-oxide
Results: Chalcocite + pH 4 H2SO4 – wet sample

## Slide 37: Conclusions
STXM has allowed us to identify the fine structure of Cu(II) peak which is otherwise elusive due to finite resolution
Fitting with a linear combination of spectra extracted from 3D images shows the distribution of species
The pre-edge feature is clearly Cu(I) sulfide – evident due to the energy and relative intensity of the peak
The change in relative intensity of the pre-edge peak is most likely from distortions in spectra caused by sample thickness
There is evidence of djurleite (Cu31S16) in the chalcocite sample in solution, but not in the dry sample

## Slide 38: Minerals Processing
Hydrophobic Particles
Hydrophilic Particles
Air Bubbles
Bacterial cell
Bio-flotation is a ‘green’ alternative
Bacterial cells and extracellular polymeric substances (EPS) used to modify surface chemistry of minerals
  Direct contact
  Indirect contact
  Indirect non-contact
Bacterial Extracellular Polymeric Substances play a vital role in surface modification
μ-Froth Flotation

## Slide 39: Leptospirillum Ferrooxidans
Spiral shaped with 0.3-0.5microns in width and 0.9-3microns in length
Chemolithoautotroph
Acidophilic
Found deep underground at mine sites
Contributes to acid mine drainage
Oxidation of Iron in aerobic conditions
https://sites.google.com/site/fmssgrade12biology/use-of-microbes-in-metal-ores
Coram, N. J. and D. E. Rawlings (2002). Applied and Environmental Microbiology 68(2): 838-845. Vilinska, A. and K. H. Rao (2008Transactions of Nonferrous Metals Society of China 18(6): 1403-1409
Notes: Aerobic Iron-oxidising bacteria which can convert metals into a soluble form. Have been found to be the primary iron-oxidizers in industrial continuous – flow biooxidation tanks. They are the dominating bacteria in biooxidation field as the high ferric-ferrous iron ratio does not inhibit the species. Important contributors in acid mine drainage.
Gram negative and spiral shaped with 0.3-0.5 microns in width and 0.9-3.0 microns in length. Chemolithautotrophic: this means that the bacteria are microbes that utilize chemicals (chemo) from the bedrock (litho) as an energy source for making their own (auto) food (trouph). Carbon fixing through ferrous iron as their electron donor and oxygen as the electron acceptor. This makes them metabotically restricted. Found deep underground in the mines enveloped in a pink biofilm which then floats on the surface of the flowing water through the mine. Coram, Nicolette J. Molecular Relationship between Two Groups of the Genus Leptospirillum and the Finding that Leptospirillum ferriplium sp. nov. Dominates South African Commercial Biooxidation Tanks That Operate at 40ºC. Applied and Environmental Microbiology vol 68(2) February 2002. 838-845.
L.F can be selectivly attached to sulphides, esentually modifying the surface of the mineral. Does not oxidize sulphur. Vilinska, A. and K. H. Rao (2008). "< i> Leptosririllum ferrooxidans</i>-sulfide mineral interactions with reference to bioflotation nad bioflocculation." Transactions of Nonferrous Metals Society of China 18(6): 1403-1409.
Life cycle and iron cycle in soil??

## Slide 40: Leptospirillum Ferrooxidans
https://sites.google.com/site/fmssgrade12biology/use-of-microbes-in-metal-ores
Coram, N. J. and D. E. Rawlings (2002). Applied and Environmental Microbiology 68(2): 838-845. Vilinska, A. and K. H. Rao (2008Transactions of Nonferrous Metals Society of China 18(6): 1403-1409
1
2
3
4
5
Spiral shaped with 0.3-0.5microns in width and 0.9-3microns in length
Chemolithoautotroph
Acidophilic
Found deep underground at mine sites
Contributes to acid mine drainage
Oxidation of Iron in aerobic conditions
Notes: Aerobic Iron-oxidising bacteria which can convert metals into a soluble form. Have been found to be the primary iron-oxidizers in industrial continuous – flow biooxidation tanks. They are the dominating bacteria in biooxidation field as the high ferric-ferrous iron ratio does not inhibit the species. Important contributors in acid mine drainage.
Gram negative and spiral shaped with 0.3-0.5 microns in width and 0.9-3.0 microns in length. Chemolithautotrophic: this means that the bacteria are microbes that utilize chemicals (chemo) from the bedrock (litho) as an energy source for making their own (auto) food (trouph). Carbon fixing through ferrous iron as their electron donor and oxygen as the electron acceptor. This makes them metabotically restricted. Found deep underground in the mines enveloped in a pink biofilm which then floats on the surface of the flowing water through the mine. Coram, Nicolette J. Molecular Relationship between Two Groups of the Genus Leptospirillum and the Finding that Leptospirillum ferriplium sp. nov. Dominates South African Commercial Biooxidation Tanks That Operate at 40ºC. Applied and Environmental Microbiology vol 68(2) February 2002. 838-845.
L.F can be selectivly attached to sulphides, esentually modifying the surface of the mineral. Does not oxidize sulphur. Vilinska, A. and K. H. Rao (2008). "< i> Leptosririllum ferrooxidans</i>-sulfide mineral interactions with reference to bioflotation nad bioflocculation." Transactions of Nonferrous Metals Society of China 18(6): 1403-1409.
Life cycle and iron cycle in soil??

## Slide 41: Extracellular Polymeric Substances
Attachment can assist with dissolution of metals
EPS composition: Polysaccharides, Proteins, Free fatty acids
  complex to form biofilm
  influenced by growth conditions
Proteins increase hydrophobicity
Polysaccharides decrease hydrophobicity, with potential of selectivity
Dwyer, R., et. al (2012) Mineral Processing and Extractive Metallurgy
Govender, Y. & Gericke, M. Minerals Engineering 2011, 24, 1122-1127.
Liu, Q.et. al (2000) International Journal of Mineral Processing
Subramanian, S. et. al (2003) International Journal of Mineral Processing
Biofilm formation from Leptospirillum ferrooxidans on Chalcopyrite

## Slide 42
Flotation Summary
Cells with PIPX collector
EPS supernatant at 48 and 72 hours
Attachment Summary
L.f selectively attaches to pyrite
Selective attachment from 0 – 168 Hrs
EPS/biofilm formation at 48 Hrs
Interaction between Leptospirillum ferrooxidans and
CuFeS2 and FeS2
L.f attachment at 48 Hr to Chalcopyrite (A) and Pyrite (B)
A
B
Belinda Bleeze, Jing Zhao and Sarah L. Harmer (2018) Selective Attachment of Leptospirillum Ferrooxidans for Separation of Chalcopyrite and Pyrite through Bio-Flotation, Minerals, 8, 86.

## Slide 43: XPEEM Iron L2,3 NEXAFS
Changes in the ratio of Fe (II): Fe (III) at different exposure times
Reasonable distribution of Fe (II)
Peak | Energy | Functionality
a | 706.8 – 707.7 | Fe L3: Transitions from Fe 2p to Fe 3d
b | 708 - 709 | Transitions from Fe 2p to: Fe 3d-S 3p hybridized states Fe oxides and hydroxides
c | 712 | Pyrite: transitions from Fe 2p to: Fe 4sp - S 3p ; and Fe 4p -S 3p hybridized states
HH Media 48 Hr
a
b
EPS – fresh 48 Hr
a
b
Kalegowda, Y. et. al (2015), Surface Science
Acres, R. G., et. al (2010) Journal of synchrotron radiation
EPS – 7 days
a
b

## Slide 44: Copper NEXAFS
Copper (II) present in EPS at 48 Hrs
Distribution changes with exposure condition
EPS – fresh 48 Hr
a
b
Peak | Energy | Functionality
a | 930 – 931.2 | Cu (II) Cu (II) oxidation products (CuO)
b | 932.3 – 932.6 | Cu (I) in Cp, Cu L3 in metallic standards
Kalegowda, Y., et. al (2015) Surface Science Acres, R. G., et. al (2010) Journal of synchrotron radiation
Todd, E., et. al (2003) Geochimica et Cosmochimica Acta
EPS – frozen 48 Hr
a
b
EPS – 72 Hr
HH Media – 48 Hr
b
b

## Slide 45: Carbon K edge NEXAFS
Increase of COOH (polysaccharides) over time
Peak | Energy | Functionality
a | 285 – 285.2 | Aromatic C-H or C=C
b | 287.3 – 287.5 | Aliphatic C
c | 288.4 – 288.8 | COOH carboxyl
Singh, B., et. al (2014) Organic Geochemistry Boese, J., et. al (1997) Journal of Electron Spectroscopy and Related Phenomena
EPS – frozen 48 hr
a
b
c
Notes: K edge comes from the s orbital, meaning there is no distinct directionality. This makes it possible to fit the spectra

## Slide 46
In situ STXM analysis of L.f on pyrite
Liquid cell allows for C K edge NEXAFS analysis of hydrated EPS
1 μm
30 μm

## Slide 47
Conclusions
Indirect – contact mechanism of attachment
  Irreversible attachment
  Presence of EPS
Iron, copper and oxygen NEXAFS all indicate the presence of metal oxides
Oxy-hydroxide formation in the absence of cells
EPS oxidises FeII to Fe3+ and removes it from the surface
EPS acts as a depressant and should be further investigated as a replacement for cyanide
Increasing presence of COOH and iron oxyhydroxides correlates the increased suppression of pyrite
Most changes/differences occur within 48 h
  early biofilm formation (attachment studies)
Fe
Bacterial cell
Fe2+
Fe3+
S2O32-
Bulk leaching solution
(O2, Fe2+, Fe3+, SO42-)
Reaction Space
(EPS with complexed Fe3+ ions)
CM
PS
Sulfur globuli
OM
Altered surface chemistry of mineral
A

## Slide 48: Acknowledgements
Connor Retallick
Zoe Pettifer
Belinda Bleeze
Prof Adam Hitchcock
Norcada Inc
National Synchrotron Radiation Research Centre (NSRRC)
BL05B2 Beamline Scientists
Australian Research Council
  Future Fellowship
  Travel Grant
Adelaide Microscopy
Ruth Williams, Lyn Waterhouse and Ken Neubauer
Australian Microscopy & Microanalysis Research Facility
Australian Nanotechnology Network
Australian Synchrotron
ELETTRA

## Slide 49: NCRIS Funding
Flinders University will acquire a Photoemission electron microscope in the next year.
Positions will be advertised:
  A Flagship Engineer with experience in PEEM and XPS
  Solid State physicist with experience in Density Functional Theory calculations

## Slide 51: Lamngmuir dosing of in situ fractured Chalcopyrite
A
B
C
D
E
F
hν = 260 eV
hν = 846 eV