## Slide 1: Tuning the Electronic Structure of NiO by Li doping for Electrocatalytic Water Oxidation
Kelvin HL Zhang
Xiamen University
kelvinzhang@xmu.edu.cn

## Slide 2
Xiamen, China
beach
The campus
Xiamen
Taiwan
Australia
Beijing

## Slide 3
XIAMEN
UNIVERSITY
3
Research in my group
Optoelectronic,
data storage devices
Clean energy materials
Transition metal d orbitals
partially filled d orbitals
electron correlation
multiple oxidization states
Wide bandgap, mobility, doping
OER
ORR
electrocatalyst
Photoelectrochemistry
Optical, electronic and magnetic properties of solid materials
Electro
catalysis
Super-conductor
Photo-elec
trocatalysis
Lithium ion battery
Giant magneto
resistance
Electronic Structure
Transparent
Oxide Semicond.
CB
VB
Eg
low bandgap, mobility, kinetics

## Slide 4
Energy and Environmental issues
Quality of life and energy
Pasten and Santamarina, energy policy 49, 468 (2012)
4

## Slide 5
Energy crisis
雾霾
酸雨
U.S. Energy Information Administration 2017
Energy and Environmental issues
Air pollution
Globe warming
Source: https://www.eia.gov/
5

## Slide 6
Electrochemical energy conversion & storage
6

## Slide 7
7
PV-Electrolysis
Photoelectrochemical
Photo-catalytic
Lewis and Nocera,
PNAS 103, 15729 (2006)
PV
Electrolysis and photochemical water splitting
Cathode: hydrogen evolution reaction (HER):
2H+ + 2e- → H2 E = 0 V (vs RHE)
Anode: oxygen evolution reaction (OER):
2H2O → O2 + 4H+ + 4e- E = 1.23 V
but slow kinetics with high overpotentials!
OER
HER
Anode Cathode
Cost-effective catalysts needed!

## Slide 8
Correlation between catalytic activity and electronic structure
IrO2 , RuO2 (Ir: $31,040/kg)
Transition metal oxides (Ni $5/kg, Co, Fe, Mn)
Suen, et al., Chem. Soc. Rev. 46, 337 (2017)
low cost, effective?
Seh et al., Science 355, 146 (2017)
Catalyst development strategies
Nanostructures
Pt3Ni
Pt
d center
Pt3Ni(111)
The activity strongly correlates with surface electronic structure
How do we design catalysts?
What determines the intrinsic activity of an electrocatalyst?
8

## Slide 9
Correlation between electronic structure and catalytic activity
Adsorptive property of a catalyst = Catalytic activity
Not so strong, not so weak = best (阴阳平衡)
Elementary steps in heterogeneous catalysis
Adsorption of reactants
Reaction of adsorbed intermediates
Desorption of products
B. Hammer et al., Advances in catalysis, 45(2000), 71-129
Norskov et al. Nature Chemistry 1 (2009), 37-46
9

## Slide 10
Correlation between electronic structure and catalytic activity
B. Hammer et al., Advances in catalysis, 45(2000), 71-129
Norskov et al. Nature Chemistry 1 (2009), 37-46
A higher d-band center (smaller Ed - EF) results in stronger bonding.
A lower d-band center (larger Ed - EF) weaker bonding.
“d band theory”, where surface physicist meet surface chemist
Too strong
Too weak
Too strong
Too weak
The binding energy of an adsorbate to a surface is largely dependent on the electronic structure of the surface
10

## Slide 11
Oxygen evolution reaction involves four proton-electron transfer steps.
The activity strongly correlates with surface electronic structure!
Norskov et. al. J. Electroanal. Chem. 607, 83 (2007).
Man et al. ChemCatChem, 3, 1159 (2011)
Four proton electron transfer steps:
1. H2O(l) + * ⇌ HO* + H+ + e-
2. HO* ⇌ O* + H+ + e-
3. O* + H2O(l) ⇌ HOO* + H+ + e-
4. HOO* ⇌ * +O2 +H+ + e-
Correlation between catalytic activity and electronic structure
11

## Slide 12
Oxygen evolution reaction involves four proton-electron transfer steps.
The activity strongly correlates with surface electronic structure!
Four proton electron transfer steps:
1. H2O(l) + * ⇌ HO* + H+ + e-
2. HO* ⇌ O* + H+ + e-
3. O* + H2O(l) ⇌ HOO* + H+ + e-
4. HOO* ⇌ * +O2 +H+ + e-
Correlation between catalytic activity and electronic structure
0.191 V at 10 mA cm-2
Science, 352, 333 (2016)
Tuning the absorption energetics of OER intermediates via doping/alloying for the design of ternary FeCoW oxyhydroxides, the best catalyst so far.
12

## Slide 13
Correlation between electronic structure and catalytic activity
eg orbital with 1 electron show the highest OER activity
Suntivich et. al.
Science 334, 1383 (2011)
t2g
eg
JR Petrie, H.N. Lee et. al. JACS 138, 2488 (2016)
Using epitaxial strain to tune the electronic structure and OER activity
13

## Slide 14
Density Functional Theory
Electronic, Optical and Magnetic Properties
Epitaxial thin films
Pulsed laser deposition
Novel Physics
doping, defect, strain crystal orientations
Electro-chemistry
Intrinsic
Material
Descriptor
Electrocatalysts
(OER, ORR)
Photoelectro-chemistry
Surface chemistry
The aim: understand the electronic structure and catalytic activity relationship
Research Approach
Solid-liquid interface
14

## Slide 15
Photoemission spectroscopy and X-ray absorption
O K-edge X-ray absorption (XAS) probe O 1s to unoccupied states with O 2p character hybridized with metal 3d, related to unoccupied density of states at CB.
XPS-VB
O 1s
O 2p6
Ni 3d8
EF
Hole
X-ray
O K-edge
XAS
CB
VB
15

## Slide 16
Cr t
2g
E
f
LaCrO
3
Cr
e
g
O2p
Eg = 3eV
Cr t
2g
E
f
Cr
e
g
O2p
La
0.75
Sr
0.25
CrO
3
Energy
Energy
CB
VB
VB
CB
Hole
Electronic structures of La1-xSrxCrO3(0≤ x ≤ 1)
Mott insulators
Eg= 2.9 eV
Transparent p-type oxide semiconductor
Insulator-to-metal transition
LaCrO3
0.25
0.50
0.65
SrCrO2.8
SrCrO3.0
Phys. Rev. B 91, 155129 (2015)
PRL 110, 077401 (2013)
Adv. Mater. 27, 5191 (2015)
APL 111, 063501 (2017)
Nat. Comm. 5, 4669 (2014)
JPCL 6, 1757 (2017)
O 1s
O 1s
XPS
O K-edge
XAS
X-ray
Works at Scott Chambers’ group in PNNL
Reversible redox phase transition
16

## Slide 17
Tuning the Electronic Structures of NiO by Li doping

## Slide 18
Transparent P-type semiconductor: Eg = 3.6 eV;
Antiferromagnetic (TN = 523 K)
Application — Hole transport layer in solar cells
— Data storage
O2-
Ni2+: 3d8
Li+
The electronic structure of NiO: a century inspiring debate
18

## Slide 19
Physicists believe NiO is a charge transfer insulator (the top of valence band is O 2p)
G. Sawatzky, et al PRL 62, 221 (1989)
G. Sawatzky, et al PRL 53, 2339 (1984)
JB Goodenough, J. Phys. Chem. Solids (1958)
Allan Jacobson JACS 115 4173 (1993)
John Harding, PRB 85, 115127 (2012)
Transparent P-type semiconductor: Eg = 3.6 eV;
Antiferromagnetic (TN = 523 K)
Application — Hole transport layer in solar cells
— Data storage
Electronic structure is interesting, because of strong electron correlation!!
Ni2+: 3d8
Electrochemists believe they are cycling Ni2+/Ni3+ redox potential
Ni 3d t2g
O 2p6
Eg= 3.6 eV
eg
eg
Energy
VS
Physicists’ picture
Chemists’ picture
VB
CB
Ni 3d t2g
O 2p6
Eg
eg
eg
Energy
VB
CB
O2-
Li+
The electronic structure of NiO: a century inspiring debate
18

## Slide 20
Most of the oxide semiconductors are n-type: ZnO, In2O3, SnO2, TiO2
It is challenging to achieve p-type oxide, because of the electronic structure of metal oxides, i.e., localized nature of O 2p at the valence band.
Medvedeva, PRL 97 086401 (2006)
CB
In 5s
VB: O 2p
Bandstructure of In2O3
“Oxide Electronics”
Hole transport layer in solar cells
Grätzel, Science (2015)
Zhang et al., J. Mater. Chem. C 6, 2275 (2018)
Search for P-type transparent oxide semiconductors
Zhang et al., J. Phys.: Condens. Matter. 28, 383002 （2016）
19

## Slide 21
CuAlO2
VBM: O 2p6 + Cu 3d10
Solution: introducing states hybridized with O 2p hybridization at the top of valence band
Late transition metal cations (Ni, Co, Cu) 3d
Lone pair states (Bi 6s2, Sn 5s2)
SnO
CB
CB
VBM: O 2p6 + Sn 5s2
JB Varley, Van der Walle et al. APL 103, 082118 (2013).
Search for P-type transparent oxide semiconductors
H. Hosono, et al. Nature 389, 939(1997).
Scanlon and Watson, Phys. Rev. Lett. 103, 096405 (2009).
20

## Slide 22
XIAMEN
UNIVERSITY
Invited topical Review: P-type Transparent Conducting Oxides, J. Phys.: Condens. Matter. 28, 383002 （2016）
?μ=10 cm2V-1s-1
CuSCN
Eg= 3.5 eV
μ=0.1 cm2V-1s-1
Thomas Anthopoulos,
Adv. Electronic Mater. (2017)
CuI
Eg= 3.1 eV
μ=44 cm2V-1s-1
Hideo Hosono,
Adv. Mater. (2018)
? μ=0.01—30 cm2V-1s-1
μ=7.6 cm2V-1s-1
ZnCo2O4
ZnIr2O4
P-type transparent oxide semiconductors
21

## Slide 23
LixNi1-xO powders (x=0, 0.06, 0.09, 0.17, 0.25, 0.32, 0.50) were synthesized by grinding NiO and Li2O and heating at 750oC in flow of O2 for 12 hours
Li randomly occupy at Ni sites for x< 0.32;
Lattice constants decrease as x increase;
Phase transition from Cubic to Rhombohedral at x>0.32;
Ionic radii
Li+ (90 pm)
Ni2+ (83 pm)
Ni3+ (70 pm)
Li doped NiO (LixNi1-xO )
Li0.5Ni0.5O
Ni2+ (3d8) Ni3+ (3d7)
NiO
Ni3+
Ni2+
Li+
22

## Slide 24
Cubic to Rhombohedra
J. Mater. Chem. C 6, 2275 (2018)
Optical and electronic properties of LixNi1-xO(0≤ x ≤ 0.5)
23
NiO 0.01 0.03 0.09 0.25 0.50
At x= 0.32, cubic to rhombohedra phase transition
With more Li doping, i.e., P-type doping, films become more conductive
“Bandgaps” from 3.6 eV to 0.5 eV, no insulator-to-metal transition

## Slide 25
XPS-VB and O K-edge XAS spectra indicate development of hole state above VB, while the materials keep a semiconducting behavior.
Combined with optical absorption, we determined the hole state is ~ 1.0 eV above VB.
O K-edge X-ray absorption (XAS) probe O 1s to unoccupied states with O 2p character hybridized with Ni 3d, related to unoccupied density of states at CB.
XPS-VB
O 1s
O 2p6
Ni 3d8
EF
Hole
X-ray
O K-edge
XAS
CB
VB
Hole
Electronic structures by XPS and O K-edge XAS spectra
24

## Slide 26
Ni K-edge NEXAFS indicates more Ni3+ states with Li doping;
EXAFS indicate Ni-O bonding length decreases;
Ni oxidation states and bond lengths
EXAFS
Ni2+
Ni3+
Ni K-edge
Ni3+
O2-
Ni2+
O1.7-
Unpublished data with Y.H. Du at SSLS (Singapore)
25

## Slide 27
LixNi1-xO (x<0.06) with enhanced p-type conductivity and work function
26
J. Mater. Chem. C 6, 2275 (2018)
LixNi1-xO

## Slide 28
LixNi1-xO (x<0.06) with enhanced p-type conductivity and work function
27
J. Mater. Chem. C 6, 2275 (2018)

## Slide 29
LixNi1-xO (x<0.06) as hole transport layer in solar cells
J. Mater. Chem. A (Accepted)
28
Advanced Materials, 29, 1702176 (2017)
in collaboration with Judith Driscoll and Richard Friend, Cambridge
The work functions of NiO can be tuned by Li or O;
The VB aligns perfect with organic perovskites.

## Slide 30
Interfacial electronic structure and band alignment at p-n heterojunctions
Appl. Phys. Lett. 112, 171605 (2018)
ACS Appl. Mater.& Interface 9, 26549 (2017)
N-SrTiO3(001)
2 nm NiO
X-ray
photoelectron
29

## Slide 31
Ink: LixNi1-xO powder+Nafion+Ethonal
Drop-casting on glassy carbon electrode
(0.30 mg/cm2)
1. Preparation of electrode
2. Electrochemical Test
LSV, CV, Tafel, EIS
Rotating disk electrode
Electrochemical Station
Electrocatalytic activity Test
30

## Slide 32
OER activities of LixNi1-xO. (a) linear scan voltammetrys vs reversible hydrogen electrode (RHE), (b) tafel splots, (c) electrochemical impedance spectroscopy and (d) cyclic voltammetry for LixNi1-xO.
LixNi1-xO showing increasing OER activity as Li doping
OER electrocatalytic activities of LixNi1-xO
31

## Slide 33
32
DFT +U calculations (with Prof J. Cheng)
G.L. Fu et al. Submitted
Correlation of OER activity with electronic structures
The hole state at 1.1 eV above VB induced by Li provide an empty state for electron transfer from OH- to the catalyst.

## Slide 34
Correlation of OER activity with electronic structures
G.L. Fu et al. Submitted
33

## Slide 35
Summary
Li doping in NiO introduce hole state at 1.1 eV above VB for new functionalities.
P-type transparent semiconductor as a hole transport layer for PV
Transparent p-n heterojunctions for UV photodetectors and photocatalytic water splitting;
Combined XRD, XPS and hard XAS spectra, DFT support formation of Ni3+ states with Li doping. Hole is of Ni 3d character!
The hole state associated with Ni3+ enhances the absorption of OH group on catalyst surface, hence the OER activity.
Enhanced control over defects/doping will enable new science and unprecedented functional properties, leading to new applications.
N- SrTiO3
P- LSCO

## Slide 36
Group: Gaoliang Fu(electrocatalyst); Jiaye Zhang(electronics);
Pulsed Laser Deposition
Judith Driscoll (Cambridge); Lang Chen (SusTech); Oliver Bierwagen (Paul-Drude-Institut, Berlin)
XPS-XAS (Diamond, Australia, Singapore)
David Payne (Imperial), Dongchen Qi (La Trobe, Australia), Anton Tadich (Australian Synchrotron) Russell Egdell (Oxford), Louis Piper (Binghamton, USA), Tien -Lin Lee (Diamond，UK); Jan Philipp Hofmann (Eindhoven);
DFT: Aron Walsh (Imperial), Jun Cheng (Xiamen)
STEM: Vlado Lazarov (York)
Scott Chambers at PNNL
Email: kelvinzhang@xmu.edu.cn
Acknowledgement

## Slide 37
存在问题！！
Nature Materials, 2017，16, 925-931
OER过程中表面非晶化, 形成Co(OH)2
氧化物中的晶格氧参与反应
OER与pH值有关系
Nature Chemistry, 2017，9, 457-465
Catalysis Today, 2016，262, 2-10

## Slide 38
关键科学问题: 电子结构与电催化OER活性内在构效关系
电子结构
原位电化学X射线
吸收谱
电催化理论计算
物理性质
3d轨道强关联
OER活性 吸附能
同步辐射光子
能谱
理论计算
单晶薄膜模型催化剂: 钙钛矿LaNiO3 和尖晶石Co3O4
掺杂
氧缺陷
晶面取向
应力
(001)
(110)
激光溅射沉积实现原子级精准调控
催化活性与电子结构关系---研究总体思路

## Slide 39
Film
RDE
(a)
Covering
Nb:STO
(c)
(b)
(d)
基于外延单晶薄膜的模型电催化

## Slide 40
In-operando — 同步辐射吸收谱(XANES & EXAFS)
XANES: 价态, 电子结构
EXAFS: 键长， 配位数
Ni K edge
XANES
EXAFS
RE
&WE
CE

## Slide 41
Low temperature CO oxidization；
Xie et al., Nature 458, 746 (2009)
Methane combustion;
Hu et al., JACS 130, 16136 (2008)
Oxygen evolution reaction;
JACS, 135, 13521 (2013); Nat. Mater. 16, 335 (2017)
尖晶石(spinel)：Co3O4, NixCo3-xO4
晶面取向
氧缺陷
有疑问或争议科学问题！
氧缺陷提高催化性能，几乎所有文献指出由于氧缺陷提高导电性所致?
从半导体物理角度, Co3O4 为p-型半导体。氧缺陷引入hole-killer, 只能降低导电性！
Co3O4 电子结构问题。
不同文献报道不同活性面:
CO oxidization: (011)>(111)=(001)
Methane combustion: (112)>(011)=(001)
OER: 极为争议;
JPCL 5, 2370 (2014); JACS138, 36 (2015);
PCCP 17, 29387(2015)
核心问题是Co2+(Td ), Co3+(Oh)哪个更活跃?
Td -Co2+
Oh-Co3+
Active site

## Slide 42
XIAMEN
UNIVERSITY
脉冲激光沉积(PLD)外延生长功能氧化物单晶薄膜和异质结
优势: 原子级精准控制生长,晶面取向,缺陷/掺杂,表界面
基于同步辐射的光电子能谱(PES) + 吸收谱(XANES & EXAFS), DFT等;
研究材料电子结构, 光学, 磁学，表界面等物理性能.
电化学，光电化学
XPS
PLD
LaCrO3
SrTiO3
研究方法

## Slide 43
Group: Gaoliang Fu; Jiaye Zhang;……
Pulsed Laser Deposition
Judith Driscoll (Cambridge); Lang Chen (SusTech); Oliver Bierwagen (Paul-Drude-Institut, Berlin)
XPS-XAS (Diamond, Australia, Singapore)
David Payne (Imperial), Dongchen Qi (La Trobe, Australia), Anton Tadich (Australian Synchrotron) Russell Egdell (Oxford), Louis Piper (Binghamton, USA), Tien -Lin Lee (Diamond，UK); Jan Philipp Hofmann (Eindhoven);
DFT: Aron Walsh (Imperial), Jun Cheng (Xiamen)
STEM: Vlado Lazarov (York)
Scott Chambers at PNNL
Email: kelvinzhang@xmu.edu.cn
Acknowledgement

## Slide 44
Physicists believe NiO is a charge transfer insulator (the top of valence band is O 2p)
G. Sawatzky, et al PRL 62, 221 (1989)
G. Sawatzky, et al PRL 53, 2339 (1984)
JB Goodenough, J. Phys. Chem. Solids (1958)
Allan Jacobson JACS 115 4173 (1993)
John Harding, PRB 85, 115127 (2012)
Transparent P-type semiconductor: Eg = 3.6 eV;
Antiferromagnetic (TN = 523 K)
Application — Hole transport layer in solar cells
— Data storage
O2-
Electronic structure is interesting, because of strong electron correlation!!
Ni2+: 3d8
Electrochemists believe they are cycling Ni2+/Ni3+ redox potential
Ni 3d t2g
O 2p6
Eg= 3.6 eV
eg
eg
Energy
Ni 3d t2g
O 2p6
Eg
eg
eg
VS
Physicists’ picture
Chemists’ picture
Energy
VB
CB
VB
CB
Li+
The electronic structure of NiO: a century inspiring debate

## Slide 45: P-type transparent conducting oxide as hole transport layer in solar cells
Chen, Grätzel et al Science 2015
Yang, et al Nat. Nanotech 2016

## Slide 46
Reciprocal space map of LixNi1-xO (x=0, 0.006, 0.03, 0.06, 0.09) thin films on MgO(001)
O2-
Ni2+
Li+
LixNi1-xO

## Slide 47
Summary
Sr doped LaCrO3 as a new p-type TCOs
Ordered oxygen vacancies in SrCrO3-x leading to fast redox at low temperature
The fundamental electronic structure is elusive and inspiring; Li doping NiO can introduce hole state for new functionalities.
Enhanced control over defects/doping will enable new science and unprecedented functional properties, leading to new applications.
N- SrTiO3
P- LSCO
Ni 3d t2g
O 2p6
Eg= 3.5 eV
eg
eg
Energy
28

## Slide 48
XIAMEN
UNIVERSITY
Perovskite Transition Metal Oxides
Lev Perovski
Russian mineralogist
HTc superconductor; Bednorz and Müller, Zeitschrift für Physik B, 64,189 (1986)
Colossal magnetoresistance; Jin and Ramesh et al. Science, 264 413 (1994)
electrocatalyst, solar cells (Special Issue: PEROVSKITES, Science, 2017)
ABO3
B=Cr3/4+
A=La3+, Sr2+
14
A: lanthanide or alkaline earth metal e.g., La3+, Sr2+;
B: transition metal (TM) cations, e.g. Cr;

## Slide 49: Why Sr doped LaCrO3
XIAMEN
UNIVERSITY
Sr doped LaCrO3 is important material for SOFC and catalytic applications
Pure LaCrO3 is a Mott insulator with bandgap of 2.9 eV; The top of VB mainly from Cr 3d t2g states; SrCrO3 is a metallic oxide.
15
Ti3+
3d1
x=0.05
V3+
3d2
x=0.17
Cr3+
3d3
Mn3+
3d4
x=0.17
Fe3+
3d5
Co3+
3d6
x=0.17
Ni3+
3d7
Metallic
Cu2+
3d9
x=0.03
LaTiO3
LaVO3
LaCrO3
LaMnO3
LaFeO3
LaCoO3
LaNiO3
La2CuO4
Bandgaps of parent LaM3+O3
Insulating?
Insulating?
Sr doping (x) for insulator-to-metal transition (La1-xSrxMO3)
Imada, Fujimori, Tokura, Rev. Mod. Phys. 70, 1039 (1998)

## Slide 50: Why Sr doped LaCrO3
XIAMEN
UNIVERSITY
A
Cr t2g
O2p
Cr eg
A
B
Eg
Optical absorption spectra of LaCrO3
forbidden
B
Sr doped LaCrO3 is important material for solid oxide fuel cell and catalytic applications
Pure LaCrO3 is a Mott insulator with bandgap of 2.9 eV; The top of VB mainly from Cr 3d t2g states; SrCrO3 is a metallic oxide.
Phys. Rev. Lett. 110, 077401 (2013)
Adv. Funct. Mat., 23, 2952 (2013)
16

## Slide 51
Sr掺杂对La1-xSrxCrO3(0≤ x ≤ 1)电学, 光学性质的影响
O 1s
O 1s
XPS
O K-edge
XAS
X-ray
理解LaCrO3的本身能带结构;
Cr和其他3d TM 钙钛矿一样,存在MIT转变;
较低温度(250oC)发生可逆的氧化-还原(Redox)反应。
Phys. Rev. B 91, 155129 (2015); Adv. Mater. 27, 5191 (2015);
Nat. Comm., 5, 4669 (2014); Appl. Phys. Lett. 111, 063501 (2017);

## Slide 52
高质量外延单晶薄膜, 异质结, 表界面修饰 (custom-designed)
我们可以提供
基于同步辐射的光电子能谱(PES) + 吸收谱(XANES & EXAFS)
表界面电子结构， 电荷转移； 价态， 配位数，键长
Email: kelvinzhang@xmu.edu.cn
27

## Slide 53
2
Electrochemical Energy Conversion

## Slide 54
同步辐射光源(Synchrotron radiation)
欧盟7个
美国5个
日本3个
新加坡 1个
中国上海
同步辐射光源(Synchrotron radiation)，一种利用高速运行的电子(相对论性)在磁场中偏转时产生同步辐射的高性能新型, 超高强度的光源。
简单原理: 变化的电场产生磁场！
Diamond, UK
4
I09, B07(ambient pressure XPS), I06(XMCD)

## Slide 55
1. 采集电子结构信息(价带,导带的态密度)
不仅可以采集组分,价态,配位数,键长
基于同步辐射的光电子能谱(PES)+吸收谱(XANES & EXAFS)
英国Diamond Light Source
5

## Slide 56
基于同步辐射的光电子能谱(PES)+吸收谱(XANES & EXAFS)
英国Diamond Light Source
2. 不仅是surface sensitive;
Hard X-ray XPS有空间分辨
15 nm
3 nm
Electron mean free path
Seah & Dench, Surf. Interface. Anal.1,2(1979)
3. Ambient-pressure XPS
In-Operando XANES&EXAFS
6

## Slide 57
研究方向二: 透明氧化物半导体电子结构
Ga2O3, BaSnO3
Missile Warning Sensor
Understanding the electronic structure is important !

## Slide 58
方向一:透明氧化物半导体(In2O3、Ga2O3、BaSnO3)
触摸屏,光伏
紫外探测，导弹预警
透明 — 大于3.1 eV 带隙
导电性 — 半导体掺杂
In2O3
Sn掺杂In2O3 (ITO)
带隙
>3.1 eV
Ef
导带
Energy
价带
导带
Ef
Energy
价带
带隙
>3.1 eV
Understanding the electronic structure is important !
《阿凡达》
Facchetti, T. J. Marks,Transparent Electronics: From Synthesis to Applications (Wiley, 2010)
KHL Zhang et al. Phys. Rev. Lett. 110, 056803 (2013)
KHL Zhang, Scott Chambers, Oxide Semiconductors (Wiley, 2019)
8

## Slide 59
2. 大部分是N-型, 实现P-型氧化物半导体是本领域的难题；
中国是主要铟原料供应国， 却是ITO薄膜重要进口国
1. 铟的地壳含量较少, 价格越高(与银相当)
已商业化透明导电电极Sn掺杂的In2O3（ITO）占据95%的市场份额, for Flat Panel Displays.
面临的挑战和机遇
U.S. Geological
Survey 2015
14

## Slide 60
Pure In2O3, ZnO and SnO2 show considerable free electron densities up to 1x1018 cm-3
The origin of n-type conductivity?
Historically, the n-type conductivity was attributed to oxygen vacancies (Vo)
However, DFT and experiments show the state of Vo is deeply localized
O2-
In
In3+
e
e
DFT calculation of the formation energy of intrinsic defect in SnO2
A. Zunger et al. PRL 88, 095501 (2002)
科学问题: n-type conductivity in undoped materials
15

## Slide 61
Zhang, Cowley, et al. ACS Nano 6, 6717 (2012)
Zhang, Egdell, et al. Phys. Rev. B 84, 233301 (2011)
Walsh, Zhang, Catlow et al. Phys. Rev. B 83, 161202 (2011)
In2O3 薄膜, 纳米结构可控生长
实验与理论结合, 揭示In2O3表面能各向异性所控制的生长形貌, 为In2O3的纳米合成提供指导。
在(111)面上实现缺陷少, 高迁移率In2O3外延薄膜。
Surface | Tasker Type | energy
100 | polar | 1.95
110 | Neutral | 1.07
111 | Quadrupolar | 0.89
DFT 计算In2O3晶面表面能(J/m2)
In3+
O2-
In3+
O2-
In3+
O2-
17
Notes: 61

## Slide 62
Epitaxial growth of In2O3 and 3%Sn-doped In2O3 (ITO) on YSZ (111)
Carrier concentrations (n) determined by Hall measurement and further verified by Infrared reflectivity.
The amount of free carrier put the Fermi level of In2O3 at 0.1 eV below CBM, while 0.3 eV above CBM for ITO
In2O3
n= 2 × 1018 cm-3
ITO
n= 1 × 1021 cm-3
VB
O2p6
EF
CB
In5s
Sn4+ 5s
VB
O2p6
EF
CB
In5s
18

## Slide 63
Surface electron accumulation and downward band bending at the surface region of In2O3
In2O3: n= 3 × 1017 cm-3
ITO: n= 1 × 1021 cm-3
O2p6
KHL Zhang, PDC King and RG Egdell, et. al Phys. Rev. Lett. 110, 056803 (2013)
A well-defined peak observed at Fermi level (EF) for In2O3 ??
The peak intensity corresponds to carrier concentration of 2×1020cm-3.
Note the bulk carrier concentration for In2O3 is only 3 × 1017cm-3
19

## Slide 64
In2O3 表面电子结构研究
ZnO, maybe?
SnO2 ---- Phys. Rev. B, 90 155413 (2014);
SrTiO3 --- Nat. Mater. 13, 1085 (2014);
InN---- Phys. Rev. Lett. 92, 036804 (2004);
一系列基于同步辐射光电子能谱发现In2O3表面存在表面二维电子气。解决了自1980年以来关于氧化铟表面电子态的争论。
Zhang, Egdell*, King, et. al., Phys. Rev. Lett. 110, 056803 (2013) (PRL亮点论文)
Zhang, Egdell, et al. Chem. Mater. 21, 4353 (2009); Zhang, et al. Surface Science 6, 6717 (2012)
体相
表面
In2O3
In 5s2
In 5s2
表面二维电子气
2 nm
10 nm
2 nm
Electron mean free path
Surf. Interface. Anal.1,2(1979)
hγ=1000 eV
hγ=6000 eV
EF
20

## Slide 65
In2O3 表面电子结构研究
ZnO, maybe?
SnO2 ---- Phys. Rev. B, 90 155413 (2014);
SrTiO3 --- Nat. Mater. 13, 1085 (2014);
InN---- Phys. Rev. Lett. 92, 036804 (2004);
一系列基于同步辐射光电子能谱发现In2O3表面存在表面二维电子气。解决了自1980年以来关于氧化铟表面电子态的争论。
Zhang, Egdell*, King, et. al., Phys. Rev. Lett. 110, 056803 (2013) (PRL亮点论文)
Zhang, Egdell, et al. Chem. Mater. 21, 4353 (2009); Zhang, et al. Surface Science 6, 6717 (2012)
体相
表面
In2O3
In 5s2
In 5s2
表面二维电子气
2 nm
15 nm
3 nm
Electron mean free path
Surf. Interface. Anal.1,2(1979)
21

## Slide 66
The surface VO have low ionization energy and act as the source for the 2DEG.
1.6% of surface VO sites gives rise to 2DEG
A gap state (GS) is observed at 1.5 eV below CB from our photoemission measurement;
DFT calculation show bulk VO is 1.1 eV below CBM.
Too deep to be ionized to generate free electrons
Microscopic origin: oxygen vacancies (Vo)？
Lany and Zunger, Phys. Rev. Lett. 108, 016802 (2012)
22

## Slide 67
基于同步辐射的光电子能谱(PES) + 吸收谱(XANES & EXAFS)
表面一价 In+ 5s2存孤对电子存在！
Sn2+, Pb2+, Bi3+
Mudd, McConville, Zhang, et. al., Phys. Rev. B (Submitted)
23

## Slide 68
Implications for device applications
Conductance vs NO2 concentration
In2O3 nanowire
O3 or NO2
DH Zhang, et al. Nano Lett. 4, 1919 (2004).
2DEG (downward band bending) are also observed in SnO2, CdO, IGZO, SrTiO3,InN, which may explain intrinsic n-type conductivity.
SnO2 ----Phys. Rev. B, 90 155413 (2014);
CdO -----Phys. Rev. B, 78, 165127 (2008);
SrTiO3 ---Nature materials 10, 114 (2011);
InN------- Phys. Rev. Lett. 92, 036804 (2004);
IGZO----J. Appl. Phys. 109, 073726 (2011)
The exist of 2DEG explains why these oxides can be used as ultra-sensitive gas sensor:
2DEG is sensitive to the oxidizing gas, so does the conductance.
2DEG in IGZO surface
24

## Slide 69
二维电子气(2DEG)的调控
ACS Nano 11, 6040 (2017)
25
In2O3
4 nm NiO
1.2 nm NiO
Ef