## Slide 1: Rational Design of Nano-Catalysts for Sustainable Chemicals and Fuels: Insights from Theory and Simulation
Catherine Stampfl
School of Physics, The University of Sydney, Sydney, New South Wales 2006, Australia
Notes: The title of my talk is “Rational Design of Nano-Catalysts for Sustainable chemicals and Fuels” Insights from Theory and Simulation”

## Slide 2
Motivation
1
oil
coal
natural gas
The remaining service life
Significant pressure to develop new green/sustainable
energy sources.
Depletion of fossil fuels
Pollution
Notes: As we are all aware, there is significant pressure to develop new green/sustainable energy sources, such as wind , solar, amd nuclear energy and so on. This is due to both the depletion of fossils fuels – the remaining service life of coal is around 200 years, natural gas, bit over 50 years, and oil, around 40 years – and to environmental pollution caused by traditional energy utilization.

## Slide 3
Achieving sustainable resources is a Grand Challenge of this century
Catalysts can play a key role in the development of sustainable production of chemicals
and fuels, notably bio-derived and solar mediated
A. F. Lee et al.
Chem. Soc.
Rev., 2014,
43, 7887
Notes: Catalysts can play a key role in this development, for sustainable production of chemicals and fuels. The are used in “chemical synthesis”, “solar fuels/chemicals”, biorefining, fossil fuel refining.

## Slide 4
Catalysis is ubiquitous in all aspects of everyday life.
It empowers new product development and
refinement across a wealth of industries, including
- life sciences
- pharmaceutical and
agricultural sectors,
- electronics,
- chemicals,
- renewable energy
technologies.
Contributes to 35% of
the world’s GDP
Catalysts
with catalyst

## Slide 5
scale
S. Mitchell et al. Chem. Soc. Rev., 2013, 42, 6094
Theory/
computation
Many stages
In the
development
of new
catalysts
scale of
catalyst
Notes: In the development of new catalysts there are many different stages, from the initial idea, synthesis, characterization, mechanism, to the scale up and testing. Along the way there is a loop of optimization. Correspondingly, the scale of the catalyst being investigated ranges through from atomic to metre. For theory and computation, we are focussed on the atomic and nanoscale.

## Slide 6
Examples of how theory and computation can be
used in synergy with experiment to:
Understand and interpret –
Effects of Layered Supports of graphitic carbon
nitride with Ru Nanoparticles for Ammonia Synthesis
Outline
Kesterite I2-II-IV-V4 semiconductors
and Hybrid 2D materials
“AI” - Machine learning -
2. Prediction and screening –
Bifunctionalization of Metal-organic Framework
catalysts
Notes: In the talk I will discuss some recent examples from our research of how theory and computation is used in synergy with experiment to 1, understand and interpret experimental results, screen and predict new potential catalysts, and 3. Do machine learning of a class of materials in order to identify and predict structures with desirable properties. In particular, Effects of Layered Supports of graphitic carbon nitride with Ru Nanoparticles for Ammonia Synthesis, Bifunctionalization of Metallorganic Framework catalysts, and machine learning of Kesterite I2-II-IV-V4 semiconductors And Hybrid 2D materials.

## Slide 7: Ammonia Synthesis
Use solar energy to produce ammonia from abundant nitrogen gas and water
Beneficial for both relieving energy demands and developing a sustainable
chemical industry.
Very important chemical – fertilizer, building block
for synthesis of pharmaceutical products
160M tons per year.
Haber-Bosch has some disadvantages;
uses high value-added clean energy H2,
harsh reaction conditions (high
temperature 400-500 C and pressure,
150-300 bar)
1. Understand and interpret
Notes: Ammonia is a very important chemical – fertilizer, building block for synthesis of pharmaceutical products, 160M tons per year. Our first example involves the idea of using solar energy as the driving force to produce ammonia from abundant nitrogen gas and water over two-dimensional graphitic carbon nitride with Ru nanoparticles. Over the catalyst, adsorbed atomic hydrogen is produced from water, and nitrogen gas is dissociated prior to reaction steps to form ammonia.

## Slide 8: Ammonia Synthesis
2D semiconductor materials attracting significant
recent interest in catalysis and other fields, new
properties and opportunities to tailor them
The graphitic carbon nitride (g-C3N4) structure acts
as both support and light harvester. Ru nanoparticles
act as electron trap and active centre
Two forms of g-C3N4 were prepared:
Bulk:
Formed by
thermally
decomposing
in urea at 550C
for 4 hrs
Exfoliated:
synthesized by
exfoliating bulk
form
Nanoparticles
at step edges
Nanoparticles
dispersed
Huimin Liu et al. submitted

## Slide 9
Around 2.6 times more ammonia produced over the bulk
Ru-K/g-C3N4 than the exfoliated one
WHY ?

## Slide 10: First-principles calculations
Associative dissociation
H2 + 2* = 2H*
N2 + 2* = 2N*
N* + H* = NH*+*
NH* + H* = NH2*+*
NH2* + H* = NH3*+*
NH3* = NH3 + *
Cleavage of the N2 bond is the rate-determining step
Investigate the structure and energetics of nitrogen
dissociation over the two catalysts
Direct dissociation
Consider both pathways
Consider both catalysts

## Slide 11: First-Principles investigations
Determine favourable
structures for Ru11
nanoparticle
Most favorable
Exfoliated, single layer

## Slide 12
Determine favourable
structures for Ru11
nanoparticle –
favours step edge
Most favorable
Bulk-like system

## Slide 13: Reaction Energy for N2 dissociation
Bulk – direct N2 dissociation,
barrier 0.71 eV
Lowest energy barrier for
direct N2 dissociation
over bulk Ru/g-C3N4
– higher rate of ammonia formation
- Stronger nanoparticle-substrate interaction
Two catalysts different
mechanism:
Exfoliated – associative N2
dissociation, barrier 1.13 eV
Agreement with Experiment

## Slide 14
2. Prediction and screening
Anode: 2H2 – 4e– → 4H+
Cathode:O2 + 4H+ + 4e– → 2H2O
Promising
clean and sustainable
power source
Rate of oxygen
reduction at cathode
is much
slower than the
reaction at the anode.
Determines the
performance
Most effective
electrocatalysts
for cathode
based on platinum
group metals.
Drawbacks -high
price, poor
durability,
methanol
poisoning effects
Polymer electrolyte fuel cell
Bifunctional MOF catalysts

## Slide 15
Need to find new low cost and high durability non-precious group metal (PGM) alternative electrocatalysts; recent investigations
- metal-free heteroatom-doped carbon materials,
- transition metal−nitrogen−carbon catalysts,
- transition metal oxides
Metal-organic Framework
(MOF) catalysts
high surface area
uniformly distributed coordinated metal
Over
MOFs materials
6000 members of
crystalline framework
materials
controllable porous structure

## Slide 16
Ideal Catalyst for ORR/OER
O2(g) + 4H+ + 4e−↔OOH* + 3H+ + 3e−
OOH* + 3H+ + 3e−↔ O* + H2O(aq) + 2H+ + 2e−
O* + 2H+ + 2e−↔ OH* + H+ + e−
OH* + H+ + e−↔ H2O(aq)
ORR
OER
(oxygen reduction reaction)
(oxygen evolution reaction)
Norskov et al., J. Phys. Chem. B 108, 17886 (2004)
U=0V equivalent to gas-phase
hydrogen oxidation reaction
U=1.23V where fuel cell has the
maximum potential allowed by
thermodynamics
(R1)
(R2)
(R3)
(R4)
ORR and OER are reverse reactions; share
same reaction pathway and free energy diagram
only difference is reaction direction

## Slide 17
Metal Dithiolene nanosheets
Investigate metal dithiolene nanosheets as ORR/OER catalysts
9 different metal centres
P. Zhang et al. Catal. Sci. Tech. 8, 3666-3672 (2018).
Notes: In this work, MC4S4 nanosheets with nine different central metals (where M = Fe, Co, Ni, Ru, Rh, Pd, Os, Ir and Pt) as ORR catalysts have been systemically studied.

## Slide 18
Atomic structure of M3(THT)2
C H
S M
Atomic
structure of the
unit cell
There are
three metal
sites per
unit cell
P. Zhang et al. Catal. Sci. Tech. 8, 3666-3672 (2018).

## Slide 19
Adsorption structures of ORR intermediates

## Slide 20
Reaction Free Energy diagrams of ORR/OER on M3(THT)2
Co
best
ORR
Fe
best
OER

## Slide 21
Atomic structure of FexCo3-x(THT)2
Consider combination
of Co and Fe, i.e.,
FeCo2
Fe2Co
P. Zhang et al. Catal. Sci. Tech. 8, 3666-3672 (2018).

## Slide 22
ORR/OER on FexCo3-x(THT)2
Good
ORR
Good
OER

## Slide 23
ORR on M3(THT)2
OER on M3(THT)2
Predict FexCo3-x(THT)2 nanosheets potential
promising bifunctional catalyst for ORR and OER
P. Zhang et al. Catal. Sci. Tech. 8, 3666-3672 (2018).
FexCo3-x(THT)2 nanosheets promising bifunctional catalysts
“Volcano Plots” - activity as function of key intermediate binding strength

## Slide 24: 3. Machine Learning Materials
Machine Learning the Band-gap
of 1568 kesterite I2-II-IV-V4 compounds
L. Weston and C. Stampfl Phys. Rev. Mat. accepted
The zinc-blende-based kesterite structure.
The cations with valence I (c-I), II (c-II), and
IV (c-IV) blue, red, and green spheres.
The anion has a valence VI (a-VI) and is
indicated by a yellow sphere.
Kesterite I2-II-IV-V4 semiconductors are promising
solar absorbers
Use a combination of accurate first-principles
calculations and machine learning to predict
the properties of the band gap (and if direct or
indirect) for 1568 kesterite I2-II-IV-V4 semiconductors

## Slide 25: Machine Learning the Band-gap of 1568 kesterite I2-II-IV-V4 compounds
L. Weston and C. Stampfl
Phys. Rev. Mat. accepted
Accurate hybrid
functional calculations
for 200 randomly
selected materials
Used to train machine
learning models
Use 12-dimensional feature space for predictor of the
magnitude of the band-gap

## Slide 26: Machine Learning the Band-gap of kesterite I2-II-IV-V4 compounds
The stability of these 242 compounds is assessed by calculating the enthalpy of formation and making use of the Materials Project database [A. Jain et al. APL Mater. 1, 011002 (2013)] - 34 found to be stable/metastable
For the I2-II-IV-VI4 compounds, we consider: I = Li, Na, K, Rb, Cs, Cu, Ag; II = Be, Mg, Ca, Sr, Ba, Zn, Cd, Hg; IV = C, Si, Ge, Sn, Ti, Zr, Hf; and, VI = O, S, Se, Te.
Model R2 RMSE (eV)
Linear Regression 0.796 0.590
SVR-L 0.789 0.592
SVR-RBF 0.957 0.283
Decision Tree 0.823 0.492
Random Forest 0.874 0.435
Boosted Reg. Tree 0.934 0.358
SVR – support vector regression
L- linear
RBF – radial bias function

## Slide 27: Machine Learning the Band-gap of 1568 kesterite I2-II-IV-V4 compounds
A violin plot for the predicted
band gap distributions for the
oxides, sulﬁdes, selenides and
tellurides.
The width of each distribution
at a given energy indicates the
number of materials with a
band gap around that energy
The oxides have larger band gaps with a mean band gap Eav = 3.82 eV; distribution
over a very wide energy range
Trend moving down the periodic table for the anions is for smaller band gaps and
a more localized distribution. For the tellurides, Eav = 1.78 eV
L. Weston and C. Stampfl
Phys. Rev. Mat. accepted

## Slide 28: Machine Learning the Band-gap of 1568 kesterite I2-II-IV-V4 compounds
The direct–indirect predictions over all materials studied, 70% are found to have indirect gaps
Prediction of direct versus
indirect band-gap more
challenging – required more
feature engineering and
training.
Resulting method predicts
the nature of the band gap
with an accuracy of 89 %
using logistic regression.
L. Weston and C. Stampfl
Phys. Rev. Mat. accepted

## Slide 29
Band-gap properties of 1568 kesterite I2-II-IV-V4 compounds
L. Weston and C. Stampfl
Phys. Rev. Mat. accepted
The 34 stable/metastable structures
with predicted band-gaps in the
optimum range 1.2-1.8eV
All results

## Slide 30: 3. Machine Learning Materials
Hybrid 2D materials
Using DFT and Machine Learning
can predict the interlayer distance
of 1432 bilayer structures and
band-gaps
Hybrid materials built from
2D monolayers are gaining
attention as novel materials
with potentially more easily
tuneable properties
Electronic structure calculations can
make these predictions accurately, but are too
time-consuming to calculate the properties
of every possible multilayer hybrid 2D material

## Slide 31: Machine Learning Hybrid 2D Materials
Sherif Abdulkader Tawik,* Olexandr Isayev, Catherine Stampfl, Joe Shapter, David A. Winkler and Michael J. Ford, Submitted
Calculations for 267 bilayer systems from the 53 monolayer structures
Obtain predicted interlayer distances for 1432 structures
The number of bilayers in which each monolayer is a component

## Slide 32
Machine Learning Hybrid 2D materials
DFT calculated
Interlayer distances
for the training
take into account van der
Waals interaction between
layers
Descriptor – relevant
mathematical representation
of the structure and properties of
Materials
Use: “Property-Labelled Materials
Fragments” [1] modified for 2D
materials
[1] O. Isayev et al, Nat. Comm. 8, 15679 (2017)

## Slide 33
(a) Feedforward Neural Network
(b) Random Forest
(c) Relevance vector Machine
(d) Support vector Machine
Machine Learning Hybrid 2D Materials
Four Machine Learning models
are trained and performance
compared
Shows comparison between
the interlayer distances in
the bilayers obtained using DFT
and the ML approaches
Interlayer distances
Sherif Abdulkader Tawik,* Olexandr Isayev, Catherine Stampfl, Joe Shapter, David A. Winkler and Michael J. Ford, Submitted

## Slide 34
Machine Learning Hybrid 2D Materials
Interlayer distances
Sherif Abdulkader Tawik,* Olexandr Isayev, Catherine Stampfl, Joe Shapter, David A. Winkler and Michael J. Ford, Submitted
 | NN |  | RF |  | RVM |  | SVM | 
Smallest 5 | PtS2¦PtS2 | 2.10 | PtS2¦PtS2 | 2.12 | PdS2¦PdS2 | 1.75 | PtS2¦PtS2 | 2.02
 | PdS2¦PdS2 | 2.12 | PdS2¦PtS2 | 2.16 | PdS2¦NiS2 | 2.01 | PdS2¦PdS2 | 2.12
 | PtS2¦PtSe2 | 2.16 | PdS2¦PdS2 | 2.18 | PtS2¦PtS2 | 2.06 | PdS2¦NiS2 | 2.21
 | PdS2¦PtS2 | 2.22 | PdSe2¦PtS2 | 2.22 | PdS2¦NiTe2 | 2.09 | PdS2¦NbS2 | 2.27
 | PdSe2¦PtS2 | 2.22 | PdSe2¦PdS2 | 2.24 | PdS2¦NbS2 | 2.15 | PdS2¦1T-NbS2 | 2.28
Largest 5 | GaSe¦WTe2 | 3.63 | MoTe2¦MoTe2 | 3.63 | MoTe2¦TaTe2 | 3.66 | WTe2¦1T-MoTe2 | 3.65
 | WTe2¦WTe2 | 3.64 | MoTe2¦PdTe2 | 3.67 | PdTe2¦TaTe2 | 3.70 | ReTe2¦WTe2 | 3.66
 | PdTe2¦BoronNitride | 3.65 | MoTe2¦WTe2 | 3.69 | WTe2¦WTe2 | 3.76 | MoTe2¦PdTe2 | 3.68
 | PdTe2¦Graphene | 3.66 | ReTe2¦WTe2 | 3.70 | MoTe2¦PdTe2 | 3.77 | WTe2¦WTe2 | 3.73
 | GaSe¦WCl2 | 3.68 | WTe2¦WTe2 | 3.72 | MoTe2¦WTe2 | 3.80 | MoTe2¦WTe2 | 3.74
interlayer distances for 1432 structures – band gaps for 210

## Slide 35: 2D bilayers
A recent data mining study[1] reported the existence of 1,825 2D materials that could be exfoliated from known experimental inorganic compounds.
This set can make ~1.7 million bilayer structures, around 109 trilayers.
This quickly becomes an
intractable problem for DFT
to explore/screen
– could be task for ML
[1] N. Mounet et al. Nat. Nano, 13, 246 (2018)

## Slide 36: Acknowldegements
This work was supported by resources provided by
the National Computational Infrastructure (NCI), with funding from the Australian Research Council, ARC

## Slide 37: Acknowledgements
Huimin Liu, Ping Wu, Haitao Li, Zibin Chen, Xin Zeng, Yuxiang Zhu, Yijiao Jiang, Xiaozhou Liao, Brian Haynes, Jinhua Ye, Catherine Stampfl, Jun Huang
N2 reduction over Ru/g-C3N4
Bifunctionalization of Metallorganic
Framework (MOF) catalysts
UTS
Lawrence Berkeley
laboratory
Prof D. Winkler
Machine Learning Materials
Prof J. Shapter
Dr Leigh Weston
Dr Sherif Tawfik
Dr O. Isayev
Prof. Mike Ford
Dr Peng Zhang

## Slide 38
Questions?

## Slide 39
The work function of
bulk Ru is 5.4 eV;
That of g-C3N4 is
4.13 eV (or 3.39 eV)
Work function

## Slide 40
Electronic structure of M3(THT)2
 | Fe | Co | Ni
Eg | 0.24 | 0.38 | 0.33
Spin | Polar | Polar | Unpolar
 | Ru | Rh | Pd
Eg | 0.65 | 0 | 0.24
Spin | Unpolar | Unpolar | Unpolar
 | Os | Ir | Pt
Eg | 0.98 | 0 | 0.33
Spin | Unpolar | Unpolar | Unpolar

## Slide 41
d-band center (eV)
Fe | Ru | Os
-1.23 | -1.88 | -2.05
Co | Rh | Ir
-1.56 | -2.13 | -.59
Ni | Pd | Pt
-1.88 | -2.62 | -3.01

## Slide 42
Ead | OOH | O | OH
Fe | 1.36 | 3.92 | 2.51
Ru | 1.76 | 4.86 | 2.35
Os | 1.96 | 5.59 | 3.18
Co | 0.87 | 3.77 | 2.07
Rh | 0.96 | 4.03 | 2.08
Ir | 0.95 | 3.91 | 2.18
Ni | 0.51 | 3.68 | 1.93
Pd | 0.64 | 3.74 | 2.05
Pt | 0.49 | 3.63 | 1.90
Fe/Fe2Co | 1.37 | 3.95 | 2.52
Co/Fe2Co | 0.89 | 3.56 | 2.07
Fe/FeCo2 | 1.37 | 3.98 | 2.58
Co/FeCo2 | 0.86 | 3.75 | 2.02

## Slide 43
Electronic structures of M3(THT)2

## Slide 44
 | Fe | Co | Ni | Fe2Co | FeCo2 | Fe2Ni | FeNi2
Eg | 0.24 | 0.38 | 0.33 | 0.30 | 0.35 | 0.27 | 0.30
Spin | Polar | Polar | Unpolar | Polar | Polar | Polar | Polar
 | Ru | Rh | Pd | Ni2Pd | NiPd2 | Fe2Ir | FeIr2
Eg | 0.65 | 0 | 0.24 | 0.30 | 0.27 | 0.03 | 0
Spin | Unpolar | Unpolar | Unpolar | Unpolar | Unpolar | Polar | Polar
 | Os | Ir | Pt | Rh2Ir | RhIr2 | Ni2Ir | NiIr2
Eg | 0.98 | 0 | 0.33 | 0 | 0 | 0 | 0
Spin | Unpolar | Unpolar | Unpolar | Unpolar | Unpolar | Unpolar | Unpolar

## Slide 45
Fe | Fe/Fe2Co | Fe/Fe2Co
-1.23 | -1.14 | -1.15
Co | Co/FeCo2 | Co/FeCo2
-1.56 | -1.56 | -1.57
d-band center (eV)

## Slide 46
Motivation
1
Three technologies for
harvesting the energy
of the sun, producing
electricity or H2
(hydrogen) fuel:
Photovoltaics
Photocatalysts
Fuel cells
Notes: Because the energy crisis caused by the depletion of fossil fuels and the environmental pollution caused by the traditional way of energy utilization, it is urgently to develop new green/sustainable energy sources, including nuclear energy, wind energy, water conservancy, solar energy and so on.

## Slide 48: Ammonia Synthesis
Synthetic ammonia process is also called Haber-Bosch process which produces ammonia from gaseous N2 and H2. The elementary reaction steps are the following,
H2 + 2* = 2H*
N2 + 2* = 2N*
N* + H* = NH*+*
NH* + H* = NH2*+*
NH2* + H* = NH3*+*
NH3* = NH3 + *
Cleavage of the strong N2 bond is
The rate-determining step
Haber-Bosch has disadvantages such
As using high value-added clean energy H2,
Harsh reaction conditions (high temperature 400-500 C
And pressure, 150-300 bar)

## Slide 49
Motivation
Two factors determine the performance of ORR catalysts:
1. The elemental composition and the interactions between different components
2. Specific surface area and porous structure
Chem. Soc. Rev. 2015,44,2168.
Notes: Two factors determine the performance of ORR catalysts: the first one is the elemental composition and the interactions between different components, which determines the intrinsic catalytic activity of catalysts.

## Slide 50
MOFs materials
high surface area
uniformly distributed coordinated metal
controllable porous structure
Notes: MOFs materials, consisting of well-organized metal centers and organic linkers, are appealing for ORR catalysts due to their high surface areas and well-defined porous structures. The high surface area and the uniformly distributed coordinated metal atoms of MOFs maximize active site density, and the controllable porous structure will be favorable to the sufficient exposure of active sites and good transport properties of ORR-relevant species. These advantages make MOFs as promising electrocatalysts for ORR.
A key issue in determining the performance of the ORR catalysts is the metal/ligand structures in the MOF materials. Although many pioneering investigations on MOF-derived ORR catalysts have been carried out, only limited MOF structures have been studied.

## Slide 51
Volcano relationship
J. Phys. Chem. B 2004,108,17886.
Adsorption energy
Activity
Notes: One example is the classic volcano relationship between the catalytic activity of ORR catalyst and the adsorption strength of O atom on the surface of metal catalyst. It is cleat that Pt displays the best ORR catalytic activity due to its favorable adsorption strength of ORR intermediates. Based on the Sabatier principle, an ideal ORR catalyst should bind the ORR intermediates not too strongly nor too weakly. From this figure we know that, Ag and Au on the right leg donot display good catalytic activity due to their weak adsorption of ORR intermediates. On the other hand, Fe and Co on the left leg also donot exhibit good catalytic because of their strong adsorption strength.

## Slide 53
Machine Learning Hybrid 2D Materials

## Slide 55: Urea

## Slide 56: Pharmaceutical produced from ammonia: Sulfanilamide (sulphanilamide) sulfonamide antiobiotic molecule

## Slide 57
Reaction Free Energy diagrams of ORR/OER on M3(THT)2
Schematic free energy diagrams of ORR/OER at electrode potential U=0 (a)
and (b) U=1.23 V.