## Slide 1: Defects physics in emergent 2D material SnSe with binary phosphorous structure
Yi Zheng (郑 毅)
Department of Physics, Zhejiang University
phyzhengyi@zju.edu.cn
http://person.zju.edu.cn/yizheng
1

## Slide 2: Contents
Unique SnSe
  Binary BP
  Thermoelectric
Defects physics in SnSe
  Hole doping by SnSe2
  3D Fermi surface by point dislocations
Conclusions and Perspective
2

## Slide 3: Our Device Lab
I. Topological Semimetals
  Weyl SMs
    PRB 93, 12112(R) (2016); ESI highly cited
    Front. Phys. 12, 127205 (2017)
II. Novel 2D materials
  SnSe Family
  SnSe2 Family
  ….
3

## Slide 4: Binary BP
XV
XIV
XIII
XVI
XVII
4

## Slide 5: Motivation
Y. B. Zhang group
Nat. Nano 2014, 2015, 2016
Semi-Dirac transition
“Giant Stark Effect”
Science 349, 723 (2015)
5

## Slide 6: Motivation
6

## Slide 7: Motivation
a: NaCl-type
b:R-1 InAs GaSb
D-1 GeTe ZnS
c:R-2 PtSe2
D-2 WSe2
PtSe2
7

## Slide 8: Motivation
Intrinsic p-type Semi？
high ZT (Physics? Electronic structure)
Stable in air (Exfoliation and devices)
8

## Slide 9: Figure of merit, ZT
Seebeck coefficient
Conductivity
Thermo-
conductivity
SnSe:
Due to phonon anharmonicity in SnSe,
Lowest lattice thermal conductivities known for crystalline materials .
Li et. al., Nat. phy. 2015
9

## Slide 10: High ZT: General Picture
I. Unharmonic Phonon
II. Multi-valley
III. Other mechanisms
Single Parabolic Band
10

## Slide 11: SnSe2 Microdomains
Wang et. al., Nat. Commun. 9, 47 (2018)
11

## Slide 12: SnSe2 Microdomains in SEM
12

## Slide 13: Extrinsic Hole Doping
Metallic
Semiconducting
13

## Slide 14
Methods | Growth steps One step for self flux and Bridgeman Two steps for PVD |  |  |  | Se:Sn | SnSe2 | point dislocations | n (1018)
Self Flux (SF) |  |  |  |  |  |  |  | 
 | 1. Heating up | 2. Persistent time |  | 3. Cooling |  |  |  | 
 | 10 hrs to 950oC; all batches | 1500 mins | SF1 | natural cooling: 1day | 1 | 0.9% | 4.5×104 mm-2 | 1.16
 |  |  | SF6 |  | 1 | 0.3% |  | 0.69
 |  |  | SF7 |  | 1 | 3.73% |  | 1.23
 |  | 3000 mins | SF3 | 4000mins to 400oC | 1 | <0.3% | none | 0.592
 |  |  | SF5 |  | 1 | none |  | --
 |  | 6000 mins | SF8 | 9999mins to 400oC | 1 | <0.1% |  | --
 |  | 9999 mins | SF10 | natural cooling: 1day | 1 | <0.1% |  | --
 |  |  | SF11 |  | 1 | 2.6% |  | 1.079
 |  |  | SF12 |  | 0.95 | <0.3% |  | 0.794
Bridgeman (BR) | 10 hrs to 950oC | 9999mins | BR1 | natural cooling；1day | 1 | 2.49% | none | 0.699
 |  |  | BR2 |  | 1 | Not uniform Some >1% Some <0.3% |  | 0.591
PVD | Step1 |  |  | Step2 | 1 | none | Aera1: 5×104 mm-2 Aera2~Aera10: None | --
 | same as batch1 step1 | Grind the single crystal to powder |  | 700oC----800oC In a two-zone furnace persistent for one week |  |  |  | 
14

## Slide 15: Extrinsic Hole Doping
15

## Slide 16: SnSe-SnSe2 Phase Diagram
16

## Slide 17: Interfacial Charge Transfer
17

## Slide 18: Scanning Kelvin Probe Microscopy
1
2
3
4.39 eV
4.56 eV
4.85 eV
SKPM potential
topography
18

## Slide 19: ARPES study of SnSe: Pudding mold
Pudding mold
Kazuhiko, JPSJ, 2007
Nat. Commun. 9, 47 (2018)
19

## Slide 20: ARPES study of SnSe: Multi-valley
Zhao et. al., Science, 2016
Nat. Commun. 9, 47 (2018)
20

## Slide 21
Fermi Surface
EB=0.4
EB=0.3
EB=0.2
Kz
Ky
EB=0.05
Ky
EB=0.1
Ky
EB=0.05
EB=0.1
ARPES: Constant Energy Cuts
21

## Slide 22: ARPES: Constant Energy Cuts
Fermi Surface
EB=0.4
EB=0.2
EB=0.5
EB=0.6
Ky
Kz
Kz
Ky
Ky
EB=0.2
22

## Slide 23: Multi-Valley Seebeck
23

## Slide 24: Weak Localization: Intervalley Scattering
Nat. Commun. 9, 47 (2018)
24

## Slide 25: Anisotropic WL
25

## Slide 26: Anisotropic MR
26

## Slide 27: 3D Fermi Surface
Nat. Commun. 9, 47 (2018)
27

## Slide 28: Point Dislocations
4.5*104 mm2
28

## Slide 29: Interweaving of SnSe Monolayers
Nat. Commun. 9, 47 (2018)
29

## Slide 30
Bismuth-doped n-SnSe: Transport
Unpublished
30

## Slide 31
DFT
Bismuth-doped n-SnSe: ARPES
Unpublished
31

## Slide 32
Exotic Energy Bands and Defects Physics in SnSe
  Pudding-mold shaped VB
    Multi-valley transport
    Quasi-linear (Dirac-like) dispersion
  Two types of peculiar defects
    Local SnSe2 phase segregation
      - Main hole doping mechanism in SnSe
    Point dislocations
      - 3D Fermi surface!
Perspective:
  2D limit, correlated System
    Multi-ferroicity (Ferroelectric+Ferroelasticity)
    Unharmonic Phonon modes (Electron-phonon)
  Electronic devices…
Conclusions
32

## Slide 33: Collaborators
SIMIT, Prof. Dawei Shen (ARPES)
AP Yunhao Lu (DFT)
NUS Assit. Prof Jiong Lu (STM)
Prof. Zhu-An Xu
MOST of China
33

## Slide 34: Our Group
DFT
Exp.