## Slide 1
Manipulating the electronic structure and
magnetism of spin-orbit Mott insulator by
tailoring superlattices
Dawei Shen （沈大伟）
Shanghai Institute of Microsystem and Information
Technology (SIMIT), Chinese Academy of Sciences

## Slide 2
Acknowledgements
Congcong Fan, Dr. Zhengtai Liu, Wanling Liu, Dr. Jishan Liu, Prof. Mao Ye SIMIT, CAS;
Prof. Akio Kimura,
Hiroshima U; Dr. Yukiharu Takeda and
Yuji Saitoh, SPring-8;
Prof. Peng Wang and Prof. Xiangang Wan, Nanjing U; Prof. Yunhao Lu and Prof. Yang Liu, Zhejiang U; Dr. Arthur Ernst, MPI-MSP.
SrIrO3 growth and their electronic structure tuning through superlattices; transport, photoemission and XMCD measurements on films and superlattices
Hard X-ray photoemission, XAS and XMCD measurements on SrIrO3 films and related super-
lattices at Spring-8
Scanning TEM and theoretical supports and helpful discussions
Grants: MOST, CAS and NSFC
Notes: .

## Slide 3
Spin
Lattices
Charge
3d-electrons
More competing degrees of freedom in 4d-/5d-electron system
Orbital
5d-
electrons
Spin liquid
Mott insulators, HTC?
Topological insulators
Quantum spin Hall effects
Kitaev-model systems
Weyl
Semi-
metals

## Slide 4: Outline
Oxide Molecular Beam Epitaxy
Angle-Resolved Photoemission Spectroscopy
New tools for investigating and manipulating novel states of matters
Manipulating the electronic structure of topological crystalline semimetal perovskite SrIrO3 by tailoring superlattices
Notes: In our case, we used the combo of oxide MBE, in-situ ARPES and XMCD to study 5d electron oxide systems.

## Slide 5
RHEED oscillation (<1%)
Oxide Molecular Beam Epitaxy : “Atomic Spray Painting”
O2 or O3
Superlattice, Interface
New Phase
Courtesy of Dr. Carolina Adamo

## Slide 6
Complementary characterizations through ARPES and XMCD
Angle-Resolved Photoemission
Spectroscopy
（ARPES）
X-ray Magnetic
Circular Dichroism （XMCD）
1. Element specific magnetic properties

## Slide 7: The necessity and possibility of synergistic collaborations
Atomically clean surfaces
Restricted to cleavable samples
Not sensitive to magnetism
Films grown under ultra-high vacuum conditions, not energetic deposition
Epitaxial growth allows for study of “uncleavable” materials
Artificial interfaces/super-
lattices
ARPES
Kind of bulk sensitive
High sensitivity to magnetism
Easy measurements on films/superlattices
XMCD
OMBE

## Slide 8
Integrated Oxide MBE + ARPES at SIMIT
ARPES System
Oxide MBE
Transfer chamber

## Slide 9
Shanghai integrated Platform for Energy and
Environment-friendly Materials (SiP∙ME2)
New generation of platform for in-situ electronic structure probing
03U Beamline
Endstation

## Slide 10
Comparison with other beamlines
Beamlines | In-situ means | Light sources |  |  |  | ARPES |  | 
 |  | Flux Photon/s | Photon Energy eV | Resolu-tion E/∆E | Spot Size 𝛍m | Analy-zer | Resolu -tion meV | Temp K
SiPME2 | OMBE /PLD | 1.3x1013 | 5.9-400 | 33000@21.6eV | ~80 | DA30 | 0.73 | 4.5-400
Elettra APE | Sputtering | 2x1011 | 8-120 | 30000 | 50 | DA30 | 6 | 15~1000
ALS 7.0.2.1 | PLD | 3x1012 | 20-1000 | 30000 | <10 | R4000 | 10 | 15-2500
ALS 10.0.1.1 | ╳ | 1x1013 | 17-350 | 35000 | 100 | R4000 | 10 | 20-1000
SLS SIS | PLD | 2x1013 | 10-800 | 100000 | 50 | R4000 | 5 | 15~400
Diamond I05 | ╳ | 5x1012 | 18-240 | >20000 | 70 | R4000 | 5 | 10-300
SSRL 5-4 | MBE | 8x1011 | 7-40 | 20000 | 100 | R4000 | 3 | 5~300
Notes: .

## Slide 11: Outline
New tools for investigating and manipulating novel states of matters
Manipulating the electronic structure of topological crystalline semimetal perovskite SrIrO3 by tailoring superlattices
Z. Liu and DWS, Sci. Rep (2016); C. C. Fan and DWS, AIP Adv. (2017);
W. L. Liu, DWS, in preparation

## Slide 12
F. Wang, PRL, 2011; H. Watanabi, PRL, 2013
Sr2IrO4: spin-orbit Mott insulator high-Tc SC parent?
In remarkable analogy of (LaSr)2CuO4 in many aspects:
Share K2NiF4 crystal structure
Mott insulator before carrier doping
Pseudospin j = ½ maps to similar Hubbard model
B. J. Kim, PRL, 2008
An ideal system for the comparison study of cuprates and I-M transition is desired!
Unconventianal SC
B. J. Kim, PRL, 2012

## Slide 13
Electronic structure evolution of carrier-doped Sr2IrO4
Both MBE- and flux- grown lightly La doped Sr2IrO4 show evident Fermi arcs; Effective doping levels: MBE: x~0.046, Flux: x~0.05
Both samples exhibit insulating ground state, down to ∼50 K followed by an upturn at lower temperature, comparable to UD cuprates.
No signs of superconductivity.
M. Y. Li and DWS, CPL, 2015
A. Torre, PRL, 2015

## Slide 14: Manipulating iridates by tailoring superlattices
O3 2x10-6Torr
SrIrO3 epitaxial superlattices
SrTiO3
SrIrO3
Time
1 loop
m loops
SrIrO3/SrTiO3/SrIrO3… (m=1)
@620 ℃
SrIrO3(100)/STO(100)
SrTiO3(100)/STO(100)

## Slide 15
SrIrO3 based superlattices
RHEED
RHEED pattern & intensity oscillation
X-Ray Diffraction

## Slide 16: The HAADF TEM Pattern of the Superlattices
15 u. c. m=1/2 SLs on STO（001） substrates
Superlattices
STO buffer
STO substrate

## Slide 17
R-T curves
Valence bands
When m ≤ 2 system becomes insulator, MIT takes places;
Jeff = state shift down from Fermi level;
Jeff = mixes with Jeff = state，and textbook band-control Mott transition.
Superlattices: metal-insulator transition

## Slide 18
SrTiO3
Diamagnetic
A real quantum phase transition, and the origin?
SrIrO3
Paramagnetic
SrTiO3
Diamagnetic
Emergent weak ferromagnetism
ground state
Even different from Sr2IrO4
Emergent magnetism in the superlattices
PRL 114, 247209 (2015)

## Slide 19
O K-edge
Ti L-edge
Ti signal from STO substrate?
Increasing
intensity
at Ti edge
Increasing percentage of SrTiO3
0%
33%
50%
X-ray absorption spectra of (SrIrO3)m/(SrTiO3)

## Slide 20
m=1/2
m=1
m=2
m=∞
O2p -
O2p - Ti3d
Pre-edge states (529, 530.8eV): O2p hybridized with Ir5d and Ti3d
XAS at O K-edge of SLs
Corresponding XMCD signals responsible for ferromagnetism
XAS and XMCD of (SrIrO3)m/(SrTiO3) at oxygen K-edge
Ti3d
Notes: One

## Slide 21
Emergence of magnetic ordering of Irjeff=1/2 states
The m=1 SIO/STO develops a canted in-plane AFM (weak FM), in contrast to Sr2IrO4
Canted in-plane (low-dimensional) AFM ordering in monolayer IrO6
Rotation of the IrO6 octahedral due to
lattice mismatch
Dzyaloshinskii-Moriya
(DM) interaction
Sr2IrO4 (H=0)
SIO/STO (m=1)
PRL 114, 247209 (2015); PNAS 113, 6397 (2016)

## Slide 22
Circular-polarized-XAS and XMCD for m = 1 sample (TC=130K)
Ti L23 edges
No net Ti XMCD signals for superlattices !
According to this data, non-magnetic or just AFM for Ti! Plausibly Ti4+ would be non-magnetic!
Is this the truth?

## Slide 23
No charge transfer at interfaces in m=1/2 SL No Ti3d XMCD signal
STO Buff
HAADF-STEM
Collaborate with Prof. P. Wang @NJU, M. Ye @SIMIT
Standard Ti4+ in buffer layers, no oxygen vacancies
Negligible change of valence for Ti atoms in m=1/2
No distinct XMCD signal around 530.8 eV (Ti3d states)
XMCD
STO
STO
SIO
STO
STO
SIO
Ti L-edge
O K-edge
EELS based on STEM
Ti4+
Ti4+
Ti4+
Ti4+
m=1/2

## Slide 24
-2
Micron, 2012, 43(4): 532
STO Buff
STO
SIO
SIO
STO
SIO
SIO
m=2
HAADF-STEM
EELS based on STEM
Ti3+
Ti4+
Ti4+
Ti3+
Ti4+
Ti L-edge
O K-edge
Standard Ti4+ in buffer layers, no oxygen vacancies
Evident charge transfer at interfaces between IrO6 and TiO6 in m=2, Ti3+ states
XMCD signal around 530.8 eV (hybridized with Ti3d)
XMCD
Pronounced charge transfer at interfaces in m=2
Collaborate with Prof. P. Wang @NJU, M. Ye @SIMIT

## Slide 25
Moderate charge transfer at interfaces in m=1
STO Buff
SIO
STO
SIO
SIO
STO
m=1
HAADF-STEM
EELS based on STEM
STO
Ti4+~3+
Ti4+
Ti4+
Ti4+
Ti L-edge
O K-edge
Ti4+~3+
Standard Ti4+ in buffer layers, no oxygen vacancies
Moderate valence change for Ti in m=1
Small XMCD signal around 530.8 eV (Ti3d)
XMCD
Collaborate with Prof. P. Wang @NJU, M. Ye @SIMIT

## Slide 26
The charge transfer across nonpolar interfaces;
Electrons transferring from Ir to Ti: for m=2, larger in-plane octahedral rotation
would result in more prominent charge transfer than for m=0.5.
Charge transfer tuning by oxygen octahedral rotation manipulation
Rotation of the IrO6 octahedral due to
lattice mismatch
First-principles
simulation

## Slide 27
Emergence of magnetic ordering at interfaces
O2p-Ti3d K-edge shows substantial XMCD signal, while Ti L2,3 doesn’t.
SIO/STO (m=1)
No Ti net FM: less lattice constant
mismatch and smaller SOC render
the non-canted AFM, no net Ti L edge XMCD signal.
The observed XMCD signal at the O K-edge
(O2p-Ti3d hybridization) originates from the oxygen atoms at the interface due to the charge transfer between Ir and Ti.
The oxygen atoms at interfaces (symmetry broken) exhibit emerging weak FM due to strong SOC and crystal field.

## Slide 28
We conclude…
We fabricate a family of perovskite SrIrO3 based superlattices by means of oxide MBE technique.
Through tuning the band width, we could manipulate the ground state of the superlattices (m=0.5/1, Mott insulators with canted AFM; m=∞, paramagnetic semimetal).
In-situ photoemission measurements confirm the Mott insulator-
metal transition in these superlattices.
XMCD findings clarify that the emergent ferromagnetic order at
interfaces, with Ir character in the Jeff=1/2 orbital and O character
between Ir and Ti, which originates from the interplay of electron
correlations, crystal field and spin-orbit coupling in the low
dimension.
The manipulation of electronic structure in SIO/STO SLs is not simply only due to the change of dimensionality, but also due to the interfaces.

## Slide 29
Thank you!

## Slide 30
Perovskite SrIrO3: lattice symmetry protected line nodes?
Predicted robust node lines due to
combination of SOC and lattice symmetry
  Semimetal with no magnetism
  Low carrier density
A strong topological insulator
once the mirror symmetry is broken
PRB 86, 085149 (2012); arXiv:1504.07641; arXiv:1506.03449
Notes: The simplest iridate is the perovskite SrIrO3, and it has long been predicted to be the candidate of the so-called topological crystalline semimetal. There exists the lattice symmetry protected line nodes in the band structure. However, the synthesis of bulk single-crystalline 113 is very difficult and so far no

## Slide 31
High quality single crystal film of SrIrO3
XRD results
Smooth and uniform Laue oscillation
The FWHM is identical to substrates
TEM results
Regular lattices
Sharp interface between SIO and STO
XRD patterns of SrIrO3(100) films
with different stains
Notes: However, high-quality single crystalline 113 films could be achieved by means of oxide MBE methods. Our group is among the first serval research groups who have successfully fabricate high quality 113 films by MBE. Actsaully, we have tried various films with different strains, and the resulting XRD patterns prove the superior quality of films. While, we found the 113 films deposited on STO substrates are superior to others. The clear laue oscillation and the narrow FWHM of rocking curve indicates the

## Slide 32
Simultaneous intersection of the Fermi level by hole- and electron-like bands;
The direct evidence that the perovskite SrIrO3 has a semimetallic ground state.
Direct observation of the semi-metallicity caused by strong SOC

## Slide 33
Topological crystalline protected Dirac node lifting
Band dispersions around U point
DFT
Topological protected Dirac node is lifted!

## Slide 34
Dirac node lifting
Symmetry operations of the Pbnm perovskite ABO3
Dirac nodes with different symmetries
Strain effect: n-glide symmetry is broken
Gapped Dirac node due to absence of n-glide operation
PRB 93, 085118 (2016)
Epitaxial perovskite SrIrO3 is a topological crystalline semimetal, but with the crystalline symmetry protected Dirac node lifted due to strain!