## Slide 1: Neutron scattering for restricted dimensionality in magnetism: interfaces, surfaces and more!
Kirrily Rule
Australian Centre for Neutron Scattering

## Slide 2: Outline
Neutrons for magnetic scattering
  Diffraction
  Inelastic neutron scattering
Thin films and interfaces
  FePt3
  BiFeO3
Magnetic nanoparticles
  Silver doped LaMnO3
Frustrated magnetic chains
  Linarite
J1 = FM
J2 = AFM

## Slide 3: OPAL - multi-purpose reactor
Medical radioisotopes
Scientific research
Neutron activation
Silicon irradiation

## Slide 4: Advantages of neutrons
Wavelength
Strong interaction
Highly penetrating
Magnetic moment
Non-destructive
Energy

## Slide 5
KOOKABURRA
BILBY
JOEY
DINGO
PELICAN
SIKA
PLATYPUS
QUOKKA
ECHIDNA
WOMBAT
KOWARI
KOALA
TAIPAN
3He filling station
15 Neutron Beam Instruments
+ SAXS & X-ray Reflectometry + PPMS
EMU
SPATZ
The Australian Centre for Neutron Scattering

## Slide 6
Elastic Neutron Scattering
No loss of energy
Examines the change in momentum or angle of the neutrons.
Inelastic Neutron Scattering
Examines both momentum and energy dependencies.
Uses these to characterize a systems vibrational, magnetic, and lattice excitations.

## Slide 7: Excitations in materials
Nuclear excitations can tell us about
Interatomic potentials & bonding
Phase transitions & critical phenomena (soft modes)
Fluid dynamics
Diffusion processes
Momentum distributions & Superfluids ( eg. He)
Interactions (eg. electron-phonon coupling)
Magnetic inelastic scattering can tell us about
Exchange interactions
Single-ion and exchange anisotropy (determine the spin Hamiltonian)
Phase transitions and critical phenomena
Quantum critical scaling of magnetic fluctuations
Other electronic energy scales (eg CF and SO)
Interactions (eg spin-phonon coupling)

## Slide 8
Two different modes:
Inelastic scattering
  To measure excitations and dynamics in materials
  Energy range:
    ~5-90meV (PG), ~30-200meV (Cu)
  Energy resolution:
    ~ 1 meV (PG)
Elastic scattering
  To measure diffraction when a high signal to noise ratio is required
  Wavelength range:
    1-4 Å (PG) 0.6-2.5 Å (Cu)
Types of samples:
Single crystals
Powder
Multi-crystal arrays including thin films
TAIPAN

## Slide 9
2θM
2θS
2θA
1
2
3
Source
Detector
Monochromator (PG002)
Analyser (PG002)
Sample
Triple Axis Spectrometer

## Slide 10
TAIPAN – Be-filter
  Lattice and molecular excitations in complex materials in the form of phonon density of states
  Molecular vibrations as “fingerprints” of surroundings
  Future energy storage (hydrides)
  Oil and chemical industry catalysts (zeolites)
  Nano-crystalline materials for industry
  Coal studies
  Nuclear Fuels

## Slide 11: FePt3: Chemical Order  Antiferromagnetism
Fe Occupies Corners
Pt Occupies Faces
Deposition at Tdep ~ 900 K
(001)
(002)
X – ray Diffraction
MgO
Saerbeck et al., PRB 82, 134409 (2010),
Saerbeck et al.,Procedia Engineering 36, 488 (2012)

## Slide 12: FePt3: Chemical Disorder  Ferromagnetism
Deposition at Tdep = 800 K
(002)
X – ray Diffraction
Disorder
Random Distribution of Fe and Pt
MgO
Saerbeck et al., PRB 82, 134409 (2010),
Saerbeck et al.,Procedia Engineering 36, 488 (2012)

## Slide 13: Chemical order modulation
Chem. Order:
AFM
Chem. Disorder: FM
Disorder
+
Fe on Corners
Pt on Faces
Random Distribution of Fe + Pt

Modulation of Deposition Temperature
MgO(100)
FM
AFM
FM
AFM
…but only one material!
Saerbeck et al., PRB 82, 134409 (2010),
Saerbeck et al.,Procedia Engineering 36, 488 (2012)

## Slide 14: Chemical order modulation
Chem. Order:
AFM
Chem. Disorder: FM
Disorder
+
Fe on Corners
Pt on Faces
Random Distribution of Fe + Pt
Saerbeck et al., PRB 82, 134409 (2010),
Saerbeck et al.,Procedia Engineering 36, 488 (2012)
Tc ~ 300K

## Slide 15: High Angle Neutron Diffraction
Thin Film
(S = 2800Å)
5 x Multilayer
(0 ½ ½) AFM order
(0 ½ ½)
(0 ½ ½)
S = 86 %
Saerbeck et al.,Procedia Engineering 36, 488 (2012)
Ferromagnet
Interface (Frustration)
Antiferromagnet

## Slide 16
Multiferroic thin films
Multiferroics – materials which possess 2 or more of the following, with coupled order parameters:
(anti) ferromagnetism
(anti) ferroelectricity
(anti) ferroelasticity
BiFeO3 is both magnetic and strongly ferroelectric at room temepraure.
BiFeO3 has an incommensurate magnetic structure with a spin cycloid periodicity of ~62-64nm

## Slide 17: Spin cycloid in a 100nm BiFeO3 film
NATURE COMMUNICATIONS | 7:12664 | DOI: 10.1038/ncomms12664
Bulk: k|| [110]
100nm film: k|| [112] and
k┴ [11-2]

## Slide 18
NATURE COMMUNICATIONS | 7:12664 | DOI: 10.1038/ncomms12664
ICM magnetic satellite peaks
Cycloid propagation length = 64.7 nm, which is consistent with the bulk value.

## Slide 19: Ag doped nanoparticles of LaMnO3
Hollow sphere aggregates made via the spray pyrolysis method – diameters ~ 70nm
Desired Ag Concentration | EDS Result
2.5% | 2.65%
5% | 4.78%
10% | 10.5%
Ag doping gave an O-rich phase
What role does the Ag play in: Magnetism, stoichiometry, Jahn-Teller distortions and phonon propagation?
How does this compare to the bulk?

## Slide 20: Neutron elastic scattering - TAIPAN
Bulk LaMnO3 | Nano La1-xAgxMnO3* (x = 0, 0.025, 0.05, 0.1)
Stoichiometric | O-rich
J-T around 700K | J-T at RT due to Mn4+
Long range effects | Broadening of features due to finite size effects

## Slide 21: Dynamic properties – LaMnO3
ToF neutron energy loss data
Bulk, stoichiometric LaMnO3
~750K = Jahn-Teller transition
Wdowik et al., PRB 86, 174305 (2012)
PELICAN
TAIPAN
10% Ag sample
300K

## Slide 22: Low dimensional spin systems
One dimensional quantum magnets
Magnetic coupling in only 1 direction
Low spin state magnetic ions
S = ½ or 1 (typically Cu)
Interesting field induced phases
Bose-Einstein condensation (superfluid He)
1 or 2 magnon states
Multipolar phases
Spin nematic phases
Why?
• “easy“ to describe!
Comparison between experiment
and theory is possible with different models
which can help us understand the magnetic
interactions.
CuGeO3
Arai et al PRL 77 3649
6K
22

## Slide 23: Linarite, PbCuSO4(OH)2
23
Monoclinic: P21/m
a = 9.682
b = 5.646
c = 4.683
β = 102.65°
Wolter et al., PRB 85, 014407 (2012)
Rule et al., PRB 95, 024430 (2017)
TN = 2.75K
|ΘCW| = 27K
f = |ΘCW|/TN~10

## Slide 24: J1-J2 frustrated spin chain model (s = ½)
from Furukawa et al. PRL 105 257205 (2010)
J1 = FM
J2 = AFM

## Slide 25
Elastic neutron scattering – high field B||b
μ = 0.44 μB
Phase V

## Slide 26
Inelastic Neutron scattering
L-direction
K-direction
Rule et al., PRB 95, 024430 (2017)
From LSWT we estimate
J1 = -114K,
J2 = 37K and
Jic = 4K
α ~ 0.32

## Slide 27: Conclusions
Neutron scattering is a particularly effective tool for understanding magnetic materials
While often considered a bulk probe, it can also be utilised for materials with reduced dimensionality
Thin films and interfaces
Magnetic nanoparticles
Low dimensional magnets
TAIPAN at ANSTO is a versatile and highly configurable neutron instrument which can be tuned for each scientific problem
Proposal now being accepted (deadline 15th September)
https://neutron.ansto.gov.au/

## Slide 28
Thank you!
T. Searbeck, F. Klose
J. Bertinshaw, R Maran, S Callori, V Ramesh, J Cheung, S Danilkin, W-T Lee, S Hu, J Seidel, N Valanoor, C Ulrich
M. Westlake, M. Tehei, M. Lerch, J Horvat.
B. Willenberg, M Schaepers, L. Heinz, S. Suellow, A. Wolter-Giraud, G. Ehlers, R Mole, S. Nishimoto, S. Drechsler