## Slide 1
The 9th Vacuum and Surface Science Conference of Asia and Australia
VASSCAA-9 13-16 AUG 2018, Sydney
Mild Plasma Configuration
Yielding Efficient Doping on Graphene Surface
Goo-Hwan Jeong
Department of Materials Science and Engineering
Kangwon National University, Chuncheon 24341, Korea

## Slide 2
1. Overview on graphene and doping
2. Graphene synthesis and plasma doping
3. Results and discussion
(1) Structural aspects
(2) Functional doping aspect
(3) Doping stability aspect
4. Summary
Outline

## Slide 3
- The thinnest material sheet, yet the strongest
(5 times stronger than steel and much lighter)
- Is a semimetal
(Electrical properties can be modulated)
- Has high electron mobility (>10000 cm2/Vs at RT) ballistic conduction
- Has very high current densities (109A/cm2)
- Is a superb heat conductor
- Is a novel material for applications such as sensors, composites, transistors,
transparent conductive films, thermal transport media, batteries and solar cells
Graphene
Nobel Prize in 2010

## Slide 4
Application fields of graphene
Flexible display
Transparent devices
Smart window
Solar cell
Secondary battery
Fuel cell
Super capacitor
Nanoelectronics
RFID, Sensors
Conductive ink
EMI shielding
Printing electrode
Aerospace
Automobile
Graphene
LED heat sink
Heat dissipation
Light &
High-strength
composite
Transparent electrode
Future
nanoelectronics
Energy
Devices
Heat dissipation
Printing Electronics
4/36

## Slide 5
Tuning of electronic properties of graphene
Structure modification
Chemical doping
Ref) X. Li et al., Science 319, 1229 (2008)
L. Pisani et al., Phys. Rev. B 75, 064418 (2007)
Band gap (eV)
Width (nm)
Armchair edge
Zigzag edge
Ref) S. Park et al., Nat. Nanotechnol. 4, 217 (2009)
Y. J. Yu et al., Nano Lett. 9, 3430 (2009)
Low temperature
Quick treatment
Plasma-induced damage
Thermal treatment
Plasma treatment
Simple method
High temperature
Time consuming process
Methods for chemical doping of graphene
N
B
n-doping
p-doping
Nano-ribbon
Graphene
sheet

## Slide 6
D- and Dʹ-band (1350, 1620 cm-1): Defect-induced peaks
G-band (1580 cm-1): Graphitic tangential vibration
2D-band (2700 cm-1): Overtone of D-band
Intensity ratio of D- and G-band (ID/IG)  A mount of defect
Intensity ratio of G- and 2D-band (IG/I2D)  The number of layer
Monolayer graphene
IG/I2D: ~0.3
Profile of 2D: Single Lorentzian
Position of 2D < 2700 cm-1
Ref) Z. Ni et al., Nano Res. 1, 273 (2008), A.C. Ferrari et al., Phys. Rev. Lett. 97, 187401 (2006)
Raman spectrum of graphene

## Slide 7
NH3 plasma (0.4 W, 3 sec)
Before plasma treatment
After plasma treatment
D
Dʹ
2D
G
Doping by plasma process
Ref) Y. C. Lin et al., APL 96, 133110 (2010), H. M. Jeong et al., Nano Lett. 11, 2472 (2011), S. H. Park et al., J. Mater. Chem. C 2, 933 (2014)
● Structure degradation due to plasma-induced damage during doping
Suppression of defect formation & Optimization of efficient doping condition
D
N-doping:
ICP, NH3
D
D
N-doping:
ICP, N2, 500 W
Effect of plasma parameters toward defect-free doping on graphene
Plasma condition optimization for ‘efficient chemical doping’

## Slide 8
1. Overview on graphene and doping
2. Graphene synthesis and plasma doping
3. Results and discussion
(1) Structural aspect
(2) Functional doping aspect
(3) Doping stability aspect
4. Summary
Outline

## Slide 9
< Thermal CVD system >
Substrates: 300 nm Ni/ SiO2/ Si
200 nm Ni/ Mo sheet
Feedstock: Methane (CH4)
Temperature: 1000˚C
Synthesis time: 5 min
Graphene synthesis by CVD
Graphene synthesis on
Ni, Pt, Cu and Ni-Mo is possible.

## Slide 10
Other studies on graphene
10/36
● CVD-grown graphene on Ni, Cu, Ni/Mo and Pt substrates
Wafer-scale growth
Synthesis mechanism study
Low-Temp. synthesis
Ni : C-precipitation induced growth
Ni/Mo : Mixing of C-adsorption & precipitation
Cu and Pt : C-adsorption driven growth
PDMS
● CVD-graphene application
Flexible Transparent
Conductive Film
Flexible Transparent
Defrost Film
TEM membrane
‘Graphene-SWNT’
All-carbon device

## Slide 11
Graphene preparation for doping study
11/36
Mech-exfoliation
from graphite

## Slide 12
Biased substrate (Down-cathode)
Grounded substrate (Up-cathode)
Comparative plasma configurations
Ion-bombardment type
Harsh plasma formation
Plasma-immersion type
Mild plasma formation
Gas: NH3
Pressure: 0.3 Torr
Applied voltage: -450 ~ -700 V
Applied power: 0.45, 1, 1.3, 1.65, 2.4, 2.8 W
Time: 3 ~ 3600 sec

## Slide 13
Plasma power & treatment time ∝ (ID/IG) & (ID’/IG)
High plasma power Higher ion energy & dose
Longer plasma treatment time Lager ion dose
Γi = ni(kTe/M)1/2
Di = Γit
Ref) M. A. Lieberman and A. J. Lichtenberg, Principle of Plasma Discharges and Materials Processing, John Wiley & Sons (1994)
Impinging ion flux (Γi) & ion dose (Di)
ni: ion density
k: Boltzmann’s constant
Te: electron temperature
M: ion mass
t: ion irradiation time
Parameters to investigate the plasma effects
Ei = e(Vp-Vt)
Vt (down) = - 450 V
Vt (up) = 0 V
e: electric charge
Vp: plasma potential
Vt: target potential
Ion bombardment energy (Ei)
Ei (down) > Ei (up)

## Slide 14
1. Overview on graphene and doping
2. Graphene synthesis and plasma doping
3. Results and discussion
(1) Structural aspects
(2) Functional doping aspect
(3) Doping stability aspect
4. Summary
Outline

## Slide 15
● Structure change of graphite
Amorphous
carbon (a-C)
Tetrahedral
a-C (ta-C)
(Ref) A. C. Ferrari et al., Phys. Rev. B 61, 14095 (2000)
Nanocrystalline
graphite (NC-G)
Graphite
● Size of in-plane crystallites (La)
Stage 2
(a-C)
ID/IG ∝ La2
Stage 1
(NC-G)
ID/IG ∝ 1/La
Tuinstra-Koenig
Amorphization
Defect formation
A three stage model for graphitic structure
● Structure evaluation from Raman
ID/IG
ɷ̜G

## Slide 16
Effect of plasma power on graphene structure
D
G
Dʹ
2D
Formation of defects on graphene (Transition stage)
Structural degradation of graphene (Stage 2)
Harsh plasma (Down-cathode)

## Slide 17
NH3 plasma: 0.3 Torr, 10 sec
Harsh plasma (Down-cathode)
Effect of plasma power on graphene structure

## Slide 18
Mild plasma (Up-cathode)
Effect of plasma power on graphene structure
Low plasma power below 1.3 W (Stage 1)  Effective doping without structural damage
High plasma power  Higher ion energy & dose : Stage 1  Transition  Stage 2

## Slide 19
Mild plasma (Up-cathode)
Effect of treatment-time on graphene structure
Longer plasma treatment time  Higher ion dose : Stage 1  Transition
Short treatment time below 30 sec  Effective doping without structural damage

## Slide 20
Structure evolution using mild plasma
Mild plasma (Up-cathode)

## Slide 21
Size of in-plane crystallites (La)
La: size of in-plane crystallites
λ: laser excitation wavelength
ID/IG: intensity ratio of D- and G-band
Ref) B. Guo et al.; Nano Lett. 10 (2010) 4957
L. G. Cancado et al., Appl. Phys. Lett. 88 (2006) 163106
Size of in-plane crystallites (La)

## Slide 22
Size of in-plane crystallites (LD)
Ref) A. C. Ferrari et al., Phys. Rev. B 61, 14095 (2000)
M. M. Lucchese et al., Carbon 48, 1592 (2010)
λ: laser wave length (532 nm), C, C': constants related λ
Type of defect formed on graphene
ID/ID' (slope)
Stage 1 7.38: point defect
Transition 5.93: point defect  sp3 increase
Stage 2 2.77: sp3 increase
Crystallites & Type of defect
Ref) A. Eckmann et al., Nano Lett. 12, 3925 (2012)
P. Venezuela et al., Phys. Rev. B 84, 035433 (2011)
 ID/IG ∝ 1/LD (T-K relation)
 ID/IG ∝ LD2 (sp3 increase)
Stage 1: >8 nm & Transition: 5-8 nm
Stage 2: < 5 nm

## Slide 23
Mild plasma (Up-cathode)
Harsh plasma (down-cathode)
OES analysis results
656.3 nm
(Hα)
656.3 nm
(Hα)
391.4 nm
(N2+)
391.4 nm
(N2+)
425.32 nm
(N)
425.32 nm
(N)
486.1 nm
(Hβ)
486.1 nm
(Hβ)
H2
N2
N2
H2
Avantes, Ava Spec, ULS2048L-RS
- Integration time: 1 s
- Averages: 3 times
► In the mild plasma system,
peaks related with hydrogen (Hα and Hβ) are stronger than those of nitrogen (N2+ and N)
► Further study is necessary to clarify the effect of various active species.

## Slide 24
1. Overview on graphene and doping
2. Graphene synthesis and plasma doping
3. Results and discussion
(1) Structural aspect
(2) Functional doping aspect
(3) Doping stability aspect
4. Summary
Outline

## Slide 25
N-bonding configurations and Raman result
Plasma
n-doping
Both electron and hole doping
Up-shift of G-band position (ωG)
Decrease of FWHMG
Change of Fermi level by extra charge carriers
ΔωG = 0.6 cm-1  Δn∼2.4 × 1011 cm-2.
N-C bonding configuration
Doping evaluation from Raman spectrum

## Slide 26
Samples | Intensity ratio (%)
 | N 1s /C 1s
Pristine | 0.26
0.45 W (Stage 1) | 3.34
2.4 W (Stage 2) | 10.34
NH3 plasma: up-cathode, 10 sec
Bonding characterization: XPS

## Slide 27
Bonding characterization: XPS results
Stage 1: Increase of all components including amine bond
Stage 2: Increase of pyrrolic-N. Deacrease of pyridinic-N. Decrease of C=C

## Slide 28
Doping
Doping
Effect of plasma power on functional doping
Mild plasma (Up-cathode)
Harsh plasma (down-cathode)
Stage 2
Transition
Stage 1

## Slide 29
Doping level at optimum condition
n = 1.8 × 1012 cm-2
Change of Fermi level by extra charge carriers
ΔωG = 0.6 cm-1  Δn∼2.4 × 1011 cm-2
Optimum condition: up-cathode, 0.45 W, 10 sec
Effect of treatment time on functional doping
Mild plasma (Up-cathode)
Stage 2
Transition
Stage 1

## Slide 30
15 μm
(a)
Electrode
Electrode
Graphene
3 μm
(b)
(c)
Vacuum-annealed
Plasma-treated
As-fabricated
Similar doping level compare with Raman result is obtained
High carrier mobility is obtained owing to the n-doping w/o structure degradation
Doping characterization using FET device
n = Cg(Vg-VDirac)/e
Charge density (n): 2.07 × 1012 cm-2
n: charge density
Cg: gate capacitance (11.6x10-9 F/cm2)
e: electric charge
Vg: gate voltage
VDirac: gate voltage at Dirac point
Doping level from Raman: n = 1.8 × 1012 cm-2
58.2
-1.1
-29.6
/ CgVg
L, W: channel length, width
Cg: gate capacitance (11.6x10-9 F/cm2)
Vg: gate voltage
μ : carrier mobility
Ids: drain-source current
Vds: drain-source voltage
Carrier mobility (n)
2.1  2.4  4.1 x 103 cm2/Vs

## Slide 31
1. Overview on graphene and doping
2. Graphene synthesis and plasma doping
3. Results and discussion
(1) Structural aspect
(2) Functional doping aspect
(3) Doping stability aspect
4. Summary
Outline

## Slide 32
Doping stability after vacuum annealing
● NH3 plasma treatment
● Vacuum annealing
Equipment: High vacuum chamber
Pressure: 10-6 Torr
Temperature: 100, 300, 500ºC
Time: 1 h
Equipment: DC-plasma system
Pressure: 0.3 Torr
Applied voltage: 450 V
Applied power: 0.45 W
Time: 10 s
● Characterization
Raman, XPS, and Wettability

## Slide 33
Effect of anneal temperature on doped graphene
Plasma: 0.45 W, 10 sec
Annealing: 10-6 Torr, 1 h
Higher temperature  Decreases of ID/IG & IG/I2D  Structural healing of doped graphene
Vacuum annealed
NH3 plasma treated
As-fabricated
100˚C
300˚C
500˚C
La= ~29.1 nm
N = 35
N = 35
La (nm) = (2.4 X 10-10)λ4(ID/IG)-1
La= ~14.7 nm

## Slide 34
100˚C
300˚C
500˚C
G
G
G
Small decreases of ΔωG & Increase of ΔFWHMG  Recovery of doped graphene
High doping stability can be expected
n = 1.2 × 1012 cm-2
n = 1.2 × 1012 cm-2
N = 35
N = 35
Vacuum annealed
NH3 plasma treated
As-fabricated
Effect of anneal temperature on doped graphene

## Slide 35
As synthesized
After NH3 plasma treatment
After vacuum annealing
Contact angle : 71˚
61˚
60˚
XPS and wetting characterization
Intensity ratio (N1s/C1s)
As synthesized: 0.02 (2%)
Plasma treated: 0.06 (6%): Plasma-doped
Vacuum annealed: 0.05 (5%): Highly stable
Investigation of doping stability
Pyrrolic N
Pyridinic N
Graphitic N
• Intensity decrease of pyrrolic-N component is observed  Structure healing
• Intensity of pyridinic-N component is similar  Stable doping
• High intensity ratio of N to C (N1s/C1s)  Stable doping of nitrogen on carbon networks

## Slide 36
Summary
We demonstrated here the mild plasma configuration yielding efficient doping on graphene surface. To employ various ion bombardment energies and plasma doses, we changed the plasma input power and treatment time.
The up-cathode system, which provided a low-energy ion process, was more suitable for plasma doping than the down-cathode system because of its suppression of high-energy ion-induced damage.
For plasma doping, the optimum plasma conditions were obtained in Stage-1. The doping level estimated from Raman analysis was similar to that from FET device. The electron mobility of plasma-treated graphene increased due to the n-type doping on the graphene.
XPS indicated that graphitic-N and pyridinic-N contribute to the formation of C-N bonds in the doped graphene in Stage-1. On the other hand, pyrrolic component is responsible for structure degradation in Stage-2.
It is found that the crystallite size of the plasma-treated sample increases after vacuum annealing and the degree of the structure healing is enhanced with increase of annealing temperature.
The nitrogen doping level after the annealing shows similar value compare with the plasma-doped sample meaning high doping stability.
Notes: The order is as follow.

## Slide 37
Thank you
Collaboration with
FET: Prof. Sangwook Lee (Ewha Womans Univ. , Korea)
FET: Dr. Dong-Hoon Shin (Ewha Womans Univ., Korea)
Main experiment: Byeong-Joo Lee (Ph. D candidate)
Budget: National Research Foundation of Korea (2013-2015, 2016-2018)
Notes: The order is as follow.