## Slide 1
Adsorption and absorption of hydrogen
in Titanium dioxide
K. Fukutani
2018/08/14
Institute of Industrial Science
The University of Tokyo
Co-workers:
Y. Ohashi, N. Nagatsuka, A. Sakurai
S. Ogura, S. Ashihara

## Slide 2
Interaction of H with TiO2 surfaces
Behavior of proton and electron
at TiO2 surfaces
Photocatalytic water splitting
and H2 generation
TiO2
Hydrogen sensor
H-induced conductivity
2H+ + 2e- → H2
proton
electron
+
H

## Slide 3
Rutile TiO2(110)
Anatase TiO2(101)
s
p
Ti4+(3d0)O2-(2p6)
O2p
bonding
anti-
bonding
eg
t2g
Ti3d
eg
eg
t2g
t2g
Band gap
~3 eV
Electronic structure of TiO2

## Slide 4
Background 1
X.Y. Lin et al., ChemPhysChem 9, 253 (2008)
K. Fukada et al., JPSJ 84, 064716 (2015).
O
Ti
H
H adsorption on rutile TiO2(110):
OH formation
・Charge transfer
from H to Ti
・Formation of in-gap state
・Electronic excited state
at ~2.5 eV above EF
A. Argondizzo et al., PRB 91, 155429(2015)
Z. Wang et al., JACS 137, 9146 (2015).
e-

## Slide 5
Background 2
O
Ti
H
Hydrogenation of TiO2
Enhancement of solar absorption
Wang et al., Adv. Func. Mater. 23, 5444 (2013).
Nandasiri et al., JPCL 6, 4627 (2015)
High pressure
Plasma
Ion implantation
H implantation at 40 keV
Importance of disorder

## Slide 6
Purpose of the present study
Sample:
rutile TiO2(110) & anatase TiO2(101)
Atomic H dose:
adsorption on the surface
H ion irradiation at 500 eV
incorporation of H into the near-surface region
How much H is present at the surface / near-surface region?
What is the effect of H on the electronic structure?
How H behaves upon heating?
O
Ti
H
SRIM: penetration depth ~8 nm
Notes: nmat_5_665

## Slide 7: Experiment 1:Nuclear reaction analysis (NRA)
ER
ER+D E
g yield
ER
ER+D E
15N Energy (E0)
15N+1H →12C+α+γ（4.43MeV）
Resonance energy(ER) = 6.385 MeV
Resonance width = 1.8 keV
Stopping power
Depth resolution< 5 nm
Lateral resolution< 30 mm
sensitivity < 1019/cm3
M. Wilde & KF, Surf. Sci. Rep. 69 (2014) 196.
Notes: Nuclear reaction we use

## Slide 8
Experiment 2: photoemission
Laser
（～100 fs）
0.85-
1.0 eV
BBO (OPA)
1.55 eV
BBO (SHG)
0.55-
0.70 eV
1.7-2.0 eV
BBO (4HG)
3.4-4.0 eV
Ti:Saphire
l/2 plate
He I
（21.22 eV）
e analyzer
・HeI：1-photon PES
occupied state
・Laser：2-photon PES
unoccupied state

## Slide 9
Rutile TiO2(110)
Anatase TiO2(101)
s
p
Ti4+(3d0)O2-(2p6)
O2p
bonding
anti-
bonding
eg
t2g
Ti3d
eg
eg
t2g
t2g
Band gap
~3 eV
Electronic structure of TiO2

## Slide 10
delocalized
localized
polaron
U
H → H+ + e-
Hydrogen adsorption
Electron doping & polaron formation
Hou &Terakura,
JPSJ 79,114704 (2010)
(H+ O2- → H- + O + e-)
Excess e-
-
-
+
+
e-
+
+
-
-
M. Setvin et al., PRL 113 (2014) 086402
d

## Slide 11
Hydrogen adsorption on r-TiO2 & a-TiO2
rutile-TiO2 (110)
Downward shift of VBM
Presence of in-gap state
rutile:〇, anatase: ×
Decrease of work function
anatase-TiO2 (101)

## Slide 12
NRA: Hydrogen coverage
rutile-TiO2 (110)
anatase-TiO2 (101)
Notes: (1ML =cm-2)
(1ML =5.17×〖10〗^14cm-2)

## Slide 13: Band bending and surface dipole
H+
e-
EF
CB
VB
Surface
dipole
BB：band bending
proton：on the surface
electron：subsurface & bulk
JPCC_115_7562 (2011)
JPCM 24, 435504 (2012)
rutileTiO2(110)

## Slide 14
Band bending & electron affinity
EF
CB
VB
Surf.
dipole
BB
Rutile TiO2(110)
Anatase TiO2(101)
Rutile<Anatase
K. Fukada et al., JPSJ 84 064716 (2015)
N. Nagatsuka et al. in prep.
Rutile>Anatase

## Slide 15
Hydrogen on r-TiO2 & a-TiO2
VB
CB
Rutile
Anatase
EF
CB
VB
IGS
EF
CB
VB

## Slide 16
Diffusion of Hydrogen
Thermal desorption:
no significant signal < 10-3 ML
Diffusion into bulk
UPS: disappearance of
surface dipole
Notes: (1ML =cm-2)
(1ML =5.17×〖10〗^14cm-2)

## Slide 17
・ Enhanced IGS intensity
~10 times larger than H-ads. surface
1P-PES：H-irradiated r-TiO2(110)
EF
CB
VB
IGS
Surface gets metallic?
・ Downward band bending ~0.5 eV:
・ No change around VBM

## Slide 18
NRA：H-irradiated TiO2(110)
8.2 ML at saturation
5.6 at. %
Cf. H adsorption
0.47 ML
Annealing at 673 K
UPS: in-gap state
Reduction of H: 8.2 → 1.4 ML
Reduction of IGS
Notes: Most of H comes from a deeper region, the amount of H near the surface within 1 nm

## Slide 19
2P-PES：H/ rutile-TiO2(110)
傾き=0.94
Resonance at ~3.5 eV
No particular dispersion
localized
Slope=0.94
VB
CB
EF
-0.8
2.7
IGS
ExS
-3
E-EF
(eV)

## Slide 20
Photon energy (eV)
Peak position (eV)
Photon energy (eV)
Intensity (arb. u.)
2P-PES：H-irradiated TiO2(110)
Resonance at ~3.5 & ~3.7 eV
Slope~1

## Slide 21
2.3 eV
0 eV
Peak1
Peak2
Peak3
2P-PES：H/Anatase-TiO2(101)
VB
CB
EF
Evac
1.5 eV
Peak 1
Peak 2
Peak 3

## Slide 22
With increasing H coverage
Deviation from G by 0.1 -1
Dispersion：H/Anatase-TiO2(101)
Cf. dispersion of SS on a vicinal surface：PRB 77, 085425 (2008)
･disappearance of
clean surface feature
･appearance of
H-induced feature
Large dispersion
delocalized

## Slide 23: Comparison with black titania
Plasma-treated/ ultrasonic treated
C. Fan et al., Sci. Rep. 5, 11712 (2015)
X. Chen et al., Science 331, 746 (2011); Sci. Rep. 3, 1510 (2013)
Tailing of VB
High pressure H2

## Slide 24
H-ads.
VB
CB
EF
-0.8
2.7
IGS
ExS
-3
E-EF
(eV)
VB
EF
-0.8
2.7
-3
H-irradiated
CB
Rutile TiO2
VB
EF
2.3
-3
H-ads.
CB
Anatase
No significant change in VB
JPCM, 24, 195003(2012)
Theoretical calculations
eg
t2g
Ti3d
O2p

## Slide 25: Summary
Hydrogen adsorption and absorption at
rutile TiO2(110) and anatase TiO2(101) surfaces
with NRA, 1P-PES and 2P-PES
H adsorption: saturation coverage=0.48 ML
el. ground state
rutile: in-gap state, anatase: no in-gap state (metallic)
el. excited state above EF
rutile: ~2.7 eV (localized), anatase: ~2.3 eV (extended)
2. H irradiation at 500 eV
concentration: ~5 at. % within ~10 nm
enhancement of In-gap state (~10 times larger)
thermal diffusion of H

## Slide 26
Nandasiri et al., JPCL 6, 4627 (2015)
H implantation at 40 keV
followed by annealing

## Slide 27
JPCC_115_7562 (2011)
JPCM 24, 435504 (2012)
x
z
Most stable
Electron hopping barrier:<0.3 eV
(Adiabatic or non-adiabatic?)
I: 1st layer Ti5c
II: 1st layer Ti
III: 2nd layer Ti6c
Ⅰ
Ⅱ
Ⅲ
Ⅳ
Ⅴ
Ⅵ
similar
(from left)
84%(dz2), 16(dx2-y2)
Notes: 2 electrons
polaron stabilization
spin-spin interaction
polaron-Ov interaction

## Slide 28
The TiO6 octahedron is alternately aligned in 90˚ different directions.
(110) surface
Coordinate transformation

## Slide 29
混成による 寄与
（平面波）
入射面
○ ×
px，pyの縮退が解ける
→表面状態
Notes: 計算は加藤さん
Ｓ偏光で中間状態がｐxy軌道（ｍ＝＋１，－１）とするには，ｐｘに励起してｐｙから放出にしないといけない
縮退が解けるとこうならない

## Slide 30
Polarization dep.
入射面 |  | 入射面 | 
P | S | P | S
14.4 | 0 | 3.76 | 1
14.4 | 0 | 3.76 | 1
p
s
p
s
強度比
: :

## Slide 31
Ti4+
s
p
Ti4+(3d0)O2-(2p6)
O2p
bonding
anti-
bonding
eg
t2g
Ti3d
eg
eg
t2g
t2g
Band gap
~3 eV
O2-
stable
unstable
Electronic structure of TiO2
Surf. Sci. Rep., 48, 53 (2003)
Rutile TiO2
Basic structure：
TiO6
Notes: Oh vs Td

## Slide 32
1P-PES：H-adsorbed TiO2(110)
EF
CB
VB
Surf.
dipole
H+d
－
+
BB
Downward band bending
Presence of In-gap state (IGS)
Charge transfer from H to Ti
0.2 eV

## Slide 33: H on rutileTiO2(110)
→ Diffusion of H into the interior
H+
e-
Clean H ad. 550 K 620 K
Recovery of Dc
Cf. X.Y. Lin et al., ChemPhysChem 9, 253 (2008)

## Slide 34
2P-PES: Polarization dependence
H-ads.
p
s
p
s
H-irrad.
No intensity at
s-pol. in inc.
Similar intensity in
s-pol. incidences
Presence of two types of TiO6

## Slide 35: Comparison with black titania
Tailing of VB ultrasonic treated
L.-B. Mo et al., APL 105, 202114 (2014)
M. Mehta et al., J. Mater. Chem. A 4, 2670 (2016)