## Slide 1
Diamond Surface Functionalisation and Doping for Carbon-based Electronics
Dongchen Qi
ARC Future Fellow and Senior Lecturer
School of Chemistry, Physics and Mechanical Engineering
Queensland University of Technology

## Slide 2: The Evolution of Electronic Materials
First transistor (Bell Lab), 1947
1952 - Present
A Carbon Future?
Organic Semiconductor
Diamond
CNT
Graphene
Notes: The evolution of electronic materials seems to follow a very interesting trend along the carbon group (or group 14) of elements in the periodic table.
The first transistor made on germanium was invented by Bell Lab in 1947, and it marks the beginning of solid-state electronic devices. In 1952, the first silicon transistor was invented in the same laboratory, and quickly silicon became the backbone of microelectronics until today. We have witnessed an exponetial growth in the computation power of silicon transistors, dictated by the famous Moore’s law which states that the number of transistors packed in a chip doubles in every 18 months, which means the transistor dimensions get smaller and smaller. A few weeks ago, IBM just announced that they have developed 5 nm fabrication process. Will this growth be everlasting? Definitely not, because eventually the quantum effects start to take dominance and the cost and energy disspation vastly outweigh the performance gain as the device continue shrinking.
So how to solve this problem? We basically have two choices: a completely new device architecture (like quantum computation) or new material systems. So what will be the future material platform for next-generation devices? It appears if we follow the trend and continue moving upward carbon seems to be very natural choice.
Indeed, in recent decades carbon-based materials have receive intensive attention for building next-generation electronics. This includes 1D CNT, 2D graphene, a vast number of organic semiconducting molecules and polymers, and of course diamond.

## Slide 3: The Obligatory Table of Diamond
Property | Diamond | Comparison
Band gap and optical window | 5.5 eV, 225 nm and larger. | Sapphire, 8.8 eV, 180-5500 nm.
Thermal Expansion Coefficient | 1.1×10-6 /K (!!) | Invar, 1.3×10-6 /K
Thermal conductivity | > 20 W/cm. K (r.t.) | Copper, 4 W/cm.K
Young’s modulus | 1220 GPa | WC, 450-650 GPa
Hardness (Vickers) | 8000(10 on Mohs) | TiC, 2400
Sound Velocity | 12000 m/s | Iron, 5130 m/s
It’s a rule: every general talk on diamond must start with this table.
Mostly stolen from Paul May at UoB (www.chm.bris.ac.uk/motm/diamond/diamprop.htm).
Natural diamond
CVD diamond
HPHT Diamond
Notes: Diamond is much more than just a gorgeous germstone. It is also an amazing material with a range of extraorindary material properties, and I’ve listed only a few here. It often possesses the most extreme properties in many regards, from mechanical, thermal, electronic, chemical.
Natural diamond of course is very scarce, and for industrial applications people need synthetic diamond. HPHT can produce diamond crystals but tends to be small and energy consuming. The most practical methods of producing large, high quality diamond crytals is by chemical vapor deposition. The cost can be potentially very small as you need carbon-containing precusor gases like methane. The major challnege now with CVD growth is how to increase the size of diamond wafers.

## Slide 4: Applications
Notes: Endowed with these exceptional material properties, diamond can find applications in almost every technological domains. For example, used in drills and polishing tools by exploiting its extreme hardness. Used for building electronic components which is the focus of today’s talk. For used as heat sinks in power device. Used for quantum computation by harvesting the unique quantum properties of the nitrogen-vacancy centres in diamond. Or to treat wastewater by taking advantage of the wide electrochemical potential window of diamond electrodes. diamond is also bio-compatile, meaning it can be implanted in human bodies without causing any medical implications. An elegant example of this is the Bionic eye project developed in Melboure Uni. The NV centres inside diamond is also extremely sensitive to external spins and it can be made into extremely sensitive quantum and biological sensors. Quite often an application would make use not just one but a combination of properties.
(There are many other applications that are not included in this slides. But I hope it helps to convince you that diamond is truly a wonderful material.)

## Slide 5: The Diamond (001) Surfaces
Ideal truncated 1x1
bare C(001)-2x1
hydrogenated C(001)-2x1:H
Reactive
Used as a template substrate for organic functionalization
Passivated, non-reactive
NEA, very low IP
Supports 2DHG and device applications.
“Interface is the device”
Herbert Kroemer
2000
𝝅 bond
+
-
Notes: Herbert Kroemer, who one the Nobel Prize in Physics in 2000, has a famous quote ”Interface is the device”. He meant for silicon heterostructures, but it equally applies to most other materials and the devices built upon.
Diamond is no exception. Almost all the applications mentioned in the previous slide depends critically on the surface properties and functionalities of diamond. (afterall surface is what a material is exposing itself to the external world). The most studied diamond surface is the (001) surface. In the ideally truncated structure, each topmost carbon atom has two dangling bonds, and the surface will undergo surface reconstruction to reduce its surface energy. In ultrahigh vacuum environment, the neighbouring carbon atoms will form a dimer via a sigma bond, the remaining two dangling p-orbitals form a strained pi-bond. So the entire bare diamond 001 surface behaves like a giant unsaturated organic molecules with many double bonds. So this surface can readily react with organic molecules, and serves as a template substrate for organic functionalisation.
If we expose the bare surface to hydrogen plasma in a plasma reactor, the surface will become hydrogen-terminated. This hydrogen passivation makes the surface very stable and chemically inert. You can put a H-terminated diamond sample in your cabinet and remeasure it after a year and surface properties won’t change. In reality, we always start with a H-terminated sample, put it in UHV and heat it up to about 1000 C to completely desorb H to get the bare surface.
Another consequence of H termination is it creates a surface dipole layer because of the dipolar C-H bond. The dipole layers pulls down the vacuum level to an extent that it is directly below the surface conduction band minimum, leading to a negative electron affinity. NEA surface is usually a very good electron emitter, because secondary electrons that thermalise to the bottom of conduction band can be emitted into vacuum without any energy barriers. This strong secondary electron emission can be directly measured by photoemission if one measures the low kentic energy region of the spectra. These sharp peaks are electrons emitted directly from diamond CBM. And the emission intensity is several orders of magnitude higher that from the bare surface which has a regular positive EA if we lay them together in the same plot.

## Slide 6: Organic Functionalisation of Bare Diamond (001) Surface
Functionalisation with small molecules
Diam. Rel. Mater. 15, 711 (2006)
J. Phys. Chem. B 110, 5611 (2006)
Langmuir 23, 5611 (2007)
Chem. Mater. 20, 6871 (2008)
J. Phys. Chem. C 112, 2487 (2008)
Langmuir 26, 165 (2010)
Functionalisation with organic semiconductor molecules
CuPc
Reduced surface work function and enhanced secondary electron emission
C
C
C
C
Notes: As I said, the bare diamond surface dimers behave very much like a ethylene molecule, so it can react with other molecules quite readily, by which we can easily anchor functional molecules on diamond surface to realise surface functionalisation.
For example, we dosed a molecule called 1,3butadiene molecule on bare diamond surface, and the molecule can react with the surface dimer at room temperature via the 4+2 cycloaddition by breaking the pi bond and forming a cyclohexene-like structure. The resulting structure retains a double bond which allows further reaction to occur.
Similarly, conjugated organic semiconducting molecules such as CuPc can also be covalently archored to bare diamond surface as confirmed by photoemissions.
Both reactions transforms the bare diamond surface from a regular positive electron affinity surface with low electron emissions to a NEA surface with very high electron emissions. The reason is quite simple. All these molecules have numerous terminal C-H bonds which will point into the vacuum after moleules anchored to diamond surfces. They thus create a dipole layer similar to the H-terminated diamond surface, leading to the observed NEA, and facilitate electron emissions.

## Slide 7: Why NEA diamond surface matters?
Source of Solvated Electrons
Diamond (with NEA) when illuminated with UV light injects free electrons directly into solution to enable chemical reactions
R. J. Hamers et al., Nat. Mater. 12, 836 (2013)
Notes: So what applications are there for the functionalised diamond surfaces with a NEA? Apart from applications in cold cathode, field emitters which certainly benefit from high electron emission surfaces, an emerging field is in photocatalyst. The underlying principle is simple: diamond with NEA when illumiated …. . And diamond essentially works as a solid state source of solvated electrons with high reducing power.
An elegant example is recently shown by Hamers’ group in Wisconsin Madison. They have demonstrated reduction of N2 to ammonia at ambient termpertures and pressures with a H-terminated diamond immersed in water and illuminated with UV light.
There are limitations in H-termination for this purpose:
Firstly when diamond is in contact with water, there will be a significant upward band bending in diamond that greatly reduces electron emission.
Secondly, surface is prone to slow oxidation in solvents (hydroxl groups and ether-bridged oxygen species).
More robust NEA surfaces for diamond are needed. The surface functionalisation of diamond potentially can provide a promising way to achieve this as we can engineer the surface chemistry while maintaining the NEA.

## Slide 8: Motivation for a New Termination
http://aappsbulletin.org/myboard/read.php?Board=featurearticles&id=140
Nitrogen-Vacancy Centres - Negatively charged defects in diamond
Near-surface NVs have potential for:
  Nanomagnetometry
  Biosensing
Sensitive to surface termination
  Decoherence, unstable fluorescence, spectral broadening
  Current terminations less than ideal for intended applications
A diamond magnetometry system
Notes: Apart from the H-termination and organic termination via surface functionalisation, we are also searching for other types of termination. The motivation for a new termination is to do the N-V centres in diamond which are negatively chaged defects in diamond. There are well-defined electron spin states associated with these defect centres they are very sensitive to external electron and magnetic fields. So in addition for applications in quantum computation, NV centres in diamond can be employed for use in nanomagnetometry and biosensing.
The NV centres apparently have to be very close to diamond surface in order to sense molecules on diamond surface. Consequently, the surface termination of diamond becomes very critical to maintain the spin coherence of those near-surface NV centres. The current termination like H-termination is not ideal for this application since the upward band bending I mentioned earlier tends to alter the charge state of the NV centres. The in-gaps states associated other types of termination like O-termination also leads to decoherence, reducing the sensitivity of devices.

## Slide 9: Marrying Silicon with Diamond A New Silicon-terminated Diamond Surface
H-diamond
Si source
1ML Si deposited
(amorphous)
side
top
annealing
920 ℃
LEED
2x1 reconstruction
(2-domain)
3x1 reconstruction
(2-domain)
A. Schenk et al., Appl. Phys. Lett. 106, 191603 (2015)
Notes: In the search or new termination protocal for diamond quantum sensing, silicon comes into our mind for a few reason. Firstly, silicon, like carbon has nuclear-spin-free isotopes (Si 28, Si 30) so it offer spin-free termination avoid inteferenace with the NV centres. Secondly, Si is know to form stable Sp3 bonds as in SiC. Also Sicion has a rich surface chemistry which allows for further functionalisations.
So we start with a regular H-terminated diamond which shows the 2x1 surface reconstruction LEED patterns. We then evaporated about 1 monolayer Si from a silicon source directly onto diamond. The evaporated Si layer is amorphous so the LEED spots become diffused. Then the surface is anealed up to 920 C for a short while. The high T annealing has multiple functions: it desorb the H to allow underlying carbon to bond with silicon atoms. It evaporates away excessive silicon atoms. We end up with a new silicon-terminated diamond surface with 3x1 surface periodicity. By analysing high-solution photoemissin specra of C 1s and Si 2p, we arrive at a structural model shown here. Each Si atoms is bonded with two underlying carbon atoms.
XPS data:
C1s: downward band-bending from Bulk diamond component about 0.23 eV; C3: C-Si-O
Si 2p: C5 Si bonded to O

## Slide 10: Surface Electronic Structures of Si-terminated Diamond
Surface Brillion Zone
H-diamond (2x1)
Si-diamond (3x1)
Normal emission PES spectra
Angle-resolved PES spectra
A new occupied surface state (SS) at around 1.9 eV in relation to the Si-termination.
This SS hardly disperse along the surface.
The SS could be associated with the dangling bonds of terminating Si atoms.
The ordered Si DBs open up new opportunities for quantum registers through further surface functionalisation based on the rich silicon chemistry.
dangling bond
Nanotechnology 27, 275201 (2016)
H-Diamond
Si-Diamond
Notes: To determine the electronics structures of the Si-terminated surface in order to assess its implication to NV centres, we performed both angle-integrated and angle-resovled PES at the valence bands.
Normal emission reveal a new states at around 2eV that does not disperse with energy, therefore ascribed as occupied surface states.
This states also hardly disperse along the surface , and this is consistent with the non-dispersive dangling bonds. (Energy position consistent with that to Si surface) So we believe this SS is associated with the dangling bonds of terminating Si atoms.
The order Si DBs prvides a periodic arrars of DBs, and it allows for further surface fucntioanlsiation to dliberately couple shallow NV centres to surface spins in a quantum regsiter scheme.

## Slide 11: Surface Electronic Structures of Si-terminated Diamond
C-K-edge NEXAFS
Energies determined with reference to C 1s of
Bulk C C1 C2
Nanotechnology 27, 275201 (2016)
H-terminated
Si-terminated
NEA surface
Notes: C K-edge NEXAFS provides important information on the unoccupied states of the surface. The spectra on top is for the H-terminated surface. It shows typical structures for bulk diamond. The surface information is mostly contained in the pre-edge region including the states associated with C-H bonds and some dangling bonds due to imperfect termination.
After Si termination, the pre-edge part changes completely. It consists of multiple states that can be deconvoluted by peak fitting. These states are unoccupied states arising from the silicon termination. We can plot these states with respect to diamond band gap and examine their relative alignment with the relevant states of NV centres which are green lines here. The black and grey are VB and CB edges. Note si-terminated surface is also a NEA surface so vacuum level is below CB shown as dark grey lines here. Blue line is the occupied surface state shown in the valence band specra in previous slide.
Because we don’t know exactly the origin of the elecrons undergoing NEXAFS transitions for these four states, we have three potential energy level alignment scniarios depending taking the bulk diamond C 1s and two surface components as references to align. But no matter in which case, these in-gap states lie close to the NV centres states and may potentially interfere with the functioning of NV centres. But the spatial distribution of these unoccupied states is also important. If the state is highl localised, then their exitence will hardly affect the NV centres. But if the states is spatially extended penetrating below diamond surface, then NV centres that are within the range of these states may potentially be influenced. We don’t have an defnie answer yet as for the implication of these states. Further experiments need be done to fully assess the application of the silicon termination for improving diamond quantum sensing performance.

## Slide 12: Diamond as an Electronic Material
Johnson’s Figure of Merit (JFOM)
Diamond RF power transistors hold great promise as a replacement for vacuum tubes in wireless communication systems.
But realisation of this prospect has been impeded by the lack of effective doping.
Notes: Having looked at how we can engineer diamond surfaces through different terminations, let’s shift our focus back to diamond itself as an electronic material for building electronic devices.
in combination with excellent thermal conductivity,
Military, aerospace…
low solubility of dopants
Johnson’s Figure of Merit is a measure of high power capability.
High power also leads to high power density.

## Slide 13: Surface Conductivity of Diamond – Inspiration from Nature
The Fact:
Air-induced surface conductivity on hydrogenated diamond surface
p type; “2DHG”
in the order of 10-4 to 10-5 Ω-1
Areal hole density: 1012 to 1013 cm-2
Mobility: 10 to 200 cm2V-1S-1
M. I. Landstrass et al., Appl. Phys. Lett. 55, 1391 (1989)
R. S. Gi et al., Jpn. J. Appl. Phys 34, 5550 (1995)
F. Maier et al., Phys. Rev. Lett. 85, 3472 (2000)
P. Strobel et al., Nature 430, 439 (2004)
V. Chakrapani et al, Science 318, 1424 (2007).
electrons
The Origin:
Surface Transfer Doping Model
Notes: Two prerequisites:
It took about one decade since the first report of diamond surface conductivity for the underlying mechanism to be elucidated. In the surface transfer doping model, which was proposed Maier in 2000, the sub-surface hole accummulation that gives rise to the p-type surface conductivity form as a consequence of sponteneous electron transfer for the diamond valence band to electron accepting states of surface adsorbates. In the case of air-induced surface conducity, the atomphseric molecules that dissolve in the naturally adsorbed water layer on diamond provide such electron accetping energy states. This charge exchange will continue until the fermi levels on both sides are bring into equilibrium. This upward bending essetnailly create an highly asymetric potential well that confine the accujulated holes on diamond surface. But these holes are mobile along surface, thus giving rise to the surface conducting channel.
red/ox couples

## Slide 14: Diamond Surface Electronics
Diamond FET with 53 GHz cut-off frequency
S. A. O. Russell, S. Sharabi, A. Tallaire & D. A. J. Moran, Electron Device Letters, IEEE 33, 1471 (2012).
H. Kawarada, Jpn. J. of Appl. Phys. 51, 090111 (2012).
Kawarada et. al, P.S.S.(a). 208, 2005 (2011)
Bio and Chemical sensing
Control of underlying NV charge state
Grotz et. al, Nature Comm.3, 729 (2012)
Notes: Because bulk diamond is so difficult to be doped, this naturally occurred, air-induced surface conductivity provides a sensible route to realising electronic devices on diamond surfaces. Several types of devices have been demonstrated. This inlcude high-f transistors with… diamond transistor support relatively high power density of 2.1 W/mm. The hole channel can be solution gated, this gives rise to devices for achieving bio and chemical, as well as quantum sensing.

## Slide 15: Quantum Transport of the 2DHG on Diamond Surface
Quantum oscillations
Y. Takahide, et al., Phys. Rev. B 89, 235304 (2014)
Coulomb blockage
M. V. Hauf et al., Phys. Rev. B 89 (2014)
Phase coherent quantum magnetotransport
Weak localisation  weak anti-localisation
Unusual tunable spin-orbit interaction
G. Akhgar, et al., Nano Lett. 16, 3768 (2016)
M. Edmonds, et al., Nano Lett. 15, 16 (2014)
Notes: Meanwhile, the two-dimentional nature of the hole conducting layer has also been recently proved by a few quantum transport studies.
Kanawada’s group
The oscillation only depends on the perpendicular component of the magnetic field, thus suggesting the 2-dimensional nature of the transport.
Garrido’s group
Coulomb blockage effect by further confine the 2DHG to 0 D quantum islands through in-plane gating.
The La Trobe team led by Chris Pakes also made important discovey towards understanding the phase coherennt quantum magnetotransport of the 2D hole layer. They have observed an unexpected transition from WL to WAL by lowering down temperature, signaling a strong spin-orbit interaction energy, much stronger than what has been achieved in graphene. And this SO interaction can be tuned over a wide range by ionic liquid gating, giving rise to applications in spintronics.

## Slide 16: Problems with Air-induced Surface Doping
Poor thermal stability
Significant variance in device performance and characteristics
Drain current degradation
Early source-drain breakdown (limits power handling)
M. Kasu et al., Diamond Relat. Mater. 16, 1010 (2007)
Notes: Despite these successes, the dependence on fragile water layer to induce surface conductivity presents a lot of problems for the device applications in real life.
Device operation is sensitive to ambient enviroment like humidity. Consequently, even the same device will display different performance and characterisitics over a few days.
drain current degrades over time.
Suffer from early source-drain breakdown way before the berakdown field of bulk diamond. When the breakdown occurs, the micrograph shows protrusions on the contact suggesting trapped gas underneath as a results of device operation.

## Slide 17: Surface Transfer Doping of Diamond by Solid State Acceptors
Further improving the device stability and power handling requires alternative solid state surface acceptors.
Desirable properties of surface acceptors
Electron affinity > ionisation energy of diamond (~ 4.0 eV)
Easy to deposit
Thermally stable
Non-conductive
conduction
valence
Ei
-
-
-
-
-
Acceptor ions
EA
p-type

## Slide 18
Surface Transfer Doping by F4-TCNQ
++
band bending of 0.8 eV
C-1:C-2~2:1
Hole accumulation in diamond
-
Cyano groups extracting electrons from diamond
High resolution synchrotron radiation (SR)-based XPS reveals electrons are transferred from diamond to F4-TCNQ with holes accumulated on diamond
JACS, 129, 8084 (2007)

## Slide 19: Surface Transfer Doping by F4-TCNQ
Valence bands
Negatively charged molecular polaron states
E
Work Function
Before
After
F4-TCNQ acts as an highly efficient molecular acceptor for p-type surface transfer doping of diamond.
Diamond becomes degenerate at surface. EF-VBM = -0.4 eV
JACS, 129, 8084 (2007)

## Slide 20: Other Molecular Acceptors
Doping yield and efficiency are closely correlated with their electron affinities
Interface dipole term
band bending term
Notes: We’ve also studied STD of diamond with other types of moleuclar acceptors with diffeernet electron afiinity values. The doping yield and effieicneyc….
One can model the doping effiency and hence the indcued areal hole density as a function of molecular coverage by assuming that the occupation of the acceptor LUMO follows the Fermi-Dirac distribution, and the STD process is essentially a self-limiting process due to the presence of interface dipole and band bending.

## Slide 21: Beyond Doping Diamond
e-
graphene
organic semiconductor
Adv. Funct. Mater. 17 1339 (2007)
J. Am. Chem. Soc., 129, 10418 (2007)
Adv. Funct. Mater. 28 10409 (2016)
n p
lateral MoS2 p-n diode
Notes: This surface transfer doping scheme can also be readily applied to other semicondcutor systems. We have demonstrated this on graphene and an organic semiconductor film. In 2009 we pulbished a review article which is the First paper systematically summarise the application of STD to engineering conductivity of emerging semiconducting materaisl at nanosclae where convnetional bulk substititional doping usually fail.
Recently, Prof. Jiansheng Jie’s gourp in Soochow U has also reviewed in details recent progresses in utilising this doping strategy for low-dimensitonal nanostructtures including 2D materials. The device schematics shown on the right illustrates how to build a p-n junction on MoS2 for building ultrasenetisve light detectors by using the transer doping approach. (In this example, BN capped region remains n-type while AuCl3 covered region become p-type.)

## Slide 22: Surface Transfer Doping of Diamond with Transition Metal Oxides
Advantage of using TMO as surface acceptors for diamond
Extremely high electron affinity attainable
Thermally and chemically stable
Passivation effect
May act as gate dielectric at the same time
High promise to enable high-power, high-frequency diamond devices with superior thermal and operational stability.
Notes: Although high electron affinity organic molecules like F4-TCNQ and C60F48 can dope diamond surface with excellent doping yield, and they serve as excellent proof of concepts to demonstrate solid state doping of diamond, these molecules still lack the required thermal and chemical stability for practical device applications. We then turn our focus to a class of high work function TMOs including MoO3 V2O5 WO3.
These oxides have been widely used in organic electronics community for modifying electrode work function to faciliate charge injection or extraction.

## Slide 23: Surface Transfer Doping of Diamond by MoO3
Spectroscopic
Transport
Appl. Phys. Lett. 103, 202112 (2013).
Unpublished, 2018
In-situ four-probe
Notes: In 2013, we firstly demonstrate STD of diamond using MoO3 both by PES measurements and hall effect measurements. Again the rigid shift in the diamond C 1s component indicates the strong upward band bending. And we can also see the negatively charged oxide clusters from Mo 3d spectra. Hall measurements in VdP gemoetry showed that the hole density in more than doubled as comapred to the air doped diamond surface.

## Slide 24: Surface Transfer Doping of Diamond by V2O5
6-fold increase in hole density
Enhanced thermal stability
Appl. Phys. Lett. 108, 042103 (2016)
Transfer doping and energy level alignment at interface
Improved long-term operational stability
Sci. Rep., 8, 3342 (2018)
air-doped
Notes: Recently, we have also demonstrated the superior doping performance of V2O5 for transfer doping diamond. Transport measurements reveal a 6-fold increase in hole density after V2O5 doping. Furthermore, the hole channel produced by V2O5 has a much higher thermal stability up to 300 C as compared to the air-induced hole channel, which quickly degrades above 100C. The devics doped by these TMOs also yields much imporved long-term operational stablity with minimum hole density variation over half a month period

## Slide 25: Device Fabrication on Diamond Surface
Alignment marker formation
Active region (H-terminated) definition and device isolation by oxygen plasma
Ohmic contact formation
in-situ pre-annealing
TMO deposition
Gate formation
O-termination
H-termination
Hall bar device
Notes: Having successfully demonstrated the great potential of TMOs in achieving high performance and thermally stable surface transfer doping of diamond, the focus of my group lies in applying this doping scheme in building high-performance and robust diamond transistors.
We have developed a whole device fabrication protocals via standard photolithogarphy process that alllow us to fabricate various types of devices on H-dimond.
One key step is to define the active region and device isolation through oxygen plasam so that only the active channel area is H-terminated while the rest is O-terminated and hence insulting.
Ohmic contact was formed by Pladium we found it shows much lower contact resistance than conventionally used Ti/Pt/Au trilayer contacts.
This gives us standard hall bar device with air doping.

## Slide 26
Quantum Transport
metallic conduction
Phase-coherent quantum magneto-transport
WAL
WL
Transition from WL to WAL as temperature decreases suggests unusually high spin-orbit coupling (Rashba effect).
V2O5 doping
MoO3 doping
Lɸ
Lso
Lso
Lɸ
Water
MoO3
V2O5
~T0.5
~T0.5
Unpublished
Notes: decreases linearly with temperature and approaches zero as T→0 due to Nyquist dephasing.7,8 The spin coherence length ( = (ħ/(4 )) . ) and phase coherence length ( = (ħ/(4 )) . ) are plotted as a function temperature in Fig. S6. varies with temperature according to ~ . , with an exponent that is expected for a 2D in contrast to a 3D system.7

## Slide 27: MOSFETs
Leakage current
Output curves
Transfer curves
Saturation Drain Current | On-resistance | Threshold Voltage | Transconductance | Hole Mobility
0.35 mA/mm @ VGS = -1.6 V | 6.4 kΩ∙mm @ VGS = -1.6 V | 0.8 V | 0.17 mS/mm | 48 cm2V-1s-1
Successfully demonstrated MOSFET operation based on V2O5 induced surface doping, in which V2O5 also serves as the gate dielectrics.
Unpublished results
Notes: As a proof of concept, we also fabricated a diamond MOSFETs in which the V2O5 acts both as surface acceptors to induce a hole conducting channel and gate dielectrics. transistors shows typical output and transfer charcterisitcs expected from a long-channel transistor. Our transistor a quite long channel length (438 um) and therefore the saturation current is relatively low compared to state of the art diamond MOSFET with Al2O3 dielectric and air doping channel. The current is expected be increased substantially when we reduce the device dimension.

## Slide 28: Outlook
Scaling down device to sub-100 nm for high power and high-frequency operation.
Gate metal
TMO
Channel
Drain
Source
Gate metal
TMO
Source
Drain
Channel
Notes: To achieve high power and high-f operation, and to realise our goal of developing robust diamond MOSFET with a better perforamnce than the current state-of-the art and on par with GaN RF power transistors, a key step is to scale down device dimensions eventually to sub-100 nm. For this we need deveelp new fabrication protocals which is the current focus of my group. We have recently fabricated sub-10 um channel length devices with both linear and circular channel. The circular design can effectively increase the channel width, thus enhance the current density.

## Slide 29: Outlook
Novel quantum devices
Excitonic electron-hole bilayers: diamond-2D material heterojunction
1D and 0D devices,
dimensionality cross-over, single-hole transistors
-
+
-
2D MoO3 grown by ALD
Excitonic transport: Coulomb drag, dissipationless transport
Notes: The 2DHG induced by TMO doping with extremely high density present us a ideal platform to exlore quantum transport phenomena and novel device architectures. For example, by using in-plane gating scheme we can potentially tune the dimensioanlity of hole gas from 2D to 1D to 0D. It will be interesting to see if any exotic quantum transport phenomena would occur at the dimentionality cross-over. We can also envision a single hole transistor device, in which the side gate electrostatically define a isolated quantum island while the pluger gate above the TMO modulate the discrete Coulomb charging enery levels.
An even more interesting device architecture we have envisioned is the so-called excitonic electron-hole bilayers which fomed by a layer of 2DEG in close proximity to 2DHG. What is interesting in this type of system is electrons and holes which are spaticall separated can be coupled together to form excitons, and these excitons can undergo a bose-einstein condenstae like phase transition into a superfluid ground state. This device concept can be potentially realised by coupling a high electron affinity 2D oxide such as alpha-MoO3 on diamond and the spontaneous charge transfer acorss the interface will form spatically separated hole gas and electron gas. We have recently successfully synthesis 2D MoO3 on diamond by ALD process at MCN. The goal is to measure this excionic transport by meausuring the so-called Coulomb drag applying curent in one layer and measuring voltage drop in the other. This type of device may have implication for realising dissipationless transport.

## Slide 30
Energy Level Alignment

## Slide 31: Summary
Diamond surfaces presents a rich playground for realising physical and chemical functionalities through surface functionalisation.
Surface transfer doping with transition metal oxides provides a viable solution to engineering high-performance diamond transistors.
The tunale 2DHG on diamond opens up new vistas for the development of a multitude of novel device architectures.
Diamond continues to shine as a wonderful material!
Notes: I hope I have showed to you that
Help to unlocking the true potential of this wonderful material

## Slide 32: Acknowledgements
La Trobe University: Kaijian Xing, Golrokh Akhgar, Alex Schenk, C. Pakes, Lothar Ley
University of Melbourne: Jeffery McCallum
Australian Synchrotron: Anton Tadich, Bruce Cowie
National University of Singapore and SSLS: Andrew Wee, Wei Chen, Loh Kian Ping, Jun Ding
University of Glasgow: David Moran, Stephen Russell, Kevin Crawford
Funding: La Trobe Uni., ARC (DP and FT), Australian Synchrotron, MCN

## Slide 33
Thank You!