## Slide 1
Electronic correlations in graphene
studied using
angle-resolved photoemission
Choongyu Hwang
Department of Physics
Pusan National University
South Korea
Lawrence Berkeley
National Laboratory
Pusan Natl. Univ.
Department of Physics
Max Planck-
POSTECH
Research Initiative
National Research
Foundation of
Korea

## Slide 2
Postdoc
Dr. Hyejin Ryu
Graduate student
Jinwoong Hwang
Advanced Light Source
Lawrence Berkeley Natl. Lab. (USA)
Hwang Research Group
Lawrence Berkeley
National Laboratory
Pusan Natl. Univ.
Department of Physics
Max Planck-
POSTECH
Research Initiative
National Research
Foundation of
Korea

## Slide 3
S. Louie
A. Zettl
UC Berkeley Collaborators
A. Lanzara
M. L. Cohen
J. B. Neaton
A. Fedorov
ALS Collaborators
S. –K. Mo
J. Denlinger
LBNL Collaborators
A. Ismach
Y. Zhang
R. Dynes
Theoretical Support
A. Castro Neto
C. –H. Park
Natl. Univ.
of Singapore
Seoul Natl. Univ.
D. –Y. Kim
HPSTAR, China
B. I. Min
POSTECH Collaborators
J. –H. Park
K. Kim
Postdoc
Dr. Hyejin Ryu
Graduate student
Jinwoong Hwang
Collaborators
Notes: There have been a lot of help from excellent collaborators.
Prof. Alessandra Lanzara has supported all these works and all of our group members have been great help in every part even beyond physics.
With strong emphasis, Prof. Antonio Castro Neto has been wonderful help in understanding complicated physics in graphene. Also there have been great help from beamline scientists at Advance light source and from sample grower at lawrence berkeley national laboratory.
I also appreciate all the help from our collaborators in UC berkeley, Prof. Steven Louie, Prof. Dung-Hai Lee, Prof. Robert Dynes, Prof. Alex Zettl, Prof. Ramamoorthy Ramesh, Prof. Eugene Haller, and their students.

## Slide 4
Outline
1. Why do we study electrons?
3. Dream about strongly correlated electron phases
in a 2D world: graphene
Role of a dopant: spin-spin interactions: Kondo effect
Role of a substrate: electron-electron interactions
2. How do we study electrons?
Notes: First of all, let me introduce outline of my talk.
I will briefly introduce magnetic and electronic properties of graphene that will be followed by brief introduction my main experimental tool, angle-resolved photoemission spectroscopy or ARPES.
Then I will discuss about our recent studies on magnetic ordering and fermi velocity engineering in graphene.

## Slide 5
Outline
1. Why do we study electrons?
3. Dream about strongly correlated electron phases
in a 2D world: graphene
Role of a dopant: spin-spin interactions: Kondo effect
Role of a substrate: electron-electron interactions
2. How do we study electrons?
Notes: First of all, let me introduce outline of my talk.
I will briefly introduce magnetic and electronic properties of graphene that will be followed by brief introduction my main experimental tool, angle-resolved photoemission spectroscopy or ARPES.
Then I will discuss about our recent studies on magnetic ordering and fermi velocity engineering in graphene.

## Slide 6
Why do we need to study electrons?
Ultimately, the
electric,
magnetic,
chemical,
mechanical,
optical, thermal, and structural properties of matter depend on the
behavior of electrons and location of atoms.

## Slide 7
Highly correlated systems
Non-correlated system
Ground state
With external perturbation
Correlated system
The responses are different due to
correlation effects!

## Slide 8
Energy scale of importance
Superconducting gap
~ 1 – 100 meV
Optical phonons
~ 40 – 70 meV
Magnons
~ 10 – 40 meV
Pseudogap
~ 30 – 300 meV
Multiphonons and multimagnons
~ 50 – 500 meV
Orbital fluctuations
~ 100 meV – 1.5 eV
Mott gap
~ 1 eV – 3 eV

## Slide 9
Electron-electron interaction in Fermi liquid
Fermi liquids
Galilean invariance
Yi et al., PRL (2011)
E–EF (eV)
k (p/a)
Rb0.8Fe2S2
Rb0.8Fe2SSe
Rb0.8Fe2Se2
Notes: In order to understand electron-electron interactions, it is important to note the difference between Fermi liquids and Dirac Fermions.
Fermi liquids are described by Galilean invariant theories whose main parameter is effective mass. For Fermi liquids, as electron-electron interactions become stronger, the effective mass becomes heavier so that Fermi velocity is decreasing.
In the same analogy with Fermi liquid, the main parameter of Dirac fermions is velocity which is described by Lorentz invariant theories. Similar to Fermi liquid, velocity is also affected by electron-electron interactions. However, with increasing interactions, the velocity is also increasing in contrast to Fermi liquid.
Base on this theoretical expectation along with the easiness of graphene to modify electron band structure, graphene is viewed as a prototypical two dimensional electron system for Fermi velocity engineering.

## Slide 10
Spin-spin interaction in metallic sea
Giant magneto-resistance
FM/AFM oscillation
Magnetic skyrmions
RKKY interaction
r
J
Rappoport et al., EPL (2011)
Kondo effect
Jang et al., arXiv:1704.08247v1

## Slide 11
Outline
1. Why do we study electrons?
3. Dream about strongly correlated electron phases
in a 2D world: graphene
Role of a dopant: spin-spin interactions: Kondo effect
Role of a substrate: electron-electron interactions
2. How do we study electrons?
Notes: First of all, let me introduce outline of my talk.
I will briefly introduce magnetic and electronic properties of graphene that will be followed by brief introduction my main experimental tool, angle-resolved photoemission spectroscopy or ARPES.
Then I will discuss about our recent studies on magnetic ordering and fermi velocity engineering in graphene.

## Slide 12
Angle-Resolved PhotoEmission Spectroscopy
Binding Energy
Momentum
Photo-electrons
EF
Dispersion and
self energy
Fermi surface
K
G
EF
ED
E-ED=-0.8 eV
Notes: ARPES is photon-in electron-out method which directly shows how electrons are bound within a crystal as a function of momentum and binding energy.
A horizontal cut of this 3-dimensional data give Fermi surface which gives important information on the electronic properties of a system. A vertical cut gives information of energy-momentum dispersion and electron self-energy.

## Slide 13
Angle-Resolved PhotoEmission Spectroscopy
A(k,w) spectral function, M(k) Matrix element, f(w) Fermi function
Electron self-energy
Electron band structure
Fermi velocity
Charge carrier concentration
K
G
EF
ED
E-ED=-0.8 eV
Quantum phases
Berry’s phase
Sign of hopping integrals
Hwang et al., PRB (2011)
Notes: ARPES is photon-in electron-out method which directly shows how electrons are bound within a crystal as a function of momentum and binding energy.
A horizontal cut of this 3-dimensional data give Fermi surface which gives important information on the electronic properties of a system. A vertical cut gives information of energy-momentum dispersion and electron self-energy.

## Slide 14
Outline
1. Why do we study electrons?
3. Dream about strongly correlated electron phases
in a 2D world: graphene
Role of a dopant: spin-spin interactions: Kondo effect
Role of a substrate: electron-electron interactions
2. How do we study electrons?
Notes: First of all, let me introduce outline of my talk.
I will briefly introduce magnetic and electronic properties of graphene that will be followed by brief introduction my main experimental tool, angle-resolved photoemission spectroscopy or ARPES.
Then I will discuss about our recent studies on magnetic ordering and fermi velocity engineering in graphene.

## Slide 15
Dream about strongly correlated electron phases
Graphene
Thinnest two-dimensional material
Playground to explore electronic correlations
predicted in a two-dimensional limit
Mott insulator
Kondo effect
Superconductivity
Magnetism
Exciton condensation
etc.
Abnormal quantum Hall effect
ultrahigh conductivity
1 THz transistor
half metallicity,
quantum spin Hall effect
spin valves
etc.
Energy
Momentum
& linear band with chirality

## Slide 16
Graphene
Graphene + substrate
electron-electron
interactions
Dream about strongly correlated electron phases
A light element, carbon, only with 6 electrons confined in a 2D system
spin-spin
interactions
Graphene + adsorbates

## Slide 17
Electron-electron interactions in Fermi liquids
Fermi liquids
Galilean invariance
Yi et al., PRL (2011)
E–EF (eV)
k (p/a)
Rb0.8Fe2S2
Rb0.8Fe2SSe
Rb0.8Fe2Se2
Notes: In order to understand electron-electron interactions, it is important to note the difference between Fermi liquids and Dirac Fermions.
Fermi liquids are described by Galilean invariant theories whose main parameter is effective mass. For Fermi liquids, as electron-electron interactions become stronger, the effective mass becomes heavier so that Fermi velocity is decreasing.
In the same analogy with Fermi liquid, the main parameter of Dirac fermions is velocity which is described by Lorentz invariant theories. Similar to Fermi liquid, velocity is also affected by electron-electron interactions. However, with increasing interactions, the velocity is also increasing in contrast to Fermi liquid.
Base on this theoretical expectation along with the easiness of graphene to modify electron band structure, graphene is viewed as a prototypical two dimensional electron system for Fermi velocity engineering.

## Slide 18
Graphene on dielectric substrates
momentum
E - EF (eV)
0.05 Å-1
Siegel, Hwang et al., PNAS (2011)
Hwang et al., Sci. Rep. (2012)
0.0
- 0.5
-1.0
G
K
M
SiC(0001)
h-BN
Quartz

## Slide 19
Fine Structure Constant
0
0
1.0
3
vF / v0
1
2
G/Quartz
G/BN
LDA
G/SiC(0001)
0.5
1.5
Fermi liquids vs. Dirac fermions
Hwang et al., Sci. Rep. (2012)
Dirac Fermions
Lorentz invariance
Das Sarma et al., PRB (2007)
Non-Fermi liquid behavior
by a dielectric substrate
Increasing curvature
Increasing el-el interactions

## Slide 20
Fine Structure Constant
0
0
1.0
3
vF / v0
1
2
G/Quartz
G/BN
LDA
G/SiC(0001)
0.5
1.5
Control parameters of el-el interactions
Non-Fermi liquid behavior
by a dielectric substrate
Crossno et al., Science (2016)
Possible formation of
strongly coupled Dirac fluids
by temperature
a smart choice of a substrate
+
proper control of temperature
||
strong electronic correlations?
Hwang et al., Sci. Rep. (2012)

## Slide 21
Graphene on SrTiO3
2. Host material
for exotic properties
FeSe/STO
Ge et al., Science (2015)
LAO/STO
Brinkman et al.,
Nature (2007)
15000
0.3
1
3
10
30
100
300
SrTiO3
Temperature (K)
Dielectric constant e
Muller et al.,
PRB (1979)
1. Interesting material
by itself
2DEG
Meevasana et al.,
Nat. Mater. (2011)
Quantum Paraelectricity
Scott, RMP (1974)
SrTiO3

## Slide 22
Strong enhancement of el-el interaction
ReS (eV)
0.0
0.4
k-K (Å-1)
0.02
-0.14
180 K
13 K
ReS (eV)
0.0
0.4
k-K (Å-1)
0.02
-0.14
0.0
0.2
180 K
LDA
1. Departure from linearity
2. Logarithmic self-energy
0.0
- 0.6
-1.2
-0.02
-0.14
E - EF (eV)
k-K (Å-1)
G
K
0.0
–1.0
–2.0
–1.7
–0.7
0.3
180 K
Decreasing T
H. Ryu, C. Hwang et al., Nano Lett. 17, 5914 (2017)
strong electron-electron interaction
Temperature-controlled

## Slide 23
Outline
1. Why do we study electrons?
3. Dream about strongly correlated electron phases
in a 2D world: graphene
Role of a dopant: spin-spin interactions: Kondo effect
Role of a substrate: electron-electron interactions
2. How do we study electrons?
Notes: First of all, let me introduce outline of my talk.
I will briefly introduce magnetic and electronic properties of graphene that will be followed by brief introduction my main experimental tool, angle-resolved photoemission spectroscopy or ARPES.
Then I will discuss about our recent studies on magnetic ordering and fermi velocity engineering in graphene.

## Slide 24
Role of a dopant: Kondo effect
Decreasing temperature
Local
magnetic
moment
(4f or 3d electrons)
T > TK
Formation of
many-body
ground state
(Kondo resonance)
T < Tcoh
Screening by
spins of
metallic
background
T ≈ TK
Formation of a resonant-type hybridized many-body ground state

## Slide 25
How do we know the Kondo effect?
Chen et al., Nature Phys. (2011)
Transport: scaling
Transport: increasing r
de Boer et al., Physica (1933)
Resistance
Temperature
Spectroscopy:
Zero-bias resonance peak
Ren et al., Nano Lett. (2014)
Spectroscopy (ARPES):
T-dependent hybridization
Denlinger et al., arXiv:1312.6637

## Slide 26
Graphene: partially decorated with Cerium
–2.5
–2.0
–1.5
–1.0
–0.5
0.0
–0.4
0.0
0.4
kx (Å–1)
E – EF (eV)
–2.5
–2.0
–1.5
–1.0
–0.5
0.0
–0.4
0.0
0.4
kx (Å–1)
G
K
Max.
Min.
36 K
Ephoton= 80 eV
As-grown
graphene
Graphene
with cerium
+
-0.2
0.0
0.2
-3
-2
-1
0
Energy (eV)
Momentum (Å-1)

## Slide 27
Graphene: partially decorated with Cerium
E – EF (eV)
–2.5
–2.0
–1.5
–1.0
–0.5
0.0
–0.4
0.0
0.4
kx (Å–1)
35 K
Ephoton= 120 eV
Graphene
Cerium
Buffer layer
Top view
Side view
DFT+U
Tight-binding
Ce 4f
Graphene
As-grown
graphene
Ce 5d
Localized 4f electron from cerium
+
Metallic background from graphene
||
Are they interacting with each other?

## Slide 28
Energy spectrum close to Fermi energy
290 K
kx (Å–1)
290 K
–1.0
0.0
1.0
G
K
kx (Å–1)
–1.0
0.0
1.0
0.0
–1.0
E – EF (eV)
J. Hwang, C. Hwang et al., Nano Lett. 18, 3661 (2018)

## Slide 29
Energy spectrum close to Fermi energy
290 K
kx (Å–1)
290 K
–1.0
0.0
1.0
G
K
kx (Å–1)
–1.0
0.0
1.0
0.0
–1.0
E – EF (eV)
210 K
210 K
0.0
–1.0
J. Hwang, C. Hwang et al., Nano Lett. 18, 3661 (2018)

## Slide 30
Energy spectrum close to Fermi energy
290 K
kx (Å–1)
290 K
–1.0
0.0
1.0
G
K
kx (Å–1)
–1.0
0.0
1.0
0.0
–1.0
210 K
210 K
0.0
–1.0
110 K
110 K
E – EF (eV)
0.0
–1.0
J. Hwang, C. Hwang et al., Nano Lett. 18, 3661 (2018)

## Slide 31
Energy spectrum close to Fermi energy
290 K
kx (Å–1)
290 K
–1.0
0.0
1.0
G
K
kx (Å–1)
–1.0
0.0
1.0
0.0
–1.0
210 K
210 K
0.0
–1.0
110 K
110 K
E – EF (eV)
0.0
–1.0
18 K
18 K
0.0
–1.0
J. Hwang, C. Hwang et al., Nano Lett. 18, 3661 (2018)

## Slide 32
0.2
18 K
60 K
110 K
160 K
210 K
260 K
290 K
Spectral Intensity (a. u.)
E – EF (eV)
–0.6
–0.4
–0.2
0.0
E – EF (eV)
–0.6
–0.4
–0.2
0.0
0.2
Subtracted Intensity (a. u.)
18 K
60 K
110 K
160 K
210 K
260 K
Temperature-dependent spectral change
20 K
300 K
E – EF (eV)
K
K+M
0.0
–0.4
–0.2
G
K
DOS
K
K+M
DOS
Calculations within the Dynamic Mean-Field Theory
J. Hwang, C. Hwang et al., Nano Lett. 18, 3661 (2018)

## Slide 33
Realization of Kondo resonance in a 2D limit
Kondo peak
Spin-orbit side band
20 K
300 K
E – EF (eV)
K
K+M
0.0
–0.4
–0.2
G
K
DOS
K
K+M
DOS
Calculations within the Dynamic Mean-Field Theory
EF
4f7/2
4f5/2
Photoemission final states (Kondo resonance)
EF
4f7/2
4f5/2
EF
4f7/2
4f5/2
4f14f0 ionization peak
Spin-orbit side band
Kondo peak
ħw
J. Hwang, C. Hwang et al., Nano Lett. 18, 3661 (2018)

## Slide 34
Realization of Kondo resonance in a 2D limit
Kondo peak
Spin-orbit side band
20 K
300 K
E – EF (eV)
K
K+M
0.0
–0.4
–0.2
G
K
DOS
K
K+M
DOS
Calculations within the Dynamic Mean-Field Theory
E – EF (eV)
kx (Å–1)
Max.
Min.
0.0
–0.4
–0.6
–0.2
0.0
–0.4
0.2
–0.2
36 K
G
K
kink
–0.4
–0.1
–0.5
–0.1
–0.3
MDC
Fit
kx (Å–1)
Kondo effect
in the sea of 2D Dirac fermions,
Graphene
J. Hwang, C. Hwang et al., Nano Lett. 18, 3661 (2018)

## Slide 35
Decreasing T
Viable route towards superconducting and
magnetic graphene at high temperatures
Dream about strongly correlated electron phases?
Smart choice of substrate and adsorbate/dopant
leading to even stronger electronic correlations
Summary
Magnetic correlations
Enhanced electronic correlations
Non-Fermi liquid behavior of charge neutral graphene
T-dependent electronic correlations in graphene
A binary compound of graphene and a magnetic impurity
Kondo effect in graphene

## Slide 38
What do we learn from momentum resolution?
E-EF (eV)
Intensity
BSCCO
Z.X. Shen et al., PRL (1993)
A
B
metallic
superconducting

## Slide 39
Spin resolved photoemission
To access spin degrees of freedom
Time resolved photoemission
To study excitation and phase transitions
What is missing? Time and Spin
The future of photoemission

## Slide 40
1) Is there a Quantum Critical
Point?
2) What is the nature of NFL region?
3) What defines the Pseudogap (PG)
phase?
4) What are the basic excitations?
5) Is SC a consequence of QCP or is
it hiding the QCP?
6) Are PG and SC state competing
states of matter?
Temperature
g = Doping
FL
UD
OD
F
Quantum
Critical
(NFL)
SC
CDW
DDW
SDW
FL
FM
g
gc
AFM
VB
Quantum
Critical
(NFL)
The mystery of high TC superconductivity
- Why do we need these additional resolutions?
We need time and spin resolutions

## Slide 41
Pump-Probe, ultrafast ARPES:
Quasiparticle lifetimes
Coherent oscillations
Ultrafast phase transitions
Closing/opening of gaps
…
Possibilities:
sample






Energy conservation
EB = ħω - EK – ΦA
Angle / momentum conservation
k║ √Ek sin θ
Time Resolution
A(k, ω, t-t′)
Photoelectron intensity
Time-resolved ARPES

## Slide 42
The power of time + momentum resolution
High-Tc superconductors
Zhang, Hwang et al., Nature Comm. 5, 4959 (2014)
Tc< 2 K
Tc=91 K

## Slide 43
Spin resolved photoemission
To access spin degrees of freedom
Time resolved photoemission
To study excitation and phase transitions
What is missing? Time and Spin
The future of photoemission

## Slide 44: Spin-ARPES
Spin resolution
Px, Py, Pz
Fundamental magnetism
Colossal magnetoresistance
Magnetic phase transitions
FeAs superconductors
Topological Insulators
…
Critical for:
sample







Energy conservation
EB = ħω - EK – ΦA
Angle / momentum conservation
k║ √Ek sin θ
Time resolution
A(k, ω, t-t′)
Spin + time-resolved ARPES

## Slide 45
45°
x
y
z
p-pol
spectrometer
Py
Pz
q
b
e -
Full Spin Polarization Maps:
Standard ARPES:
45°
x
y
z
spectrometer
Py
Pz
q
b
e -
s-pol
6 eV laser
Spin-resolved Geometry:
Photoelectron spin polarization is fully flipped by rotating photon polarization!
Light-spin interactions in topological insulator
Jozwiak, Hwang et al., Nature Phys. 9, 293 (2013)

## Slide 46
EF
4f7/2
4f5/2
Singlet ground state
EF
4f7/2
4f5/2
EF
4f7/2
4f5/2
Photoemission final states
EF
4f7/2
4f5/2
EF
4f7/2
4f5/2
4f14f0 ionization peak
Spin-orbit side band
Kondo peak
ħw
Singlet ground states vs PES final states

## Slide 47
Graphene: partially decorated with Cerium
–2.5
–2.0
–1.5
–1.0
–0.5
0.0
–0.4
0.0
0.4
kx (Å–1)
E – EF (eV)
–2.5
–2.0
–1.5
–1.0
–0.5
0.0
–0.4
0.0
0.4
kx (Å–1)
G
K
Max.
Min.
36 K
Ephoton= 80 eV
As-grown
graphene
Graphene
with cerium
+
-0.2
0.0
0.2
-3
-2
-1
0
Energy (eV)
Momentum (Å-1)

## Slide 48
Realization of Kondo resonance in a 2D limit
Kondo peak
Spin-orbit side band
20 K
300 K
E – EF (eV)
K
K+M
0.0
–0.4
–0.2
G
K
DOS
K
K+M
DOS
Calculations within the Dynamic Mean-Field Theory
EF
4f7/2
4f5/2
Photoemission final states (Kondo resonance)
EF
4f7/2
4f5/2
EF
4f7/2
4f5/2
4f14f0 ionization peak
Spin-orbit side band
Kondo peak
ħw
Hwang et al., Nano Lett. 18, 3661 (2018)
Kondo effect
in the sea of 2D Dirac fermions,
Graphene