## Slide 1: High resolution and radiation-damage free inverse photoelectron spectroscopy
Hiroyuki Yoshida
Chiba University
VASSCAA-9
Sydney, Australia
Aug. 14, 2018

## Slide 2: Chiba University Japan
Narita airport
Chiba Univ

## Slide 3: Organic semiconductor devices
organic light emitting diode (OLED)
organic solar cell
(OSC)
- light weight, flexible, low-cost
- new materials can be developed
by organic synthesis
PCE > 17%
(Aug 9, Science)

## Slide 4: Organic light emitting diode (OLED)
－
＋
metal electrode
transparent electrode
＋
-
hole
electron
-
-
-
＋
＋
＋
light
organic
semiconductor
＋
-

## Slide 5: Organic light emitting diode (OLED)
－
＋
metal electrode
transparent electrode
＋
-
hole
electron
-
-
-
＋
＋
＋
light
＋
-
＋
hole
molecules
-
electron
molecules
organic
semiconductor
LUMO
HOMO

## Slide 6: Energy level diagram of OLED
HTL
5.3
ETL
EL
+
-
+
-
-
+
anode
cathode
HOMO
LUMO
hn

## Slide 7: Outline
Energy levels of unoccupied states
  low energy inverse photoelectron spectroscopy
  enhancement of signal by surface plasmon
Intermolecular overlap of molecular orbitals
  splits of occupied and unoccupied levels
  angle-resolved inverse photoelectron spectroscopy

## Slide 8: Energy level of semiconductor
HOMO level
LUMO level
energy
unoccupied states
valence states
conduction band
valence
band
-
+
electron
hole
vacuum level
Fermi level
electron affinity
ionization energy

## Slide 9: Charge transport in organic semiconductor
＋
-
HOMO
LUMO
Notes: 分子が集まって、固体になる。
分子軌道が相互作用して、固体の準位ができる。相互作用が大きければ、準位の広がり（バンド幅）が広がる。
価電子準位－ＨＯＭＯ準位、空準位ーＬＵＭＯ準位
準位が密になるとわかりにくい。そこで、エネルギーに対して、準位の密度 ―状態密度を描くことが多い。
電荷は、 ホールは価電子帯上端、電子は空準位の下端
では、電荷が入るとどうなるか？

## Slide 10: PES and IPES
photoelectron spectroscopy PES
inverse photoelectron spectroscopy IPES
photon
-
electron
photon
-
electron
e-
Ek
EB
HOMO
hn
LUMO
e-
Ek
EB
hn

## Slide 11: Inverse photoelectron spectroscopy (IPES)
Resolution > 0.5 eV
Sample damage
Dose (1977)
electron gun
Geiger-Muller tube＋filter
bandpass
detector
5－15 eV
hn
CaF2, SrF2
10 eV
IIPES/IPES
= (lelectron/lphoton)2
= 10-3 (hn =1000 eV)
= 10-5 (hn =10 eV)
J. B. Pendry,
PRL 45, 1357 (1980).
low cross section
Notes: 逆光電子分光の効率が低い

## Slide 12: Two issues of conventional IPES
PES
IPES
Ionization energy
electron affinity
？
low energy resolution
CuPc
binding energy / eV
2
3
0
-3
1
-1
-2
Intensity (arb. units)
10
5
0
-5
binding energy / eV
scan 1
scan 2
electron current
1/1500
n-C36H74
radiation damage

## Slide 13: How can we solve the two issues？
-
-
-
low resolution
？
sample damage

## Slide 14: Decrease the electron energy …
-
-
high energy electron
damage!
low energy electron
no damage!
5-15 eV
< 4 eV

## Slide 15: Energy levels of inverse photoelectron
valence
unoccupied
-
-
hn
Ek
EB
hn
Ek
EB
5-15 eV
< 4 eV
vacuum
ultraviolet
near
ultraviolet
10 eV
5 eV
conventional IPES
low-energy IPES
Yoshida, Chem. Phys. Lett., 539–540, 180 (2012)
Yoshida, Anal. Bioanal. Chem. (Trend2014)
Notes: 逆光電子分光の効率が低い

## Slide 16: Low energy inverse photoelectron spectroscopy (LEIPS)
bandpass filter
photomultiplier
e-
sample
electron gun
lens
vacuum
0.1 eV
H. Yoshida, Rev. Sci. Instrum., 85, 016101 (2014).
H. Yoshida, Chem. Phys. Lett., 539–540, 180-185(2012)
Evac
e -
LUMO
HOMO
-
near UV
photon
3-5 eV
low energy
electron
< 5 eV
EA
high resolution
damage free

## Slide 17: Sensitivity curves of photon detectors
3
4
5
0.00
0.05
0.10
0.15
quantum efficiency
photon energy / eV
4.5 eV
3.7 eV
0.20 eV
0.11 eV
Present work
0.8 eV
Conventional detector
0.4 eV
9.0
9.5
10.0
10.5
SrF2＋I2
intenisty (arb. unit)
photon energy / eV
CaF2＋I2

## Slide 18: Overall resolution： HOPG image potential state
0.55 eV
Banik et al., (2005)
Conventional
LEIPS
0.25

## Slide 19: Radiation damage to bis-PCBM
Present work (0 - 4 eV, 0.5 mA)
Conventional (10 eV, 0.5 mA)
-4
-3
-2
-1
0
intensity (arb. units)
energy from Evac/ eV
0 min
1 min
5 min
15 min
-4
-3
-2
-1
0
energy from Evac / eV
intensity (arb. units)
0 min
30 min
2 hours

## Slide 20: Low energy inverse photoelectron spectra (LEIPS) of C60 films
Conventional (Dose, 1977)
LEIPS(Yoshida, 2012)
K. Kanai, et al., Appl. Phys. A 95, 309 (2009).
low resolution, damage
4.5 eV
4.03 eV
0
2
4
6
energy from
E
vac
(eV)
intensity (arb. units)
high resolution
no damage

## Slide 21: Electron Affinities of fullerenes
C60
PC61BM
C70
PC71BM
bis-PCBM
3.98±0.06 eV
4.00±0.04 eV
3.84±0.04 eV
3.81±0.06 eV
3.52±0.04 eV
3.74±0.07 eV
ICBA
H. Yoshida, J. Phys. Chem. C 118, 24377 (2014).

## Slide 22: EA of organic semiconductors
H. Yoshida, Anal. Bioanal. Chem. 406, 2231 (2014) -Trend2014

## Slide 23: Electron affinities by LEIPS
http://adv.chiba-u.jp/nano/yoshida_lab/index.htm
Yoshida, J. Electron Spectrosc. Relat. Phenom., 204, 116 (2015).

## Slide 24: Our LEIPS apparatus (appeared in comic strips)

## Slide 25: Experimental techniques
effect of hole
complicated data
high resolution
life-time measurement
direct probe
low resolution
2 photon PES (2PPE)
IPES
hn1
+
vacuum level
e-
hn
Ek
e-
Ek
hn2
-
-

## Slide 26: HOMO level + optical gap
photoemission spectrosc, photoabsorption spectrosc.
EB
Evac
e-
hn
Ek
＋
EB= hn -Ek
optical gap
＋
-
HOMO
LUMO

## Slide 27: LEIPS spectra of OLED materials
ｔris(4-carbazoyl-9-ylphenyl)amine
（2,9-dimethyl-4,7-diphenyl-1,10-phenanthroline ）
4,4'-Bis(carbazol-9-yl)
biphenyl
tris(2-phenylpyridinato)
iridium(III)

## Slide 28: Energy levels of OLED materials
energy / eV
2.0
6.0
4.0
LUMO
CBP
BCP
Ir(ppy)3
TCTA
Alq3
HOMO
5.8b
6.1a
5.6a
6.7a
1.6
1.8
1.9
1.8
2.1
6.0a
Yoshida, Yoshizaki, Org. Electron. 20, 24 (2015).

## Slide 29: Energy levels of OLED materials
energy / eV
2.0
6.0
4.0
optical
LUMO
CBP
BCP
Ir(ppy)3
TCTA
Alq3
HOMO
5.8b
6.1a
5.6a
6.7a
3.2a
2.4b
3.0a
3.0a
6.0a
3.3a
optical gap
a. C. Adachi, R. Kwong and S. R. Forrest, Org. Electron. 2, 37-43 (2001).
b. S. H. Kim, J. Jang and J. Y. Lee, Appl. Phys. Lett. 91, 083511 (2007).

## Slide 30: Energy levels of OLED materials
energy / eV
2.0
6.0
4.0
LUMO
CBP
BCP
Ir(ppy)3
TCTA
Alq3
HOMO
5.8b
6.1a
5.6a
6.7a
1.6
1.8
1.9
1.8
3.2a
2.4b
3.0a
3.0a
2.1
6.0a
3.3a
optical gap
Yoshida, Yoshizaki, Org. Electron. 20, 24 (2015).
optical
LUMO

## Slide 31: Enhancement of LEIPS signal by Surface Plasmon Resonance
+
-
plasmon
electron
photon
nanoparticle
organic semiconductor
wavelength
(nm)

## Slide 32: Ag nanoparticles
Vacuum deposition: Ag / ITO glass

## Slide 33: Extinction spectra of Ag nanoparticles
Ag 3 nm
Ag 30 nm
Ag 50 nm
Notes: この図は光の波長に対する消光率を示したスペクトルです。表面プラズモン共鳴波長では消光スペクトルにピークが見られます。赤のAgの平均膜厚が3nmでは550nm、青のAg30nmは400nm、緑のAg50nmでは450nm付近にブロードなピークが観測されました。すなわち、これらの波長では、表面プラズモン共鳴によりLEIPS強度の増強が期待できます。
そこで、増強が期待されない260nmと増強が期待される387nmの2つの検出波長を用いて、これらのAgナノ粒子のLEIPSスペクトルを測定しました。

## Slide 34: LEIPS spectra of Ag
Ag 3 nm
Ag 50 nm
Ag 30 nm
Ag flat
3 times
3 times
Ag nanoparticles

## Slide 35: Organic semiconductor/Ag NP
Cu phthalocyanine (CuPc)
thickness : 5~40 nm
depo rate : 0.15 nm min⁻1
vacuum : 1.0×10⁻⁷ Pa
CuPc
Ag NP
ITO substrate
reference
Notes: 本研究では、代表的な有機半導体ある銅フタロシアニン(CuPc)を用いました。
先ほど信号増強を確認したAgナノ粒子上にCuPcを蒸着しました。CuPcの平均膜厚を5～40 nmの間で変えながら、LEIPS測定を行いました。
また、表面プラズモン共鳴の起こらないITO上にも同じ条件でCuPcを蒸着し、同様のLEIPS測定を行って比較しました。

## Slide 36: LEIPS spectra of organic semiconductor
Ag nanoparticles
Ag 3 nm
Ag 50 nm
Ag 30 nm
ITO
3 times
5 times
CuPc

## Slide 37: Wavelength of the plasmon resonance
CuPc / Ag NP
Ag nanoparticle
Ag 30 nm
Ag 50 nm
Ag 3 nm

## Slide 38: Summary of LEIPS and SPR
0
1
2
3
energy (eV)
intensity
5 times
CuPc
e-
hn
Ag

## Slide 39: Outline
Energy levels of unoccupied states
  low energy inverse photoelectron spectroscopy
  enhancement of signal by surface plasmon
Intermolecular overlap of molecular orbitals
  splits of occupied and unoccupied levels
  angle-resolved inverse photoelectron spectroscopy

## Slide 40: Carrier transport in organic semiconductor
HOMO
＋
hole
－
electron
transfer integral:
LUMO

## Slide 41: Intermolecular overlap of MO
MO overlap
conductivity
energy split
＋
＋
energy levels
small
small
small
large
large
large
Notes: 分子が集まって、固体になる。
分子軌道が相互作用して、固体の準位ができる。相互作用が大きければ、準位の広がり（バンド幅）が広がる。
価電子準位－ＨＯＭＯ準位、空準位ーＬＵＭＯ準位
準位が密になるとわかりにくい。そこで、エネルギーに対して、準位の密度 ―状態密度を描くことが多い。
電荷は、 ホールは価電子帯上端、電子は空準位の下端
では、電荷が入るとどうなるか？

## Slide 42: Energy level split and formation of energy band structure
2
∞
3
4
n = 1
LUMO
HOMO

## Slide 43: Energy level split and formation of energy band structure
2
∞
3
4
n = 1
LUMO
HOMO

## Slide 44: Challenges
Precise examination of LUMO energy levels
Layer-by-layer growth into 1D columnar structure
J. Phys. Chem. C, 122, 12090 (2018). ACS Editors’ Choice

## Slide 45: Challenges
Precise examination of LUMO energy levels
Layer-by-layer growth into 1D columnar structure
J. Phys. Chem. C, 122, 12090 (2018). ACS Editors’ Choice

## Slide 46: Sn phthalocyanine
a
Sn

## Slide 47: Structure of thin films (LEED)
PbPc / graphene
SnPc / graphene
2 ML
2 ML
 | 1 ML | 2 ML | T (PbPc)
(Å) | 13.81 | 13.47 | 12.89
(Å) | 13.90 | 13.99 | 13.12
g (°) | 91.65 | 101.9 | 96.20
 | 1 ML | 2 ML | T (PbPc)
 | 13.81 | 13.47 | 12.89
 | 13.90 | 13.99 | 13.12
g (°) | 91.65 | 101.9 | 96.20
 | 1 ML | 2 ML | M (PbPc)
(Å) | 13.84 | 13.67 | 12.74
(Å) | 13.88 | 13.70 | 12.74
g (°) | 91.76 | 90.34 | 90
 | 1 ML | 2 ML | M (PbPc)
 | 13.84 | 13.67 | 12.74
 | 13.88 | 13.70 | 12.74
g (°) | 91.76 | 90.34 | 90

## Slide 48: Molecular packing (DRS)
monoclinic
triclinic
Miyamoto et al., Thin Solid Films 256, 64 (1995)
monoclinic
triclinic
SnPc/graphene
－ 1 ML
－ 2 ML
－ 2.8 ML
PbPc/graphene
－ 1 ML
－ 2 ML
T
M
monomer

## Slide 49: UPS and LEIPS spectra of SnPc/HOPG
-3
-2
-1
0
1
2
intensity (arb unit)
energy from EF (eV)
5ML
4ML
3ML
2ML
1ML
LUMO
LEIPS
UPS
HOMO
HOMO-1

## Slide 50: Energy split based on Hückel method
1.2
4
2
∞
3
4
n = 1
5

## Slide 51: Energy split in bilayer (n=1,2)
-3
-2
-1
0
1
2
intensity (arb unit)
energy from EF (eV)
2 ML
1 ML
LEIPS
UPS

## Slide 52: Energy split in bilayer (n=1,2)
-3
-2
-1
0
1
2
intensity (arb unit)
energy from EF (eV)
2 ML
1 ML
LEIPS
UPS

## Slide 53: Energy split in multilayer (n=1-5)
-3
-2
-1
0
1
2
intensity (arb unit)
energy from EF (eV)
5 ML
4 ML
3 ML
2 ML
1 ML
LUMO
HOMO
HOMO-1
J. Phys. Chem. C, 122, 12090 (2018). ACS Editors’ Choice

## Slide 54: Band dispersion of pentacene
H.Yoshida et al. Phys. Rev. B.77.235205(2008)
energy(eV)
2
1
0
-1
Γ
M’
Γ
M’
Y. Nakayama et al. J. Phys. Chem. Lett. (2017)
band calculation
angle-resolved UPS
unoccupied
states
valence states
Notes: 半導体の電荷輸送機構を理解するためには、正孔の伝導を担う価電子準位と、電子の伝導を担う空準位においてそれぞれのエネルギーと波数の関係、バンド分散を把握することが必須である。
無機半導体については価電子準位、空準位ともに実測がなされているが、有機半導体については両方についての計算や価電子準位の実測はなされているが、空準位に関しては手付かずな部分が多い。
そこで、本研究では、有機半導体の空準位のバンド分散測定を目指し、装置の開発を行った。

## Slide 55: Band dispersion of unoccupied states
q
hn
e
k//
E
vacuum level
Ek
Eb
hn
angle-resolved LEIPS

## Slide 56: Low energy electron (less than 5 eV)
Erdman-Zipf electron gun
bias
-20～-15 V
energy
20 eV
Simulation (Simion8.1)
100
200
0
0.2
0.4
0.6
energy (eV)
Emission current(mA)
0
P. Erdman, E. Zipf, Rev. Sci. Instrum. 53, 225 (1982)
cathode
lenses
energy
20 eV
bias
-17 V
θ=0 °
20 eV
bias
-17 V
θ=45 °
Notes: 従来のLEIPS装置ではErdman-Zipf型電子銃を電子源として使用していた。
この電子銃では、カソードで発生した熱電子を収束電極によって試料に収束させる。
下図は横軸が電子線のエネルギー、縦軸がこの電子銃から取り出すことのできる電流量を示す。
この曲線からわかる通り、この電子銃ではLEIPSで使用する5 eV以下の電子線を取り出すことができない。
そこで従来のLEIPS装置では電子銃から20 eV程度のエネルギーを持った電子線を照射し、試料や電子銃にバイアス電圧を印加して試料近傍で減速させ、5 eV以下の低速電子線を試料に入射させていた。
右図は荷電粒子についての、電場と軌道のシミュレーション結果である。青線が電子線を表し、赤線が等電位線を表す。
どちらも20 eVの電子線を照射し、試料に17Vのバイアス電圧を印加して3 eVに減速している。
垂直入射の場合は等電位線が試料に対して水平に生じるため電子線はまっすぐに試料に届くが、試料を回転させた場合には等電位線が乱れ、電子線の軌道が曲げられてしまう。

## Slide 57: New electron source
energy
1～5 eV
bias
0 V
bias
0 V
3 eV
Erdman-Zipf electron gun
present work
Notes: そこでバイアス電圧を用いずに低速電子線を制御できる電子源を開発した。
Erdman-Zipf型電子銃から収束電極の枚数を増やし、低速電子線の制御を狙った。
下図は電極の数を増やす前後のシミュレーションである。
電極の枚数を増やすことで、電子源内の等電位線をより細かく制御できるようになった。
これによってシミュレーションの結果、1～5 eVの低速電子線の制御ができるようになった。
これによってバイアス電圧を印加する必要がなくなり、試料を回転させても電子線が曲げられることがなくなった。

## Slide 58: AR LEIPS apparatus
mirror
sample (rotatable)
electron gun
photon detector
pump
quartz window
permalloy chamber
additional
magnetic shield
Notes: 電場を遮蔽するために、電子線から絶縁体が見えないようにし、導電体であっても表面の仕事関数を一定にし、電子線の周りの物体を電子線に対して軸対称にした。
電子源の先端にノズル状のパーツをつけ、試料を保持するマニピュレータは表面の仕事関数が一定になるよう全体にコロイダルカーボンを塗布し、さらに試料後方にコロイダルカーボンを塗布した銅メッシュを配置した。
さらに、集光鏡前面にもコロイダルカーボンを塗布した銅メッシュを配置した。

## Slide 59: AR-LEIPS of HOPG (graphite)
Effective mass m*/me
K. Takahashi et al, Phys. Rev. B 85, 075325 (2012)
5.0
4.8
4.6
4.4
4.2
4.0
3.8
kinetic energy (eV)
-4
-2
0
2
4
5.2
+30°
+25
+20
+16
+12
+8
+4
0
-4
-8
-12
-16
-20
θ
image potential state
Notes: 続いて、実際に角度分解測定を行い、性能評価を行った。
試料には高配向熱分解グラファイト(以降HOPGと呼称)を使用し、その鏡像準位の分散を測定した。
左のグラフは横軸に入射電子のエネルギー、縦軸に強度をとり、試料の角度ごとにプロットしたものである。
右のグラフは横軸に試料表面平行方向の波数、縦軸に各波数(角度)におけるピークの位置をプロットしたものである。
鏡像準位は自由電子的な分散をすることが知られており、右のグラフの赤の実線はプロット点を二次関数でフィッティングしたものである。
この二次関数から電子の有効質量が0.99±0.10と得られ、この値が二光子光電子分光法で得られた値とよく一致することから、本装置では角度の定量性良く角度分解LEIPSの測定が行えたものと判断した。

## Slide 60: Conclusion
Energy levels of unoccupied states low-energy inverse photoelectron spectroscopy (LEIPS)
  unoccupied states can be examined with the precision similar to the occupied states by photoelectron spectroscopy.
  LEIPS signal can be enhanced by surface plasmon resonance
Intermolecular electronic coupling
  Energy level splitting of occupied and unoccupied states evolving into the 1D band.
  Band dispersion by angle-resolved LEIPS

## Slide 61: Acknowledgements
Chiba University
Lab members
Kyoto University
  Mr. Kazuto Yamada
  Prof. Naoki Sato
Financial Support
JST PRESTO
JST A-STEP
Kakenhi

## Slide 62: Lab members in Chiba University

## Slide 63: Lab members in Chiba University
plasmon

## Slide 64: Lab members in Chiba University
plasmon
AR-LEIPS

## Slide 65: Lab members in Chiba University
plasmon
AR-LEIPS
LEIPS

## Slide 66: Conclusion
Energy levels of unoccupied states low-energy inverse photoelectron spectroscopy (LEIPS)
  unoccupied states can be examined with the precision similar to the occupied states by photoelectron spectroscopy.
  LEIPS signal can be enhanced by surface plasmon resonance
Intermolecular electronic coupling
  Energy level splitting of occupied and unoccupied states evolving into the 1D band.
  Angle-resolved LEIPS
Inverse photoelectron spectroscopy can be a powerful and useful technique.

## Slide 68: Organic semiconducting molecules
PTCDA
C24H8O6
Pentacene C22H14
Fullerene C60
O
O
O
O
O
O
P3HT
Alq3

## Slide 69: HOMO split in PbPc dimer
S.Kera et al, Phys. Rev. B. 75, 121305 (2007)
PbPc/HOPG
lead phthalocyanine (PbPc)
a
Pb

## Slide 70: Polymorphs of PbPc single crystal
Triclinic (T)
Monoclinic (M)
K.Ukei, Acta Cryst. B29, 2290 (1973)
Y.Iyechika et al, Acta Cryst. B38, 766 (1982)
HOMO
LUMO
HOMO-1

## Slide 71: Periodic table

## Slide 72: Workfunction
monoclinic
triclinic
0
1
2
3
4
5
4.2
4.3
4.4
4.5
4.6
work function (eV)
thickness (ML)
PbPc
SnPc

## Slide 73: Molecular orbitals of SnPc
HOMO-1
HOMO
LUMO
π-orbital
π-orbital
metal

## Slide 74: LEIPS appeared in comic strips

## Slide 75: Organic Photovoltaic Cells
donor
acceptor
C60
PCBM
bis-PCBM
ICBA
-
photon
＋
-
＋
-
LUMO
HOMO
LUMO
HOMO
metal
metal
Notes: 薄膜
吸収する光、電圧→エネルギーダイヤグラム

## Slide 76: UPS and LEIPS spectra
55°
33°
90°
molecular
orientation θ
PNQ
on graphene
PNQ
on SiO2
PNQ
on pentacene
a) graphene
b) SiO2
c) pentacene
UPS
LEIPS

## Slide 77: Polarization energies
(a) G. Heimel, et al., Nature Chem. 5, 187 (2013).
unit ： eV
Ig = 7.89 a
Ag = 1.54 a
P- = 1.54
gas
55°
33°
90°
1.10
P+ = 0.70
1.47
1.05
0.37
A = 3.32
2.83
2.34
I = 6.85
6.45
6.18

## Slide 78: Cyclic voltammetry
in solution

## Slide 79: PCBM as a p-type semiconductor
Y. Ie, M. Karakawa, S. Jinnai, H. Yoshida, A. Saeki, S. Seki, S. Yamamoto, H. Ohkita, Y. Aso
BCN-HH-BCN
PC61BM
-4.2
-4.1
-6.08
-6.64
CV

## Slide 80: LEIPS of BCN-HH-BCN and PCBM
Y. Ie, M. Karakawa, S. Jinnai, H. Yoshida, A. Saeki, S. Seki, S. Yamamoto, H. Ohkita, Y. Aso Chem. Commun., 50, 4123-4125 (2014)
BCN-HH-BCN
PCBM
CV
PC61BM
BCN-HH-BCN
4.2
6.08
4.1
6.64
＋
-
PC61BM
BCN-HH-BCN
3.81
6.08
4.45
6.64
LEIPS
-
＋