## Slide 1
X-ray dichroism studies of magnetic anisotropies in ferromagnetic thin films
The 9-th Vacuum and Surface Science Conference of Asia and Australia (VASSCAA-9)
August 13-16, 2018, Sydney, Australia
Atsushi FUJIMORI
University of Tokyo

## Slide 2
X-ray dichroism studies of magnetic anisotropies in ferromagnetic thin films
The 9-th Vacuum and Surface Science Conference of Asia and Australia (VASSCAA-9)
August 13-16, 2018, Sydney, Australia
SR-SX
XMCD
XMLD
RIXS
ARPES
hn
Linear polarization
Circular polarization
Atsushi FUJIMORI
University of Tokyo
e
hn

## Slide 3
Atsushi FUJIMORI
University of Tokyo
X-ray dichroism studies of magnetic anisotropies in ferromagnetic thin films
The 9-th Vacuum and Surface Science Conference of Asia and Australia (VASSCAA-9)
August 13-16, 2018, Sydney, Australia
L10-phase FePt
La1-xSrxMnO3
H
Sample rotation
hn
SR

## Slide 4
L10-phase FePt
La1-xSrxMnO3
H
Sample rotation
hn
SR
Acknowledgement
G. Shibata, K. Ikeda, Y. Takahashi, Y. Nonaka, K. Ishigami, Z. Chi, T. Harano, T. Kadono (UTokyo)
Soft x-ray MCD: T. Koide, K. Amemiya, M. Sakamaki (KEK-PF)
Y. Takeda (JAEA SPring-8)
Hard x-ray MCD: M. Suzuki, N. Kawamura (JASRI SPring-8)
La1-xSrxMnO3 thin film: M. Kitamura, M. Minohara, K. Yoshimatsu, H. Kumigashira (KEK-PF)
L10-ordered FePt thin film: K. Takanashi, T. Seki (IMR, Tohoku U)
Cluster-model calculation: A. Tanaka (Hiroshima U)
JSPS-KAKENHI Basic Research S (22224005, JSPS, 2010-2014) & A (15H02109, 2015-2018)

## Slide 5
XMCD
Spin-orbit splitting
Photon energy
Photon energy
Photon energy
10~20 eV
Mspin
Morbital
Absorption
XMCD =
I(s+) – I(s -)
s+
s -
XMCD d(hn)
Spin
sum rule
Orbital
sum rule
3
3
A3-A2
Circular
polarized light
Sample
s -
s+
X-ray magnetic circular dichroism (XMCD)
Element specific
Free from impurities, substrates, ..
X-ray absorption (XAS) spectra
Core level
Valence
level
Spin-orbit
splitting
s -
s+
B. T. Thole et al., PRL (1992), P. Carra et al., PRL (1993)
Mspin + (7/2)MT
MT = -mBT : Magnetic dipole

## Slide 6
Magnetic anisotropy of ferromagnets
Coercivity of permanent magnets
Perpendicular magnetization for high-density information storage
a
qM
qH
Ku: uniaxial MAE per volume M: magnetization
H: applied magnetic field
M. J. D. Coey, Magnetism and Magnetic Materials (Cambridge, 2009)
Magnetic anisotropy energy (MAE)
for uniaxial cases
Magnetic anisotropy 
qH  qM (except for qH = qM = 0o or 90o)
Spin-orbit interaction is necessary.

## Slide 7
a
qM
qH
M-H curves for different H angles
qH ＝
Magnetization hysteresis of a single-domain
ferromagnetic nanoparticle
M. J. D. Coey, Magnetism and Magnetic Materials (Cambridge, 2009)
MAE
Zeeman
Stoner-Wohlfarth model

## Slide 8
a
qM
qH
Magnetization hysteresis of a single-domain
ferromagnetic nanoparticle
MAE
Zeeman
Stoner-Wohlfarth model
M. J. D. Coey, Magnetism and Magnetic Materials (Cambridge, 2009)
M-H curve averaged over different H angles

## Slide 9
S. Yamamoto et al., APL (2005)
FePt SiO2
bare FePt
particles
Y. Takahashi, AF et al., PRB (2014)
oxidized Fe
Fe L2,3 XMCD of L10-phase FePt single-domain nanoparticles
L10 (fct, a>c)
Fe
Pt

## Slide 10
Fit using the angle-averaged Stoner-Wohlfarth model
Single Hc
Distributed Hc
Expt
Hc distribution
oxidized Fe
Fe in FePt
M-H curves deduced from XMCD intensities
Fe L2,3 XMCD of L10-phase FePt single-domain nanoparticles
Y. Takahashi, AF et al., PRB (2014)
 MAE with Ku 〜 2.7 × 106 J/m3
cf. Ku 〜 3×106 J/m3 (thin film)
Y. Takahashi, AF et al., PRB (2014)

## Slide 11
Magnetic anisotropy of nanoparticle
a
qM
qH
Ku: uniaxial MAE per volume M: magnetization
H: applied magnetic field
M. J. D. Coey, Magnetism and Magnetic Materials (Cambridge, 2009)
Magnetic anisotropy energy (MAE)
Magnetic anisotropy 
qH  qM (except for qH = qM = 0o or 90o)
Zeeman
MAE
Stoner-Wohlfarth model

## Slide 12
M. J. D. Coey, Magnetism and Magnetic Materials (Cambridge, 2009)
Magnetic anisotropy energy (MAE)
Magnetic anisotropy of thin film
Ku: uniaxial MAE per volume M: magnetization
H: applied magnetic field
axis
film
Hdemag
Zeeman
MAE
Stoner-Wohlfarth model
Magnetic anisotropy 
qH  qM (except for qH = qM = 0o or 90o)

## Slide 13
M. J. D. Coey, Magnetism and Magnetic Materials (Cambridge, 2009)
Magnetic anisotropy energy (MAE)
Magnetic anisotropy of thin film
Ku: uniaxial MAE per volume M: magnetization
H: applied magnetic field
axis
film
Zeeman
MAE
SA
Stoner-Wohlfarth model
Shape anisotropy
caused by demagnetization field
Hdemag
H
H||
Ku = E|| - E > 0  Perpendicular magnetic anisotropy (PMA)
Magnetic anisotropy 
qH  qM (except for qH = qM = 0o or 90o)

## Slide 14: Vector-type superconducting magnet
Horizontal coil
Vertical coil
~16 cm
M. Furuse et al., IEEE Trans. Appl. Supercond. (2012)
H
hn
SR
Sample rotation
SuperPower®
YBCO wire

## Slide 15
To beamline
Kicker magnets
Electron trajectory
Undulator I
Undulator II
Fast
switching
~10 Hz
Fast polarization switching undulator at the soft x-ray beam line BL-16A of KEK-PF
Apple II-type undulators
rom undulator 
Vector-type SC
XMCD（1.4 T）
Depth resolved
XAFS/XMCD
Electromagnet XMCD (1.2 T)
SC magnet
XMCD (5T)

## Slide 16
Angular-dependent XMCD of La0.6Sr0.4MnO3 film on SrTiO3(001)
L2,3
Mn L2,3 XMCD
H
Sample rotation
hn
@Apple II undulator BL-16, KEK-PF
Superconducting vector magnet
k
hn
G. Shibata, AF et al., npj Quantum Mater. (2018)

## Slide 17: Phase diagram of hole-dope La1-xSrxMnO3
A. Urushibara, Y. Tokura et al. , PRB (1995)
Half-metal

## Slide 18
Y. Tokura
 High-spin state
e
3
orbitals
Hund’s rule
> Crystal field
Mn
O
MnO6 octahedron
Giant magneto-resistive manganites

## Slide 19
compressive
tensile
Electronic phase diagram of La1-xSrxMnO3 under epitaxial strain
FM
FM
C-AFI
C-AFI
A-AFM
A-AFM
Y. Konishi et al., JPSJ (1999)

## Slide 20
Magnetic anisotropy of strained La0.67Sr0.33MnO3 films on SrTiO3 and LaAlO3 substrates
F. Tsui et al., APL (2000)
compressive
tensile
LaAlO3
SrTiO3
H
H||
H 
H||
M
M

## Slide 21
L2,3
Mn L2,3 XMCD
H
Sample rotation
hn
@Apple II undulator BL-16, KEK-PF
Superconducting vector magnet
k
hn
G. Shibata, AF et al., npj Quantum Mater. (2018)
Angular-dependent XMCD of La0.6Sr0.4MnO3 film on SrTiO3(001)

## Slide 22
Angular-dependent XMCD of strained La1-xSrxMnO3 film on SrTiO3 and LaAlO3 substrates
compressive
tensile
M
M
La0.6Sr0.4MnO3/SrTiO3(001)
La0.7Sr0.3MnO3/LaAlO3(001)
+
+
+
+
MAE
MAE
G. Shibata, AF et al., npj Quantum Mater. (2018)
MAE
Magnetic dipole

## Slide 23
M. J. D. Coey, Magnetism and Magnetic Materials (Cambridge, 2009)
Magnetic anisotropy energy (MAE)
Magnetic anisotropy of thin film
Ku: uniaxial MAE per volume M: magnetization
H: applied magnetic field
axis
film
Zeeman
MAE
SA
Stoner-Wohlfarth model
Shape anisotropy
caused by demagnetization field
Hdemag
H
H||
Ku = E|| - E> 0  Perpendicular magnetic anisotropy (PMA)
Magnetic anisotropy 
qH  qM (except for qH = qM = 0o or 90o)

## Slide 24
Angular-dependent XMCD of strained La1-xSrxMnO3 film on SrTiO3 and LaAlO3 substrates
Ku = (4.0±0.4)×104 J/m3 > 0
out-of-plane easy axis
Ku = - (1.9±0.1) x 104 J/m3 < 0
in-plane easy axis
compressive
tensile
M
M
La0.6Sr0.4MnO3/SrTiO3(001)
La0.7Sr0.3MnO3/LaAlO3(001)
+
+
+
+
MAE
MAE
G. Shibata, AF et al., npj Quantum Mater. (2018)
MAE
Magnetic dipole

## Slide 25
Microscopic theory of magnetic anisotropy
spin-flip term
G. van der Laan, JPCM (1998)
Magnetic anisotropy energy (MAE):
||, 
Ku = E|| - E
H
H||
x: spin-orbit coupling L: orbital moment
S: spin moment
T: magnetic dipole
> 0  Perpendicular magnetic anisotropy (PMA)
spin-conserved term
(Bruno term)
Easy axis
Hard
axis
MAE
Ea
Bruno
relation
P. Bruno, PRB (1989).
M
M
||
|

## Slide 26: Bruno model: Magnetic anisotropy vs orbital-moment anisotropy
orb
orb
a
P. Bruno, PRB (1989)
D. Weller et al., PRL (1995), J. Stöhr, JMMM (1999)
Co L2,3 XPCD of Au/Co multilayer
Magnetic anisotropy energy
M
M
M
M
M
M
Perpendicular magnetic anisotropy (PMA)
Bruno model: Successful for Ni/Fe, Co/Fe, Co/Au, …. Interfaces, alloy thin films, …
z: spin-orbit coupling
Notes: 結晶磁気異方性 (MCA) と軌道磁気モーメントの関係としてBrunoの式が提唱されています。Bruno の関係によれば、
磁化容易軸方向の軌道磁気モーメントは困難軸方向より大きい
磁気異方性エネルギーは磁化容易軸方向と困難軸の軌道磁気モーメントの差に比例する
ということです。
つまり、Brunoの関係によれば、「結晶磁気異方性の増加、つまりL10規則度の増加に伴い、容易磁化軸方向と困難軸方向の軌道磁気モーメントの差が増加する」ことが期待されますが、以前我々が行ったFe L23端XMCDの実験ではそのような結果が得られませんでした。
加えて、オーダーしたFePt 合金の MCA の起源は Pt 5d 軌道の強いスピン軌道相互作用であり、ソロヴィエフ (Solovyev) らの第一原理計算によればオーダーしたFePt合金のPtはFeより15倍以上のMCAエネルギーもっているということが分かっています。
そこで今回我々はPtに注目して、L10規則度を変えたFePt薄膜の XMCDを面直及び面内磁場配置で測定し、まずはBrunoの関係を用いて、磁気異方性の度合いがPtの軌道角運動量の異方性の度合いによって発現しているかを調べることを目的に実験を行いました。
#----------------------------------------------------------------------------
加えて、オーダーしたFePt 合 金の MCA の起源は Pt 5d 軌道の強いスピン軌道相互作用であり [2]、スピン軌道相互作用の 2 次摂動を考慮し た第一原理計算によればオーダーした FePt 合金の Pt は Fe より 15 倍以上の MCA エネルギーを持っています [3]。これらは L10オーダーしたFePt 薄膜の MCA の起源も同様に Pt 5d 電子の軌道角運動量である可能性を示唆しています。実際、われわれの行ったFeL23端XMCDの実験では、L10 規則度の増加に伴う面直および面直磁場配置の軌道磁気モーメントの差の増加が見られませんでした。
#Bruno モデルがDOSの計算に使うハートリーフォックモデルでは平均場近似が仮定されているので、計算されたDOSはスピンの向きが異なる電子間の電子相関効果を考慮できない。
#----------------------------------------------------------------------------
電子配位子場モデルでは、結晶磁気異方性（MCA) のミクロな起源は図のように考えられている。
+z方向に外部磁場Hをかけて、スピン方向を揃えた原子のd電子を考える。
スピン方向の周りを回転運動するd電子の軌道モーメント<Lz> は-2 から +2 までの値を取る。
最も低いエネルギー準位はスピン方向が外部磁場Hと逆方向の Lz = -2 状態になる。
この原子が四隅に負または正の電荷をもつ原子の作る平面の中心にある状態を考える。
軌道上を運動する電子は負イオンの場合クーロン斥力、正イオンの場合クーロン引力をうける。
軌道上を運動する電子は2つの逆向きに進む定常波 +/-Lz の重ね合わせからなる定常波、図のような定常波をつくる。
(電子の面内軌道は分子軌道が形成されたことで消失した(図はdx2-y2とdxy)。ともいえる。)
ゆえに、軌道に付随する接合面に垂直な方向の軌道モーメントは消失する。
これに対して、近傍にイオンがいないために、電子は接合面に垂直な方向に動きにくくなる。
軌道に付随する面内軌道モーメントは消失しない。
図に示すような単純なモデルによれば、原子の軌道モーメントの異方性は結合環境の異方性に関係がある。
単層膜では、軌道モーメントL(morb=-muBL/h)は結合面内で大きく、結合面に垂直な方向で小さくなると予想できる。
多層膜の場合、これは逆になる場合がある。
#D. Weller らはCo(0001)の膜厚を変えながら図のような構造のAu(111)/Co(0001)/Au(111)薄膜を作成し、Co L3,2 XMCDを面直および面内磁場配置で測定した結果に基づき、Bruno の関係の正当性を実験的に検討しました。Coの膜厚を薄くすると結晶磁気異方性が強くなることがしられていましたが、面内と面直磁場配置で測定したXMCDから求めた軌道モーメントの差が大きくなったことから、Brunoの関係が実験的に確かめられました。

## Slide 27
Y. Tokura
 High-spin state
e
3
orbitals
Hund’s rule
> Crystal field
Mn
O
Very weak spin-orbit coupling in eg orbitals.
MnO6 octahedron
Orbital moment Morb is too weak to detect
Giant magneto-resistive manganites
by XMCD.

## Slide 28
XMCD
Spin-orbit splitting
Photon energy
Photon energy
Photon energy
10~20 eV
Mspin
Morbital
Absorption
XMCD =
I(s+) – I(s -)
s+
s -
XMCD d(hn)
Spin
sum rule
Orbital
sum rule
3
3
A3-A2
Circular
polarized light
Sample
s -
s+
X-ray magnetic circular dichroism (XMCD)
Element specific
Free from impurities, substrates, ..
X-ray absorption (XAS) spectra
Core level
Valence
level
Spin-orbit
splitting
s -
s+
B. T. Thole et al., PRL (1992), P. Carra et al., PRL (1993)
Mspin + (7/2)MT
MT = -mBT : Magnetic dipole

## Slide 29
XMCD sum rules in conventional (longitudinal) geometry
Spin sum rule
: Unit vector || photon helocity
Orbital sum rule
Sample
hn
H
Mspin
Morb
MT
: Magnetic dipole

 0 for cubic symmetry

## Slide 30
XMCD in transverse geometry (T-XMCD)
: Unit vector || photon helicity
X
Spin sum rule
Orbital sum rule
H. A. Dürr and G. van der Laan, PRB (1995)
||
|
: Magnetic dipole
Sample
hn
H
Mspin
MT
Morb

## Slide 31
k
hn
MT
G. Shibata, AF et al., npj Quantum Mater. (2018)
XMCD in transverse geometry (T-XMCD)
Orbital sum rule 
M||orb - Morb changes sign between tensile and
compressive strain.
According to Bruno model, Ku  E|| - E should
also change sign, consistent with MAE.
However, the sign of M||orb - Morb cannot be
determined with sufficient accuracy.

## Slide 32
Easy axis
Hard
axis
MAE
Ea
Beyond the Bruno model – Magnetic dipole
spin-flip term
G. van der Laan, JPCM (1998)
Magnetic anisotropy energy (MAE):
||, 
Bruno
relation
Ku = E|| - E
H
H||
x: spin-orbit coupling L: orbital moment
S: spin moment
T: magnetic dipole
> 0  Perpendicular magnetic anisotropy (PMA)
P. Bruno, PRB (1989).
spin-conserved term
(Bruno term)
M
M
||
|
small

## Slide 33
XMCD in transverse geometry (T-XMCD)
: Unit vector || photon helicity
X
Spin sum rule
Orbital sum rule
H. A. Dürr and G. van der Laan, PRB (1995)
||
|
: Magnetic dipole
X

Sample
hn
H
Mspin
MT
Morb

## Slide 34: Magnetic dipole MT reflecting the spin-density anisotropy
〈S〉
: position operator of electron,
〈S〉
defines the anisotropic distribution of spin density rspin(r)
J. Stöhr and H. König, PRL (1995), H. A. Dürr and G. van der Laan, PRB (1996)
〈ST〉 < 0
〈ST〉 < 0
〈ST〉 > 0
〈ST〉 > 0
x2-y2
3z2-r2
〈ST〉 ~ 0
〈ST〉 ~ 0
〈T〉
〈T〉
Qxx
Qyy
Qzz
Q: Quadrupole tensor
where
Qzz>0
Qzz<0

## Slide 35
k
hn
MT
G. Shibata, AF et al., npj Quantum Mater. (2018)
XMCD in transverse geometry (T-XMCD)
T (MT) changes sign between tensile and
compressive strain.
Spin sum rule 
〈ST〉 > 0
〈ST〉 < 0

## Slide 36: Magnetic dipole MT reflecting the spin-density anisotropy
〈S〉
: position operator of electron,
〈S〉
defines the anisotropic distribution of spin density rspin(r)
J. Stöhr and H. König, PRL (1995), H. A. Dürr and G. van der Laan, PRB (1996)
〈ST〉 < 0
〈ST〉 < 0
〈ST〉 > 0
〈ST〉 > 0
x2-y2
3z2-r2
〈ST〉 ~ 0
〈ST〉 ~ 0
〈T〉
〈T〉
Qxx
Qyy
Qzz
Q: Quadrupole tensor
where
Qzz>0
Qzz<0
LSMO/STO
LSMO/LAO

## Slide 37
Easy axis
Hard
axis
MAE
Ea
Beyond the Bruno model – Magnetic dipole
spin-flip term
Magnetic anisotropy energy (MAE):
||, 
Bruno
relation
Ku = E|| - E
H
H||
x: spin-orbit coupling L: orbital moment
S: spin moment
T: magnetic dipole
> 0  Perpendicular magnetic anisotropy (PMA)
P. Bruno, PRB (1989).
spin-conserved term
(Bruno term)
M
M
||
|
small
G. van der Laan, JPCM (1998)

## Slide 38
Angular-dependent XMCD of strained La1-xSrxMnO3 film on SrTiO3 and LaAlO3 substrates
Ku = (4.0±0.4)×104 J/m3 > 0
out-of-plane easy axis
Ku = - (1.9±0.1) x 104 J/m3 < 0
in-plane easy axis
compressive
tensile
M
M
La0.6Sr0.4MnO3/SrTiO3(001)
La0.7Sr0.3MnO3/LaAlO3(001)
+
+
+
+
MAE
MAE
G. Shibata, AF et al., npj Quantum Mater. (2018)
MAE
Magnetic dipole

## Slide 39
Magnetic anisotropy
M
Magnetic dipole as the origin of magnetic anisotropy?
Orbital anisotropy
Magnetization induced by H
Orbital polarization induced by H
H
M
?

## Slide 40
Observation of anisotropic charge density induced by H by x-ray magnetic linear dichroism (XMLD)
V-pol
Mspin
H || z
H-pol
hn
y
z
x
Qij ≡ δij – 3rirj
〈Qzz〉 = 〈1 – 3z2/r2〉
∝ ∫L3+L2 (XMLD) d(hv)
^
^
XMLD
Integral of
XMLD
〈Qzz〉
L3
L2
XMLD sum rule
H
V
B. Thole et al., PRL 55 (1985)

## Slide 41
Mn L2,3 XMLD of La0.6Sr0.4MnO3/SrTiO3(001)
G. Shibata, AF et al., submitted to JPSJ
XMLD
intensity
 M2

## Slide 42
Magnetic anisotropy
M
Magnetic dipole as the origin of magnetic anisotropy?
Orbital anisotropy
Magnetiztion induced by H
Orbital polarization induced by H
H
M
?
G. Shibata, AF et al., submitted to JPSJ

## Slide 43
L10-ordered FePt thin film with strong perpendicular anisotropy
M-H curves
T. Seki, K. Takanashi et al., J. Phys. D (2011)
S: Degree of L10 order
S = 0.8
S = 0.5
S = 0.4
L10 (fct, a>c)
Fe
Pt
H
H||
anneal

## Slide 44
Fe L2,3 XMCD of L10-ordered FePt thin film
L10 (fct, a>c)
Fe
FePt Fe L2,3 XMCD
K. Ikeda, AF et al., APL (2017)
Mspin(Fe) ~ 2 mB
Pt
Easy axis
Hard
axis
MAE
Ea
Bruno
relation
H
H||
M
M

## Slide 45
Pt L2,3 XMCD of L10-ordered FePt thin film
FePt Pt L3 XMCD
Pt L2 XMCD
Bruno relation
violated !
Mspin(Pt) ~ 0.3 mB
L10 (fct, a>c)
Fe
Pt
K. Ikeda, AF et al., APL (2017)
H
H||
Easy axis
Hard
axis
MAE
Ea
M
M

## Slide 46
 |  | Fe |  | Pt | 
 |  | Mspin (mB) | Morb (mB) | Mspin (mB) | Morb (mB)
Experiment XMCD M-H | out-of-plane | 2.00 | 0.20 | 0.30 | 0.036
 | in-plane | 1.80 | 0.15 | 0.29 | 0.041
 | Morb (-¦¦) | - | 0.05 | - | -0.005
 | MAE (¦¦-) = Ku (MJ/m3) | 4.7 |  |  | 
First-principles calculation | out-of-plane | 2.77 | 0.0802 | 0.35 | 0.0486
 | in-plane |  | 0.0690 |  | 0.0616
 | morb (out - in) | - | 0.0112 | - | -0.0130
 | MAE (in - out) = Ku (MJ/m3) | -0.887 |  | 14.28 | 
Comparison with first-principles calculations:
Roles of Fe 3d and Pt 5d electrons in MAE
“Bruno”
Non-Bruno
Non-Bruno
Non-Bruno
Notes: 有効数字
Solovyev 、Fe L edge 等の結果をまとめtる => MAE mainly comes from Pt sites ちゃんと oral で
Solovyev. 産総研 contact …? absolute valueの解析を進める。

## Slide 47
First-principles calculation by I. V. Solovyev et al., PRB (1995)
 |  | Fe |  | Pt | 
 |  | Mspin (mB) | Morb (mB) | Mspin (mB) | Morb (mB)
Experiment XMCD M-H | out-of-plane | 2.00 | 0.20 | 0.30 | 0.036
 | in-plane | 1.80 | 0.15 | 0.29 | 0.041
 | Morb (-¦¦) | - | 0.05 | - | -0.005
 | MAE (¦¦-) = Ku (MJ/m3) | 4.7 |  |  | 
First-principles calculation | out-of-plane | 2.77 | 0.0802 | 0.35 | 0.0486
 | in-plane |  | 0.0690 |  | 0.0616
 | Morb (-¦¦) | - | 0.0112 | - | -0.0130
 | MAE (¦¦-) = Ku (MJ/m3) | -0.887 |  | 14.28 | 
Comparison with first-principles calculations:
Roles of Fe 3d and Pt 5d electrons in MAE
“Bruno”
Non-Bruno
Non-Bruno
Non-Bruno
Pt dominates MAE and hence PMA!
<<
Notes: 有効数字
Solovyev 、Fe L edge 等の結果をまとめtる => MAE mainly comes from Pt sites ちゃんと oral で
Solovyev. 産総研 contact …? absolute valueの解析を進める。

## Slide 48
 | Bruno | Magnetic dipole MT
Fe |  | 
Pt |  | 


MAE of L10-ordered FePt thin film

## Slide 49
Easy axis
Hard
axis
MAE
Ea
Beyond the Bruno model – Magnetic dipole
spin-flip term
Magnetic anisotropy energy (MAE):
||, 
Bruno
relation
Ku = E|| - E
H
H||
x: spin-orbit coupling L: orbital moment
S: spin moment
T: magnetic dipole
> 0  Perpendicular magnetic anisotropy (PMA)
P. Bruno, PRB (1989).
spin-conserved term
(Bruno term)
M
M
||
|
G. van der Laan, JPCM (1998)

## Slide 50
Angular-dependent XMCD
H
Sample rotation
hn
@Apple II undulator BL-16, KEK-PF
Superconducting vector magnet
XAS and XMCD spectra of
L10-ordered FePt thin film
S = 0.4
K. Ikeda, G. Shibata, AF et al.
k
hn
G. Shibata, AF et al., npj Quantum Mater. (2018)

## Slide 51: Magnetic dipole MT reflecting the anisotropic spatial distribution of spin density
〈T〉
〈S〉
: position operator of electron,
〈T〉
Qxx
Qyy
Qzz
〈S〉
Defines the anisotropic distribution of spin density rspin(r)
J. Stöhr and H. König, PRL (1995), H. A. Dürr and G. van der Laan, PRB (1996)
Q: Quadrupole tensor
where
〈ST〉 < 0
〈ST〉 < 0
〈ST〉 > 0
〈ST〉 > 0
〈ST〉 ~ 0
〈ST〉 ~ 0
Qzz>0
Qzz<0

## Slide 52
Zeeman
MAE
SA
Stoner-Wohlfarth model
Magnetic anisotropy measured by angular-dependent XMCD
k
qH (deg)
-MH + SA
-MH + SA + MAE
-MH + SA
-MH + SA + MAE
-MH + SA + MAE + T
-MH + SA + MAE + T
Expt
Ku = 0.38 MJ/m3
K. Ikeda, G. Shibata, AF et al.
+ T: Magnetic dipole
Fe L2,3-edge XMCD intensity
k
hn
G. Shibata, AF et al., npj Quantum Mater. (2018)

## Slide 53
G. van der Laan, JPCM (1998)
Easy axis
Hard
axis
MAE
Ea
Beyond the Bruno model – Magnetic dipole
spin-flip term
Magnetic anisotropy energy (MAE):
||, 
Bruno
relation
Ku = E|| - E
H
H||
x: spin-orbit coupling L: orbital moment
S: spin moment
T: magnetic dipole
> 0  Perpendicular magnetic anisotropy (PMA)
P. Bruno, PRB (1989).
spin-conserved term
(Bruno term)
M
M
||
|
〈ST〉 < 0
Does not explain the PMA

## Slide 54
 | Bruno | Magnetic dipole MT
Fe |  | 
Pt |  | 


MAE of L10-ordered FePt thin film
 ?

  May be explained by the anisotropic spin distribution of Pt 5d electrons?
   Further angular-dependent XMCD studies at the Pt L edge are needed.

## Slide 55
Easy axis
Hard
axis
MAE
Ea
Beyond the Bruno model – Magnetic dipole
spin-flip term
Magnetic anisotropy energy (MAE):
||, 
Bruno
relation
Ku = E|| - E
H
H||
x: spin-orbit coupling L: orbital moment
S: spin moment
T: magnetic dipole
> 0  Perpendicular magnetic anisotropy (PMA)
P. Bruno, PRB (1989).
spin-conserved term
(Bruno term)
M
M
||
|
large
small

4d, 5d TM
G. van der Laan, JPCM (1998)

## Slide 56
L10-phase FePt
La1-xSrxMnO3
H
Sample rotation
hn
SR
Conclusion
MA of 3d transition-metal and alloy thin films can be explained by Morb anisotropy (the Bruno model).
Weak MA of LSMO thin films driven by epitaxial strain is difficult to explain by the Bruno model because of too small Morb and too small Morb anisotropy. On the other hand, the MA can explained by the spin-density anisotropy MT.
Strong PMA of L10-ordered FePt thin film cannot be explained by the Bruno model. The MT of Pt 5d electrons should play the major role owing to their very strong spin-orbit interaction.
Outlook
Further angular-dependent XMCD studies at the heavy-metal L2,3 edges (in the hard x-ray region).
Temperature dependence of MAE, Morb anisotropy, and MT .
Origin of MAE in cubic systems (CoFe2O4, Fe3O4 etc).

## Slide 58
Core levels for x-ray absorption for XMCD
菅野暁，藤森淳，吉田博編：
新しい放射光科学（講談社，2000）
3d transition
elements
4d transition
elements
5d transition
elements
Lanthanides
Actindes
Mn,Fe
Pt
O
La
Light
elements
Soft x ray
Hard x ray
VUV
3d
5d
 L2,3 edge
2p
Energy
Atomic number
 K edge
 M2,3 edge
 N2,3 edge
 N4,5 edge
 M4,5 edge
4d
4f
5f

## Slide 59
Magnetic anisotropy of ferromagnet with cubic symmetry
M. J. D. Coey, Magnetism and Magnetic Materials (Cambridge, 2009)
Magnetic anisotropy energy
Anisotropy energy surface
M-H curves
Easy axis: [001]
Easy axis: [111]
[001]
[111]

## Slide 60: XMCD apparatus with the vector-type superconducting magnet
hn
hn


## Slide 61
Temperature dependence of MAE in La0.6Sr0.4MnO3/SrTiO3(001)
Angle dependence of Mn L2,3 XMCD
intensity
Temperature dependences of
Msat and Ku
LSMO (20 ML)/STO
(<0)
TC
G. Shibata et al., unpublished

## Slide 62
Magnetization of La0.6Sr0.4MnO3
Temperature dependence of MAE in manganite thin films
J. O’Donnell et al., APL (1998)
K. Yoshimatsu et al., APL (2009)
MAE of La0.67Ca0.33MnO3
 Ku