## Slide 1
Electron Accumulation at Semiconducting Surfaces
C.F. McConville
College of Science, Engineering & Health
RMIT University, Melbourne, Victoria 3001, Australia
and
Department of Physics, University of Warwick
Coventry CV4 7AL, UK.
Ninth Vacuum and Surface Science Conference of Asia and Australia (VASSCAA-9)
Sydney, Australia
12th – 16th August 2018

## Slide 2
What is Surface Electron Accumulation?
Accumulation
Depletion
In the case of a semiconducting material the surface electron density can be said to be in a state of:

## Slide 3
n-type
p-type
Surface space-charge layers

## Slide 4
Historical Surface Electron Accumulation (1)
The first recorded (published) examples of electron accumulation were seen with bombarded, thermal annealing, and O-treated ZnO (0001) single crystals.
Measured the effect of surface Hall mobility as a function of surface electron density.
Hall mobility of electrons in quantized accumulation layers on ZnO surfaces
Y. Grinshpan, M. Nitzan & Y. Goldstein
Phys. Rev. B. 19 (1979) 1098
Electron accumulation on ZnO surfaces could also be induced by exposure to H – as measured using HREELS & STM

## Slide 5
Historical Surface Electron Accumulation (2)
While surface electron accumulation can be induced, as for ZnO, the first example of this phenomena occurring naturally at a semiconductor surface was seen with InAs(001).
As -
In -
Intrinsic electron accumulation layers on
reconstructed clean InAs(100) surfaces
M. Noguchi, K. Hirakawa & T. Akoma
Phys. Rev. Letts. 66 (1991) 2243
High-resolution electron energy loss spectroscopy of the As- and In-terminated InAs(100) surfaces.
Much work was also directed towards passivation this and other InAs surfaces- particularly with sulphur (S) - deposited in a number of different forms e.g. ammonium sulphide (NH4)2Sx
M.J. Lowe, et al. Surface Sci. 523 (2003) 179
L.A. Bailey et al. Appl. Phys. Letts. 95 (2009) 19211

## Slide 6
Potential Electron Accumulation
Systems
Semiconductors
III-V’s & TCO’s
InAs
InN
ZnO
CdO
Ga2O3
In2O3
SnO2

## Slide 7
Potential Electron Accumulation
Systems
Semiconductors
III-V’s & TCO’s
InAs
InN
ZnO
CdO
Ga2O3
In2O3
SnO2

## Slide 8
Band-gap energies
& Lattice constants

## Slide 9
Introduction to InN (1)
Pre-2002
Early samples of InN were either polycrystalline produced by reactive RF-sputtering of indium targets (Tansley & Foley ~ 1986)
The most quoted value of the band gap was 1.89 eV – based on a strong IR absorption edge.
(n~7 x 1016 cm-3, m ~ 4 x 103 cm2/ Vs)
However, some doubt over this value from as early as 1989 when MOVPE single-crystal InxGa1-xN samples grown by Matusoka et al. which extrapolated to a much lower band gap value for InN.
Single-crystalline [7] T. Matsuoka et al, Sixteenth International symposium on GaAs and Related Compounds, Karuizawa, Japan, 25–29 September 1989, Institute of Physics, Bristol, (1990), p. 141.
Polycrystalline samples [2], dc discharge, [3] reactive cathodic sputtering and [4] RF-sputtering

## Slide 10
N2 Gas
Matching
Circuit
High Frequency
Supply
QMS
RHEED
Screen
Ga
Al
Mg
In
Knudsen
Cell
Beam
Monitor
Pyrometer
Shutter
RHEED
E-Gun
RF Radical
Cell
InN : Growth by PA-MBE
Growth temperature ~470 - 500 oC at ~0.6 mm/h
- InN epi-layer thicknesses from 200 nm – 7.5 mm
(n ~ 1017 -1018 cm-3, m ~ 2000 cm2 V-1s-1, dislocation densities ~106 - 107 cm-2 )
e//<11-20>
e//<10-10>
RHEED patterns observed in-situ during InN growth

## Slide 11
Introduction to InN (2)
Post-2002
2002 - Davydov et al., reported InN having a band gap of ~0.9 eV on single crystal MBE grown material with n ~ 0.9 – 1.2 x 1019 cm-3
Followed shortly by Wu et al., citing a band gap of 0.7 – 0.8 eV again with MBE grown single crystalline samples with n ~ 5 x 1018 cm-3. Directly observed Moss-Burstein shift.
Large difference between poly- and single-crystalline InN “…polycrystalline samples show similar behaviour to InNOx
Consensus was achieved with the most recent values of the band gap giving 0.65 eV at 300 K (although 1.4 eV was occasionally quoted by a wide-gap minority).
However, it is clear that high quality InN still suffers from high unintentional n-type conductivity.
T. Inushima et al., Phys. Rev B 68, 235204 (2003)
J. Wu et al., Appl. Phys. Lett. 80, 3967 (2003)

## Slide 12
Selected area electron diffraction shows only wurtzite InN pattern with no evidence of a secondary phase .
g = (0002)
g = (2110)
250 nm
250 nm
C-plane sapphire
InN
AlN
GaN
C-plane sapphire
InN
AlN
GaN
Wurtzite InN: material quality
No indium clusters or inclusions
C. J. Lu, Hai Lu, and William J. Schaff,
Appl. Phys. Lett. 83, 2817 (2003)
XRD from InN grown by PAMBE
demonstrating high structural quality
in the epilayers

## Slide 13
“…metal contacts, including Ti, Al, Ni and a Hg probe all form an Ohmic contact on InN without annealing…”
H. Lu, W. J. Schaff et al., Appl. Phys. Lett. 82, 1736 (2003)
non-zero intercepts
InN /AlN: n2D = 4.3×1013 cm-2
InN /GaN: n2D = 2.5×1013 cm-2
Evidence of significant electron accumulation at InN surfaces
BUT does the clean surface accumulate electrons?
AND is it an intrinsic property of InN?
Earlier electrical characterisation
of InN

## Slide 14
High-Resolution Electron Energy Loss Spectroscopy

## Slide 15
Intrinsic electron accumulation at
clean InN(0001)-(1×1) surfaces
Plasmon peak dispersion

Surface electron accumulation
The layered profile is used to simulate spectra and is used to solve the Poisson equation within the MTFA
(to account for non-parabolicity)
I. Mahboob, T. D. Veal, C. F. McConville, Hai Lu and W. J. Schaff,
Phys. Rev. Lett. 92, 036804 (2004).
T = 300 K
nss = 2.4 × 1013 cm-2
EF(z=0) = 1.46 eV wrt VBM
Eg0 = 0.64 eV
m0*= 0.045m0
mF*(bulk) = 0.120m0
Poisson solution
Layer profile

## Slide 16
Full spectrum solar
photovoltaic materials
Efficient solar cells use multiple semiconductors with fixed energy gaps (e.g. GaInP / GaAs / Ge triple junction cell) to capture as much of the solar spectrum as possible.
The direct energy gap of In1-xGaxN spans nearly the energy range 0.7 eV – 3.4 eV of the solar spectrum, and not 2.0 eV – 3.4 eV as reported in the literature (dotted line).
Multi-junction solar cells based on In1-xGaxN could have efficiencies as high as 60-70%.
Ge
GaAs
GaInP
m
Ga content in
In1-xGax N alloy
Literature
LBNL, 2002
Perfect matching of band gap of In1-xGaxN to solar spectrum
Energy (eV)
Energy (eV)
J. Wu et al. J. Appl. Phys. 94 (2003) 6477.
Solar Flux
(1021 photons/sec/m2/mm)

## Slide 17
C. G. Van de Walle, Phys. Rev. Lett. 85, 1012 (2004);
S. Lany and A. Zunger, Phys. Rev. Lett. 98, 045501 (2007)
Interest in materials which both conduct electricity and are optically transparent (e.g. In2O3, SnO2, CdO)
Wide spread use as transparent electrodes, e.g., in solar cells, LCD displays, LEDs etc.
J. Meyer et al. Adv. Mats, 24, 5408 (2012)
G. Thomas, Nature 389, 907 (2007)
P.D.C. King & T.D. Veal, JCMP 23, 334214 (2011)
Increased interest in oxides for active layer in devices e.g., transparent transistors, short wavelength photonic devices, chemical sensors, UV/visible LEDs.
G. Fiori et al., Nature Nanotechnology 9, 788 (2015)
A. Tsukazaki et al., Nature Materials 4, 42 (2005) &
Science 315, 1388 (2007)
Many fundamental properties of these materials are simply not well known.
Origins of conductivity in TCO’s hotly debated, particularly in high-quality, epitaxial materials.
Oxide Semiconductors

## Slide 18
Transparent conducting oxides (TCO’s)
Semiconducting
TCO’s
CdO
ZnO
Ga2O3
In2O3
SnO2

## Slide 19
Conventional compound semiconductors (e.g: GaAs or InSb)
have both cations and anions of similar size and electronegativity
Significantly cation-anion mis-
matched semiconductors (SCAMS)

## Slide 20
ViGS derive from entire bulk band structure → character changes from donor-like close to VB to acceptor-like close to CB
Energy at which they have equal probability of being donor- like or acceptor-like is the branch­ point energy or the charge neutrality level (CNL).
Any break of the periodicity → complex Bloch vectors are allowed in band gap (evanescent waves)
Localized virtual gap states (ViGS) result with wave vectors
kSS = p /a +iq
Electronic band structure derives from solutions of the Schrödinger equation – for a periodic medium, the solutions are Bloch states.
Virtual gap states and the CNL
W. Walukiewicz, Appl. Phys. Lett. 54 (1989) 2094

## Slide 21
J. Tersoff, Phys. Rev. B 32, 6968 (1985)
Charge neutrality level (CNL)
Charge neutrality level can thought of as a mid-gap energy level across the BZ.
InN band structure, showing CNL position in CB at the G – point and typical surface Fermi level (Epin) associated with the surface electron accumulation. Tersoff’s method to approximate the position of the CNL: ECNL = ½ [EV + EC ] where EV = Ev – 1/3 DSO and EC is the indirect band CBM.

## Slide 22
CdO
In2O3
ZnO
Large size and electronegativity mismatch → low Γ-point CBM
  CdO & ZnO DFT calcs: A. Schleife et al. Phys. Rev. B 73, 245212 (2006)
  In2O3 DFT calcs: F. Fuchs & F. Bechstedt, Phys. Rev. B 77, 155107 (2008)
Comparing TCO band structures
In all these cases the CBM lies below the CNL

## Slide 23
CNL expected to dictate charge state for native defects, hydrogen, and surface states
  P. D. C. King, T. D. Veal, C.F. McConville et al.
  Phys. Rev. B 79, 035203 (2009)
If the CNL lies above CBM in SCAMS → native defects, hydrogen and surface states should be donors even in n-type material
Hence CNL above the CBM leads to electron accumulation
Important implications for both the conductivity and the dopability of materials.
Implications of CNL in SCAMS

## Slide 24
CNL always lies above the CBM in SCAMS → electron accumulation
CNL position relative to band edges dominates the electronic properties
Unifying energy level for native defects, hydrogen and surface states
Character changes from donor-like close to VB to acceptor-like close to CB
Powerful predictive tool of conductivity and dopability for other materials
Experimental band line-ups

## Slide 25
Core levels give information on surface termination / contamination
Surface electronic structure from angle­ resolved photoemission (ARPES) measurements to determine E vs. k
X-ray photoelectron spectroscopy

## Slide 26
SR-Angle resolved photoemission spectroscopy (ARPES)

## Slide 27
bcc–In2O3(100) and (111) films grown on YSZ substrates by PAMBE at 650°C. The bcc-(111) and rh–(0001) films are grown on sapphire by MOCVD at 400–600°C
HRTEM and SAED confirm crystal structure, good epitaxial matching of epilayer with substrate and excellent crystalline order up to surface
A. Bourlange et al., Appl. Phys. Lett. 92, 092117 (2008)
Growth of high quality epitaxial In2O3

## Slide 28
In2O3(111) films exhibit unreconstructed (1×1) surfaces from LEED and STM
K. H. L. Zhang, D. J. Payne, R. G. Palgrave, V. K. Lazarov, W. Chen, A. T. S. Wee, C. F. McConville, P. D. C. King, T. D. Veal, G. Panaccione, P. Lacovig, and R. G. Egdell, Chem. Mater. 21, 4353 (2009)
E. H. Morales, Y. He, M. Vinnichenko, B. Delley and U. Diebold, New J. Phys. 10, 125030 (2008)
STM of an In2O3(111) surface

## Slide 29
V. Christou, R. G. Egdell, et al., J. Appl. Phys. 88, 5180 (2000)
Y. Gassenbauer, R. Schafranek, A. Klein, et al., Phys. Rev. B 73, 245312 (2006)
In2O3 surface space-charge
(pre-2008)
Before 2008:
VB-XPS located surface EF at ≈ 3 eV above VBM
With an assumed band-gap of 3.6 eV this implies upward band bending and hence:
Surface electron depletion

## Slide 30
F. Fuchs & F. Bechstedt, Phys. Rev. B 77, 155107 (2008) A. Walsh, et al., Phys. Rev. Lett. 100, 167402 (2008)
P. Erhart, et al., Phys. Rev. B 75, 153205 (2007)
R. L. Weiher and R. P. Ley, J. Appl. Phys. 37, 299 (1966)
However, theory consistently finds negligible evidence for the indirect nature of the band gap.
Onset of significant optical absorption only occurs above eV in bcc–In2O3
Weak absorption below this
Traditionally attributed to indirect band gap of eV, direct band gap of about eV
In2O3 band gap

## Slide 31
DFT calculations show band edge
transitions are parity forbidden →
minimal dipole transition matrix
elements around band gap energy
A. Walsh et al., Phys. Rev. Lett. 100, 167402 (2008)
F. Fuchs, F. Bechstedt, Phys. Rev. B 77, 155107 (2008)
Optical band gap > fundamental
band gap (by approx. 0.8 eV)
Is the theoretical valence band
structure found experimentally?
What is the fundamental band gap
of In2O3?
In2O3 band gap

## Slide 32
In2O3 band gap (optical)
P. D. C. King et al., Phys. Rev. B 79, 205211 (2009)
bcc Eopt (expt) = 3.55 ± 0.05 eV
Theoretical calculations show that the optical gap is 0.62 eV larger than the fundamental gap
Fundamental gap of bcc In2O3:
EG (expt) = 2.93 ± 0.15 eV
Same proceedure for rh - In2O3:
EG (expt) = 3.02 ± 0.15 eV
Fundamental band gaps similar for both bcc and rh polymorphs despite very different optical gaps
Consistent with theoretical calculations.

## Slide 33
P.D.C. King, T.D. Veal, C.F. McConville, et al. Phys. Rev. Lett. 101,116808 (2008) &
Phys. Rev. B 79, 205211 (2009)
Electron accumulation at In2O3 surfaces
VB-XPS gives VBM to Fermi level separation at surface of 3.4 eV
CB emission indicates Fermi level is pinned above CBM at the surface
Simulation of IR reflectivity spectra implies n = 7.4 x 1018 cm-3
Hall measurements give a value of n = 7.5 x 1018 cm-3
NP statistics indicate that Fermi level lies only 0.02 eV above the CBM in the bulk.
Hence the Surface EF > Bulk EF implying electron accumulation

## Slide 34
Growth & Structure of ZnO
ZnO has wurtzite crystal structure
Hydrothermal and melt-grown bulk samples and MBE and MOVPE samples have all been studied with very similar results
Dependence of surface electronic properties on crystal polarity investigated.
Band gap experimentally established as 3.37 eV at RT.
Hybrid functional DFT under-estimates the band gap at 2.8 eV.

## Slide 35
ZnO Valence Band DOS
DFT VB-DOS and VB-XPS agree for ZnO. DFT d-levels too low.
P. D. C. King, T. D. Veal, C.F. McConville, et al., Phys. Rev. B 79, 205205 (2009)

## Slide 36
VB of hydrothermal bulk ZnO
M.W. Allen & S.M. Durbin, Appl. Phys. Lett. 92, 122110 (2008)
M.W. Allen, T.D. Veal, C.F. McConville, S.M. Durbin et al. Phys. Rev. B 81, 075211 (2010)
Tokyo Dempa hydrothermally-grown
ZnO samples
Bulk doping level n = 3 x 1014 cm-3
(possibly due to Li impurity compensation)
Surface Fermi level (EFs) is at:
:- 3.69 eV for Zn-polarity
:- 3.60 eV for m-plane
:- 3.50 eV for O-polarity
Similar, only 0.2 eV difference in barrier height with sample face for optimized Schottky diodes.

## Slide 37
M.W. Allen, T.D. Veal, C.F. McConville, S.M. Durbin et al. Phys. Rev. B 81, 075211 (2010)
Poisson solution hydrothermal bulk ZnO
Charge profile for the m-plane Tokyo Dempa sample.
Surface EF = 3.60 eV
Electron accumulation and 0.46 eV downward band-bending observed.
:- Bulk cc. is n = 3 x 1014 cm-3
:- Surface sheet density is
n = 3.5 x 1012 cm-3
All surfaces exhibit electron accumulation: small differences due to differences in energy distribution of surface states and/or different charge transfer due to contaminants.

## Slide 38
Epitaxial growth and structure of CdO(001)
CdO films grown on r-plane sapphire by MOCVD at 380OC
XRD confirms crystal structure and high quality – (004) FWHM of 0.14O
(001)CdO ⁄⁄ (0112)Sapphire

## Slide 39
Epitaxial growth and structure of CdO
CdO films grown on r-plane sapphire by MOCVD at 380OC
XRD confirms crystal structure and high quality – (004) FWHM of 0.14O
(001)CdO ⁄⁄ (0112)Sapphire
LEED shows sharp (1x1) clean surface after 600OC anneal

## Slide 40
Calculated CdO band structure
VBM is away from Γ due to p-d repulsion (Cd 4d – O 2p) being symmetry forbidden
for the rock-salt structure.

## Slide 41
DFT VB-DOS and VB-XPS agree for CdO. DFT d-levels too low.
P. D. C. King, T. D. Veal, C.F. McConville et al. , Phys. Rev. B. 79, 205205 (2009)
CdO valence band DOS

## Slide 42
P.D.C. King, T.D. Veal, C.F. McConville, et al. Phys. Rev. B 79, 035203 (2009)
Do we have electron accumulation at the surface of CdO?
CNL marks the cross-over point for surface states to be donor-like (below) to acceptor-like (above) this energy
EF pinned below CNL at surface
Unoccupied donor ViGS
Positive surface charge
Bands bend downwards at surface
Space charge balances the surface charge
Surface EF > Bulk EF
Electron accumulation results
Consistent with CNL positions from defects and hydrogen

## Slide 43
P.D.C. King, T.D. Veal, C.F. McConville, et al., Phys. Rev. Lett. 104, 256803 (2010)
Quantized 2D electron gas at the surface of CdO

## Slide 44
VB bending comes directly from the XPS measurements.
Assuming same band bending for the CB gives only a single subband – well above lower of the 2 observed in ARPES
Stronger band bending of CB than the VB indicates a deeper potential well at the surface
P.D.C. King, T.D. Veal, C.F. McConville et al.
Phys. Rev. Lett. 104, 256803 (2010)
Band-gap is smaller at the surface
than in the bulk –
Band-gap renormalization (BGR)
Quantized 2D electron gas at the surface of CdO
EF

## Slide 45
P. D. C. King, T. D. Veal, C. F. McConville et al., Phys. Rev. B. 79, 035203 (2009)
Effect of varying the Poisson potential
Solve Poisson’s equation to find the potential – modified Thomas Fermi approx.
Solve the Schrödinger equation in this potential to find the subbands location and dispersion (including CB non-parabolicity).

## Slide 46
Sub-band photon energy dependence in CdO

## Slide 47
IO5 ARPES end-station -
Diamond Light Source

## Slide 48
ARPES –MBE grown CdO(001)
preliminary analysis
Clearly visible kink in the inner & outer band
Blue line is just a polynomial fit.
Visible on both sides in the spectra
Possible e-e and e-ph interactions
- around 50 meV below the Fermi level (EF)
Inner Band
Outer Band

## Slide 49
ARPES –MBE grown CdO(001)
Kinks - preliminary analysis

## Slide 50
Initial Fitting of sub-bands and kinks

## Slide 51
Surface band-gap tuning
Rb on CdO
Rb low coverage estimated at 0.4 ML after 4 sec. exposure gives a
237 meV downward shift in the higher binding energy state

## Slide 52
Rb is added  surface state density increases and surface band gap shrinks
Band-gap shrinks linearly with surface electron density
(a) 4.05 x 1013 cm-3 (b) 5.31 x 1013 cm-3 (c) 6.36 x 1013 cm-3 (d) 7.21 x 1013 cm-3
Surface band-gap tuning
Rb on CdO

## Slide 53
Surface 2D electron liquid at an
SrTiO3 Surface
W. Meevasana, P.D.C. King, et al. Nature Materials, 10, 114 (2011)
Creation and control of a 2D electron liquid at an STO surface by exposure to intense UV light

## Slide 54
Co-existence of a topological state and 2D electron gas in Bi2Se3
P.D.C. King, P. Hofmann & co-workers, Nature Communications. 10, 1038 (2010)

## Slide 55
Co-existence of a topological state and a 2D electron gas
kz-dependence of the electronic structure Bi2Se3
ARPES measurements taken at 181 photon energies between 14 and 32 eV.
P.D.C. King, P. Hofmann & co-workers
Nature Communications 10, 1038 (2010)

## Slide 56
Accumulation in a Ferromagnetic Oxide: EuO
Electronic structure of Ferromagnetic EuO
P.D.C. King & co-workers, Nature Communications (2018)

## Slide 57
Accumulation in a Ferromagnetic Oxide: EuO
Fermi surface contours of EuO:Gd with increased charge carrier doping
P.D.C. King & co-workers, Nature Communications (2018)

## Slide 58
Some of the most fundamental properties of III-V and metal oxide semiconductors – including InN, CdO and In2O3 ­ are being (re)discovered due to the availability of higher quality, epitaxial materials.
Low Γ-point CBM is responsible for defects, impurities, hydrogen and surface states all acting as donors → electron accumulation
Electrons trapped by the surface potential and the conduction band edge result in a series of quantized sub-­band states.
Direct observation of many body interaction effects, both e-e and e-phonon coupling via kinks in ARPES spectra.
Quantized energy states and the band-gap at the surface, can be tuned by modifying the surface electron density (e.g. with the addition of an alkali-metal).
New materials including SrTiO3, EuO, MoS2 and Bi2Se3 all showing surface electron accumulation
Enormous potential for new epitaxial oxides in transparent electronics.
Thanks to EPSRC, ERDF & Science City Research Alliance (SCRA) for many levels of funding and support.
Summary & Conclusions

## Slide 59
T.D. Veal, P.D.C. King, J.J. Mudd, P. H. Jefferson, S. Vasheghani Farahani,
L.F.J. Piper, K. Krupski, A. Krupski & M. Walker
Department of Physics, University of Warwick, UK
M. Hoesch, P. Dudin, Timur Kim & Tien Lin Lee
Diamond Light Source, Harwell Science and Innovation Campus, Oxfordshire, UK
M. Fuglsang-Jensen, M. Bianchi, E. D. L. Rienks, & Ph. Hofmann
Institute for Storage Ring Facilities, University of Århus, Denmark
A. Schleife, F. Fuchs, J. Furthmüller, & F. Bechstedt
Institut für Festkörpertheorie und Theoretische Optik, Friedrich-Schiller-Universität, Germany
J. Zúñiga-Pérez & V. Muñoz-Sanjosé
Departamento de Fisica Aplicada y Electromagnetismo, Universitat de Valéncia, Spain
K. H. L. Zhang, A. Bourlange, D. J. Payne, & R. G. Egdell
Chemistry Research Laboratory, University of Oxford, UK
Colleagues & Collaborators

## Slide 60
McConville
(RMIT)
Egdell
(Oxford)
Mudd
(Warwick)
King
(St. Andrews)
Veal
(Liverpool)
Zuniga-Perez
(CNRS)
Munoz-Sanjose
(Valencia)
Schleife
(UCSB)
Hofmann
(Aarhus)
Bechstedt
(Jena)
Hoesch
(Diamond)
Team TCO
P. H. Jefferson
S. Farahani
L.F.J. Piper
M. Walker
D. J. Payne
A. Bourlange
K. H. L. Zhang
M. P. Dudin
Timur Kim
Tien-Lin Lee
M. Fuglsang
M. Bianchi
E. D. L. Rienks

## Slide 61
Warwick Castle
(1068 – present)
Thank you for your attention
c.f.mcconville@warwick.ac.uk

## Slide 62
Thank you for your attention
chris.mcconville@rmit.edu.au

## Slide 63
CFM - EPSRC Grant
Mind-Map

## Slide 64
Origin of the electron accumulation on InN
I. Mahboob, T. D. Veal, L. F. J. Piper, C. F.McConville, H. Lu, W. J. Schaff,
F. Bechstedt, and J. Furthmüller, Phys. Rev. B 69, 201307(R) (2004)
EB – Branch point or “mid-gap” energy
Corresponds to the cross-over point from acceptor-like to donor-like surface states.
InN exhibits an unusually low Г-point CBM, so that EB lies high within the conduction band (i.e. 1.4 eV above the VBM).
To ensure charge neutrality, EF tends to EB, resulting in downward band bending.
Equilibrium is achieved when the charge from the band bending cancels the charge from the surface donor-like states.
A similar situation occurs for InAs - BUT EB is much higher above the CBM for InN
~1.4 eV

## Slide 65: Breakdown of common-cation rule
(ii) size contribution:
All III-Vs have negative volume deformation potentials – the volume increases, the band gap decreases. This effect tends to dominate, hence the observed band gap variation.
However, highly ionic III-V’s & II-VI’s have very small volume deformation potentials, allowing the chemical contribution to dominate.
Extreme case, large size & electronegativity mismatch - InN, ZnO & CdO, all have narrow band gaps (for the cation) and low CBM at the Г- points.
Both ZnO and InN exhibit
surface electron accumulation
Semiconductor band-gaps are determined by:
i.e. Highly mis-matched alloys (HMA’s)
chemical contribution: A fixed volume common-cation system makes the band gap decrease going from MSb to MAs and MP to MN (M = Al, Ga, In).

## Slide 66
Intrinsic electron accumulation at
clean InN(0001)-(1×1) surfaces

## Slide 67: InN : at the extreme of band-edge trends
In general, as the cation varies from Al→ Ga→ In, the Γ -point CBM shifts downwards, but as atomic size decreases as the anion varies Sb→ As→ P→ N, the Γ-point VBM shifts downwards with respect to EB
Both InAs and InN are materials which accumulate electrons at the free surface (shaded). This is due to the Γ-point CBM lying below EB
InN represents the extreme III-V
as it lies at the end-points of both
the cation and the anion trends.
L.F.J. Piper, Ph.D. thesis
University of Warwick (2006)

## Slide 68
Doping trends of III-Vs
Proximity of band edges with respect to EB (or ultimate stabilised Fermi level), determines the doping limits.
W. Walukiewicz Physica B 302-3 (2001) 123.
Easier for p-type doping
Easier to p-type dope if the valence band edge lies close to EB
Easier to n-type dope if the conduction band edge lies close to EB
Easier for n-type doping
Both GaN and InN are much easier to n-type dope than p-type, but based on this, p-type doping will be much harder for InN.
For InN, EB lies ~0.9 eV above the Γ-point CBM, hence EF << EB. Hence it is highly energetically favourable for defects introduced during growth to be predominantly donor-like.
(EF ~ EB at n ~ 4 x1020 cm-3)
.

## Slide 69
HAXPES has much increased probing depth compared to conventional XPS
  20 nm at 6054 eV vs. 5 nm at 1486 eV (or around 4x larger)
This increases the probing depth & reduces the surface sensitivity
This in turn reduces the need to surface preparation
  Useful in the case of CdO as annealing to produce high quality surfaces significantly reduces the bulk carrier concentration
  Possibly due to the removing hydrogen - incorporated during CVD growth and (as expected) acting as donors.
  Surfaces are O-depleted as a result of the annealing process
Why use HAXPES to study CdO surfaces?
The IO9 beam line @ Diamond Light Source
provides both soft (100 - 2100 eV) & (2.1 - 20 keV) hard X-rays

## Slide 70
Photoionization Cross Sections
M. B Trzhaskovskaya et al., Atomic & Nuclear Data Tables, 77, 97 (2001) and 92, 245 (2006)
All the cross sections fall with increasing photon energy - but at different rates
Note significantly faster drop off of the O 2p photoionization cross-section

## Slide 71
CdO cleaned by UHV Annealing
Hydroxide, carbonate
-OH, CdCO3
Atmospheric Contamination
CdO
CdO peaks have been aligned to account for changes in bulk carrier concentration and band bending caused by annealing.
(Taken with a Laboratory Al Ka XPS source hv = 1485 eV)

## Slide 72
HAXPES vs. SXPES
Contamination components are very much reduced in HAXPES
More dramatic in O1s peak as hv = 600 eV gives a KE of ~70 eV, which coincides with the minimum escape depth of the Universal curve. Hence probing depth changes by > 10 x on moving from SXPES to HAXPES
The peak shift of approx. 0.4 eV is assigned to the band bending present at the surface.
HAXPES
SXPES
J. J. Mudd, C.F. McConville, et al., PRB, 89, 035203 (2014)

## Slide 73
HAXPES Valence Band
Shift observed assigned to bulk CB filling
Supported by increased intensity close to the Fermi level for the higher carrier concentration.
VB shift of ~0.3eV is measured by extrapolation of the VB leading edge.
J. J. Mudd, C.F. McConville, et al., PRB, 89, 035203 (2014)

## Slide 74
CB filling and band gap re-normalization (BGR)
Experimentally a VBM shift of 0.3 eV is measured
Using Hall effect measurements and carrier statistics a shift of 0.43 eV is predicted, in excess of the measured value.
However, if the band gap renormalisation (BGR) – a band-gap shrinkage of 0.07 and 0.20 eV is predicted for the low and high concentrations respectively - is also considered, then a shift of 0.3 eV is predicted - in excellent agreement with expt data.
J. J. Mudd, C.F. McConville, et al., PRB, 89, 035203 (2014)

## Slide 75
Cd 3d5/2 & O1s Core Level Fits
HAXPES allows the core levels of the as-grown sample to be analysed while still accounting for contamination.
The higher carrier concentration exhibits stronger asymmetry on the higher BE side of the peaks.
A two peak model is used to fit all the core levels ……..
J. J. Mudd, C.F. McConville, et al., PRB, 89, 035203 (2014)

## Slide 76
Cd 3d5/2 & O1s Core Level Fits
J. J. Mudd, C.F. McConville, et al., PRB, 89, 035203 (2014)
There are at least two possible explanations:
The effects of the conduction band plasmons or the effect of final state screening on the core-level line shapes.
The plasmon energy extracted from the peak fits converted to carrier concentration is in excellent agreement with the Hall data – supporting the idea the broadening is due to plasmon satellites.

## Slide 77
Cd 3d5/2 & O1s Core Level Fits
But ……………. for the annealed samples the plasmon energy indicated a higher carrier concentration than observed from Hall effect data – suggesting that surface electron accumulation is playing a significant role in the final state screening effects.
May need some more theory ….!!!
J. J. Mudd, C.F. McConville, et al., PRB, 89, 035203 (2014)

## Slide 78
UHV-PLD, STM-AFM & XPS

## Slide 79
LEED pattern after UHV anneal 30 minutes @ 600oC.
Sharp 1x1 pattern observed with low intensity background
Would tend to indicate a clean, and well ordered surface structure.
CdO cleaned by UHV Annealing

## Slide 80
Sub-band photon energy dependence in CdO
Both the visible 2D quantum well states vary in intensity, but persist up to photon energies around 120 eV.

## Slide 81
Differing from our previous ARPES work on CdO(001), now 3 bands can clearly be resolved.
The improved resolution, MBE grown samples, lower sample temperature (5K) and increased flux of IO5 all add to the improved data quality.
States vary in intensity but persist from hν = 17-120 eV
Fermi surface from ARPES: MBE grown CdO(001)

## Slide 82
Thank you for your attention
c.f.mcconville@warwick.ac.uk

## Slide 83
Sub-band photon energy dependence in CdO

## Slide 84
Surface band-gap tuning
Rb on CdO
Rb low coverage estimated at 0.4 ML after 4 sec. exposure gives a
237 meV downward shift in the higher binding energy state
J.J. Mudd et. al. (in preparation for submission in 2015)

## Slide 85
Coaxial impact collision ion
scattering spectroscopy (CAICISS)
Conceived by M. Aono et al. RIKEN, Tokyo, Japan

## Slide 86
Surface Structure of CdO by CAICISS
[100]
[110]
CdO cleaned in vacuum @
Sharp (1x1) LEED pattern
No contamination from XPS
CAICISS data shows good agreement with the bulk rock-salt structure including small relaxations
Surface peak at ~80o is not well modelled

## Slide 87
Surface structure of CdO by CAICISS
Peak at 80o ’s can be fitted by modelling surface oxygen deficiencies
Optimised Fit
(bulk & outer relaxations)
1st layer O completely removed
All O removed (14 layers!)

## Slide 88
DFT band structure & VB PDOS
LDA and PBE conventional functional predict semi-metallic behaviour, LDA+U predicts semiconducting but with a underestimated band gap.
J.J. Mudd, et al., PRB, 89, 165305. (2014)

## Slide 89
CdO
In2O3
ZnO
Large size and electronegativity mismatch → low Γ-point CBM
  CdO & ZnO DFT calcs: A. Schleife et al. Phys. Rev. B 73, 245212 (2006)
  In2O3 DFT calcs: F. Fuchs & F. Bechstedt, Phys. Rev. B 77, 155107 (2008)
Comparing TCO band structures

## Slide 90
ViGS derive from bulk band structure → character changes from donor-like close to VB to acceptor-like close to CB
Energy at which they have equal donor- and acceptor-like character is the branch­ point energy of the ViGS or the charge neutrality level.
Any break of the periodicity → complex Bloch vectors are allowed in band gap (evanescent waves)
Localized virtual gap states (ViGS) result with wave vectors
kSS = p /a +iq
Electronic band structure derives from solutions of the Schrödinger equation – for a periodic medium, the solutions are Bloch states.
Virtual gap states & the CNL

## Slide 91: Plasmon Energy
Plasmon energy and the carrier concentration are related by the expression
Therefore can convert measured plasmon energy (peak separation) into a carrier concentration.
Sample | Plasmon energy | from Plasmon energy | from Hall measurement
As grown | 460 meV | 2.5 x 1020 cm-3 | 2.4 x 1020 cm-3
Annealed | 245 meV | 5.9 x 1019 cm-3 | 1.8 x 1019 cm-3
Very good agreement for as-grown sample HAXPES sensitivity is “bulk like” little surface effect.
Annealed sample shows higher carrier concentration than Hall indicating electron accumulation is present enhancing the carrier concentration.
J. J Mudd et al., PRB, 89, 035203 (2014)

## Slide 92: VB Photon Energy Dependence
J. J Mudd, et al., PRB, 89, 165305. (2014)
Normalised at peak II.
Peak I shows strong relative increase with increased photon energy – arrow 1
The region in the centre of the VB shows a relative increase with photon energy – arrow 2

## Slide 93: DFT LDA+U Weighted PDOS
At 600 eV photon energy Cd and O have similar contributions
At 7935 eV photon energy Cd contributions dominate the VB shape.
Cd 5s becomes dominant in peak I at the highest energy
Cd 5p also becomes significant in the centre of the VB

## Slide 94
Position of the CNL expected to dictate charge state for native defects, hydrogen, and any surface states
  P. D. C. King, T. D. Veal, C.F. McConville et al.
  Phys. Rev. B 79, 035203 (2009)
CNL above CBM in SCAMS → native defects, H, and surface states should be donors even in n-type material
The CNL above the CBM leads to electron accumulation
Important implications for both conductivity and dopability
Implications of CNL in TCO’s

## Slide 95
VB bending comes directly from the XPS measurements.
Assuming same band bending for the CB gives only a single subband – well above lower of the 2 observed in ARPES
Stronger band bending of CB than the VB indicates a deeper potential well at the surface
P.D.C. King, T.D. Veal, C.F. McConville et al.
Phys. Rev. Lett. 104, 256803 (2010)
Band-gap is smaller at the surface
than in the bulk –
Band-gap renormalization (BGR)
Quantized 2D electron gas at the surface of CdO

## Slide 96
C. G. Van de Walle, Phys. Rev. Lett. 85, 1012 (2000);
S. Lany and A. Zunger, Phys. Rev. Lett. 98, 045501 (2007)
Interest in materials which both conduct electricity and are optically transparent (e.g. In2O3, SnO2, CdO)
Widespread use as transparent electrodes, e.g., in solar cells, LCD displays, LEDs
G. Thomas, Nature 389, 907 (1997)
But maybe graphene is the ultimate transparent conducting electrode?
Increased interest in oxides for active layer in devices e.g., transparent transistors, short wavelength photonic devices, chemical sensors, UV/visible LEDs
K. Nomura etal., Science 300, 1269 (2003)
Tsukazaki etal., Nature Materials 4, 42 (2005)
A. Tsukazaki etal., Science 315, 1388 (2007)
D. Zhang etal., Nano. Lett. 4, 1919 (2004).
Many fundamental properties of these materials simply not known
Origins of conductivity in TCO’s hotly debated, particularly in high-quality, epitaxial materials
Oxide Semiconductors

## Slide 97: I09
The bulk sensitivity of HAXPES allows for better comparison to bulk calculations.
The wide photon energy range accessible at I09 allows the change in photoionization cross sections to be exploited.

## Slide 98
Full spectrum solar cell
Efficient solar cells use multiple semiconductors with fixed energy gaps (e.g. GaInP / GaAs / Ge triple junction cell) to capture as much of the solar spectrum as possible.
The direct energy gap of In1-xGaxN spans nearly the energy range 0.7 eV – 3.4 eV of the solar spectrum, not 2.0 eV – 3.4 eV as reported in the literature (dotted line).
Multi-junction solar cells based on In1-xGaxN could have efficiencies as high as 50%.
J. Wu et al. J. Appl. Phys. 94 (2003) 6477.
Ge
GaAs
GaInP
m
Ga content in
In1-x Gax N alloy
Literature
LBNL, 2002
Perfect matching of band gap of In1-xGaxN to solar spectrum
Energy (eV)
Energy (eV)
Solar Flux
(1021 photons/sec/m2/mm)

## Slide 99
CdO
In2O3
ZnO
Large size and electronegativity mismatch → low Γ-point CBM
  CdO & ZnO DFT calcs: A. Schleife et al. Phys. Rev. B 73, 245212 (2006)
  In2O3 DFT calcs: F. Fuchs & F. Bechstedt, Phys. Rev. B 77, 155107 (2008)
CBM lies below the ‘CNL’ and gives electron accumulation.
Comparison of band structures

## Slide 100
CNL always lies above CBM in SCAMS
Dominates electronic properties (i.e. position relative to band edges)
Unifying energy level for native defects, hydrogen and surface states
Powerful predictive tool for other materials
Experimental Band line-ups

## Slide 101
Fundamental properties of metal oxide semiconductors ­ In2O3 CdO ­ are being (re)­discovered in the light of higher quality epitaxial materials.
Low Γ-point CBM in all HMC’s is responsible for defects, impurities, hydrogen and surface states all acting as donors.
Surface electron accumulation is a common property of In2O3 and CdO - and other HMC's such as ZnO, InAs & InN.
Electrons trapped by surface potential results in quantized sub­band states.
Quantized energy states can be tuned by modifying the surface (e.g. with alkali-metals).
Enormous potential for epitaxial oxides in transparent electronics.
Development of p-type doping of oxides or inherently p-type oxides (Cu2O, NiO, SrCuO2 etc.) is now required for devices.
Thanks to EPSRC, ERDF & AWM Science City for funding
Summary & Conclusions

## Slide 102
C. G. Van de Walle, Phys. Rev. Lett. 85, 1012 (2000);
S. Lany and A. Zunger, Phys. Rev. Lett. 98, 045501 (2007)
Interest in materials which both conduct electricity and are optically transparent (e.g. In2O3, SnO2, CdO)
Widespread use as transparent electrodes, e.g., in solar cells, LCD displays, LEDs
G. Thomas, Nature 389, 907 (1997)
But maybe graphene is the ultimate transparent conducting electrode?
Increased interest in oxides for active layer in devices e.g., transparent transistors, short wavelength photonic devices, chemical sensors, UV/visible LEDs
K. Nomura etal., Science 300, 1269 (2003)
Tsukazaki etal., Nature Materials 4, 42 (2005)
A. Tsukazaki etal., Science 315, 1388 (2007)
D. Zhang etal., Nano. Lett. 4, 1919 (2004).
Many fundamental properties of these materials simply not known
Origins of conductivity are hotly debated
Oxide Semiconductors

## Slide 103
Significantly Cation-Anion Mismatched Semiconductors

## Slide 104
Band gap energies & lattice constants

## Slide 105
Conventional compound semiconductors (e.g.: GaAs or InSb) have both cations and anions of similar size and electronegativity
Significantly Cation-Anion
Mismatched Semiconductors

## Slide 106
n-type
p-type
Surface space-charge layers

## Slide 107
J. Tersoff, Phys. Rev. B 32, 6968 (1985)
Charge Neutrality Level (CNL)
Charge neutrality level can thought of as a mid-gap energy level across the BZ.
band structure, showing CNL position in CB at G and typical surface Fermi level (Epin) associated with InN’s surface electron accumulation. Tersoff’s method for approximating the position of the CNL: ECNL = ½ [EV + EC ] where
EV = Ev – 1/3 DSO and EC is the indirect band CBM.

## Slide 108
Core levels give information on surface termination / contamination
Surface electronic structure from angle­ resolved photoemission (ARPES) measurements to determine E vs. k
X-ray Photoelectron Spectroscopy

## Slide 109
Angle Resolved Photoemission Spectroscopy (ARPES)

## Slide 110
Epitaxial growth and structure of CdO
CdO films grown on r-plane sapphire by MOCVD at 380OC
XRD confirms crystal structure and high quality – (004) FWHM of 0.14O
(001)CdO ⁄⁄ (0112)Sapphire

## Slide 111
Epitaxial growth and structure of CdO
CdO films grown on r-plane sapphire by MOCVD at 380OC
XRD confirms crystal structure and high quality – (004) FWHM of 0.14O
(001)CdO ⁄⁄ (0112)Sapphire
LEED shows sharp (1x1) clean surface after 600OC anneal

## Slide 112
CdO band structure
VBM is away from Γ due to p-d repulsion (Cd 4d – O 2p) being symmetry forbidden
for the rock-salt structure.

## Slide 113
DFT VB-DOS and VB-XPS agree for CdO. DFT d-levels too low.
P. D. C. King, T. D. Veal, C.F. McConville et al. , Phys. Rev. B. 79, 205205 (2009)
CdO valence band DOS

## Slide 114
P. D. C. King, T. D. Veal, C.F. McConville, et al. Phys. Rev. B 79, 035203 (2009)
Electron Accumulation in CdO
CNL marks the cross-over point for surface states to be donor-like (below) to acceptor-like (above) this energy
EF pinned below CNL at surface
Unoccupied donor ViGS
Positive surface charge
Bands bend downwards at surface
Space charge balances surface charge
Surface EF > Bulk EF
Electron accumulation results
Consistent with CNL positions from defects and hydrogen

## Slide 115
P.D.C. King, T.D. Veal, C.F. McConville et al., Phys. Rev. Lett. 104, 256803 (2010)
Quantized 2D Electron Gas in CdO

## Slide 116
VB bending comes directly from the XPS measurements.
Assuming same band bending for the CB gives only a single subband – well above lower of the 2 observed in ARPES
Stronger band bending of CB than VB indicates a deeper potential well at the surface
P. D. C. King, T. D. Veal, C. F. McConville et al., Phys. Rev. Lett. 104, 256803 (2010)
Band-gap is smaller at the surface than in the bulk
Quantized 2D Electron Gas in CdO

## Slide 117
P. D. C. King, T. D. Veal, C. F. McConville et al., Phys. Rev. B. 79, 035203 (2009)
Effect of varying the Poisson potential
Solve Poisson’s equation to find the potential – modified Thomas Fermi approx.
Solve the Schrödinger equation in this potential to find the subbands location and dispersion (including CB non-parabolicity).

## Slide 118
Surface band-gap tuning
Rb on CdO
Rb low coverage estimated at 0.4 ML after 4 sec. exposure gives a
237 meV downward shift in the higher binding energy state

## Slide 119
Surface band-gap tuning
Rb on CdO
Rb is added  surface state density increases and surface band gap shrinks
Band-gap shrinks linearly with surface electron density
(a) 4.05 x 1013 cm-3 (b) 5.31 x 1013 cm-3 (c) 6.36 x 1013 cm-3 (d) 7.21 x 1013 cm-3

## Slide 120
Sub-band photon energy dependence in CdO

## Slide 121
Growth & Structure of ZnO
ZnO has wurtzite crystal structure
Hydrothermal and melt-grown bulk samples and MBE and MOVPE samples have all been studied with very similar results
Dependence of surface electronic properties on crystal polarity investigated.
Band gap experimentally established as 3.37 eV at RT.
Hybrid functional DFT under-estimates the band gap at 2.8 eV.

## Slide 122
ZnO Valence Band DOS
DFT VB-DOS and VB-XPS agree for ZnO. DFT d-levels too low.
P. D. C. King, T. D. Veal et al., Phys. Rev. B 79, 205205 (2009)

## Slide 123
VB of hydrothermal bulk ZnO
M.W. Allen & S.M. Durbin, Appl. Phys. Lett. 92, 122110 (2008)
M.W. Allen, T.D. Veal, C.F. McConville, S.M. Durbin et al. Phys. Rev. B 81, 075211 (2010)
Tokyo Dempa hydrothermally-grown
ZnO samples
Bulk doping level n = 3 x 1014 cm-3
(possibly due to Li impurity compensation)
Surface Fermi level (EFs) is at:
:- 3.69 eV for Zn-polarity
:- 3.60 eV for m-plane
:- 3.50 eV for O-polarity
Similar, only 0.2 eV difference in barrier height with sample face for optimized Schottky diodes.

## Slide 124
M.W. Allen, T.D. Veal, C.F. McConville, S.M. Durbin et al. Phys. Rev. B 81, 075211 (2010)
Poisson solution hydrothermal bulk ZnO
Charge profile for the m-plane Tokyo Dempa sample.
Surface EF = 3.60 eV
Electron accumulation and 0.46 eV downward band-bending observed.
:- Bulk cc. is n = 3 x 1014 cm-3
:- Surface sheet density is
n = 3.5 x 1012 cm-3
All surface s exhibit electron accumulation: small differences due to differences in energy distribution of surface states and/or different charge transfer due to contaminants.

## Slide 125
CdO
In2O3
ZnO
Large size and electronegativity mismatch → low Γ-point CBM
  CdO & ZnO DFT calcs: A. Schleife et al. Phys. Rev. B 73, 245212 (2006)
  In2O3 DFT calcs: F. Fuchs & F. Bechstedt, Phys. Rev. B 77, 155107 (2008)
CBM lies below the ‘CNL’ and gives electron accumulation.
Comparison of band structures

## Slide 126
CNL always lies above CBM in SCAMS
Dominates electronic properties (i.e. position relative to band edges)
Unifying energy level for native defects, hydrogen and surface states
Powerful predictive tool for other materials
Experimental Band line-ups

## Slide 127
Fundamental properties of metal oxide semiconductors ­ In2O3 CdO ­ are being (re)­discovered in the light of higher quality epitaxial materials.
Low Γ-point CBM in all HMC’s is responsible for defects, impurities, hydrogen and surface states all acting as donors.
Surface electron accumulation is a common property of In2O3 and CdO - and other HMC's such as ZnO, InAs & InN.
Electrons trapped by surface potential results in quantized sub­band states.
Quantized energy states can be tuned by modifying the surface (e.g. with alkali-metals).
Enormous potential for epitaxial oxides in transparent electronics.
Development of p-type doping of oxides or inherently p-type oxides (Cu2O, NiO, SrCuO2 etc.) is now required for devices.
Thanks to EPSRC, ERDF & AWM Science City for funding
Summary & Conclusions

## Slide 128
P.D.C. King, J.J. Mudd, T.D. Veal, P. H. Jefferson,
S. Vasheghani Farahani, M. Walker & W. M. Linhart
Department of Physics, University of Warwick, UK
A. Bourlange, D. J. Payne, K. H. L. Zhang, & R. G. Egdell
Chemistry Research Laboratory, University of Oxford, UK
M. Fuglsang-Jensen, M. Bianchi, E. D. L. Rienks, & Ph. Hofmann
Institute for Storage Ring Facilities, University of Århus, Denmark
A. Schleife, F. Fuchs, J. Furthmüller, & F. Bechstedt
Institut für Festkörpertheorie und Theoretische Optik, Friedrich-Schiller-Universität, Germany
J. Zúñiga-Pérez & V. Muñoz-Sanjosé
Departamento de Fisica Aplicada y Electromagnetismo, Universitat de Valéncia, Spain
Colleagues & Collaborators

## Slide 129
McConville
Egdell
Mudd
King
Veal
Zuniga-Perez
Munoz-Sanjose
Schleife
Hofmann
Bechstedt
Fuchs
World Cup
2014

## Slide 130
McConville
Egdell
Mudd
King
Veal
Zuniga-Perez
Munoz-Sanjose
Schleife
Hofmann
Bechstedt
Fuchs
EURO 2016 ??

## Slide 131
Coaxial impact collision ion
scattering spectroscopy (CAICISS)
Conceived by M. Aono et al. RIKEN, Tokyo, Japan

## Slide 132
Surface Structure of CdO by CAICISS
[100]
[110]
CdO cleaned in vacuum @
Sharp (1x1) LEED pattern
No contamination from XPS
CAICISS data shows good agreement with the bulk rock-salt structure including small relaxations
Surface peak at ~80o is not well modelled

## Slide 133
Surface structure of CdO by CAICISS
Peak at 80o ’s can be fitted by modelling surface oxygen deficiencies
Optimised Fit
(bulk & outer relaxations)
1st layer O completely removed
All O removed (14 layers!)

## Slide 134
UHV-PLD, STM-AFM & XPS

## Slide 135
Electronic Properties of
Transparent Conducting Oxide Semiconductors
C.F. McConville
Deputy Pro-Vice Chancellor for Research & Innovation
RMIT University, Melbourne, Australia
formerly
Director, Science City Research Alliance (SCRA) & Professor of Experimental Physics
Department of Physics, University of Warwick, UK.
Second International Conference on Applied Surface Science (ICASS-2)
Dalian, China
12th – 15th June 2017

## Slide 136
X-ray Photoelectron Spectroscopy
Core levels give information on surface termination / contamination
Surface electronic structure from angle­ resolved photoemission (ARPES) measurements to determine E vs. k

## Slide 137
Transparent conducting oxides (TCO’s)
Semiconducting
TCO’s
CdO
ZnO
Ga2O3
In2O3
SnO2

## Slide 138
Growth & Structure of ZnO
ZnO has wurtzite crystal structure
Hydrothermal and melt-grown bulk samples and MBE and MOVPE samples have all been studied with very similar results
Dependence of surface electronic properties on crystal polarity investigated.
Band gap experimentally established as 3.37 eV at RT.
Hybrid functional DFT under-estimates the band gap at 2.8 eV.

## Slide 139
ZnO Valence Band DOS
DFT VB-DOS and VB-XPS agree for ZnO. DFT d-levels too low.
P. D. C. King, T. D. Veal, C.F. McConville, et al., Phys. Rev. B 79, 205205 (2009)

## Slide 140
VB of hydrothermal bulk ZnO
M.W. Allen & S.M. Durbin, Appl. Phys. Lett. 92, 122110 (2008)
M.W. Allen, T.D. Veal, C.F. McConville, S.M. Durbin et al. Phys. Rev. B 81, 075211 (2010)
Tokyo Dempa hydrothermally-grown
ZnO samples
Bulk doping level n = 3 x 1014 cm-3
(possibly due to Li impurity compensation)
Surface Fermi level (EFs) is at:
:- 3.69 eV for Zn-polarity
:- 3.60 eV for m-plane
:- 3.50 eV for O-polarity
Similar, only 0.2 eV difference in barrier height with sample face for optimized Schottky diodes.

## Slide 141
M.W. Allen, T.D. Veal, C.F. McConville, S.M. Durbin et al. Phys. Rev. B 81, 075211 (2010)
Poisson solution hydrothermal bulk ZnO
Charge profile for the m-plane Tokyo Dempa sample.
Surface EF = 3.60 eV
Electron accumulation and 0.46 eV downward band-bending observed.
:- Bulk cc. is n = 3 x 1014 cm-3
:- Surface sheet density is
n = 3.5 x 1012 cm-3
All surfaces exhibit electron accumulation: small differences due to differences in energy distribution of surface states and/or different charge transfer due to contaminants.