## Slide 1: Neutron studies of iron-based superconductors
Jie-Yu (Shirley) Yang
Advisor: Prof. Maw. Kuen. Wu, and Prof. Chih-Hao Lee
Taiwan-National Tsing Hua University/Academia Sinica
Aug. 13, 2018
The 9th Vacuum and Surface Science Conference
of
Asia and Australia

## Slide 2: Outline
Motivation
Structural and magnetic model
Experimental
  Sample synthesis
  Magnetic susceptibility
  Neutron measurements
Analysis and results
Summary

## Slide 3: Motivation
EPL, 111 (2015) 27004
FIG. 1.(a) XRD (b) magnetic susceptibility for K2-xFe4+ySe5 polycrystalline.
FIG. 2. Magnetic susceptibility measurement for K1.9Fe4A0.5Se5, A=Cu/Mn.
To study the correlation between magnetic structure and superconductivity.
To identify whether the magnetic transitions observed at 125 K in the stoichiometric K2-xFe4+ySe5, related to Verwey transition (as that observed in Fe3O4).
J. Phys.: Condens. Matter 20 (2008) 142201
Fe3O4
125 K

## Slide 4
CHIN. PHYS. LETT. Vol. 28, No. 8 (2011) 086104
Fig. 1. Magnetic susceptibility and resistivity for bulk K0.8Fe1.6Se2.
Fig. 2. Neutron powder diffraction patterns of the K0.83(2)Fe1.64(1)Se2 superconductor.
Fig. 3. Crystal and magnetic structure of K0.8Fe1.6Se2 in the low-temperature I 4/m unit cell.
Structure model-experiment: Tetragonal I 4/m K0.8Fe1.6Se2

## Slide 5
PHYSICAL REVIEW B 84, 020406(R) (2011)
FIG. 1.(a) The schematic representation of the vacancy ordered √5 ×√5 lattice structure in each iron plane. (b) The ordered spin configuration.
FIG. 2.(a) The magnetic Brillouin zone. (b) The spin-wave spectrum.
Spin wave model-theory
FIG. 3. Temperature dependence of (a) the per-iron magnetic moment and (b) the longitudinal uniform susceptibility.
The correlation between anti-ferromagnetism (AFM) and superconductivity remains unknown.
K0.8Fe1.6Se2
30 meV
55 meV
70 meV

## Slide 6: Sample synthesis
K+Fe+Se
quartz
Fe vacancy order
Ball milling box
Ball milling machine
Furnace
Samples K2-xFe4+ySe5
#1 K2Fe4Se5_annealing
K2Fe4Se5
#2 K1.9Fe4.2Se5 (SC)
K1.9Fe4.2Se5_annealing
#3 K1.9Fe4Cu0.2Se5
K1.9Fe4Cu0.2Se5_annealing
#4 K1.9Fe4Mn0.2Se5
K1.9Fe4Mn0.2Se5_annealing

## Slide 7: TAIPAN experiment: Thermal 3-Axis Spectrometer
Energy transfer E=ℏω=Ei-Ef
Ef: fixed at 14.87 meV
ECHIDNA experiment:
High-resolution powder diffractometer
Ge(331)
λ=2.4395 Å

## Slide 8: Magnetic susceptibility
A= Fe: Superconducting Tc=30 K
A= Cu: totally suppress superconductivity
A= Mn: Tc shift to lower temperature~28 K.
A= Fe: Superconducting with 125 K transition
A= Cu: 125 K transition
A= Mn: Tc shift to lower temperature~20 K.

## Slide 9: Neutron measurements: ECHIDNA experiment: High-resolution diffractometer Lattice constant
Samples | Magnetic moment (μB) | a=b (Å) | c (Å)
#1 K2Fe4Se5 | 2.817(23) | 8.72126(54) | 14.10288(15)
#2 K1.9Fe4.2Se5 | 2.683(54) | 8.71535(23) | 14.11369(65)
#2-annealing | 3.007(45) | 8.71739(16) | 14.10608(46)
#3 K1.9Fe4Cu0.2Se5 | 2.478(33) | 8.71701(81) | 14.13734(23)
#3-annealing | 2.871(33) | 8.72172(83) | 14.12850(23)
#4 K1.9Fe4Mn0.2Se5 | 2.663(41) | 8.73086(15) | 14.10628(41)
#4-annealing | 3.208(39) | 8.72525(22) | 14.10379(44)
Extra irons doped sample with smaller a-axis and larger c-axis.
The magnitude of magnetic moment increases after annealing.
At 300 K

## Slide 10: ECHIDNA experiment Transitions of magnetic order and structure
K2Fe4Se5_annealing
Temperature(K)
K2Fe4Se5
TN~530 K
TS~560 K
TN: magnetic order-disorder transition temperature
TS: structure transition temperature
TN < TS
Magnetic peak
Fe-vacancy order

## Slide 11: Summary of neutron powder diffraction
The magnetic order-disorder transition temperature is at 530 K, and the structure transition temperature is at 560 K.
K1.9Fe4A0.2Se5, A=Fe, Cu, annealing samples display Verwey-like transition in χ-T. No structural or magnetic transition is detected in the NPD patterns collected below and above 125 K.
Superconducting sample has larger c-axis and smaller a-axis, compared to the parent compound.
Quenched sample has smaller a-axis, which increases after annealing.

## Slide 12: TAIPAN experiment: thermal 3-aixs spectrometer
TN<650 K

## Slide 13: Summary of inelastic neutron scattering
The magnetic order becomes disorder above 650 K, and the coherent vibrations merge into the background.
The magnon excitation seems different for the annealing and quenched K2Fe4Se5.
Thank you for your attention!
Acknowledgement
ANSTO
Institute of Physics, Academia Sinica, Taiwan
Helpful discussion: Anton Stampfl, Chin-Wei Wang

## Slide 14
K2Fe4Se5_annealing | 5 K | 60 K | 300 K | 650 K
Peak position 1 (meV) / error | 18.50 / 0.324 | 18.80 / 0.357 | 18.50 / 0.071 | 18.89 / 0.402
2 | 23.33 / 0.439 | 24.46 / 0.994 | 23.52 / 0.116 | 23.83 / 0.546
3 | 27.21 / 0.377 | 27.22 / 0.715 | 27.17 / 0.237 | 28.02 / 0.375
4 | 33 / 0 | 33.44 / 0.408 | 33.19 / 0.447 | 31.66 / 1.309
5 | 43.08 / 0.653 | 42.55 / 1.907 | 43.66 / 0.571 | 40.51 / 2.080
6 | 45.56 / 0.815 | 44.49 / 0.433 | 52.25 / 1.661 | 44.68 / 0.307
7 (Background) | 7.17 / 1.072 | 14.41 / 0.386 | 14.16 / 1.134 | 6.14 / 0.921
K2Fe4Se5_quench | 5 K | 60 K | 300 K | 650 K
Peak position 1 (meV) / error | 10.36 / 0.191 | 13.84 / 1.543 | 14.26 / 0.247 | 18.53 / 0.265
2 | 18.64 / 0.168 | 18.64 / 0.253 | 18.23 / 0.163 | 23.04 / 0.338
3 | 23.68 / 2.601 | 28.03 / 4.643 | 23.30 / 0.495 | 26.56 / 0.536
4 | 26.53 / 0.225 | 25.94 / 2.752 | 26.71 / 0.290 | 33.27 / 0.400
5 | 39.72 / 0.357 | 41.10 / 1.565 | 41.91 / 0.449 | 40.38 / 0.232
6 | 43.60 / 0.308 | 44.43 / 0.677 | 44.45 / 0.239 | 44.09 / 0.263
7 (Background) | 38.84 / 2.797 | 33.11 / 2.117 | 19.95 / 0 | 6.95 / 0.672

## Slide 15: Introduction to iron-based superconductors
LaFeAsO | BaFe2As2 | LiFeAs | FeSe | KFe2Se2
Tc ~ 28 K (55 K for Sm) | Tc ~ 38 K K Co | Tc ~ 18 K | Tc ~ 10 K Pressure (37K) Lattice distorts 1 UC Interface (53K onset) | Tc ~ 32 K Pressure Tc ~ 48K at 12.5 Gpa 245 & 122 phases co-exist
Takahashi et al. Nature 453, 376 (2008) | Rotter et al. PRL 101, 107006 (2008) | Wang et al. Sol. St. Comm 148, 538 (2008) | Hsu et al. PNAS 105, 14262 (2008) | Guo et al., PR B82, 180520 (2010) Sun et al. Nature 10813 (2012)

## Slide 16
EPL, 95 (2011) 37007
PHYSICAL REVIEW B 82, 180520R (2010)

## Slide 18
Ei | 9 meV | 15 | 20 | 30 | 35 | 40
FWHM | 0.4 | 0.9 | 1.5 | 2.9 | 3.5 | 4
K2Fe4Se5_annealing | 18 | 23 | 27 | 33 | 43 | 45
Ref | 1.3 | 1.8 | 2.6 | 3.3 | 4.3 | 4.5
K2Fe4Se5_annealing@5 K | 3.53 | 1.3 | 3.64 | 4.7 | 4.7 | 9.8
K2Fe4Se5_annealing@60 K | 2.76 | 2.35 | 4.77 | 1.41 | 4.7 | 6.0
K2Fe4Se5_annealing@300 K | 1.13 | 1.3 | 3.13 | 2.7 | 6.13 | 8
K2Fe4Se5_annealing@650 K | 1.6 | 3.1 | 2.12 | 6.32 | 8.2 | 1.8
K2Fe4Se5_quench | 10@5K/14/33@650K | 18 | 26@60K/23 | 28@60K/27 | 40@5K/42 | 45
Ref | 0.5/0.8 | 1.3 | 2.5/1.8 | 2.7/2.6 | 4.2 | 4.5
K2Fe4Se5_quench@5 K | 1.3 | 1.8 | 1.3 | 1.9 | 1.2 | 4.5
K2Fe4Se5_quench@60 K | 1.5 | 2.1 | 3.5 | 3.9 | 4.5 | 4.6
K2Fe4Se5_quench@300 K | 1.18 | 1.3 | 1.37 | 1.18 | 3.25 | 1.41
K2Fe4Se5_quench@650 K | 6.3 | 1.6 | 1.9 | 3.7 | 1.4 | 2.4