## Slide 1
Modifying the magnetic reversal mechanism of exchange biased MnxOy/Ni80Fe­20 bilayers through additional O+ implantation
Ji Zhang a,b,, Grace L. Causer b,c, Xinzhi Liu b,d, Mihail Ionescu b,, Ko-Wei Lin e Frank Klose f and Sean Li a
a School of Materials Science and Engineering, University of New South Wales, Sydney, Australia
b Australian Nuclear Science and Technology Organisation, Australia
c Institute for Superconducting and Electronic Materials, University of Wollongong, Wollongong, NSW 2500, Australia
d Helmholtz-Zentrum Berlin für Materialien und Energie, Hahn-Meitner-Platz 1, Germany
e Department of Materials Science and Engineering, National Chung Hsing University, Taichung 402, Taiwan
f Guangdong Technion-Israel Institute of Technology, PR China

## Slide 2: Exchange bias (EB)
Moment M
Field H
HC1
HC2
Field cooling
TN
TC
TN
TC
Field H
Moment M
HEB
HC1
HC2
Notes: A brief introduction of EB.
It is a pinning effect arised from FM and AFM interface, induced by field cooling from the a sample below neel and blocking temperature of AFM material.

## Slide 3: Why are we still interested in EB?
Applications in real world
Giant magnetoresistance read-heads
Contributing factors to EB
Nanoparticles: Crystal structure, magnetic structure, chemical composition etc.
Thin films: Anisotropy, layer thicknesses, interface roughness etc.
Focus of this study
Potential application in spintronic devices
Method to achieve
Ion beam implantation
Altering the magnetism and chemistry of a particular layer in thin film sample via ion beam implantation
Magnetic spin reversal before and after ion implantation

## Slide 4: Experimental methods
As-grown thin film
Ta-O / Mn-O(11 nm) / Ni80Fe20 (23 nm) // SiO2 / Si
Ion beam implantation
8 keV O+ ion implantation: fluences of 1016, 1017 and 1018 ions/cm2 in ANSTO
Characterisation
TEM,
PPMS-VSM and
PNR
Low Energy Ion Implanter
Polarised Neutron Reflectometer

## Slide 5: TEM images before and after ion implantation
Si
MnxOy
NiFe
TaxOy
SiO2
Carbon coating
1017 ions/cm2
50 nm
SiO2
NiFe
Mn-O
Ta-O
Carbon coating
Si
As-grown
50 nm

## Slide 6: Bulk magnetic properties before and after ion implantation
Notes: Unit explain, measured sequence explain. HE and HC, detal Ms, step-like

## Slide 7: PNR instrument introduction
SLDtotal = SLDtotal nuc +/- SLDtotal mag = (bnuc 1 +/- bmag 1) × N1 + (bnuc 2 +/- bmag 2) × N2 …
Non-spin-flip: R++, R--
Spin-flip: R-+, R+-
Notes: Explain R++ R --, sample set-up, measuring sequence.

## Slide 8: Magnetic depth profile measured by PNR
As-grown
1017 ions/cm2
Each layer of samples:
(1) Si,
(2) SiO2,
(3) NiFe,
(4) Mixed Mn-O-NiFe,
(5) Mn-O,
(6) Ta-O,
(7) Mixed NiFe-NiFeOᵪ,
(8) MnxOy,
(9) Mixed Ta-TaaOb-MnxOy

## Slide 9: Magnetic reversal measured by PNR
As-grown
1017 ions/cm2
M// = MSample x sin(θ)
θ
100% coherent spin rotation
~80% coherent spin rotation
Notes: Fitting model explain.

## Slide 10: Conclusion
Samples were successfully O+ ion implanted with 8 keV at 1016, 1017 and 1018 ions/cm2 fluences.
Implanted sample shows improved HE and HC.
PNR analyses of sample before and after O+ ion implanted shows the chemical and magnetic structures.
During spin reversal, as-grown sample ~80% undergo coherent spin rotation, and ~20% of the spins undergo magnetic domain nucleation and motion
1017 ions/cm2 implanted sample shows fully coherent spin rotation.

## Slide 11: Acknowledgements
Funding Supports
Collaborators
Khai-Han and Steve who made the sample

## Slide 12
(a)
(b)
(c)
(d)

## Slide 13
(a)
(b)

## Slide 14
(a)
(b)