## Slide 1: Diamond-Edge Gaskets for the Ultrahigh Vacuum Systems
Gao-Yu Hsiung
National Synchrotron Radiation Research Center (NSRRC), Hsinchu, Taiwan
E-mail: hsiung@nsrrc.org.tw

## Slide 2: Outline
Introduction
Concepts: Diamond-Edge Gasket
Experimental Test
Conclusions

## Slide 3: Ultrahigh Vacuum (UHV) System
Pressure: P < 110-7 Pa (~ 110-9 mbar)
Leak Rate: QL < 110-10 Pa∙m3/s (~ 110-9 mbar∙l3/s)
All Metal Materials (typically)
Thermal Outgassing Rate after Baking:
q < 110-9 Pa∙m3/(s∙m2) (~110-12 mbar∙l/(s∙cm2))
(~ 3.3107 Molecules/(s∙cm2) )
1013
1
10-3
10-6
10-9
10-12
10-15
(mbar)
UHV
101325
100
0.1
10-4
10-7
10-10
10-13
(Pa)

## Slide 4: National Synchrotron Radiation Research Center, Hsinchu, Taiwan
TLS (1.5 GeV, 360 mA) 1993 ~
TPS (3 GeV, 400 mA) 2015 ~
Activity Center
Guest House II
Conference Rooms
Cafeteria
Parking
Administration
& Operation
Administration Offices
User Office
Control room
Main Gate
Guest Hose I

## Slide 5: Taiwan Photon Source (TPS) 3 GeV, 500 mA, 1.6 nm∙rad

## Slide 6: 4m-long Aluminum Bending Chamber
4m Aluminum Bending Chamber
Electron Beam
Synchrotron Light

## Slide 7: Ultrahigh Vacuum Systems for the Accelerator Light Sources
Extremely low density of the residual gas molecules in the beam ducts: to mitigate the beam loss from nuclear scattering, ion trapping instability. (Ultrahigh Vacuum)
Residual Gas Molecules
Ion Trapping Instabilities
(Ions from Residual Gases)
Beam Loss
(Gas-Scattering)
Bremsstrahlung Radiation
(Inelastic Gas-Scattering)
e – beam (bunch)
Beam Duct

## Slide 8: Low-carbon clean surface after Ethanol CNC machining for the TPS Bending Chambers
CNC Machining Processes (sprayed with pure alcohol)
< Class 10,000 @0.1mm
O
Al
C
Ethanol CNC machining
Low Carbon
Oil-Free CNC Machining for the TPS B-chambers (~ 4 m) in Clean Room
TPS Aluminum B-chamber
Experience from the TPS

## Slide 9: Thermal Outgassing Rate (Aluminum) q (Ethanol) ~ 1.410-14 Torr·l/(s·cm2)
(c) Chemical cleaning
q72 = 9.5×10-14 Torr·L/s·cm2
(b) Ethanol CNC Machining
q72 = 1.4×10-14 Torr·L/s·cm2
(a) O3 Water Cleaning
q72 = 4.8×10-15 Torr·L/s·cm2
♦♦♦ (a) O3 Water Cleaning
---- (b) Ethanol CNC Machining
xxx (c) Chemical Cleaning
After Baking :
(a)
(b)
(c)
TPS Result

## Slide 10: Smooth Beam Ducts for the Accelerator Light Sources
Very smooth cross section of the beam ducts: to avoid the interaction of the wake field excited via the non-smooth structure such as the steps or the gaps. (Low Impedance)
e – beam (bunch)
Beam Duct
No Steps
No Gaps

## Slide 11: RF-Bridge Aluminum plates between Flanges to mitigate the impedance
Knife Edge (contact bridge)

## Slide 12: Markets (Aluminum UHV Systems)
Future Accelerator Light Sources (Ultra-low emittance)
  beam ducts with small apertures (I. D. < 20 mm)
Large Flat Panel Displays and Solar Cell Panels
  4 m long large processing chambers
  Rectangular valves & flanges
Research & Processing UHV chambers
  MBE, STM, surface analysis, etc.

## Slide 13: Aluminum Conflat Flanges (Currently)
Mirror Finishing on the surface of the Knife-edge
Hard-coating (CrN, TiN, TiC) on the surface
Drawbacks：
Higher cost
Difficult for repairing
Single supplier

## Slide 14: Leakage on the machined aluminum flange
Porous cracks found on the edge-sealing part
Smooth edge-sealing on Back-side of gasket
Knife edge is difficult to machine
Non-smooth surface

## Slide 15: Rectangular Flanges for high-radiation zone (No O-ring seals!)
Drawbacks：
Multi-stages of CNC machining process
Difficult for repairing

## Slide 16: Metal-wire sealing for large flanges
Drawbacks：
Risk of leakage
Difficult for repairing

## Slide 17: Helicoflex metal gaskets
Higher sealing-torques (may damage the aluminum surface)
Delta-type for UHV
Drawbacks：
Higher cost
Difficult for repairing
Single supplier

## Slide 18: Concept: Diamond Edge (DE-) Gasket
Diamond (Shape) Edge Gasket

## Slide 19: LEP-type joints (Aluminum Flange)
*Courtesy: W. Unterlerchner, CERN/LEP-VA/89-50
CERN LEP (July 1989 ~ Nov. 2000)
- Large Electron-Positron Collider
√

## Slide 20: DE-Gaskets for TPS BPM Flanges (> 340 flanges sealing)
Ra < 0.4 μm
Torque > 40 kg∙cm
(Leak-tight)
*Courtesy: I. T. Huang, Proc. IPAC2012, WEPPD023

## Slide 21: Conversion between the CF & the DEF Aluminum flanges
Al DE-Gasket
(Knife-edge)
Al Gasket
(Flat)
Conflat Flange
(Knife-edge)
DE Flange
(Flat)

## Slide 22: Typical dimension of 35 DEF Gasket
Circular gasket can be made by lathing.
Non-circular gasket must be made by (CNC) milling.

## Slide 23: Features of the DE-Gasket
DE-Gasket sitting on DEF (Flat) Flange
Material：Aluminum alloy A1050O
Cross sections: Any shape with smooth closed loop
Machining method：CNC Machining
Vacuum Quality：UHV (P < 1×10-7 Pa)
Dimension: can be Standardized (Mass Production)
Diamond Edge Gasket

## Slide 24: Specifications
A. DE-Gasket：
a: Outer Diameter (long)
b: Outer Diameter (short)
d: Width ( > 3.5 mm)
f: Diameter of Edge
g: Height of Edge ( > 4.5 mm)
B. DEF Flange：
e: Depth of flat surface ( < 2 mm)
Inner dimension of flange, Sa & Sb, corresponding to a & b: < 0.2 ~ 0.4 mm
C、H、M、S: Standard dimension corresponding to those of CF Flanges

## Slide 25: Future Light Sources
8th International Particle Accelerator Conference (IPAC17), May 14-19 (2017), Copenhagen, Denmark

## Slide 26: More than 10 projects have launched
Emittance < 500 pm rad
*TPS: 1600 pm rad

## Slide 27: Risky RF bridge (spring loading & pumping slots)
Loose Contact …
Arcing (due to Loose Contact)

## Slide 28: Non-reliable RF Contact spring
Dis-location …
(miss-contact…)
Dropped

## Slide 29: Inner diameter of beam duct: Reduced
LER16 workshop, SOLEIL, 26 October 2016

## Slide 30: How to mount the RF-contact parts? Can it be replaced?
I.D. 10 mm
Function of DE-gasket with the RF shielding
UHV sealing performance

## Slide 31: Can the flange be made with same aperture of the beam duct?
Same cross section

## Slide 32: Directly Machining the flanges on the chambers
DEF Flanges profits：
Precise CNC machining
Directly machined flanges
No knife-edge damage
Low cost
High reliability
CF-Flanges risks:
Deformation from Welding
Knife edge on chamber: difficult for machining and repairing
1
2
3
2
3

## Slide 33: Experimental Test
Gauge Calibration System
Measurement of the Outgassing Rate for the Extractor Ion Gauge
Long beam duct with small aperture for the future light sources
DE-Gaskets with non-circular shape
Special DE Gaskets for the Aluminum extruded beam duct

## Slide 34: 1. Gauge Calibration System
Aluminum 3-way Cube chamber
(Ethanol CNC machining)
Aluminum
(35DEF/35CF Reducer)
Aluminum
35DE Gasket

## Slide 35: Assembly and pumping test

## Slide 36: Ultimate pressure after baking (150 °C, 24 h)

## Slide 37: Pumping down curves & Gauge calibration curves
Gauge Calibration

## Slide 38: 2. Measurement of the Outgassing Rate for the Extractor Ion Gauge (IG1)
TMP

## Slide 39: Thermal Outgassing Rate (Throughput Method )
where
C = 0.82 L/s : Conductance of Orifice (3mm)
PIG# (Torr) : Pressure of Gauge IG#
Q : Outgassing Rate of the IG1-chamber
* Total outgassing rate of gauge IG1 after baking (Q):
Q = 0.82 (7.610-10 - 2.710-10) = 410-10 Torr L/s
PIG1
PIG2
Q Gas flow
C(orifice)
S(pump speed)

## Slide 40: 3. Long beam duct with small aperture for the future light sources
Prepare the Aluminum tubes of 1m and 2m in length (I.D. 10 mm)
Ultra-low outgassing rate: by Oil-free interior surface machining
Ultra-low impedance: by a special design of aluminum diamond-edge gasket sealing; without interior coating
Features: Simplified structure, Simplified manufacturing process, High quality, High reliability, and Low cost
1m AL-Tube (I.D. 10 mm)
Conductance ~ 0.12 l/s
2m AL-Tube (I.D. 10 mm)
Conductance ~ 0.06 l/s
IG1
IG2
IG1
IG2

## Slide 41: Preparation of the Aluminum Tube
Select the aluminum Extruded Pipe-(a) with inner diameter (I.D.): 9.6 mm.
CNC-Machining (in Ethanol) for the aluminum Flanges (without knife-edge)-(b) and the Diamond-Edge Gaskets-(c).
TIG-Weld the flanges to the pipe: full-penetrated welding-(d).
Deep-drill the inside part in Ethanol (oil-free) to I.D. = 10 mm through all the tube-(e).
(a)
(b)
(c)
(d)
I.D. 10 mm
Full-penetrated
welding
I.D. 9.6 mm
(e)
After Drilling
Before Drilling

## Slide 42: Deep-drill (in Ethanol) the inner surface through the Al tube to obtain an uniform inner diameter of 10 mm
10 mm
9.6 mm
10 mm
(Animation)

## Slide 43: Diamond Edge Gasket Sealing

## Slide 44: 1m AL-Tube Pumping Test (I.D. 10mm, interior ethanol drilling)
1 m (I.D. = 10 mm)
IG: Extractor Ion Gauge
TMP: Turbo-Molecular Pump

## Slide 45: Pumping down curve for 1m AL-Tube
Q = 5.710-11 Torr·L/s
IG1
IG2
Baking
(150°C, 24h)

## Slide 46: 1m AL-Tube (I.D. 10mm) after baking qD ~ 7.010-14 Torr∙l/s∙cm2
PL(IG1): 6.06E-10
P0(IG2): 2.12E-10
TMP
Pump

## Slide 47: 2m AL-Tube Pumping Test (I.D. 10mm, interior ethanol drilling)
IG1
IG2
TMP (300 L/s)
TMP (70 L/s)
2m AL-Tube (I.D. 10 mm)
Conductance ~ 0.06 l/s
Tandem Turbo-pumps

## Slide 48: Pumping down curve for 2m AL-Tube
Continuous pumping for 4 months (before baking)
IG1: 5.210-8 Torr
IG2: 2.910-10 Torr
IG1 on
大TMP
Reset
Bake
Pressure before baking：
IG1
IG2

## Slide 49: 2m AL-Tube (I.D. 10mm) after baking
1
(1) Baking for 2m AL-Tube
2
(2) Overall system uniformly bake out
IG1: 1.810-9 Torr
IG2: 6.810-11 Torr
Pressure after baking
1.82E-9
6.8E-11
(Ultimate Pressure)

## Slide 50: Thermal Outgassing Rate of (a) 1m , (b) 2m AL-Tubes
UHV
(a) 1m Tube
(b) 2m Tube
q < 2 10-13

## Slide 51: Summary of the Outgassing Rate for various chambers
Stainless Steel chamber
Stainless Steel chamber + AL tube
-- Pumping Down --
AL tube-1m
AL tube-2m
|-------- Ethanol Drilling --------|
Criteria of UHV
q < 210-13 Torr·l/(s·cm2)
---- Throughput Measurement-----

## Slide 52: 4. DE-Gaskets with non-circular shape

## Slide 53: Aluminum Chamber & Screen Monitor
Aluminum Chambers with DEF Flange
A6061T651 Al-alloy (hard)
CNC Machining (Ethanol) only
Flat (DEF-) Flange (without knife-edge)
Ultrahigh Vacuum (UHV) quality
Can be re-machining (Ethanol)
Al-SM with a build-in water-cooling vessel
Aluminum DE Gaskets
A1050O Al-alloy (soft)
CNC Machining (Ethanol) only
Reused for 3 times vacuum sealing
Ultrahigh Vacuum (UHV) quality

## Slide 54: 35 DE-Gaskets
Type A DE-Gasket: 45°+ 45°Knife Edge
(Ethanol CNC-machining)
Type B DE-Gasket: 20°+ 70°Knife Edge
(Lathe-machining)

## Slide 55: Functions of Screen Monitor
Profile (Shape, Image)
Position (Transverse)
Dimension (Size)
Intensity (Fluorescence)

## Slide 56: Installation #1 and baking (150°C, 24h)
Pressure after baking：
IG1 (IMG) = 7.4910-11 Torr (no pump)
IG2 (EIG) = 1.1510-10 Torr
IG1
IG2
IP/NEG
IG1
IG2
IG1
IG2

## Slide 57: Re-Installation #2 (after re-machining SM in Ethanol) & baking (150°C, 24h)
Pressure after baking：7.5810-11 Torr
Baking
Re-Install
IG1
IG2

## Slide 58: Re-Installation #3 (after re-machining SM in Ethanol and Ozone Water Cleaning) & baking (150°C, 24h)
Ozone water
Cleaning
Re-Install
Baking
IG1
IG2
Pressure after baking：1.8910-10 Torr

## Slide 59: Reused 3 times for the Rectangular DE-Gasket
(1)
(2)
(3)
DE Gasket (d)
- Reused 3 times
Lower Yield of Photon Stimulated Desorption (PSD) that speeds up the commissioning of new accelerator.
UHV (conductance limited)
7.5810-11 Torr

## Slide 60: 5. Special DE Gaskets for the Aluminum extruded beam duct
Photon Span = 2.53 mrad
Reducer Tube : Offset 3.5 mm
Incident angle: 1.5°
SR (TLS-19B)
IG2
IG1
SR

## Slide 61: Elliptical DE Gasket

## Slide 62: Assembly of the Aluminum duct with the special DEF Flanges & DE Gaskets

## Slide 63: Assembly of the Test Vacuum System

## Slide 64: [NEXT] DE gaskets for the Aluminum Ducts of the Future Light Sources

## Slide 65: Conclusions
The innovative design of the aluminum DE-gaskets for the aluminum UHV systems have been developed successfully.
The flanges of the vacuum chambers are flat without the knife-edge that is easily machined with the CNC machine-tools. Then the cross section of the DEF-flanges and gaskets can be designed any non-circular shape, e.g. rectangular, in addition to the circular one.
The precision and the reliability for the aluminum chambers with the DEF-flanges are high, while the manufacturing cost is lower.
The ultimate pressure of the aluminum system after vacuum baking has reached to < 1.010-8 Pa (~ 7.510-11 Torr). With the oil-free ethanol CNC machining process, all the DE- and DEF- vacuum components can be assembled immediately after machining in the clean room without further chemical cleaning process, which simplifies the manufacturing procedure.
The results of the experiments have successfully proved the UHV qualities of the Diamond-Edge gasket sealing, and been able to extend to wider applications.
Thanks for your attension.