## Slide 1
Chiara Neto
School of Chemistry
University of Sydney Nano Institute The University of Sydney
NSW 2006
Anti-fouling and Slippery Properties of Lubricant-Infused Surfaces
14th August 2018, VASSCAA
@netogroup
@ChiaraOz

## Slide 4
Chiara Neto
School of Chemistry
University of Sydney Nano Institute The University of Sydney
NSW 2006
Anti-fouling and Slippery Properties of Lubricant-Infused Surfaces
14th August 2018, VASSCAA
@netogroup
@ChiaraOz

## Slide 5: Slippery Liquid-infused Surfaces (SLIPS)
Surfaces inspired by the pitcher plant
The microstructure traps a lubricant layer, which makes a smooth slippery surface.
Trumpet Pitcher Plant SEM
Trumpet Pitcher Plant

## Slide 6: Slippery liquid-infused surfaces (SLIPS)
Omniphobic1
Anti-icing
Anti-fouling
Potentially anti-drag2
http://bit.ly/2z0IMJP
http://bit.ly/2lA71f6
[1] Wong, Kang, Tang, Smythe, Hatton, Grinthal, J. Aizenberg, Nature 2011, 477, 443-447.
[2] Van Buren, T.; Smits, A. J., J. Fluid Mech. 2017, 827, 448-456.

## Slide 7: Outline
4. Quantifying drag-reduction
solid
liquid
1. Anti-fouling wrinkled polymer surfaces
3. Under water superoleophobic surfaces
2. Mapping lubricant film thickness

## Slide 8: 1. Teflon Wrinkles
Teflon wrinkles spontaneously upon shrinking of shrinkable substrates.
The wrinkled substrates are superhydrophobic and resistant to wear.
λ wrinkle wavelength
h layer thickness
Ef , EsYoung’s modulus of the top film and soft substr.
Shrinks to 30% of its original size
Liam Scarratt
λ≈ 2πh(Es/3Ef) 1/3
Scarratt, et al; ACS Appl. Mater. Interfaces 8, 6743−6750 (2016)

## Slide 9: Infusion of Silicone Oil in Teflon Wrinkles
0<Θos(a) <θc
Θos(a) >θc
0<Θos(w) <θc
Θos(w) >θc
P4VP
PS
Cameron Ware
Our best infused Teflon wrinkles
have:
low roll-off angles
Cannot be marked
with markers
44°
Teflon wrinkles trap silicone oil well.
0 < Θos(a) < Θc in air (Θc = 80°)
Θos(w) = 0 in water
P4VP wrinkles are superoleophobic under water.
Θos(w) = 156º
PS wrinkles do not work.
Bico, Thiele, Quéré Colloids Surf. 2002, 206 (1-3), 41. Smith et al., Soft Matter 2013, 9 (6), 1772.
λ = 150± 20 nm
Height 290 ± 30 nm
On shrinkwrap
λ = 390 nm
Height 380 nm

## Slide 10: Roll-Off Angle on Infused Teflon Surfaces
Droplet roll-off angle ≈ adhesion
Reduced roll off for all infused Teflon wrinkles compared to dry surfaces is a measure of ‘slippery’ surfaces.
Substrate | Wrinkle λ (nm) | Dry Roll Off Angle | Infused Roll Off Angle
Silicone | Flat | 22 ± 1º | N/A
Polyshrink™ | 80 | 12 ± 1º | 4 ± 1º
 | 150 | 9 ± 1º | 4 ± 1º
 | 1190 | 17 ± 6º | 9 ± 1º
Shrink Wrap | 150 | 10 ± 6º | 3 ± 1º
 | 160 500 | 28 ± 6º | 4 ± 1º
 | 390 | 10 ± 3º | 4 ± 1º
 | 300 1600 | 20 ± 5º | 16 ± 2º
Dry wrinkles
infused wrinkles
Ware, et al, ACS Applied Materials Interfaces 10, 4173−4182, 2018.

## Slide 11: Quantifying Silicone Oil
Spun 1 min
Spun 5 min
Drained 2.5h
Fluorescence
Chart: Fluorescence of Nile Red in Silicone Oil
Chart: Calibration Curve
| 0 | 0.01 | 0.05 | 0.1 | 0.3 | 0.5 | 1
525 nm | 22.712 | 36.988 | 89.192 | 115.513 | 244.905 | 418.88 | 846.99
560 nm | 49.899 | 60.418 | 99.835 | 121.636 | 204.693 | 330.121 | 628.124
Nile Red
Ware et al, ACS Applied Materials Interfaces 10, 4173−4182, 2018.
Truis
Smith-Palmer
Sam
Peppou-Chapman
Silicon oil is extracted from the surface and fluorescence compared to the calibration curve
Fluorescence spectra for varying volumes (0−1.00 μL) of 1.00 μM Nile red in 10 cSt silicone oil;

## Slide 12: Bacterial inhibition
dry drained spun,
teflon sheared 2 weeks
Able to be molded
Surface were exposed to marine bacteria Psuedoalteromonas spp for 24 hours.
Drainage Treatment | Volume silicone Oil / µL cm-2 | Water Contact angle / ° | Roll-off angle / ° | % Inhibitiona
Drained 1 h | 0.9 ± 0.2 | 99 ± 2 | 5 ± 1 | 99 ± 1
Spun at 8000 rpm, 1 min | 0.4 ± 0.2 | 111 ± 2 | 7 ± 1 | 86 ± 9
Spun at 8000 rpm, 5 min | 0.3 ± 0.2 | 113 ± 3 | 9 ± 1 | 84 ± 10
Drained 1 h, 2 weeks shear | 0.04 ± 0.01 | 113 ± 1 | 6 ± 3 | 73 ± 13
Spun at 8000 rpm, 1 min, 2 weeks shear | 0.02 ± 0.01 | 122 ± 6 | 8 ± 4 | 76 ± 16
a) The % inhibition is relative to dry Teflon wrinkles, non-infused with silicone oil.
Only small volumes of oil (0.2 mL/m2) are required for anti-fouling behavior .
Inhibition measured by absorbance of crystal violet extracted from
the surfaces exposed to bacteria

## Slide 13: Test of anti-fouling in the ocean
Surfaces immersed in Sydney Harbour for seven weeks to test for real-world fouling.

## Slide 14: Inhibition of marine fouling
23 %
99 %
57 %
30 %
65% of fouling
released
30% of fouling
released
Surfaces immersed in Sydney Harbour for seven weeks to test for real-world fouling.
Silicon oil is non-toxic but inhibits fouling and is foul-release.
Ware, et al, ACS Applied Materials Interfaces 10, 4173−4182, 2018.
% Surface coverage by marine fouling

## Slide 15: 2. Mapping lubricant film thickness
Peppou-Chapman & Neto, submitted, 2018.
Sam
Peppou-Chapman
Position of hard substrate
Jump-in separation indicates thickness of liquid film
Mate et al. J. Chem. Phys. 1989 and 1991
Thickness reproduces ellipsometric results.
AFM Meniscus Force Measurements

## Slide 16: Mapping of lubricant thickness
Contour map of film thickness
shows areas of thick film and areas that are depleted with nanoscale accuracy.
Lubricant
Substrate
Notes: Add histogram

## Slide 17: Film depletion leads to two distinct regions
Infusion of hydrophobic Teflon leads to two populations of film thickness: one thick and one thin; the thin film population is ~ 5 nm.
0.09 ± 0.03 µL cm-2
0.09 ± 0.02 µL cm-2
0.02 ± 0.002 µL cm-2
0.02 ± 0.01 µL cm-2
0.02 ± 0.01 µL cm-2
0.02 ± 0.01 µL cm-2
Thick film
wrinkle tops
wrinkle tops
wrinkle tops
Thick film
wrinkle tops

## Slide 18: Infusion of P4VP with silicon oil
Infusion of hydrophilic P4VP also leads to two populations of film thickness:
thick and thin; the thin population is ~ 15 nm. The volume of silicone oil infused is higher (0.037 ± 0.004 µL cm-2).
Wrinkle tops
Thick film
Silicone oil spreads on and poly(4-vinylpyridine) (P4VP) in air.

## Slide 19: Interface potential of a thin liquid film
Silicon oil
Teflon/P4VP
h
Thin film unstable on Teflon
Thin film stable on P4VP
Seemann, et al.; J. Phys.: Condens. Matter 17, S267-S290 (2005).
Lubricant
thin film
Chart: Silicone oil thickness (nm)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30
Teflon | -0.00032439 | -8.1093e-05 | -3.6038e-05 | -2.0268e-05 | -1.2969e-05 | -9.0045e-06 | -6.6138e-06 | -5.0622e-06 | -3.9985e-06 | -3.2376e-06 | -2.6746e-06 | -2.2464e-06 | -1.9132e-06 | -1.6488e-06 | -1.4355e-06 | -1.2609e-06 | -1.1163e-06 | -9.9505e-07 | -8.9247e-07 | -8.0488e-07 | -7.2951e-07 | -6.6419e-07 | -6.072e-07 | -5.5719e-07 | -5.1307e-07 | -4.7394e-07 | -4.3907e-07 | -4.0789e-07 | -3.7987e-07 | -3.5461e-07
P4VP | 0.00070773 | 0.00017723 | 7.8975e-05 | 4.4577e-05 | 2.8649e-05 | 1.9992e-05 | 1.4767e-05 | 1.1372e-05 | 9.0421e-06 | 7.3727e-06 | 6.1354e-06 | 5.1925e-06 | 4.457e-06 | 3.872e-06 | 3.3989e-06 | 3.0105e-06 | 2.6877e-06 | 2.4163e-06 | 2.1858e-06 | 1.9884e-06 | 1.8178e-06 | 1.6694e-06 | 1.5394e-06 | 1.4249e-06 | 1.3234e-06 | 1.233e-06 | 1.1521e-06 | 1.0794e-06 | 1.0138e-06 | 9.5441e-07
= Hamaker constant
Disjoining pressure - van der Waals forces
1
3
2

## Slide 20: Film thickness on the wrinkle tops
60º
Peppou-Chapman & Neto, submitted, 2018.
Minimum measurable thickness of liquid varies depending on interface potential and wettability.
Silicon oil on Teflon wrinkles
Silicon oil on P4VP wrinkles

## Slide 21: 3. Under water superoleophobic surfaces
Hydrophilic P4VP films wrinkle similarly to Teflon films.
Coating thickness (nm) | wrinkle width (w, nm) | wrinkle heights (h, nm) | pitch width (p, nm) | Roughness (RRMS, nm)
16 | 90 ± 18 | 120 ± 45 | 176 ± 128 | 80 ± 20
36 | 200 ± 55 | 175 ± 68 | 279 ± 226 | 230 ± 50
241 | Sm. 1280 ± 535 Lg. 8800 ± 4000 | Sm. 1050 ± 510 Lg. 3450 ± 1200 | Sm. 1600 ± 950 Lg. 4500 ± 3450 | 970 ± 380
16 nm thick
36 nm thick
241 nm thick
Ahmed Owais
poly(4-vinylpyridine) P4VP films

## Slide 22: Underwater oil repellency of P4VP wrinkles
P4VP wrinkles are highly wettable by water, especially after plasma treatment
Wrinkled surfaces are superoleophobic underwater
The thickest coatings showed the best performance
petroleum spirit
A. Owais, T. Smith-Palmer, A. Gentle, C. Neto; Soft Matter, 2018, in press

## Slide 23: Optical transmittance
C
D
Transmittance
Reflectance
36 nm-thick P4VP
241 nm-thick P4VP
36 nm-thick P4VP
241 nm-thick P4VP
Water-infused wrinkled P4VP surfaces are transparent and as reflective as glass.
Surface | Reflectance | 
 | Dry | water-infused
Glass | 8% | 
P4VP 36 nm-thick, dry | 13% | 7%
P4VP 241 nm-thick, dry | 20% | 8%

## Slide 24: 4. Quantifying drag-reduction
NO SLIP
Universally employed.
Ok for macroscopic experiments.
No microscopic explanation.
solid
liquid
Commonly accepted for gases
and polymers.
b, slip length, quantifies slip
PARTIAL SLIP
solid
liquid
Craig, Neto, Williams, Phys. Rev. Lett. 87, 054504 (2001).

## Slide 25: AFM colloid probe – hydrodynamic force measurements
Ftotal(t) = k x
= Fh(t)+ Fd(t)+ Fv(t)
increasing
rate
approach
withdraw
No Slip
Slip

## Slide 26: Effect of wettability on slip on solid surfaces
Solvophilic surface (θ < 90°)
Slip length ~ 0 - 10 nm
Solvophobic surface (θ > 90°)
Slip length ~ 20 - 100 nm
Super-hydrophobic surface (θ > 150°)
Slip length b ~ the order of micrometers
θ > 150°
θ > 90°
θ < 90°
Langmuir 2011, 27, 6712-6719; Langmuir 2012, 28, 3465-3473;
Langmuir 2012, 28, 7768-7774
Zhu, Attard, Neto; Langmuir 2011, 27, 6701-6711;

## Slide 27: Flat surfaces can also trap lubricant
1. Leslie, Waterhouse et al Nat Biotech 2014, 32, (11), 1134-1140.
Rough self-assembled monolayer
Lubricant
Ɵ
Roll off angle Ɵ
Blood
Plastic
Flat self-assembled monolayers have been shown to trap lubricant and prevent thrombosis.1
We have used SAMs of octadecyl tricholoro silane (OTS) to trap the lubricant.
Liam Scarratt

## Slide 28: Effect of lubricant thickness on sliding angle
Chart: Roll off angle (°)
| Clean OTS | Excess Oil | 360 nm Oil | 25 nm Oil | < 1 nm Oil
Roll-Off Angle | 15 | 1 | 2 | 5 | 13
Roll off angle
Roll-off angle of 10 µl water droplets is often used to define how ‘slippery’ a surface is.
OTS SAM
Silicon oil layer
silicon
As measured by ellipsometry
Notes: Include some text.

## Slide 29: Silicone oil film dewets under water
Submerge in Water/Sucrose
h
Initial film thickness = 300 nm
Initial film thickness = 150 nm
?
= Hamaker constant
Disjoining pressure - van der Waals
Silicone oil film is stable is air
Silicone oil film
dewets under water

## Slide 30: AFM meniscus forces on silicon oil film
Oil OTS in Sucrose 60%
Clean OTS in Air
30 nm Oil OTS in Air
Clean OTS in Sucrose 60%
Approach
Withdraw
≈ 3 N/m spring constant

## Slide 31: Drag reduction by 4 nm thin silicone oil film
Sucrose 60 %
Chart: 
Chart: 
b = 24 nm
No slip boundary
Slip boundary
Experimental
○○○
b = 29 nm
No slip boundary
Slip boundary
Experimental
○○○
Separation (nm)
Force (nN)
b
b
η = 40 mPa.s
On dry OTS surface (not infused)
On infused OTS surface
Chart: Effective Slip Length b(nm)
| Silicon Wafer | OTS | OTS* | Oil Coated OTS
Silicon Wafer | 7
OTS | 24
Oil on OTS | 29
@ 40 µm/s
0.18 – 0.9 N/m spring constant

## Slide 32: Conclusions
The function of SLIPS is strongly dependent on film thickness.
The use of lubricant in wrinkled SLIPS is highly efficient.
Anti-fouling behaviour is retained overall, even if some regions are exposed, down to nanoscale films.
Sliding angles are not necessarily able to predict the local depletion.
AFM can be used to quantify regions of depletion.

## Slide 33: Acknowledgements
Liam Scarratt
Cameron Ware
Sam Peppou-Chapman
Ahmed Owais
Dr Liwen Zhu
A/Prof Truis Smith-Palmer, St. Francis Xavier University
The Neto group, June 2017
FUNDING
@netogroup
@ChiaraOz

## Slide 34
acis2019.info
Abstract deadline: September 3rd, 2018

## Slide 35: Interface potential of a thin liquid film
Silicon oil
Teflon/P4VP
PS
d
e
c strength of the short-range interaction
Van der Waals term < 0 for Teflon
Van der Waals term > 0 for P4VP
h*
Seemann, et al.; J. Phys.: Condens. Matter 17, S267-S290 (2005).
100 µm
Lubricant
thin films
Metastable film dewetting

## Slide 36: Qualitative validation of the method
Tapping mode AFM
Reconstructed from force curves
TM AFM and force curves provide qualitatively similar information.
Light Tapping
Hard Tapping

## Slide 37: Fitting force curves to obtain slip length
Fitted slip length b = 60 nm
System: dioctyl phthalate between a hydrophobised silicon substrate (contact angle ≈ 45°) and a silica colloid probe (contact angle ≈ 21°)
Experimental force
No- Slip theoretical force
Slip theoretical force
Hundreds of force curves performed in different positions on each substrate at 10 - 80 m/s approach rates.
Zhu, Attard, Neto; Langmuir 2011, 27, 6712-6719

## Slide 38: Slip measurements
Over the past 15 years there has been a lot of evidence for slip.
Colloid probe AFM remains one of the best techniques to measure slip.1,2,3,4
Reproducible average slip length 11 nm in wettable systems (21º)4 and 45 nm in partially wettable systems (45º)2
2. Zhu, Attard, Neto; Langmuir 2011, 27, 6712-6719
3. Zhu, Attard, Neto; Langmuir 2012, 28, 3465-3473
4. Zhu, Attard, Neto; Langmuir 2012, 28, 7768-7774
1.Zhu, Attard, Neto; Langmuir 2011, 27, 6701-6711

## Slide 39: Effective slip - grafted polymer brushes
no-slip
slip
Dynamic force curves captured at 40 um/s and in viscous sucrose solution
b=26 nm
± 3 nm
Dr Eric Charrault
Charrault, Lee, Neto, Soft Matter 12, 1906-1914 (2016).

## Slide 40: Interpreting ‘Slip’ on Polymer Brushes
Short chain PEG1k
b = 16 ± 4 nm
L ≈ 3 nm
rmax ≈ 10 nm
Long chain PEG30k
b = 25 ± 3 nm
L ≈ 50 nm
Penetration length
Stagnation length
400 nm
Slip of similar magnitude to the roughness: flow within the surface features
Charrault, Lee, Neto, Soft Matter 12, 1906-1914 (2016).

## Slide 41: Our Approach
Symmetric and asymmetric systems
Zhu, Attard, Neto; Langmuir 2012, 28, 7768-7774
Best practice experimental protocol
Elimination of the virtual deflection
Care to recognise nanoparticles
Repeated measurements
Zhu, Attard, Neto; Langmuir 2011, 27, 6712-6719
Shear-rate dependence
Zhu, Attard, Neto; Langmuir 2012, 28, 3465-3473
Zhu, Attard, Neto; Langmuir 2011, 27, 6701-6711
OLD
NEW
Fit algorithm & drag component
  A “blind test” reveals error of 2 nm in b and 3 % in k; non-constant drag force on cantilever

## Slide 42: Quantification of intermolecular interactions
WCA on gold is 73º ± 1
No need to have a superhydrophilic coating to achieve underwater superoleophobicity
System | Hamaker constant (× 10-20 j) | Force type | Stability of the sandwiched layer
Hexadecane/water/P4VP | 1.21 | Attraction | Metastable
Hexadecane/water/Au | -3.23 | Repulsion | Stable
Capillary forces enhance surface efficiency

## Slide 43: Soft Interfaces: Polymer Brushes
Poly(ethylene)glycol (PEG):
Mw = 1000 g/mol
Mw = 30000 g/mol,
Dr Eric Charrault
Polymer chains tethered at one end - densely
‘Grafting-to’ keeps the synthesis simple
Cloud Point (CP) conditions:
Increase T°C and ionic strength
65ºC, [K2SO4] = 2.9 M for PEG1k
40ºC, [K2SO4] = 1.8 M for PEG30k
Grafted onto gold substrates through thiols
(gold not entirely smooth)
No salt high salt conc.
lower temp higher temp
cloud
point
Charrault, Lee, Neto, Soft Matter 12, 1906-1914 (2016).