## Slide 1: Studying Structure at Interfaces by Neutron and X-ray Scattering
Stephen A. Holt

## Slide 2: Outline
Reflectivity primer
Examples
Liquid/Liquid Interface
  Approaches
  Application to Emulsions.

## Slide 3: Specular Reflectivity
Basic Concepts
  Geometry
  Scope of Method
  Contrast Variation
Planar Interfacial Structure
  < 1 nm – 100’s nm
Applied to following interfaces
  Air/Liquid
  Air/Solid
  Solid/Solid (buried interfaces)
  Solid/Liquid
  Liquid/Liquid

## Slide 4
Analagous to optical interference,
ellipsometry
Equivalent to electromagnetic radiation with the electric vector perpendicular to the plane of incidence
Depth Profiling : provides
information on concentration
or composition profile perpendicular
to the surface or interface

## Slide 5: Geometry
Kjaer et al, J. Phys. Chem. 1989, 93, 3200 - 3206
Specular Reflection
Probe change in refractive index
- Could be for any radiation.
Notes: Probe change in refractive index
Collecting data.
TOF vs fixed wavelength.

## Slide 6: n = 1 for air, and slightly <1 for other materials
Refractive Index and Scattering Length Density
n = 1 – (d + ib)
re = Bohr electron radius
= e2 / 4peomc2
= 2.818x10-15 m
ri mass density
Zi atomic number of ith atom
Mi molar mass of ith atom
Scattering Length Density

## Slide 7: Scattering ‘Power’
-0.5
0
0.5
1
1.5
2
2.5
3
Element
Neutron scattering length
(10-12 cm)
-0.5
0
0.5
1
1.5
2
2.5
3
X-ray scattering amplitude
(10-11 cm)
H
Mg
Cr
Kr
Cd
Nd
Hf
Po
Cm
H
D
Mn
Fe
Notes: Note this is the scattering amplitude not the SLD. So light elements are even worse than appears here.

## Slide 8: Two Examples
Alkane Phosphate film formation on TiO2
Gram –ve bacteria outer membrane
  Charge based interaction.

## Slide 9: Alkane Phosphate
TiO2 film ~ 250 Å thick
Dodecyl phosphate
  pH 4.5
  pH 7.0
Measured in situ
Deposition more rapid at lower pH
pH 4.5
pH 7.0
Holt et al. RSC Adv., 2013,3, 2581-2589
Notes: TiO2 Ion Beam assisted Electron Beam methods. Helia photonics , Scotland.

## Slide 10
SAM assembly proceeded more slowly at pH 7.0 which may have enabled molecular rearrangement in the film
Denser, thinner SAMs which were more resistant to increasing solution pH were produced when deposited from pH 7.0 buffer.
TiO2 Surface
pH 4.5
pH 7.0

## Slide 11: GNB Outer Membrane
Double Wall
Outer leaflet Lipopolysaccharides
Complex structure
Holt et al. Soft Matter, 2009, 5, 2576–2586. DOI: 10.1039/b822411k.
Le Brun et al. dx.doi.org/10.1021/bm400356m | Biomacromolecules 2013, 14, 2014−2022
Clifton et al. J. R. Soc. Interface 2013 10, 20130810. http://dx.doi.org/10.1098/rsif.2013.0810
Clifton et al. dx.doi.org/10.1021/la504407v | Langmuir 2015, 31, 404−412
Clifton et al. DOI: 10.1002/anie.201504287. Angew. Chem. Int. Ed. 2015, 54, 11952 –11955.
Clifton et al. DOI: 10.1021/acs.langmuir.6b00240 Langmuir 2016, 32, 3485−3494.

## Slide 12: GNB Outer Membrane
Double Wall
Outer leaflet Lipopolysaccharides
Complex structure
Holt et al. Soft Matter, 2009, 5, 2576–2586. DOI: 10.1039/b822411k.
Le Brun et al. dx.doi.org/10.1021/bm400356m | Biomacromolecules 2013, 14, 2014−2022
Clifton et al. J. R. Soc. Interface 2013 10, 20130810. http://dx.doi.org/10.1098/rsif.2013.0810
Clifton et al. dx.doi.org/10.1021/la504407v | Langmuir 2015, 31, 404−412
Clifton et al. DOI: 10.1002/anie.201504287. Angew. Chem. Int. Ed. 2015, 54, 11952 –11955.
Clifton et al. DOI: 10.1021/acs.langmuir.6b00240 Langmuir 2016, 32, 3485−3494.

## Slide 13: Fabricating a FSB GNB mimic
Langmuir Blodgett
A
Air
Water
Surface Pressure / mN m-1
Chart: 
B
Monolayer area / cm2
Air
Water
D
Rough
LPS
“Outer
Membrane”
Water Gap
“Inner
Membrane”
Water
DPPC
ThioPC
Gold
Permalloy
Silicon
C
Langmuir Schaeffer
Air
Water

## Slide 14: Structural Characterisation
Bilayer Asymmetry
  From 69:28 & 23:75 (LPS/PC) outer and inner leaflets, respectively,
  To 79:11 & 8:82 in the best.
  Determined via use of deuterated DPPC
FSB coverage > 90 %.
Chart: 
A
B
Spin up
Spin down
Distance / Å
Scattering Length Density / Å-2
D2O
H2O
Gold
C
Q / Å-1
Permalloy
Chart: 
R/RFres
Notes: Calcium in bathing solution.
Calcium in solution during preparation.

## Slide 15
Chart: 
Gold

## Slide 16: LPS size and ColN Interation
Ra and Rd LPS
Clifton et al. DOI: 10.1021/acs.langmuir.6b00240 Langmuir 2016, 32, 3485−3494.

## Slide 18: Liquid / Liquid Interface
Probing structure
  Very limited structural methods
Vacuum based techniques
  Incompatible
  Freeze fracture microscopy but …
X-ray and Neutron methods
  Also use light (ellipsometry)

## Slide 19: The Challenges
X-rays
  Synchrotron
  Up the energy brute force.
Neutrons
  Hydrogenous materials
  Transmission
Radiation
Oil
Water
Interface
Size of interface – ‘Flatness’
Attenuation

## Slide 20: NR Through bulk aqueous phase
Radiation
Oil
Water
Interface
R. Campbell et al, Eur. Phys. J. Plus (2011) 126: 107.
Interface must remain horizontal
Need to deflect neutron beam up.

## Slide 21: Trapped Oil Layer
Neutrons
Trapped Oil Layer
Aqueous Phase
Zarbakhsh et al. Meas. Sci. Technol. 10 (1999) 738–743.
Bowers et al. Langmuir 2001, 17, 140-145
Zarbakhsh et al. Faraday Discuss., 2005, 129, 155–167
Campana et al. Soft Matter, 2012, 8, 8904.
Silicon Wafer

## Slide 22: Our method – ‘soft’ interfaces
Liquid / liquid interface
Usually hydrophilic / hydrophobic
Hydrophobic proxies
  OTS
  ‘Hard Wall’
Want a ‘soft’ surface
  Penetration by species of interest.
Poly(dimethylsiloxane) – PDMS
  SDS & CTABr
Wei et al. Langmuir, 2018, 34 (31), pp 9141–9152

## Slide 23: PDMS Proxy
AFM, QCM-D and NR analysis
Demonstrate
  SDS CTABr and peptide penetrate PDMS
  But surface adsorption on OTS.
21 amino acid designed peptide.

## Slide 24: XRR at Advanced Photon Source
Bu et al. dx.doi.org/10.1021/jp508430e | J. Phys. Chem. B 2014, 118, 12486−12500
ChemMatCARS beamline – ID15C
Collaboration with Schlossman group at Uni of Chicago
Liquid Surface Spectometer

## Slide 25: XRR at Advanced Photon Source
Go to a synchrotron and need more sample !

## Slide 26: Tailored NanoEmulsions (TNEs)
Number of medical applications
  Drug delivery [Hormann et al, J. Controlled Release, 2016, 223, 85–98.]
  Molecular Imaging [Rosenblum et al. Mol. Membr. Biol., 2010, 27, 274–285]
  Vaccines [Leleux & Roy, Adv. Healthcare Mater., 2013, 2, 72–94]
Ease of Fabrication, high loading, colloidal stability
  Koo et al. Nanomedicine, 2005, 1, 193–212.
  Solans et al. Curr. Opin. Colloid Interface Sci., 2005, 10, 102–110.
  Tadros et al. Adv. Colloid Interface Sci., 2004, 108–109, 303–318
However usually at low end of design sophistication.

## Slide 27: TNEs
Decouple emulsification from functionalisation.
Peptide Stabilised Emulsions
  Sainsburyet al. Curr. Opin. Chem. Eng., 2014, 4, 11–17.
  Dexter et al. Nat. Mater. 2006, 5, 502–506.
  Zeng et al. Small, 2013, 9, 3736–3742.
Peptide 21 AA
  AM1
  Emulsification
DAMP4 (4 x AM1)
  Protein anchoring ‘surfactant’

## Slide 28: TNE Formation
Deuterated or hydrogenous DAMP4

## Slide 30: L/L Neutron Reflection

## Slide 31: XRR at L/L interface.
Flourescent studies.

## Slide 33: L/L Reflectivity
Simulation

## Slide 35: Conclusions

## Slide 36: Conclusions

## Slide 37: Acknowledgements
Platypus team
  Andrew Nelson, Anton Le Brun, Michael James (now AS)
GNB
  Luke Clifton, Jeremy Lakey, Anton Le Brun
PDMS
  Zengyi Wei, Stuart Prescott
TNEs
  Lizhong He, Frank Sainsbury, Stefania Piantavigna

## Slide 38: A user facility
Proposal deadline 15th September
Via the ACNS portal.
  https://neutron.ansto.gov.au/Bragg/proposal/index.jsp