## Slide 1
High mass‐resolution 3D ToF‐SIMS:
PCA and visualization in seconds using Graphical Processor Units (GPUs)
Peter Cumpson, James Hood, Ian Fletcher, Naoko Sano, Anders Barlow,
Newcastle University, UK
VASSCAA-9, Aug 2018
Notes: All copy must be typed over existing copy in the appropriate template. Copy and pasting text will result in changing the style of the typography.
The palette of designated colours can be found in the font toolbox under ‘More Font Colours’.
If you need to insert a new slide while on a slide with similar content, then select ‘Duplicate Slide’.
Images must be scaled to 25% in size after inserting picture ‘From File’. Then ‘Arrange’ > ‘Send To Back’.
The images click to the guidelines for positioning. Use an existing slide as a guide, then remove the pervious images.
All images must be cropped without distortion to maintain original proportions.
Template Style Notes
Image sizes are as follows:
Full page image: 2894 pixels wide x 2173 high
1 side image: 679 pixels wide x 1813 high
2 side images: 679 pixels wide x 895 high (both images)
3 side images: 679 pixels wide x 590 high (1st & 2nd image), 679 pixels wide x 600 high (3rd image)

## Slide 2
High mass‐resolution 3D ToF‐SIMS:
PCA and visualization in seconds using Graphical Processor Units (GPUs)
Peter Cumpson, James Hood, Ian Fletcher, Naoko Sano, Anders Barlow,
Newcastle University, UK
Present address;
Mark Wainwright Analytical Centre,
University of New South Wales
VASSCAA-9, Aug 2018
Notes: All copy must be typed over existing copy in the appropriate template. Copy and pasting text will result in changing the style of the typography.
The palette of designated colours can be found in the font toolbox under ‘More Font Colours’.
If you need to insert a new slide while on a slide with similar content, then select ‘Duplicate Slide’.
Images must be scaled to 25% in size after inserting picture ‘From File’. Then ‘Arrange’ > ‘Send To Back’.
The images click to the guidelines for positioning. Use an existing slide as a guide, then remove the pervious images.
All images must be cropped without distortion to maintain original proportions.
Template Style Notes
Image sizes are as follows:
Full page image: 2894 pixels wide x 2173 high
1 side image: 679 pixels wide x 1813 high
2 side images: 679 pixels wide x 895 high (both images)
3 side images: 679 pixels wide x 590 high (1st & 2nd image), 679 pixels wide x 600 high (3rd image)

## Slide 3: Imaging Mass Spectrometry
MALDI – matrix assisted. Large molecular fragment ions, limited spatial resolution
SIMS: secondary Ion Mass Spectrometry – higher spatial resolution, possibility to “depth-profile”.
In both cases spectra can be extremely complex – practically one needs help in interpretation, often by using multivariate analysis methods.
This is a problem – Modern SIMS instruments generate Tb of data differentiated by
  Precise fragment mass
  Spatial origin on the sample

## Slide 4: Agenda
New PCA algorithm for dealing with terabyte 3D datasets.
  Every mass channel in every spectrum in every voxel goes into the PCA.
  No “out of memory errors”. No peak-picking.
  Everything is PCA’d.
Faster PCA at better mass resolution:
  Two reasons why we must choose samples intelligently from all among the voxels available
    GPU memory limits
    Quadro Logarithmic Trap Analyser (slow but very high mass resolution)
Biomimetic (or Biokleptic?) solution
  Human Retina
Conclusions

## Slide 5: Agenda
New PCA algorithm for dealing with terabyte 3D datasets.
  Every mass channel in every spectrum in every voxel goes into the PCA.
  No “out of memory errors”. No peak-picking.
  Everything is PCA’d.
Faster PCA at better mass resolution:
  Two reasons why we must choose samples intelligently from all among the voxels available
    GPU memory limits
    Quadro Logarithmic Trap Analyser (slow but very high mass resolution)
Biomimetic (or Biokleptic?) solution
  Human Retina
Conclusions

## Slide 6: Agenda
New PCA algorithm for dealing with terabyte 3D datasets.
  Every mass channel in every spectrum in every voxel goes into the PCA.
  No “out of memory errors”. No peak-picking.
  Everything is PCA’d.
Faster PCA at better mass resolution:
  Two reasons why we must choose samples intelligently from all among the voxels available
    GPU memory limits
    Quadro Logarithmic Trap Analyser (slow but very high mass resolution)
Biomimetic (or Biokleptic?) solution
  Human Retina
Conclusions

## Slide 7: Agenda
New PCA algorithm for dealing with terabyte 3D datasets.
  Every mass channel in every spectrum in every voxel goes into the PCA.
  No “out of memory errors”. No peak-picking.
  Everything is PCA’d.
Faster PCA at better mass resolution:
  Two reasons why we must choose samples intelligently from all among the voxels available
    GPU memory limits
    Quadro Logarithmic Trap Analyser (slow but very high mass resolution)
Biomimetic (or Biokleptic?) solution
  Human Retina
Conclusions

## Slide 8: Agenda
New PCA algorithm for dealing with terabyte 3D datasets.
  Every mass channel in every spectrum in every voxel goes into the PCA.
  No “out of memory errors”. No peak-picking.
  Everything is PCA’d.
Faster PCA at better mass resolution:
  Two reasons why we must choose samples intelligently from all among the voxels available
    GPU memory limits
    Quadro Logarithmic Trap Analyser (slow but very high mass resolution)
Biomimetic (or Biokleptic?) solution
  Human Retina
Conclusions

## Slide 10: Mapping Pixels

## Slide 11: Mapping Pixels

## Slide 12: Mapping Pixels
Modern instruments generate huge 3D datasets of pixels (or voxels) each of which have a huge SIMS spectrum associated with that pixel (or voxel).
Navigating and interpreting these datasets is effectively impossible manually, and a challenge computationally.

## Slide 13: “Built in” PCA algorithms (e.g. MATLAB etc)

## Slide 14: Random Vectors algorithm due to Halko et al
Random Vectors (RV1)
P J Cumpson et al, Surface and Interface Analysis 47 (2015) 986.

## Slide 15: We applied this to some datasets from our J105 SIMS instrument
Citrate crystal – lots of topography
Basalt rock. Very large dataset, 512x512 image
Rat’s brain – data from John Fletcher (Gothenburg)

## Slide 16: Sodium citrate crystal (approx 1x0.7mm)
P J Cumpson et al, Surface and Interface Analysis 47 (2015) 986.

## Slide 17
PCA analysis of the entire sodium citrate ToFSIMS image using the RV2 algorithm shows (in the 11th component) small chemically-distinct regions at the surface of the otherwise relatively homogeneous sodium citrate crystal. The field of view is 1mmx1mm
Sodium citrate crystal (approx 1x0.7mm)
P J Cumpson et al, Surface and Interface Analysis 47 (2015) 986.

## Slide 18
Basalt rock sample
1.6mm by 1.6mm,
512x512 pixels
N Sano et al,
JVST A 34, 041405 (2016)

## Slide 19: PCA of a complex image
Rat brain data – Courtesy of John Fletcher @ Swedish National IMS Centre, Gothenburg
Total ion image

## Slide 20: PCA of a complex image
Rat brain data – Courtesy of John Fletcher @ Swedish National IMS Centre, Gothenburg

## Slide 21
Rat brain data – Courtesy of John Fletcher @ Swedish National IMS Centre, Gothenburg
PCA of a complex image

## Slide 22
Rat brain data – Courtesy of John Fletcher @ Swedish National IMS Centre, Gothenburg
PCA of a complex image

## Slide 23: 20kV, C60 imaging depth profile from a Yucca plant leaf
256x256um, 128x128 pixels, 120 levels
70,000 mass spectrum at each voxel
Just under 2 million voxels
Dataset just over 1Tb uncompressed, 30Gb compressed.

## Slide 24: PC1

## Slide 25: PC2

## Slide 26: PC2
Full mass resolution, entire mass range

## Slide 28: PC3

## Slide 29: PC4

## Slide 30: PC5

## Slide 32: Agenda
New PCA algorithm for dealing with terabyte 3D datasets.
  Every mass channel in every spectrum in every voxel goes into the PCA.
  No “out of memory errors”. No peak-picking.
  Everything is PCA’d.
Faster PCA at better mass resolution:
  Two reasons why we must choose samples intelligently from all among the voxels available
    GPU memory limits
    Quadro Logarithmic Trap Analyser (slow but very high mass resolution)
Biomimetic (or Biokleptic?) solution
  Human Retina
Conclusions

## Slide 33: Agenda
New PCA algorithm for dealing with terabyte 3D datasets.
  Every mass channel in every spectrum in every voxel goes into the PCA.
  No “out of memory errors”. No peak-picking.
  Everything is PCA’d.
Faster PCA at better mass resolution:
  Two reasons why we must choose samples intelligently from all among the voxels available
    GPU memory limits
    Quadro Logarithmic Trap Analyser (slow but very high mass resolution)
Biomimetic (or Biokleptic?) solution
  Human Retina
Conclusions

## Slide 34: Agenda
New PCA algorithm for dealing with terabyte 3D datasets.
  Every mass channel in every spectrum in every voxel goes into the PCA.
  No “out of memory errors”. No peak-picking.
  Everything is PCA’d.
Faster PCA at better mass resolution:
  Two reasons why we must choose samples intelligently from all among the voxels available
    GPU memory limits
    Quadro Logarithmic Trap Analyser (slow but very high mass resolution)
Biomimetic (or Biokleptic?) solution
  Human Retina
Conclusions

## Slide 35
P J Cumpson et al, Surface and Interface Analysis, DOI: 10.1002/sia.6042
A Graphical Processor Unit – “GPU” has many more processors, potentially doing the PCA calculation more rapidly.
GPU cards cost perhaps $3,000 or so, and fit in desktop PCs.

## Slide 36
Nvidia GPU with 2,880 processor cores
P J Cumpson et al, Surface and Interface Analysis, DOI: 10.1002/sia.6042

## Slide 37
Nvidia GPU with 2,880 processor cores
P J Cumpson et al, Surface and Interface Analysis, DOI: 10.1002/sia.6042

## Slide 38
Nvidia GPU with 2,880 processor cores
No more local GPU memory
P J Cumpson et al, Surface and Interface Analysis, DOI: 10.1002/sia.6042

## Slide 39: Agenda
New PCA algorithm for dealing with terabyte 3D datasets.
  Every mass channel in every spectrum in every voxel goes into the PCA.
  No “out of memory errors”. No peak-picking.
  Everything is PCA’d.
Faster PCA at better mass resolution:
  Two reasons why we must choose samples intelligently from all among the voxels available
    GPU memory limits
    Quadro Logarithmic Trap Analyser (slow but very high mass resolution)
Biomimetic (or Biokleptic?) solution
  Human Retina
Conclusions

## Slide 40
A. Makarov, Anal. Chem. 72 (2000) 1156
Quadro-logarithmic trap

## Slide 41
Quadro-logarithmic trap

## Slide 42
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.
Quadro-logarithmic trap

## Slide 43
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.
Quadro-logarithmic trap
(QLT)

## Slide 44
SIMION model
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 45
SIMION model
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 46
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 47
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 48
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 49
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 50
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 51
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 52
ToF
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 53
QLT
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 54
40kV Ar clusters
40kV C60
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 55
J C Hood and P J Cumpson, IJMER 6 (Oct 2016) p76-83.

## Slide 56
ToF
≈5ms / pixel

## Slide 57
QLT
>100ms / pixel

## Slide 58: Two different reasons to process a subset of pixels (or voxels)
Long acquisition time of FTMS methods
  can we ever hope to do PCA on 3D datasets when acquisition is 20 to 200 times slower than the ToF?
Memory limit of GPU card.
  If we want PCA in seconds or minutes we need GPU cards that can hold the entire data-cube.
  Maybe in the future GPU cards will have 20, 40 or 100Gb, but unlikely to be 10Tb!
Therefore we must sample. Don’t take an entire spectrum from each pixel (or voxel).
  Choose instead a subset of pixels (or voxels).
  But which to choose?!?!?

## Slide 59: Two different reasons to process a subset of pixels (or voxels)
Long acquisition time of FTMS methods
  can we ever hope to do PCA on 3D datasets when acquisition is 20 to 200 times slower than the ToF?
Memory limit of GPU card.
  If we want PCA in seconds or minutes we need GPU cards that can hold the entire data-cube.
  Maybe in the future GPU cards will have 20, 40 or 100Gb, but unlikely to be 10Tb!
Therefore we must sample. Don’t take an entire spectrum from each pixel (or voxel).
  Choose instead a subset of pixels (or voxels).
  But which to choose?!?!?

## Slide 60: Two different reasons to process a subset of pixels (or voxels)
Long acquisition time of FTMS methods
  can we ever hope to do PCA on 3D datasets when acquisition is 20 to 200 times slower than the ToF?
Memory limit of GPU card.
  If we want PCA in seconds or minutes we need GPU cards that can hold the entire data-cube.
  Maybe in the future GPU cards will have 20, 40 or 100Gb, but unlikely to be 10Tb!
Therefore we must sample. Don’t take an entire spectrum from each pixel (or voxel).
  Choose instead a subset of pixels (or voxels).
  But which to choose?!?!?

## Slide 61: Two different reasons to process a subset of pixels (or voxels)
Long acquisition time of FTMS methods
  can we ever hope to do PCA on 3D datasets when acquisition is 20 to 200 times slower than the ToF?
Memory limit of GPU card.
  If we want PCA in seconds or minutes we need GPU cards that can hold the entire data-cube.
  Maybe in the future GPU cards will have 20, 40 or 100Gb, but unlikely to be 10Tb!
Therefore we must sample. Don’t take an entire spectrum from each pixel (or voxel).
  Choose instead a subset of pixels (or voxels).
  But which to choose?!?!?

## Slide 62: When the 2D or 3D dataset becomes too large we are forced to sample!

## Slide 63: e.g. take every 130th pixel

## Slide 64: e.g. take every 130th pixel

## Slide 65: e.g. take every 130th pixel

## Slide 66: Sampling pixels at random

## Slide 67: Sampling pixels at random

## Slide 68: Sampling pixels at random

## Slide 69: Agenda
New PCA algorithm for dealing with terabyte 3D datasets.
  Every mass channel in every spectrum in every voxel goes into the PCA.
  No “out of memory errors”. No peak-picking.
  Everything is PCA’d.
Faster PCA at better mass resolution:
  Two reasons why we must choose samples intelligently from all among the voxels available
    GPU memory limits
    Quadro Logarithmic Trap Analyser (slow but very high mass resolution)
Biomimetic (or Biokleptic?) solution
  Human Retina
Conclusions

## Slide 70: Biomimetic (biokleptic?) solution
J C Horton et al, Sci. Rep. 5 (2015) 12364
Human Retina
Cones –
expensive high-wavelength-resol’n spectra
Rods – cheap but low-wavelength- resolution spectra

## Slide 71: Biomimetic (biokleptic?) solution
J C Horton et al, Sci. Rep. 5 (2015) 12364
Cone distribution

## Slide 72: Biomimetic (biokleptic?) solution
Human Retina

## Slide 73: Biomimetic (biokleptic?) solution
Human Retina

## Slide 74: Biomimetic (biokleptic?) solution
Human Retina
Sobol

## Slide 75: Sobol sequences
Sobol, I. M. The distribution of points in a cube and the approximate evaluation of integrals, USSR Comput. Math. Math.
Phys. 7, 4, 86-112, 1967
One example of Low-discrepancy or “sub-random” sequences found to assist in rapid convergence of MC integration problems.

## Slide 76: Sobol sequences

## Slide 77: Sobol sequences

## Slide 78
Compare performance of Sobol vs. Random sampling from basalt rock sample
512x512 pixel ToFSIMS image of rock sample, 67,111 mass values in each spectrum in each pixel

## Slide 79
Compare performance of Sobol vs. Random sampling from basalt rock sample
512x512 pixel ToFSIMS image of rock sample, 67,111 mass values in each spectrum in each pixel

## Slide 80
Compare performance of Sobol vs. Random sampling from basalt rock sample
512x512 pixel ToFSIMS image of rock sample, 67,111 mass values in each spectrum in each pixel
On-average about 40% better than random sampling

## Slide 81: Extends naturally to 3D

## Slide 82: CONCLUSIONS Random Vectors/Low Discrepancy PCA
PCA by GPU is fast (<10s) provided you don’t exceed the 12Gb memory on the GPU card
This memory limit, and the ponderous QLT will force us to do PCA on only a sample of pixels (voxels)
“Not very random” methods of sampling, such as Sobol series, are best.

## Slide 83: Thanks to
Chiefly yourselves for your attention!
Ionoptika & John Fletcher @ Swedish National IMS Centre, “go-IMS!”, Gothenburg for J105 imaging data
EPSRC for 2013 “Great 8” equipment grant that bought the J105
Nicholas Burn, Jack Calder, Joseph Ford, Andrew Kiang, Lisa Li, Joe Midgley, Jonathan Rhodes, Grant Saunby and Siyao Xu for design, simulation and precision machining & assembly.
Stuart Baker, Mike Foster and Jamie Hodgson of the CNC workshop in the School of Mechanical Engineering
Barry Gallacher and Richard Burnett at Newcastle for electronics design and fabrication.

## Slide 84
Slope set by CPU/GPU speed
Slope set by disc read speed
Set by how much you can tolerate
Physical memory in PC

## Slide 85: PCA of four Pixels