## Slide 1: Graphene Heterostructures on SiC: 2D materials towards applications
Nunzio Motta, Mojtaba Amjadipour, Jonathan Bradford, Jennifer Macleod, Josh Lipton-Duffin, Francesca Iacopi*
School of Chemistry, Physics and Mechanical Engineering
Queensland University of Technology - Brisbane - Australia
*University Of Technology Sydney - Australia

## Slide 2: Nanoscale Imaging Lab - Queensland University of Technology
Helium Ion Microscope (2014)
UHV Multiprobe System (2011)
Opening, 24 April 2018
Xe- Plasma FIB (2019)

## Slide 3: Why 2D Materials?
Electronics
  High speed electronics
  Low power consumption
Energy
  Supercapacitors
  Lithium batteries
Sensing
  Gas sensors
  Environmental monitoring
High surface to volume ratio

## Slide 4: Graphene
Graphene structure
One layer of graphite
First example of atomic 2D crystal.
The world’s strongest material
Extremely high electron mobility
Very elastic
Impermeable to any molecule
Problem:
Semimetal (no electronic gap)
No digital electronics
Graphene electronic structure
Discovered 2004
Nobel prize (Geim – Novoselov) 2010

## Slide 5: Summary
Epitaxial growth of Graphene
Opening a gap in graphene by nano-patterning
Making graphene free-standing
Graphene heterostructures
  2D in-plane heterostructures Graphene - h-BN
  2D Van der Waals heterostructures: Graphene - MoS2 (WS2)

## Slide 6: Graphene from SiC
By high Temperature annealing

## Slide 7: Graphene growth on SiC by Si sublimation
  Direct growth on semiconductor
  Compatibility with the semiconductor industry
  Clean process
  Potential combination with other 2D materials
  de Heer – Berger et al PNAS 108, 16900 (2011)
Motta, Iacopi, Coletti - Growing Graphene on Semiconductors - Pan Stanford - 2017
    Problem: Bulk SiC: very expensive
    Solution: 3C-SiC(111)/Si(111)
Graphene
SiC
SiC
SiC
SiC
Si
Si
Si
Cunning et al. Nanotechnology, 25, 325301 (2014)

## Slide 8: How does graphene grow on SiC?
SiC/Si during annealing by direct current heating in UHV
Si
F.Zarotti, B.Gupta. et al. Carbon 98 - (2016) 307-312
Si leaving SiC as a result of high temperature annealing (~1200 ˚C)

## Slide 9: How does graphene grow on SiC?
Graphene XPS peak intensity
SiC/Si during annealing by direct current heating in UHV
F.Zarotti, B.Gupta. et al. Carbon 98 - (2016) 307-312
Si leaving SiC as a result of high temperature annealing (~1200 ˚C)
2
4
6
8
10
N of Graphene layers
12

## Slide 10: Improving quality of graphene on SiC
H+ etched
Un-treated
H+ treatment
PH= 7.5 10-6 mbar
TSiC=1000˚C 15’
Annealing
P= 5 10-10 mbar
T=1250˚C 10’
Degassing
P= 1 10-9 mbar
TSiC=950˚C 10’
Annealing
P= 5 10-10 mbar
T=1250˚C 10’
P.Mondelli, et al. Nanotechnology 28 (2017) 115601

## Slide 11: Opening a gap
Quantum confinement

## Slide 12: How to open a gap
Quantum confinement on the plane
  Graphene nanoribbons
Graphene NR on Au
    Cai et al Nature Nanotech, 2014. 9 p. 896
    (Experiment)
    Barone et al Nano Letters, 2006. 6: p. 2748
    (Theory)
Notes: [1] Barone, V., O. Hod, and G.E. Scuseria, Electronic Structure and Stability of Semiconducting Graphene Nanoribbons. Nano Letters, 2006. 6(12): p. 2748-2754.
[2] Cai, J., C.A. Pignedoli, L. Talirz, P. Ruffieux, H. Söde, L. Liang, V. Meunier, R. Berger, R. Li, X. Feng, K. Müllen, and R. Fasel, Graphene nanoribbon heterojunctions. Nat Nano, 2014. 9(11): p. 896-900.

## Slide 13
Nanoscale Graphene Fabrication on SiC
M. Sprinkle et al, Nature Nanotechnology, 2010. 5(10): p. 727-731.
Patterning 4H/6H-SiC by photolithography
Graphene on SiC facets
B. V. Cunning et al, Nanotechnology, 2014. 25(32): p. 325301.
Graphene on micro-scale structures
Notes: graphene on SiC facets
Field Effect Transistor
More recently, Cunning et al [23] reported a pathway for fabricating SiC micro-structures at the wafer-level through photolithography, on which they achieved metal catalyst aided graphitisation

## Slide 14
Our goal
Employing a combination of FIB (Ga+ ions) and HIM (Helium ions) to fabricate nanoscale structures
Fabricate a transistor using this approach

## Slide 15
Ga+ FIB patterning
M. Amjadipour et al. Nanotechnology 28.34 (2017): 345602.
HIM Image
No Damage
Using Si Layer
E-beam Si evaporation
Surface protection
required!
Talk Surf Sci 6 Mojtaba Amjadipour
Notes: In this study we showed the effect Ga ion poisoning on the graphene nanoribbon fabrication, and also we propose a procedure how to overcome the damage and produce high quality grapherne on FIB patterned nanostructures of SiC.

## Slide 16: Effect of the protective layer
Si Deposition
H-Etching
Graphene Growth
M. Amjadipour et al. Nanotechnology 28.34 (2017): 345602.
After
H-etching
Notes: Figure ‎4‑9. XPS spectrum of Si 2p: (a) after atomic hydrogen etching, (b) silicon deposition, (c) milling by FIB and second atomic hydrogen etching, (d) final graphene growth.

## Slide 17
SiC
Graphene
Buffer
As Grown Graphene
H-intercalation
Free-Standing
600 ˚C, 30 mins
Free-Standing Graphene on 3C-SiC/Si(111)
Photoelectron Spectroscopy (PES) Measurement C 1s 330 eV
Buffer Layer
Graphene
H-intercalation improves flatness
M. Amjadipour et al. Nanotechnology 29 (2018): 145601.
C 1s
C 1s
Graphene
SiC
Notes: The comparison of the peak intensity further confirms this, as the ratio of graphene-related spectral weight to silicon carbide spectral weight, , remains constant through the intercalation. In this expression
The comparison of the peak intensity further confirms this, as the ratio of graphene-related spectral weight to silicon carbide spectral weight, R=(I_gr+I_S1+I_S2)/I_SiC ≅12 , remains constant through the intercalation. In this expression

## Slide 18: Opening a gap
2D Materials – Graphene heterostructures

## Slide 19: Other 2D Materials
h-BN Eg=5.2 eV
Boron Nitride - BN
TMDC | Eg (ev)
MoS2 | 1.78
MoSe2 | 1.50
MoTe2 | 
WS2 | 1.84
WSe2 | 1.52
Semiconductors
Transition metal Dichalcogenides
MXenes
Insulator
Group IV materials:
Silicene
Germanene
Stannene
Semimetals
(gap opening by electric field or doping)
Silicene

## Slide 20: Epitaxial graphene heterostructures
2D materials: building blocks
  Engineer heterostructures with new properties
  Tailor properties to suit applications
2D materials Heterostructures
Geim, A.K., et al. Nature 499(7459) 419 (2013)

## Slide 21: Graphene heterostructures on SiC
Lateral heterostructure of graphene and
h-BN on a SiC substrate
TMD/graphene/SiC van der Waals
heterostructure

## Slide 22: Graphene – h-BN in plane heterostructure
Gr
h-BN
a=2.46 Å
a=2.505 Å
graphene
h-BN
Very similar lattice constant (difference 1.8%)
Very different Energy gap (Gr=0, h-BN= 6.4 eV)
Gap opening by surface alloying
J.Bradford, J.Macleod, J.Lipton-Duffin, M.Shafiei, N.Motta In preparation
6H-SiC substrate
h-BN
Gr
1 Å
6x6 Gr
h-BN
h-BN /Gr STM images
Following Talk: Jonathan Bradford

## Slide 23: TMD/Graphene van der Waals Heterostructures
High carrier mobility of graphene complements direct optical bandgap of monolayer TMDs (e.g. MoS2, WS2).
Ideal for optoelectronic devices
Photoresponsivity improved by a factor of 104 compared to MoS2.
Other applications in gas sensing, energy storage, electronics.
Photoresponse of a MoS2/graphene photodetector
Pierucci, D. et. al. Sci. Rep. 6 (2016)
TMD/graphene/SiC van der Waals heterostructure

## Slide 24: CVD Growth of TMDs on Graphene
MoS2 grown by CVD from MoO3 and S powders.
Tube pumped down to 85 Torr under Ar
MoO3 evaporated at 800˚C and S evaporated at 300˚C.
Films characterised by AFM, XPS, STM and Raman spectroscopy.

## Slide 25: MoS2/Graphene/SiC - XPS

## Slide 26: Multilayer MoS2/Graphene/SiC
AFM image of low density multilayer
MoS2 flakes grown under 200 sccm Ar flow.
STM image of an individual MoS2 flake
(V = 1:6 V; I = 0:6 nA).

## Slide 27: MoS2 spirals on Graphene/SiC
AFM image of high density multilayer
MoS2 flakes grown under 300 sccm Ar flow.
STM image of an MoS2 spiral
(V = 2.0 V; I = 0.4 nA).

## Slide 28: MoS2/Graphene/SiC – Raman spectroscopy
Raman spectrum of MoS2/gr/SiC. Inset: Raman spectrum of gr/SiC.

## Slide 29: MoS2/Graphene/SiC – Raman spectroscopy
Graphene Raman peak positions:
6 cm-1 redshift of G peak and 4 cm-1 blueshift of 2D peak
Graphene is hole doped under laser illumination
Electron-hole pairs generated in MoS2 and separated at the interface

## Slide 30: Growth of MoS2 on 4H-SiC
12
MoS2 grown by CVD on 4H-SiC substrates.
T=750 ˚C
P= 80 Torr
Ar flux: 300 sccm
X-ray photoemission spectroscopy (XPS) and Raman spectroscopy identify the growth of MoS2 with minimal residual oxide.
Notes: Enhancement of the A1g lattice vibration (out-of-plane) is due to high density of exposed edges.
Need to understand the growth mechanism

## Slide 31: Vertical MoS2 Flakes on SiC!
12
Flakes are vertically standing with three preferred orientations.
Flakes grow preferentially at the step edges
High edge density of vertically standing flakes ideal for applications in gas sensing, field emission, etc.
SEM
AFM
Notes: Three preferred orientations are 60 degrees apart from one another, suggesting that they are aligned to the three high symmetry directions of the hexagonal SiC lattice
Need to understand the growth mechanism

## Slide 32: Conclusions
Epitaxial Graphene growth on SiC
High temperature annealing in UHV
FIB nanopatterning to open a gap
H intercalation to isolate graphene
Heterostructures of 2D materials on epitaxial graphene
Growth of in-plane graphene/h-BN heterostructures on SiC.
Spiral and multilayer growth modes of MoS2 on epitaxial graphene/SiC
Vertical flakes of MoS2 on SiC

## Slide 33: Acknowledgements
QUT Surface science group
Jennifer MacLeod
Josh Lipton Duffin
Bharati Gupta
Jonathan Bradford
Mojtaba Amjadi Pour
Nima Khoshsirat
Muhammad Imran
Michael Horn
Maryam Abyasizami
Collaborators
Francesca Iacopi (UTS)
Mahnaz Shafiei (Swinburne)
Sgarlata, Tomellini, Placidi, De Crescenzi (Tor Vergata)
Mariani, Betti, Di Bernardo, Mondelli (Sapienza)
Jinzhang Liu (Beihang)
Isabelle Berbezier (IM2NP)
Luca Camilli (DTU)

## Slide 34: Silicene
Work in progress…
Silicene on AG(111)
Silicene on graphene

## Slide 35: Silicene on Ag(111)/Mica
STM image of the silicon monolayer/Ag
(V = -1.0 V, I = 1.0 nA).

## Slide 36: Surface – Transition: SiC to graphene
3.6 nm
5.3 Å
5.3 Å
5.2 Å
4.6 Å
Graphene
4.9
4.9
4.6
5.2
SiC (3/2x√3)
2x2
STM image Vb=60 mV I=80 pA
STM image (20mV; I=80pA)
3 nm
200 nm 3C SiC (111)/Si(111) T = 1250˚C
B. Gupta, E. Placidi, C. Hogan, et al., Carbon, 91, 378 (2015)
Collaboration

## Slide 37: XPS: Number of graphene layers vs T
2D
Arrhenius formula
N(T) = A e-Ea/KT
Activation energy
Ea = 2.46 eV
A = 4.74 x 108
B.Gupta. et al. Carbon 68 ( 2014 ) 563 –572
10’ annealing
Notes: By annealing for 10’ we found an increase in the number of layers with temperature described by the Arrhenius formula

## Slide 38: Graphene thickness vs annealing time
F.Zarotti, B.Gupta. et al. Carbon 98 - (2016) 307-312
SiC
graphene
Si out-diffusion

## Slide 39: Growth law of the graphene layer
F.Zarotti, B.Gupta. et al. Carbon 98 - (2016) 307-312
h(t)
e-
hn
X-ray
(l=e- mean free path)
Exponential rise
Intensity of the normalised overlayer signal
The overall best fitting is obtained with the function
SiC
graphene
(growth law)
Overlayer signal
G + I
Notes: The intensity of the overlayer signal, normalised to the substrate signal can be fitted with an exponential rising function as a function of time.
This can be obtained by a simple argument considering the contribution of the signal coming from the different layers and the attenuation of the electron flux due to the layer thickness.
Eq. 1 of our Carbon paper (Zarotti et al)

## Slide 40: Arrhenius plot – activation energy
The slope = provides the activation energy
K1=diffusion constant
Ud*=diffusion energy
Esi= Si bond energy
So we fit all the temperatures with
From diffusion theory:
Experimental kinetics
Where:
F.Zarotti, B.Gupta. et al. Carbon 98 - (2016) 307-312
and obtain b for each T.
Activation energy
Notes: Our experimental fit of the beta coefficient provides an evaluation of the activation energy
The slope provides in fact an “apparent” activation energy.
The real activation energy is Ud* + Esi/2 =~ 5 eV, which is matching the theoretical value of energy

## Slide 41
How to produce free-Standing Graphene
Buffer layer
H-intercalation
by molecular hydrogen
on bulk SiC
Free-standing ML graphene
ML graphene + Buffer layer
Free-standing BL graphene
C. Riedl et al, Physical Review Letters, 2009. 103(24): p. 246804.
PES Measurement
S1 and S2 disappear after H-intercalation
Free-standing

## Slide 42: Energy storage
Use of graphene and Graphene oxide for improving supercapacitors energy storage

## Slide 43: Supercapacitors
High power density
Fast charge and discharge rate

## Slide 44: Supercapacitors
    Energy storage is electrostatic
      no chemical reactions
      physical phenomenon
    highly reversible

## Slide 45: 1. Exfoliated graphene
optical
SEM
SEM cross section
AFM
C=0.9 mF/cm2
C=0.7 mF/cm2
Graphene dispersion
Vacuum pumping
Porous alumina
membrane
J. Liu et al, Langmuir, 2013, Vol. 29,p13307
Vacuum filtration
Glass or PET
PVA+H3PO4
Gelled electrolyte
Glass or PET
supercapacitor
AFM results

## Slide 46: 2. Graphene + Carbon Nanotubes film
Low R graphene film
C=2.2 mF/cm2
CNT film
G
CNT
HIM image
G
CNT
SEM
SEM
graphene films as electrodes CNT films as current collectors

## Slide 47
3. Graphene/MWNT mixture
Making electrodes out of graphene-MWCNT mixture films with high roughness.
J.Liu, et al. Journal of Power Sources，274, p823 (2015)
2 mm
200 nm
Repeat process:
Grinding + suspension + filtration
C=10 mF/cm2

## Slide 48: Scaling up the production
Reduced graphene oxide
Reduced Graphene oxide( rGO) solution
  1: Blade-coating : dense paste
  2: Spray coating : liquid solution
AFM of
rGO on
mica
1
2
rGO

## Slide 49: 4. Blade coating - spray coating
Fabrication process of flexible solid-state supercapacitors
(polyimide)

## Slide 50
4. Blade vs spray: SEM analysis
Blade-coated film
Spray-coated film
C=57.5 mF/cm2
Blade coating:
0.23 mg/cm2
(C= 250 F/g)
B.Wang,et al. ACS Applied materials and interfaces 34, 22316, 2016

## Slide 51: 5. Hybrid Graphene Oxide/NaCl/Urea Films
Y. Zhao, et al. ACS Applied materials and interfaces (2017) (10.1021/acsami.7b05965)
Record capacitance: 425 F/g
@ 1A/g

## Slide 52: 5. Hybrid Graphene Oxide/NaCl/Urea Films
Y. Zhao, et al. ACS Applied materials and interfaces (2017) (10.1021/acsami.7b05965)
Capacitance improvement:
>100!

## Slide 53: Graphene sponge for Li Batteries
Study Li adsorption on graphene sponge by XPS
Collaboration
I. Di Bernardo, M.C. Asensio, C. Chen, J. Avila, Y. Ito , J.L.Duffin, P. Hines , L.Rintoul N.Motta C. Mariani, M.G.Betti, to be submitted

## Slide 54: 2D Materials for gas sensing
Graphene Oxide
AFM
SEM
Sensing NH3
Collaboration
Brescia University
1 mm
AFM

## Slide 55: Capacitance measurements
Note: the way in which capacitance is measured is very important!
Weight capacitance: Farad/g
  If the active material is very light how much space you need to get enough capacitance?
Volume capacitance: Farad/cm3
  if the active material is thin, what happens to thick layer?
Surface capacitance: Farad/cm2
  surface does not take into account thickness!