## Slide 1: Energy-resolved Neutron Imaging of Materials for Nuclear Energy
Kristian Myhre, Yuxuan Zhang, Hassina Bilheux, Jean-Christophe Bilheux, Jared Johnson, Andrew Miskowiec, and Rodney Hunt
Oak Ridge National Laboratory, USA
11th World Conference on Neutron Radiography Sydney, Australia
September 3rd, 2018

## Slide 2: ORNL currently has two complimentary neutron sources with multiple imaging beamlines
High Flux Isotope Reactor
Spallation Neutron Source
CG-1D IMAGING (dedicated)
BL-3 SNAP (shared)
BL-10 VENUS (in planning)

## Slide 3: The nuclear power industry faces significant material challenges for continued and increased use
Challenge areas include…
Structural materials
  Resistance to corrosion, radiation, high temperatures, and thermal cycling
  Qualification of repair procedures (i.e. welding) and new manufacturing methods (i.e. 3D printing)
Fuel materials
  Accident tolerance, high temperature, mixed oxide
Waste materials
  Long-term geological storage
Separation materials
  Mechanism, capacity, dynamics
Information from the International Energy Association’s (www.iea.org) 2017 Electricity Information: Overview report.
Chart: 
| Hydro | Nuclear | Natural Gas | Oil | Coal | Renewables
Percent Electricity Production | 16 | 10.6 | 22.9 | 4.1 | 39.3 | 7.1
Gross Global Electricity Production by Source

## Slide 4: Goal: Leverage ORNL’s key strengths to establish a unique characterization capability for nuclear science
Neutron sciences
Nuclear materials
Radiochemistry
Big data analysis
Neutron sources
Radiological facilities
Computing resources
Fuels and targets
Reactor materials
Waste
forms
Accelerated development and deployment of nuclear technologies

## Slide 5: Understanding the production of uranium ceramic kernels for advanced nuclear fuels has been the focus of initial studies
Image from: https://www.nextbigfuture.com/2017/03/startup-x-energy-has-started-design-of.html
Uranium ceramic kernel ~500 micron Ø
Uranium ceramic kernel ~1000 micron Ø
Graphite pebble ~6 cm Ø ~25,000 TRISO particles/pebble
Pebble bed ~100,000 to 200,000 pebbles/reactor
Sol-gel production of UO3 + C spheres
Conversion to UO2 + UC2
  Option secondary conversion (i.e. nitride)
Kernel selection
Fluidized bed CVD to deposit buffer, PyC, and SiC layers
TRISO particle selection
Embedment of TRISO particles in graphite
Pebble selection

## Slide 6: Understanding the production of uranium ceramic kernels for advanced nuclear fuels has been the focus of initial studies
Image from: https://www.nextbigfuture.com/2017/03/startup-x-energy-has-started-design-of.html
Uranium ceramic kernel ~500 micron Ø
Uranium ceramic kernel ~1000 micron Ø
Graphite pebble ~6 cm Ø ~25,000 TRISO particles/pebble
Pebble bed ~100,000 to 200,000 pebbles/reactor
Sol-gel production of UO3 + C spheres
Conversion to UO2 + UC2
  Option secondary conversion (i.e. nitride)
Kernel selection
Fluidized bed CVD to deposit buffer, PyC, and SiC layers
TRISO particle selection
Embedment of TRISO particles in graphite
Pebble selection

## Slide 7: Understanding the production of uranium ceramic kernels for advanced nuclear fuels has been the focus of initial studies (continued)
Important characteristics neutron imaging could provide
Morphology/Structure
  Layer thickness, voids, cracks, kernel sphericity and displacement
Concentrations
  Elemental, isotopic, phase
Density
Crystal phases
OPyC
SiC
IPyC
buffer
kernel
Illustration of the layer structure of a TRISO particle.

## Slide 8: Electron and optical microscopy techniques have traditionally been used for characterization
Key difficulties with these techniques include
Only provide 2D slice
  No profiling throughout sphere
Destructive and damaging sample preparation required
  Difficulties identifying real and unreal defects/features
Images from ORNL report ORNL/SR-2016/268 by J. McMurray et al. 2016

## Slide 9: Total attenuation based CT measurements show defects due to different carbon feedstocks
1 mm
Mogul L Carbon
1 mm
Raven 3500 Carbon
Defects are clearly seen as dark spots
2D still images looking at the XZ plane
2D slices moving down the Z axis
Measurements were performed at the HFIR CG-1D beamline

## Slide 10: Energy-resolved neutron imaging (ERNI) at a pulsed neutron source can obtain a wealth of spatially resolved information
What we measure
IT (x, y)
Isotopics
Epithermal spectrum
Energy resonance imaging
Crystal phases, strain, stress
Cold spectrum
Bragg edge imaging

## Slide 11: The workflow for ERNI measurements is being streamlined and automated
Plan Experiment
Data Acquisition
Post-processing
Calibration
Peak Indexing
Peak fwhm fitting by Gaussian or Lorentzian
Reconstruction
Visualization
Use ImagingReso to predict resonance signal
Angle steps (5°)
Acquisition time per angle (2hr)
Angular coverage (180°)
Use projections for reconstruction of each element using iMars3D or Octopus
Sum images for open beam
Dragonfly
Seg3D
Sum peak images for each element

## Slide 12: ERNI was used to map the Gd and U distribution in 3D
Measurements were performed at the SNS SNAP (BL-3) beamline
Left: Radiographs produced by summing peaks for Gd and U
Bottom: Resonance spectra from the whole sample region from (A) 5 to 75 eV and (B) 15 to 24 eV
A
B
Gd
U

## Slide 13: ERNI was used to map the Gd and U distribution in 3D (continued)
Gd
U

## Slide 14: ERNI was used to map the Gd and U distribution in 3D (continued)
Tomographic reconstructions of the gadolinium (left) and uranium (right) content throughout imaged UO3-Gd2O3 spheres. Advanced reconstruction methods are currently being explored for improved signal-to-noise.
Gadolinium
Uranium

## Slide 15: The conversion of kernels from oxide to carbide has been measured by Bragg-edge imaging
Chart: Wavelength (Å)
UO2 (220)
UO2 (111)
UO3 (122)
UO3-C
UO2-UC2
Bragg edge spectra from 2D measurements of uranium kernels before (blue line) and after (red line) conversion from oxide to carbide.
Neutron diffraction data of uranium kernels before (A) and after (B) conversion from oxide to carbide.
UO2-UC2
UO3-C
A
B

## Slide 16: Future: a new neutron imaging beamline is currently being built at the SNS called VENUS
Schematic representation of the Versatile Neutron Imaging Instrument (VENUS) currently planned for construction at the SNS first target station.
Estimated Beam Characteristics | 
Beam Spectrum | Epithermal, Thermal, Cold
Moderator | H2 decoupled poisoned (sharpest pulse at the SNS)
Wavelength bandwidth | ~ 2.4 Å (Time-of-Flight mode)
Spatial resolution | < 15 microns (a few microns with magnification)
Resolution Δd/d | 0.12%
Source-to-detector distance | 25 meters
Sample-to-detector distance | A few mm to tens of cm
Detection system | Camera and Micro-Channel Plate TOF detector
Flux on sample (n/s/cm2) | 1 x 107 in TOF mode 1 x 108 in white beam mode
Field of view | Up to 20 cm by 20 cm

## Slide 17: Acknowledgements
Anton Tremsin
Louis Santodonado
Jake McMurray
Tyler Reif
Jamie Molaison
Funding
Research sponsored by the Laboratory Directed Research and Development Program of Oak Ridge National Laboratory, managed by UT-Battelle, LLC, for the U. S. Department of Energy.
Beam time
This research used resources at the High Flux Isotope Reactor and the Spallation Neutron Source, a DOE Office of Science User Facility operated by the Oak Ridge National Laboratory.

## Slide 18: Thank you! Questions?