## Slide 1
Novel scintillation screen with significantly improved radiation hardness and very high light output
B. Walfort
Ch. Grünzweig, P. Trtik, M. Morgano, E. Lehmann, M. Strobl
WCNR11 2018, Sydney (Australia), 03. September 2018

## Slide 2
Introduction / Overview

## Slide 3
Introduction / Overview
Neutron Szintillation Screens
In 2005-2006 development of thin (50 – 100 micrometer) neutron sensitive scintillation screens on the basis of 6LiF/ZnS for the PSI
After success in 2006 sales of this kind of screens to the market
Since 2014 distribution of scintillation screens on the basis of Gd2O2S:Tb and Gd2O2S:Tb/6LiF for high resolution measurements
Since 2016/17 sales of PP/ZnS-scintillation screens for imaging with fast neutrons (see different presentations within WCNR-11 Malgorzata / Robert Zboray / …) (Thank you James Hunter for initiation!!!)
And from now: We will see within this presentation…

## Slide 4
Neutron Scintillation Screens
Scintillation Screen (two step mechanism):
Core reaction with ions of high capture cross section (155/157Gd, 6Li or 10B) to create a secondary radiation.
Excitation of a luminous material showing a fluorescence emission in the optimal range of the detection system.
Scintillation Screen
Typical digital camera system:
General theory behind

## Slide 5
The fluorescence mechanism:
Excitation creating a hole in the valence band and an excited electron in the conduction band
Relaxation of the excited electron to the ground level of the conduction band
Relaxation of the created hole to the top of the valence band
Fluorescence emission via an «impurity ion»
non emittive recombination of the electron and hole
Like 5) but via an impurity (defect center or impurity ion)
General theory behind

## Slide 6
Light yield:
Red solid line represents the maximum light yield
Yph = number of photons emitted by the scintillator per unit of energy absorbed
β = constant that appears approximately 2.5
Eg = band gap energy
S = transfer efficiency
Q = quantum efficiency
For the ideal situation S and Q are 100%
General theory behind

## Slide 7
From Sept. 2015 to Sept. 2017:
CTI funded development project with PSI
Reason for degradation?
Binder?
Converter?
Phosphor?
Environment?
Fitting of the curve show a two fold exponentional decay
Starting situation
Degradation of ZnS:Cu/6LiF scintillation screen during irradiation:

## Slide 8
The “Absorber”

## Slide 9
Slide presented at SCINT 2017 conference in Chamonix by Korjik
The “Phosphor”

## Slide 10
Different phosphors show different radiation hardness:
L.R. Holland, GM. Jenkins, J.H. Fisher, W.A. Hollerman, G.A. Shelby Nuclear Instruments and Methods in Physics Research B56/57 (1991) 1239-1241
The “Phosphor”

## Slide 11
Two main effects are responsible for the degradation:
I)
High energy irradiation or ions create a high density of disorder / vacancies in the crystal
Effect by the disorder / vacancies / traps:
a) Vacancies / disorder: increase of radiationless decay
b) New traps: long decay
c) Change in the surrounding of the emission center: Change in quantum efficiency
II)
High energy irradiation force a high reactivity of the surface with the environment (O2)
Change of surface chemistry destroys the luminous mechanism (radiationless decay)
The presence of oxygen in the ZnS matrix increase the migration of Cu
Degradation

## Slide 12
Different secondary irradiations / protection by varnish:
19  Standard mixture with 6LiF/ZnS
Relative I(0): 100%
20  Mixture with 10B2O3
Relative I(0): 18%
24  Standard 6LiF/ZnS mixture with high quantity of varnish
Relative I(0): 35%
Degradation

## Slide 13
Avoid oxygen:
Degradation of ZnS-phosphor by electron beam in different gas media
Argon does not stop complete degradation but fast component (oxidation process of the surface)
S.H. Chen et al. / Journal of Luminescence 109 (2004) 93–102
N.E. Brese et al. / Solid State Ionics 123 (1999) 19 –24
Degradation

## Slide 14
Sum of above and further things to do to improve:
Reduction of mechanism 1:
Use scintillator with wider band gap (but intrinsically reduced light yield)
Use emission center emitting in the orange / red region
Use phosphor with lowest possible impurities and disorder (high crystallinity)
Change from Li-6 to B-10 or Gd, due to lower energetic secondary radiations (but reduced light output)
Doping with different cations to suppress damage (self repair mechanism)
Reduction of mechanism 2:
Avoid oxygen and other reactive gases to supress reaction with environment
Degradation

## Slide 15
6-LiF / Zn(Cd)S-Scintillation screens
Main Reasons for higher radiation hardness:
Red emission shows in general higher radiation hardness and
Red emission is more efficient with standard CCD camera system
113Cd is generating conversion electrons, which are less destructive than triton and alpha particles from 6Li
Protection against air (oxygen) by use of higher varnish quantity
Use of less 6LiF in the mixture (Reduction of penetration of the phosphor by alpha particles)

## Slide 16
6-LiF / Zn(Cd)S-Scintillation screens
Main features:
After some time of irradiation 50% higher light output!
Similar resolution in comparison to the ZnS:Cu/6LiF scintillation screen
Better neutron statistics due to Cd-absorption. 113Cd (~13% abundancy) has neutron cross section of 20’000
Fluorescence lifetime is strongly reduced (see next slide)
But:
CdS is in the SVHC list (Reach, Cd causes cancer), Special precautions are required!

## Slide 17
Fluorescence Lifetime

## Slide 18
Special types:
Gd3Al2Ga3O12:Ce  Very high resolution / very short fluorescence lifetime and response!
Very short fluorescence lifetime

## Slide 19
Thank you very much for your attention
and we are looking forward to a further or new long and strong collaboration!
We are open to help you in your developments
for new types of scintillation screen!

## Slide 20
Fast Neutrons
For imaging with fast neutrons a polypropylen plate filled with a ZnS-phosphor is used. The scintillation is also a two step process. First neutrons interact with the hydrogen atoms of the polypropylene plate to build up recoiled protons. Those excite the ZnS to give the corresponding detectable light.
For information on light output / gamma sensitivity / resolution please have a look
on the poster from Malgorzata G. Makowska
or presentation by Robert Zboray
or have a look into J. Imaging 2017, 3(4), 60

## Slide 21
6LiF / ZnS-Scintillation screens
Thickness / Intensity / Resolution
With higher thickness we get higher light output
With lower thickness we get a better resolution
6LiF / ZnS-Scintillation screens (green emitting)
At NEUTRA with different setup we have a 10 times higher light output…

## Slide 22
Thickness / Intensity / Resolution
With higher thickness we get higher light intensity
With lower thickness we get a better resolution
Saturation in light output at ~30-40 mm. Absolute intensity ~1/10 of ZnS/LiF screen, but better resolution…
Gd2O2S:Tb-Scintillation screens

## Slide 23
Thickness / Intensity / Resolution
Addition of 6LiF give 30-50% higher brightness with same resolution!!!
6LiF / Gd2O2S:Tb-Scintillation screens